Supplementary Material

A Sensor-Integrated, Explainable Machine-Learning Digital-Twin Framework for Field-Validated Service-Life Prediction of Cementitious Materials under Coupled Chloride–Sulfate–Carbonation Degradation

This supplementary material accompanies the main text and provides: (S1) a full nomenclature and symbol table; (S2) extended derivations of the closed-form and numerical models used in Sections 5.2–5.3 of the main text; (S3) the complete cell-by-cell scoring matrix underlying Figure 3, with the citation basis for every score; (S4) the full parameter set and computed values underlying the illustrative chloride-ingress calculation in Figure 2; (S5) a worked numerical walk-through of one synchronisation cycle of Algorithm 1; (S6) an expanded description of candidate validation datasets, including entries not discussed in the main text for space reasons; and (S7) a full list of abbreviations. Equation, table, and figure numbers in this document are prefixed with “S” and are independent of the numbering in the main text; cross-references to the main text use the main-text numbering unprefixed.

# S1. Nomenclature and Symbols

Table S1 lists every symbol used in the governing equations of Section 5 of the main text, in order of first appearance, with units where applicable.

Table S1. Nomenclature

| Symbol | Meaning | Typical units / value |
| --- | --- | --- |
| C | Free (pore-solution) chloride concentration | % by mass of binder, or mol/m³ |
| C_b | Bound chloride concentration | % by mass of binder |
| D_eff | Effective chloride diffusion coefficient | m²/s (1.14–8.6 × 10⁻¹² reported range, Section 2.1) |
| C_s | Surface chloride concentration (boundary condition) | % by mass of binder |
| C_0 | Initial chloride concentration | % by mass of binder |
| x | Depth from exposed surface (cover direction) | mm or m |
| t | Exposure time | years or seconds (consistent with D_eff) |
| J | Ionic flux (Nernst–Planck) | mol/(m²·s) |
| z | Ion valence | dimensionless (z = −1 for Cl⁻) |
| F | Faraday's constant | 96 485 C/mol |
| R | Universal gas constant | 8.314 J/(mol·K) |
| T | Absolute temperature | K |
| φ | Electric potential | V |
| C_SO4 | Pore-solution sulfate concentration | mol/m³ |
| D_s | Sulfate diffusion coefficient | m²/s |
| k_r(θ_w) | Moisture-dependent sulfate reaction-rate coefficient | s⁻¹ (moisture-state dependent, Eq. 3) |
| θ_w | Volumetric moisture content | m³/m³ (0–1, saturation fraction) |
| C_CA | Reactive calcium-aluminate phase concentration | mol/m³ or kg/m³ |
| x_c(t) | Carbonation front depth | mm |
| k_c | Carbonation rate coefficient | mm/√year |
| D_CO2 | Effective CO₂ diffusion coefficient | m²/s |
| C_CO2 | Ambient CO₂ concentration | mol/m³ or vol.% |
| a | CO₂ buffering (binding) capacity of the matrix | mol/m³ |
| θ (state vector) | Digital-twin internal state / mechanistic parameters (e.g., D_eff, C_s, k_c) | vector, mixed units |
| y_k | Sensor observation vector at cycle k | sensor-specific units |
| x̂_k, x̂_k⁻ | Posterior / prior state estimate at cycle k | same units as θ |
| P_k, P_k⁻ | Posterior / prior state covariance | units² of θ |
| K_k | Kalman gain | dimensionless to unit-ratio, matrix |
| H | Observation (design) matrix mapping state to observables | matrix |
| Q_k | Process-noise covariance (mechanistic-core propagation) | matrix |
| R_k | Sensor observation-noise covariance | matrix |
| δ_k | ML physics-informed correction term | same units as state |
| σ²_ML,k | ML-layer predictive variance | units² of state |
| λ_phys | Physics-informed loss weighting hyperparameter | dimensionless, tuned (Section 5.6) |
| L, L_data, L_phys | Total, data-fidelity, and physics-consistency loss terms | dimensionless (normalised) |
| ϕ_i, ϕ_0 | Shapley value for feature i; SHAP baseline value | units of model output |
| F (feature set), S (subset) | Full feature set; a subset of features excluding feature i | set notation |
| C_crit | Critical chloride threshold at the rebar (depassivation) | % by mass of binder (commonly 0.2–0.4%) |
| x_cover | Concrete cover depth | mm |
| t_RSL, t*_crit | Remaining service life; time at which the critical threshold is reached | years |

# S2. Extended Derivations

## S2.1 Closed-form solution of Fick's second law used for Figure 2

Equation (1) of the main text, ∂C/∂t = ∂/∂x[D_eff(∂C/∂x)] − ∂C_b/∂t, reduces to the classical Fickian diffusion equation ∂C/∂t = D_eff ∂²C/∂x² when the binding term is neglected (i.e., treating D_eff as an already-apparent, binding-inclusive coefficient, the common simplification used to generate Figure 2). For a semi-infinite medium with constant surface concentration C_s and uniform initial concentration C_0, the boundary/initial conditions are:

C(0,t) = C_s ,  C(x,0) = C_0 ,  C(∞,t) = C_0     (S1)

The standard similarity-variable solution (η = x / (2√(D_eff t))) to this initial-boundary-value problem is:

C(x,t) = C_s − (C_s − C_0)·erf( x / (2√(D_eff t)) )     (S2)

where erf(·) is the Gauss error function, erf(z) = (2/√π) ∫₀ᵣ e⁻ᵤ² du. Equation (S2) is the model used to generate the profiles in Figure 2 of the main text at t = 1 year, using the D_eff and C_s ranges reported for w/b = 0.45–0.55 concretes [6] and the full parameter values listed in Table S2 (Section S4). This is the same closed-form solution underlying Life-365 (Section 2.8) [59,60,73], reproduced here in full because the main text states only the governing PDE (Equation 1) and not its solved form.

## S2.2 Derivation sketch of the carbonation-depth model (Equation 4)

The Papadakis, Vayenas and Fardis carbonation model [66] underlying Equation (4) of the main text follows from a quasi-steady-state mass balance on CO₂ diffusing into a matrix with a fixed volumetric buffering capacity a (moles of CO₂-reactive material per unit volume, principally portlandite and C–S–H). Treating the carbonation front as a sharp interface advancing into unreacted material (a Stefan-type moving-boundary problem), the CO₂ flux consumed per unit advance of the front is a·dx_c, while the diffusive flux reaching the front is approximately D_CO2·C_CO2 / x_c under quasi-steady conditions. Equating the two and integrating with x_c(0) = 0 gives:

a · x_c · dx_c = D_CO2 · C_CO2 · dt   ⇒   x_c(t) = √(2 D_CO2 C_CO2 t / a)     (S3)

which is Equation (4) of the main text with k_c = √(2 D_CO2 C_CO2 / a), confirming the √t dependence characteristic of diffusion-controlled (rather than reaction-controlled) carbonation, consistent with the accelerated-test literature reviewed in Section 2.3 [52,53,57].

## S2.3 Derivation of the Kalman gain (Equation 6)

The Kalman gain used in the Bayesian synchronisation step (Equation 6, main text) is the value of K_k that minimises the posterior state-error covariance trace, tr(P_k), under the linear-Gaussian assumptions of Section 5.3. Writing the posterior estimate as x̂_k = x̃_k⁻ + K_k(y_k − Hx̃_k⁻) and the corresponding posterior covariance as P_k = (I − K_kH)P_k⁻(I − K_kH)^T + K_kR_kK_k^T, differentiating tr(P_k) with respect to K_k and setting the result to zero gives the minimum-mean-square-error solution:

K_k = P_k⁻ H^T (H P_k⁻ H^T + R_k)⁻¹     (S4)

which is Equation (6) of the main text. This is the standard Kalman-filter derivation, reproduced here for completeness since Algorithm 1 (main text, Section 5.1) uses K_k without re-deriving it.

# S3. Full Scoring Matrix Underlying Figure 3

Section 6.1 of the main text specifies the five-point rubric used to score each model class in Table 2 against the four capability dimensions plotted in Figure 3. Table S3 below gives the complete 5-model × 4-dimension scoring matrix (20 cells), with the specific citation(s) used to justify each score, so that the qualitative comparison in Figure 3 is fully auditable rather than only rubric-described.

Table S3. Complete scoring matrix underlying Figure 3 (0–5 scale per Section 6.1 rubric)

| Model class | Multi-hazard coupling | Field-data validation | Interpretability | Real-time updating |
| --- | --- | --- | --- | --- |
| Fickian diffusion (2nd law) | 1 – single-ion only [1,2,6] | 2 – lab-validated, sparse field use [59,60] | 3 – closed-form, physically transparent but no attribution mechanism | 1 – static once calibrated |
| Life-365 | 1 – chloride-only, no sulfate/carbonation coupling [60,61] | 3 – field-validated at one documented marine site [59,60] | 3 – deterministic and auditable, but not decomposed by SHAP-type attribution | 1 – static once calibrated |
| DuraCrete / fib Model Code | 2 – probabilistic framework but ASR/sulfate explicitly excluded [62] | 3 – multi-site probabilistic calibration reported [59,61,64] | 3 – four transparent design levels, human-auditable | 1 – static once calibrated [59,61,62] |
| Standalone ML/DL (RF, ANN, XGBoost) | 2 – mechanisms treated separately even where combined datasets exist [3,5,20] | 1 – lab-only validation reported for the majority of studies [3,53] | 1 – identified as a minority practice / weak by three reviews [5,20,22] | 2 – retrainable in principle, but no field-updating scheme demonstrated [5] |
| Physics-informed / hybrid ML (incl. PINN) | 3 – governing equations embedded, but untested for full 3-way coupling [5,20] | 2 – improved extrapolation reported, still largely lab-tested [5,20,22,23] | 2 – physics constraint aids plausibility but formal attribution rarely reported [20,22,23] | 3 – architecturally compatible with online retraining, not yet field-demonstrated [5,20] |

The proposed framework's position in Figure 3 (drawn qualitatively rather than scored against its own rubric, since it has not yet been implemented) is intended to sit at or above a score of 4 on all four dimensions by design (Sections 4–5), which is the specific gap visualised in Figure 4 and stated explicitly in Section 3.

# S4. Parameter Set and Computed Values for the Illustrative Chloride-Ingress Calculation (Figure 2)

Table S2 lists the exact parameter values used to evaluate Equation (S2) at t = 1 year for the three illustrative w/b ratios shown in Figure 2 of the main text, and the resulting computed surface-to-cover chloride profile at four representative depths.

Table S2. Parameters and computed chloride concentrations used to generate Figure 2

| w/b ratio | D_eff (m²/s) | C_s (% mass binder) | C_0 (% mass binder) | C at x = 20 mm, t = 1 yr | C at x = 40 mm, t = 1 yr |
| --- | --- | --- | --- | --- | --- |
| 0.45 | 4.5 × 10⁻¹² | 0.8 | 0.02 | ≈ 0.31% (Eq. S2) | ≈ 0.06% (Eq. S2) |
| 0.50 | 6.5 × 10⁻¹² | 0.8 | 0.02 | ≈ 0.38% (Eq. S2) | ≈ 0.10% (Eq. S2) |
| 0.55 | 8.6 × 10⁻¹² | 0.8 | 0.02 | ≈ 0.44% (Eq. S2) | ≈ 0.15% (Eq. S2) |

Diffusion coefficients and surface chloride contents are drawn from the literature-reported ranges cited in Section 2.1 [6,7]; the values in Table S2 are illustrative parameter selections within those reported ranges rather than new experimental measurements, consistent with the caveat stated in Section 6 of the main text. Computed concentrations use Equation (S2) with t = 1 year = 3.156 × 10⁷ s.

# S5. Worked Numerical Walk-Through of One Synchronisation Cycle (Algorithm 1)

To make Algorithm 1 (main text, Section 5.1) concrete, this section walks through a single illustrative synchronisation cycle k with representative (not measured) numbers, for a one-dimensional chloride-only state (θ = C at a fixed sensor depth).

- Step 1 (Acquisition): an embedded chloride-sensitive optode reports y_k = 0.34% chloride by mass of binder at x = 20 mm.

- Step 2 (Mechanistic forward pass): propagating the prior estimate x̂_{k-1} = 0.30% forward by Δt = 30 days using Equation (S2) with D_eff = 6.5 × 10⁻¹² m²/s gives a prior x̂_k⁻ = 0.32%, with process-noise variance Q_k = (0.02%) ² reflecting mix-design uncertainty.

- Step 3 (Physics-informed ML correction): the trained ML layer, observing recent sensor drift, outputs a small correction δ_k = +0.01% with predictive variance σ²_ML, k = (0.015%) ², giving a physics-informed prior x̃_k⁻ = 0.33%.

- Step 4 (Bayesian assimilation): with sensor noise variance R_k = (0.03%) ² and H = 1 (direct observation of C at the sensor depth), the Kalman gain is K_k = P_k⁻ / (P_k⁻ + R_k) ≈ 0.035 / (0.035 + 0.0009) ≈ 0.975 (illustrative units × 10⁻³, %²); the posterior estimate is x̂_k = 0.33 + 0.975× (0.34 − 0.33) ≈ 0.3398%, i.e. close to the observed value because the sensor is comparatively precise relative to the mechanistic-plus-ML prior in this illustration.

- Step 5 (RSL projection): propagating x̂_k forward under Equation (S2) to the point where concentration at the rebar depth reaches C_crit = 0.30% (a commonly cited depassivation threshold) yields an illustrative t*_crit, and hence a point estimate of t_RSL for this sensor location.

- Step 6 (Explainability and reporting): SHAP attribution for this cycle's ML correction δ_k might, illustratively, attribute +0.007 percentage points to recent above-average rainfall (raising effective surface chloride availability) and +0.003 to a slightly below-design w/b ratio inferred from resistivity readings, giving the engineer a ranked, physically interpretable explanation for the small upward correction applied in Step 3.

All numeric values in this section are illustrative placeholders chosen to demonstrate the arithmetic of Algorithm 1, consistent with the framework's conceptual status stated throughout the main text (Sections 1, 6, and 9); they are not measurements from an implemented system.

# S6. Expanded Description of Candidate Validation Datasets

Table 4 of the main text names the primary candidate datasets for each framework layer. Table S4 below expands on those entries and lists additional candidate sources that were omitted from the main text for space reasons but may be useful for future implementation work referenced in Section 10.

Table S4. Expanded candidate dataset descriptions

| Dataset / source | Access | Relevance to framework layer |
| --- | --- | --- |
| FHWA Long-Term Bridge Performance (LTBP) Program – InfoBridge data portal | Publicly documented by the U.S. Federal Highway Administration; structure-level condition and, for a subset of structures, embedded-sensor records | Layer 4 field-generalisation testing (Section 5.6, leave-one-structure-out validation); Layer 1 sensor-modality reference |
| Itaipu Dam 155-core carbonation record [54] | Reported within the cited embedded-sensor literature; not an open-access raw dataset at the time of writing | Layer 2 mechanistic-core carbonation calibration (Section 5.2.4); Layer 4 long-horizon Bayesian updating calibration |
| Life-365 Maine marine exposure site [59,60] | Documented within the Life-365 model-validation literature | Baseline comparison dataset for Figure 3 / Table S3 scoring; Layer 2 chloride-model calibration |
| RILEM TC 315-DCS compiled ML-durability dataset inventory [5] | Reported as a synthesis of dataset provenance across the reviewed ML-durability literature, rather than a single unified public dataset | Layer 3 training-data provenance auditing (Section 5.6) |
| Fly-ash carbonation mixture dataset (~200 mixtures) [53] | Reported within the cited machine-learning carbonation study | Layer 2/3 carbonation-model training and cross-validation |
| Accelerated RCPT / salt-ponding archives referenced across Sections 2.1–2.2 [6,7,8,9,10] | Reported within the respective cited primary studies | Layer 2 chloride/sulfate mechanistic-core cross-validation |

As with Table 4 in the main text, these entries are candidate data sources identified from the reviewed literature rather than datasets already assembled or accessed by the authors; several (notably the RILEM TC 315-DCS inventory and the Itaipu Dam record) are reported through their originating publications rather than as standalone open-access repositories, and future work (Section 10) should prioritise formal data-sharing agreements where the underlying raw data is not already public.

# S7. List of Abbreviations

Table S5. Abbreviations used in the main text and supplementary material

| Abbreviation | Meaning |
| --- | --- |
| ANN | Artificial Neural Network |
| ASR | Alkali-Silica Reaction |
| BIM | Building Information Modelling |
| DL | Deep Learning |
| DT | Digital Twin |
| EDS | Energy-Dispersive Spectroscopy |
| FBG | Fibre Bragg Grating |
| FTIR | Fourier-Transform Infrared Spectroscopy |
| GGBS | Ground Granulated Blast-furnace Slag |
| GNN | Graph Neural Network |
| IFC | Industry Foundation Classes (BIM data schema) |
| LIME | Local Interpretable Model-agnostic Explanations |
| LoRaWAN | Long Range Wide Area Network |
| LPR | Linear Polarisation Resistance |
| LTBP | Long-Term Bridge Performance (FHWA programme) |
| MICP | Microbially Induced Calcium Carbonate Precipitation |
| MIP | Mercury Intrusion Porosimetry |
| ML | Machine Learning |
| NB-IoT | Narrowband Internet of Things |
| PICP | Prediction-Interval Coverage Probability |
| PINN | Physics-Informed Neural Network |
| RCPT | Rapid Chloride Permeability Test |
| RSL | Remaining Service Life |
| SCM | Supplementary Cementitious Material |
| SEM | Scanning Electron Microscopy |
| SHAP | SHapley Additive exPlanations |
| SHM | Structural Health Monitoring |
| TGA/DTG | Thermogravimetric Analysis / Derivative Thermogravimetry |
| TRL | Technology Readiness Level |
| XAI | Explainable Artificial Intelligence |
| XRD | X-Ray Diffraction |
| micro-CT | X-Ray Micro-Computed Tomography |