Table 1: Optimization of the reaction conditions for synthesis of 3da

| Entry | Catalyst | Weight (g) | Solvent | Temp. (°C) | Time (min) | Yield (%) |
| --- | --- | --- | --- | --- | --- | --- |
| 1 | g-C3N4 | 0.05 | Ethanol | r.t. | 60 | Trace |
| 2 | NiFe₂O₄ | 0.05 | Ethanol | r.t. | 100 | 70 |
| 3 | g-C3N4/NiFe₂O₄ | 0.05 | Ethanol | r.t. | 60 | 80 |
| 4 | g-C3N4/NiFe₂O₄ | 0.05 | Solvent free | r.t. | 80 | 75 |
| 5 | g-C3N4/NiFe₂O₄ | 0.05 | H2O | r.t. | 60 | 75 |
| 6 | g-C3N4/NiFe₂O₄ | 0.05 | H2O | 60 | 35 | 90 |
| 7 | g-C3N4/NiFe₂O₄ | 0.05 | H2O | 80 | 15 | 96 |
| 8 | g-C3N4/NiFe₂O₄ | 0.05 | H2O | Reflux | 5 | 96 |
| 9 | g-C3N4/NiFe₂O₄ | 0.04 | H2O | Reflux | 5 | 96 |
| 10 | g-C3N4/NiFe₂O₄ | 0.03 | H2O | Reflux | 10 | 90 |

aReaction conditions:4-nitrobenzaldehyde (1 mmol), 2-naphthol (2 mmol). All yields are isolated products

Table 2: Synthesis of xanthene derivatives 3a-3g

| Entry | Product | Time (min) | Yield (%)a | m. p. (℃, found) |
| --- | --- | --- | --- | --- |
| 3a |  | 15 | 90 | 182-185 (1) |
| 3b |  | 5 | 96 | 211-214 (2) |
| 3c |  | 5 | 98 | 282-283 (1) |
| 3d |  | 5 | 96 | 312-316 (2) |
| 3e |  | 15 | 90 | 240-243 (3) |
| 3f |  | 15 | 88 | 199-203 (3) |
| 3g |  | 10 | 90 | 224-226 (2) |

aAll yields are isolated products

Table 3. Comparison of the catalytic activity of nano g-C3N4/NiFe₂O₄ with other catalysts in synthesis of xanthene derivatives

| Entry | Catalyst/ Temp / Solvent/Time | Yield (%) | Ref. |
| --- | --- | --- | --- |
| 1 | Fe3O4@COF-SO3H/80oC/S-F/5 min | 96 | (4) |
| 2 | GO-CuFe2O4 / 125oC/ Water / 15 min | 92 | (5) |
| 3 | CuSO4.5H2O / 80oC/ S-F/5(h) | 95 | (1) |
| 4 5 6 | NiCuFe2O4/ UT/Water/ 6 min Phosphosulfonic acid/110oC/45min Cucurbit[6]uril-OSO3H/110oC/35min | 98 95 95 | (6) (7) (8) |
| 7 | g-C3N4/NiFe₂O₄/H2O/Reflux/5 min | 96 | This work |

Table 4. The in vitro cytotoxic activity of the synthesized derivatives (3a-3g) against MCF-7 cell line

| Entry | R | IC50 ± SD (µM) |
| --- | --- | --- |
|  |  | MCF-7 |
| 3a | H | > 200 |
| 3b | 3-NO2 | > 200 |
| 3c | 4-Cl | 133.7 ± 8.27 |
| 3d | 4-NO2 | > 200 |
| 3e | 4-OH | 50.0 ± 2.26 |
| 3f | 4-OMe | 89.6 ± 5.30 |
| 3g | 4-Me | > 200 |
| erlotinib | ---- | 35.5 ± 0.40 |