# Supplementary Information

## Table S1. Physicochemical properties of synthesized MOFs

| Property | Cu-BTC | MIL-100(Fe) |
| --- | --- | --- |
| Yield (%) | 58.3 ± 1.2 | 74.9 ± 1.6 |
| Particle size (nm) | 70.4 ± 3.1 | 89.6 ± 4.0 |
| Zeta potential (mV) | -45.2 ± 1.3 | -38.4 ± 1.6 |

## Table S2. Example calibration data

| Drug | Equation | R² | LOD (µg/mL) |
| --- | --- | --- | --- |
| IBU | y=0.0102x+0.004 | 0.9992 | 1.2 |
| CIP | y=0.0145x+0.003 | 0.9996 | 0.8 |
| PARA | y=0.0088x+0.002 | 0.9989 | 1.5 |

## Table S3. Example Entrapment Efficiency (n=3)

| Drug | MOF | Condition | EE (%) | Mean ± SD |
| --- | --- | --- | --- | --- |
| IBU | Cu-BTC | ACN | 99.1 | 99.1 ± 0.7 |
| IBU | MIL-100 | ACN | 100.0 | 100.0 ± 0.0 |
| CIP | Cu-BTC | pH5 | 82.6 | 82.6 ± 1.1 |
| CIP | MIL-100 | pH7 | 81.8 | 81.8 ± 0.9 |
| PARA | Cu-BTC | pH5 | 89.3 | 89.3 ± 1.8 |
| PARA | MIL-100 | pH7 | 84.7 | 84.7 ± 2.1 |

## Table S4. Example kinetic parameters

| System | Model | Rate constant | R² | Interpretation |
| --- | --- | --- | --- | --- |
| IBU/Cu-BTC | PSO | 0.015 | 0.997 | Chemisorption |
| IBU/MIL-100 | PSO | 0.021 | 0.999 | Chemisorption |
| CIP/Cu-BTC | PSO | 0.034 | 1.000 | Chemisorption |
| PARA/Cu-BTC | PSO | 0.009 | 0.989 | Hydrogen bonding |

## Placeholder Figures

Figure S1. Room temperature synthesis protocol for Cu-BTC and MIL-100.

Figure S2. UV-Visible calibration curves of (a) ibuprofen (IBU), (b) paracetamol (PARA), and (c) ciprofloxacin (CIP) at varying concentrations in aqueous buffers of pH 5.0 and pH 7.0.

Figure S3 DLS distribution of Cu-BTC and MIL-100 (a) representing the particle size and (b) representing the zeta potential.