Supporting Information

Magnetic COFs as satisfied support for lipase immobilization and recovery to effectively achieve the production of biodiesel by great maintenance of enzyme activity.

Zi-Wen Zhoua, Xiu Xinga, Jun Lia, Zu-E Hua, Zong-Bo Xieb, Na Wang a*, Xiao-Qi Yu a*

aKey Laboratory of Green Chemistry and Technology (Ministry of Education), College of Chemistry, Sichuan University, Chengdu 610064, P. R. China.

E-mail: wnchem@scu.edu.cn; xqyu@scu.edu.cn; Fax: +86-28-85415886; Tel: +86-28-85415886

bJiangxi Province Key Laboratory of Synthetic Chemistry, School of Chemistry, Biology and Material Science, East China University of Technology, Nanchang 330013, P. R. China.

E-mail: zbxie@ecut.edu.cn.

Determination of loading capacity of RML by using BSA standard curves.

Preparation of BSA standard reagents:

The BSA standard solution was prepared by solving 10mg BSA in deionized water, diluting to 10ml. The concentration of acquired BSA standard solution was 1mg/mL.

Coomassie brilliant blue staining methods (Bradford Protein Assay Kit).

I: To a 96-hole plates, 200μL of G250 staining was added into every single holes.

II: Add 50μL of BSA standard solutions with concentration gradient (Table SA).

III: Incubate about 10min.

IV: Determine the Absorbance at 595nm.

V: Prepare BSA standard curves (Figure SA). Determine the unknown protein samples by this curve.

Figure SA: The BSA standard curves using Coomassie brilliant blue staining assays

| Entry | PBS buffer | BSA standard solutions | Concentration |
| --- | --- | --- | --- |
| 1 | 900μL | 100μL | 0.1mg/mL |
| 2 | 920μL | 80μL | 0.08mg/mL |
| 3 | 940μL | 60μL | 0.06mg/mL |
| 4 | 960μL | 40μL | 0.04mg/mL |
| 5 | 980μL | 20μL | 0.02mg/mL |

Table SA: The preparation of BSA standard solution with concentration gradient

Enzymatic activity assay

Determination of auto-hydrolysis of p-NPA:

We investigated the enzymatic activity of RML and immobilized RML by hydrolysis of p-NPA. It should be considered that p-NPA will hydrolyze automatically. So the problem that auto-hydrolysis of the substrate 4-nitrophenyl acetate had to be addressed. This was done by investigating the auto-hydrolysis of 0.4 μmol/mL of p-NPA of over time (Figure SB).

Figure SB: The auto-hydrolysis of p-NPA

Preparation of p-NP standard curves:

Refer to Table SB, the p-NP standard curve (Figure SC) was determined by preparing a series of p-NP standard solutions with concentration gradient and detecting their absorbance at 405nm.

Figure SC: The standard curves of p-NP

| Entry | p-NP | PBS buffer | Concentration |
| --- | --- | --- | --- |
| 1 | 500μL | 9500μL | 0.1 μmol/mL |
| 2 | 750μL | 9250μL | 0.15 μmol/mL |
| 3 | 1000μL | 9000μL | 0.2 μmol/mL |
| 4 | 1250μL | 8750μL | 0.25 μmol/mL |
| 5 | 1500μL | 8500μL | 0.3 μmol/mL |
| 6 | 2000μL | 8000μL | 0.4 μmol/mL |
| 7 | 2500μL | 7500μL | 0.5 μmol/mL |

Table SB The preparation of p-NP standard solution with concentration gradient

The enzyme activity assay

To a tube, 500uL, 2μmol/mL of p-NPA and 2000μL of PBS buffer with immobilized RML (or 2000μL total volume of free enzyme and PBS buffer solution) were added into a tube. The absorbance at 405nm was detected. Finally, the product concentrations were corrected for the auto-hydrolysis of p-NPA and also the absorbance of p-NPA left in the solution.

Figure S1. The synthesis of COF-OMe.

Figure S2. PXRD patterns of COF-OMe

Figure S3. N2 sorption isotherms collected at 77 K.

Figure S4. Pore size distribution based on the nonlocal density functional theory method.

B

B

Figure S5. The SEM images of COF-OMe prepared by facile method in different solvents: A) Acetonitrile, B) DMSO, C) Toluene, D) n-Hexane.

Figure S6. The FTIR spectrum of Fe3O4, monomers of COF-OMe and Fe3O4@COF-OMe

Figure S7. The differential thermal gravity (DTG) image

Figure S8. Pore distribution of Fe3O4@COF-OMe and RML@Fe3O4@COF-OMe

Table S1. The textural parameters of two magnetic COFs before and after loading of RML as well as the corresponding loading capacity.

Figure S9. The confocal laser scanning microscope image of Fe3O4@COF-OMe (excitation at λ=488nm, and long emission at 490-690nm)

Figure S10. The confocal laser scanning microscope image of RML@Fe3O4@COF-OMe (excitation at λ=488nm and 543nm).

Figure S11. The EDS mapping of Fe3O4-COF-OMe (N: yellow, C: red, O: green, Fe: purple)

Figure S12. The EDS mapping of Fe3O4@COF-OMe (N: green, C: red, O: cyan, Fe: yellow)

Fig S13. The template reaction: The transesterification reaction of 2-phenol with vinyl acetate.

Figure S14. Transesterification yields in different solvents. (The yields in n-Hexane is set as 100%)

Figure S15. The tolerance of both immobilized RML and free enzyme against ultrasonic operation