Supplementary Information

Molecular-Level Understanding of Polyethylene Glycol Adsorption on TiO2(001)

at the Solid–Water Interfaces

Seungsoo Hana and Hee-Joon Chunb,*

a Department of Chemistry, Stony Brook University, Stony Brook, New York 11794, United States

b Department of Chemistry, Chungnam National University, Daejeon 34134, Republic of Korea

* Corresponding author e-mail: hjchun@cnu.ac.kr

Table S1. Data for 0.25 ML PEG-5* on TiO2(001)

| ps | EDFTPEG/H2Ol<1ML* (eV) | EDFTH2Ol<1ML* (eV) | EDFTPEGg (undissociated) (eV) | EDFTPEG* (eV) | EDFT* (slab) (eV) | EDFTPEG (dissociated) (eV)1) | EDFTPEG(g) (dissociated) (eV)2) | EDFTPEG_head*adsorption (eV)3) | EDFTPEG_chain*interaction (eV)4) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | -1212.22 | -992.80 | -212.28 | -471.25 | -257.34 | -207.36 | -207.36 | -1.63 | 0.00 |
| 2 | -1212.35 | -993.57 | -212.28 | -471.67 | -257.25 | -207.53 | -207.47 | -2.07 | -0.06 |
| 3 | -1213.34 | -994.00 | -212.28 | -470.71 | -256.34 | -207.52 | -207.44 | -2.01 | -0.08 |
| 4 | -1213.43 | -994.05 | -212.28 | -470.49 | -256.00 | -207.43 | -207.43 | -2.20 | -0.01 |
| 5 | -1213.54 | -994.81 | -212.28 | -470.80 | -256.33 | -207.65 | -207.62 | -2.15 | -0.03 |
| 6 | -1213.69 | -994.29 | -212.28 | -470.46 | -256.02 | -207.67 | -207.64 | -2.13 | -0.03 |
| 7 | -1213.54 | -994.37 | -212.28 | -470.55 | -256.18 | -207.68 | -207.65 | -2.05 | -0.03 |
| 8 | -1214.34 | -995.33 | -212.28 | -470.54 | -256.27 | -206.50 | -206.45 | -1.94 | -0.05 |
| 9 | -1214.04 | -994.17 | -212.28 | -470.28 | -256.02 | -206.44 | -206.41 | -1.94 | -0.03 |
| 10 | -1213.94 | -994.10 | -212.28 | -470.09 | -255.99 | -207.50 | -207.45 | -1.77 | -0.05 |
| Average | -1213.44 | -994.15 | -212.28 | -470.68 | -256.37 | -207.33 | -207.29 | -1.99 | -0.04 |

Table S1. continued

| ps | EDFTPEG*solvation (eV)5) | ∆HPEG* (eV)6) | EDFTPEG_head*adsorption /# of PEG (eV/PEG)7) | EDFTPEG_chain*interaction /# of monomer (eV/monomer)8) | #H-bond9) | EDFTPEG*solvation /# of O in PEG* (eV/monomer)10) | θPEG* (ML)11) | θH2O* (ML)12) | N13) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | -5.51 | -7.13 | -1.63 | 0.00 | 10 | -0.92 | 0.25 | 0.75 | 1 |
| 2 | -4.37 | -6.50 | -2.07 | -0.01 | 8 | -0.73 | 0.25 | 0.75 | 1 |
| 3 | -4.96 | -7.06 | -2.01 | -0.02 | 10 | -0.83 | 0.25 | 0.75 | 1 |
| 4 | -4.89 | -7.10 | -2.20 | 0.00 | 8 | -0.81 | 0.25 | 0.75 | 1 |
| 5 | -4.26 | -6.45 | -2.15 | -0.01 | 10 | -0.71 | 0.25 | 0.75 | 1 |
| 6 | -4.94 | -7.11 | -2.13 | -0.01 | 10 | -0.82 | 0.25 | 0.75 | 1 |
| 7 | -4.80 | -6.89 | -2.05 | -0.01 | 10 | -0.80 | 0.25 | 0.75 | 1 |
| 8 | -4.74 | -6.73 | -1.94 | -0.01 | 10 | -0.79 | 0.25 | 0.75 | 1 |
| 9 | -5.61 | -7.59 | -1.94 | -0.01 | 10 | -0.94 | 0.25 | 0.75 | 1 |
| 10 | -5.73 | -7.55 | -1.77 | -0.01 | 11 | -0.96 | 0.25 | 0.75 | 1 |
| Average | -4.98 | -7.01 | -1.99 | -0.01 | 9.70 | -0.83 | 0.25 | 0.75 | 1.00 |

1) Single point calculation for dissociated PEG where the structure and unit cell are from EDFTPEG/H2Ol<1ML*

2) Single point calculation for dissociated PEG where the structure is from EDFTPEG/H2Ol<1ML* in a large unit cell (no interactions between PEG)

3) EDFTPEG_head*adsorption=EDFTPEG/H2Ol<1ML*-EDFTH2Ol<1ML*-EDFTPEGgundissociated -∆EDFTPEG_chain*interaction

4) EDFTPEG_chain*interaction=EDFTPEGdissociated-the total number of dissociated PEG* in the unit cell×EDFTPEGg(dissociated)

5) EDFTPEG*solvation=EDFTPEG/H2Ol<1ML*-EDFTH2Ol<1ML*-EDFTPEG*+EDFT*

6) ∆HPEG*=EDFTPEG_head*adsorption+EDFTPEG_chain*interaction+EDFTPEG*solvation

7) EDFTPEGhead*adsorption# of PEG*=EDFTPEG_head*adsorptionthe total number of PEG* in the unit cell

8) EDFTPEGchain*interaction# of monomer=EDFTPEG_chain*interactionthe total number of the PEG* monomer in the unit cell

9) the total hydrogen bond number between PEG* and surrounding H2O(l) molecules

10) EDFTPEG*solvation# of O in PEG* =EDFTPEG*solvationthe total number of the oxygen atom in PEG* in the unit cell

11) the surface coverage of PEG* in the unit cell

12) the surface coverage of H2O* in the unit cell

13) the total number of desorbed H2O/unit cell during PEG adsorption

Table S2. Data for 0.50 ML PEG-5* on TiO2(001)

| ps | EDFTPEG/H2Ol<1ML* (eV) | EDFTH2Ol<1ML* (eV) | EDFTPEGg (undissociated) (eV) | EDFTPEG* (eV) | EDFT* (slab) (eV) | EDFTPEG (dissociated) (eV)1) | EDFTPEG(g) (dissociated) (eV)2) | EDFTPEG_head*adsorption (eV)3) | EDFTPEG_chain*interaction (eV)4) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | -1265.23 | -827.32 | -212.28 | -686.28 | -256.08 | -416.33 | -207.42 | -4.26 | -1.36 |
| 2 | -1265.78 | -828.00 | -212.28 | -685.67 | -255.34 | -416.35 | -207.51 | -4.43 | -1.34 |
| 3 | -1266.60 | -828.80 | -212.28 | -685.04 | -254.94 | -416.18 | -207.47 | -4.29 | -1.24 |
| 4 | -1266.29 | -829.00 | -212.28 | -685.10 | -255.05 | -416.32 | -207.55 | -4.26 | -1.23 |
| 5 | -1266.05 | -828.75 | -212.28 | -685.12 | -254.96 | -416.17 | -207.44 | -4.30 | -1.30 |
| 6 | -1266.54 | -829.27 | -212.28 | -685.09 | -254.78 | -416.36 | -207.48 | -4.35 | -1.39 |
| 7 | -1266.75 | -829.27 | -212.28 | -685.20 | -254.95 | -416.38 | -207.49 | -4.28 | -1.40 |
| 8 | -1266.29 | -828.80 | -212.28 | -685.10 | -255.01 | -416.38 | -207.39 | -3.93 | -1.59 |
| 9 | -1266.67 | -829.17 | -212.28 | -684.86 | -254.93 | -416.04 | -207.52 | -4.37 | -0.99 |
| 10 | -1266.73 | -829.59 | -212.28 | -685.05 | -254.88 | -416.49 | -207.52 | -4.15 | -1.45 |
| Average | -1266.29 | -828.80 | -212.28 | -685.25 | -255.09 | -416.30 | -207.48 | -4.26 | -1.33 |

Table S2. continued

| ps | EDFTPEG*solvation (eV)5) | ∆HPEG* (eV)6) | EDFTPEG_head*adsorption /# of PEG (eV/PEG)7) | EDFTPEG_chain*interaction /# of monomer (eV/monomer)8) | #H-bond9) | EDFTPEG*solvation /# of O in PEG* (eV/monomer)10) | θPEG* (ML)11) | θH2O* (ML)12) | N 13) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | -7.71 | -13.34 | -2.13 | -0.14 | 15 | -0.64 | 0.50 | 0.50 | 2 |
| 2 | -7.45 | -13.21 | -2.21 | -0.13 | 13 | -0.62 | 0.50 | 0.50 | 2 |
| 3 | -7.70 | -13.23 | -2.15 | -0.12 | 16 | -0.64 | 0.50 | 0.50 | 2 |
| 4 | -7.24 | -12.72 | -2.13 | -0.12 | 16 | -0.60 | 0.50 | 0.50 | 2 |
| 5 | -7.13 | -12.73 | -2.15 | -0.13 | 18 | -0.59 | 0.50 | 0.50 | 2 |
| 6 | -6.96 | -12.70 | -2.18 | -0.14 | 15 | -0.58 | 0.50 | 0.50 | 2 |
| 7 | -7.23 | -12.92 | -2.14 | -0.14 | 17 | -0.60 | 0.50 | 0.50 | 2 |
| 8 | -7.41 | -12.93 | -1.97 | -0.16 | 15 | -0.62 | 0.50 | 0.50 | 2 |
| 9 | -7.56 | -12.93 | -2.19 | -0.10 | 17 | -0.63 | 0.50 | 0.50 | 2 |
| 10 | -6.98 | -12.58 | -2.07 | -0.15 | 16 | -0.58 | 0.50 | 0.50 | 2 |
| Average | -7.34 | -12.93 | -2.13 | -0.13 | 15.80 | -0.61 | 0.50 | 0.50 | 2.00 |

1) Single point calculation for dissociated PEG where the structure and unit cell are from EDFTPEG/H2Ol<1ML*

2) Single point calculation for dissociated PEG where the structure is from EDFTPEG/H2Ol<1ML* in a large unit cell (no interactions between PEG)

3) EDFTPEG_head*adsorption=EDFTPEG/H2Ol<1ML*-EDFTH2Ol<1ML*-EDFTPEGgundissociated -∆EDFTPEG_chain*interaction

4) EDFTPEG_chain*interaction=EDFTPEGdissociated-the total number of dissociated PEG* in the unit cell×EDFTPEGg(dissociated)

5) EDFTPEG*solvation=EDFTPEG/H2Ol<1ML*-EDFTH2Ol<1ML*-EDFTPEG*+EDFT*

6) ∆HPEG*=EDFTPEG_head*adsorption+EDFTPEG_chain*interaction+EDFTPEG*solvation

7) EDFTPEGhead*adsorption# of PEG*=EDFTPEG_head*adsorptionthe total number of PEG* in the unit cell

8) EDFTPEGchain*interaction# of monomer=EDFTPEG_chain*interactionthe total number of the PEG* monomer in the unit cell

9) the total hydrogen bond number between PEG* and surrounding H2O(l) molecules

10) EDFTPEG*solvation# of O in PEG* =EDFTPEG*solvationthe total number of the oxygen atom in PEG* in the unit cell

11) the surface coverage of PEG* in the unit cell

12) the surface coverage of H2O* in the unit cell

13) the total number of desorbed H2O/unit cell during PEG adsorption

Table S3. Data for 0.75 ML PEG-5* on TiO2(001)

| ps | EDFTPEG/H2Ol<1ML* (eV) | EDFTH2Ol<1ML* (eV) | EDFTPEGg (undissociated) (eV) | EDFTPEG* (eV) | EDFT* (slab) (eV) | EDFTPEG (dissociated) (eV)1) | EDFTPEG(g) (dissociated) (eV)2) | EDFTPEG_head*adsorption (eV)3) | EDFTPEG_chain*interaction (eV)4) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | -1301.51 | -651.72 | -212.28 | -899.23 | -254.17 | -625.16 | -207.34 | -5.08 | -3.13 |
| 2 | -1301.28 | -652.37 | -212.28 | -899.39 | -254.34 | -625.86 | -207.25 | -4.08 | -4.12 |
| 3 | -1302.00 | -651.80 | -212.28 | -899.34 | -254.33 | -625.81 | -207.32 | -4.28 | -3.87 |
| 4 | -1302.22 | -652.22 | -212.28 | -899.54 | -254.27 | -626.33 | -207.42 | -4.36 | -4.07 |
| 5 | -1302.52 | -652.17 | -212.28 | -899.42 | -254.07 | -626.36 | -207.57 | -4.85 | -3.65 |
| 6 | -1302.80 | -652.43 | -212.28 | -899.59 | -254.48 | -626.17 | -207.44 | -4.41 | -3.84 |
| 7 | -1302.84 | -653.74 | -212.28 | -899.42 | -255.36 | -626.73 | -207.86 | -4.06 | -3.15 |
| 8 | -1302.47 | -652.46 | -212.28 | -899.33 | -254.40 | -626.85 | -207.90 | -4.93 | -3.15 |
| 9 | -1302.83 | -653.04 | -212.28 | -899.58 | -254.36 | -626.65 | -207.90 | -5.42 | -2.94 |
| 10 | -1302.69 | -652.93 | -212.28 | -899.41 | -254.40 | -626.71 | -207.92 | -5.21 | -2.95 |
| Average | -1302.32 | -652.49 | -212.28 | -899.42 | -254.42 | -626.26 | -207.59 | -4.67 | -3.49 |

Table S3. continued

| ps | EDFTPEG*solvation (eV)5) | ∆HPEG* (eV)6) | EDFTPEG_head*adsorption /# of PEG (eV/PEG)7) | EDFTPEG_chain*interaction /# of monomer (eV/monomer)8) | #H-bond9) | EDFTPEG*solvation /# of O in PEG* (eV/monomer)10) | θPEG* (ML)11) | θH2O* (ML)12) | N 13) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | -4.72 | -12.93 | -1.69 | -0.21 | 13 | -0.26 | 0.75 | 0.25 | 3 |
| 2 | -3.86 | -12.06 | -1.36 | -0.27 | 9 | -0.21 | 0.75 | 0.25 | 3 |
| 3 | -5.20 | -13.35 | -1.43 | -0.26 | 12 | -0.29 | 0.75 | 0.25 | 3 |
| 4 | -4.72 | -13.15 | -1.45 | -0.27 | 11 | -0.26 | 0.75 | 0.25 | 3 |
| 5 | -4.99 | -13.49 | -1.62 | -0.24 | 11 | -0.28 | 0.75 | 0.25 | 3 |
| 6 | -5.26 | -13.51 | -1.47 | -0.26 | 11 | -0.29 | 0.75 | 0.25 | 3 |
| 7 | -5.05 | -12.25 | -1.35 | -0.21 | 13 | -0.28 | 0.75 | 0.25 | 3 |
| 8 | -5.08 | -13.17 | -1.64 | -0.21 | 13 | -0.28 | 0.75 | 0.25 | 3 |
| 9 | -4.57 | -12.94 | -1.81 | -0.20 | 12 | -0.25 | 0.75 | 0.25 | 3 |
| 10 | -4.75 | -12.91 | -1.74 | -0.20 | 12 | -0.26 | 0.75 | 0.25 | 3 |
| Average | -4.82 | -12.98 | -1.56 | -0.23 | 11.70 | -0.27 | 0.75 | 0.25 | 3.00 |

1) Single point calculation for dissociated PEG where the structure and unit cell are from EDFTPEG/H2Ol<1ML*

2) Single point calculation for dissociated PEG where the structure is from EDFTPEG/H2Ol<1ML* in a large unit cell (no interactions between PEG)

3) EDFTPEG_head*adsorption=EDFTPEG/H2Ol<1ML*-EDFTH2Ol<1ML*-EDFTPEGgundissociated -∆EDFTPEG_chain*interaction

4) EDFTPEG_chain*interaction=EDFTPEGdissociated-the total number of dissociated PEG* in the unit cell×EDFTPEGg(dissociated)

5) EDFTPEG*solvation=EDFTPEG/H2Ol<1ML*-EDFTH2Ol<1ML*-EDFTPEG*+EDFT*

6) ∆HPEG*=EDFTPEG_head*adsorption+EDFTPEG_chain*interaction+EDFTPEG*solvation

7) EDFTPEGhead*adsorption# of PEG*=EDFTPEG_head*adsorptionthe total number of PEG* in the unit cell

8) EDFTPEGchain*interaction# of monomer=EDFTPEG_chain*interactionthe total number of the PEG* monomer in the unit cell

9) the total hydrogen bond number between PEG* and surrounding H2O(l) molecules

10) EDFTPEG*solvation# of O in PEG* =EDFTPEG*solvationthe total number of the oxygen atom in PEG* in the unit cell

11) the surface coverage of PEG* in the unit cell

12) the surface coverage of H2O* in the unit cell

13) the total number of desorbed H2O/unit cell during PEG adsorption

Table S4. Data for 1.00 ML PEG-5* on TiO2(001)

| ps | EDFTPEG/H2Ol<1ML* (eV) | EDFTH2Ol<1ML* (eV) | EDFTPEGg (undissociated) (eV) | EDFTPEG* (eV) | EDFT* (slab) (eV) | EDFTPEG (dissociated) (eV)1) | EDFTPEG(g) (dissociated) (eV)2) | EDFTPEG_head*adsorption (eV)3) | EDFTPEG_chain*interaction (eV)4) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | -1351.16 | -490.87 | -212.28 | -1113.14 | -254.76 | -838.87 | -212.08 | -4.48 | -4.77 |
| 2 | -1351.70 | -491.03 | -212.28 | -1113.07 | -254.28 | -839.25 | -212.04 | -4.18 | -5.48 |
| 3 | -1351.69 | -491.44 | -212.28 | -1113.09 | -254.30 | -839.06 | -212.00 | -4.55 | -5.11 |
| 4 | -1351.78 | -491.14 | -212.28 | -1111.98 | -253.22 | -839.15 | -211.98 | -4.72 | -4.91 |
| 5 | -1352.16 | -491.69 | -212.28 | -1112.61 | -253.59 | -839.55 | -212.01 | -5.04 | -4.84 |
| 6 | -1353.00 | -492.26 | -212.28 | -1112.30 | -253.30 | -839.49 | -211.88 | -4.59 | -5.29 |
| 7 | -1352.77 | -491.97 | -212.28 | -1111.68 | -252.95 | -839.24 | -211.99 | -5.93 | -3.67 |
| 8 | -1352.90 | -492.13 | -212.28 | -1111.48 | -252.74 | -839.17 | -211.94 | -6.07 | -3.53 |
| 9 | -1352.90 | -492.36 | -212.28 | -1111.81 | -252.95 | -839.58 | -212.01 | -5.86 | -3.87 |
| 10 | -1352.97 | -492.30 | -212.28 | -1111.79 | -252.84 | -839.57 | -212.02 | -6.03 | -3.79 |
| Average | -1352.30 | -491.72 | -212.28 | -1112.29 | -253.49 | -839.29 | -211.99 | -5.14 | -4.52 |

Table S4. continued

| ps | EDFTPEG*solvation (eV)5) | ∆HPEG* (eV)6) | EDFTPEG_head*adsorption /# of PEG (eV/PEG)7) | EDFTPEG_chain*interaction /# of monomer (eV/monomer)8) | #H-bond9) | EDFTPEG*solvation /# of O in PEG* (eV/monomer)10) | θPEG* (ML)11) | θH2O* (ML)12) | N 13) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | -1.90 | -11.15 | -1.12 | -0.24 | 9 | -0.08 | 1.00 | 0.00 | 4 |
| 2 | -1.88 | -11.54 | -1.04 | -0.27 | 9 | -0.08 | 1.00 | 0.00 | 4 |
| 3 | -1.46 | -11.12 | -1.14 | -0.26 | 8 | -0.06 | 1.00 | 0.00 | 4 |
| 4 | -1.88 | -11.51 | -1.18 | -0.25 | 6 | -0.08 | 1.00 | 0.00 | 4 |
| 5 | -1.46 | -11.34 | -1.26 | -0.24 | 7 | -0.06 | 1.00 | 0.00 | 4 |
| 6 | -1.73 | -11.60 | -1.15 | -0.26 | 7 | -0.07 | 1.00 | 0.00 | 4 |
| 7 | -2.07 | -11.67 | -1.48 | -0.18 | 8 | -0.09 | 1.00 | 0.00 | 4 |
| 8 | -2.04 | -11.64 | -1.52 | -0.18 | 8 | -0.08 | 1.00 | 0.00 | 4 |
| 9 | -1.67 | -11.40 | -1.47 | -0.19 | 6 | -0.07 | 1.00 | 0.00 | 4 |
| 10 | -1.72 | -11.54 | -1.51 | -0.19 | 6 | -0.07 | 1.00 | 0.00 | 4 |
| Average | -1.78 | -11.45 | -1.29 | -0.23 | 7.40 | -0.07 | 1.00 | 0.00 | 4.00 |

1) Single point calculation for dissociated PEG where the structure and unit cell are from EDFTPEG/H2Ol<1ML*

2) Single point calculation for dissociated PEG where the structure is from EDFTPEG/H2Ol<1ML* in a large unit cell (no interactions between PEG)

3) EDFTPEG_head*adsorption=EDFTPEG/H2Ol<1ML*-EDFTH2Ol<1ML*-EDFTPEGgundissociated -∆EDFTPEG_chain*interaction

4) EDFTPEG_chain*interaction=EDFTPEGdissociated-the total number of dissociated PEG* in the unit cell×EDFTPEGg(dissociated)

5) EDFTPEG*solvation=EDFTPEG/H2Ol<1ML*-EDFTH2Ol<1ML*-EDFTPEG*+EDFT*

6) ∆HPEG*=EDFTPEG_head*adsorption+EDFTPEG_chain*interaction+EDFTPEG*solvation

7) EDFTPEGhead*adsorption# of PEG*=EDFTPEG_head*adsorptionthe total number of PEG* in the unit cell

8) EDFTPEGchain*interaction# of monomer=EDFTPEG_chain*interactionthe total number of the PEG* monomer in the unit cell

9) the total hydrogen bond number between PEG* and surrounding H2O(l) molecules

10) EDFTPEG*solvation# of O in PEG* =EDFTPEG*solvationthe total number of the oxygen atom in PEG* in the unit cell

11) the surface coverage of PEG* in the unit cell

12) the surface coverage of H2O* in the unit cell

13) the total number of desorbed H2O/unit cell during PEG adsorption

Table S5. Data for ∆Gads of PEG-5* on TiO2(001)

| Coverage (ML) | EDFTPEG_head*adsorption (eV)1) | EDFTPEG_chain*interaction (eV)1) | EDFTPEG*solvation (eV)1) | ∆HPEG* (eV)1) | ∆ZPEPEG* (eV) | -T∆SPEG* (eV)2) | N1), 3) | H2O* desorption energy (eV/H2O) | Total H2O* desorption energy (eV)4) | ∆Gads (eV)5) | ∆Gdiff(n) (eV)6) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 0.25 | -1.99 | -0.04 | -4.98 | -7.01 | 0.17 | 2.29 | 1 | 0.08 | 0.08 | -4.47 | -4.47 |
| 0.50 | -4.26 | -1.33 | -7.34 | -12.93 | 0.34 | 4.58 | 2 | 0.08 | 0.16 | -7.85 | -3.38 |
| 0.75 | -4.67 | -3.49 | -4.82 | -12.98 | 0.50 | 6.87 | 3 | 0.08 | 0.24 | -5.37 | 2.48 |
| 1.00 | -5.14 | -4.52 | -1.78 | -11.45 | 0.67 | 9.16 | 4 | 0.08 | 0.32 | -1.30 | 4.07 |

1) the values are from Tables S1-S4 in the SI (∆HPEG*=EDFTPEG_head*adsorption+EDFTPEG_chain*interaction+EDFTPEG*solvation)
2) The values were adopted from Ref. [10] in the main text.
3) the total number of desorbed H2O*/unit cell during PEG adsorption
4) Total H2O* desorption energy = n × H2O* desorption energy
5) ∆Gads=∆HPEG*+∆ZPEPEG*-T∆SPEG*+Total H2O* desorption energy 
6) ∆Gdiffn=∆Gadsn-∆Gads(n-1), where n is the number of adsorbed PEG-5 molecules in the unit cell. Here, n = 1, 2, 3, and 4 correspond to PEG-5 coverages of 0.25, 0.50, 0.75, and 1.00 ML, respectively.

Table S6. Mean ± standard deviation of PEG adsorption free energies calculated from AIMD-sampled snapshots at different PEG coverages.

| PEG coverage (ML) | PEG* adsorption free energy (eV) |
| --- | --- |
| 0.25 | −4.60 ± 0.39 |
| 0.50 | −8.11 ± 0.25 |
| 0.75 | −5.76 ± 0.46 |
| 1.00 | −1.82 ± 0.19 |

Table S7. GPR-interpolated PEG adsorption free energies and 95% bootstrap confidence intervals at different PEG coverages

| PEG coverage (ML) | GPR-interpolated free energy (eV) | 95% bootstrap CI (eV) | CI width (eV) |
| --- | --- | --- | --- |
| 0.25 | −4.60 | [−4.83, −4.36] | 0.47 |
| 0.50 | −8.10 | [−8.25, −7.95] | 0.30 |
| 0.75 | −5.76 | [−6.03, −5.44] | 0.58 |
| 1.00 | −1.83 | [−1.94, −1.70] | 0.24 |

Table S8. Minimum of the GPR-interpolated PEG adsorption free energy profile

| Parameter | Value |
| --- | --- |
| PEG* coverage at the interpolated minimum (ML) | 0.51 |
| GPR-interpolated adsorption free energy (eV) | −8.11 |
| 95% bootstrap confidence interval (eV) | [−8.26, −7.96] |

* The minimum was identified from the GPR-interpolated free energy profile within the sampled coverage range and should not be interpreted as an independent prediction beyond the examined coverages.

Table S9. Optimized kernel and training-fit diagnostics for the GPR interpolation model

| Metric | Value |
| --- | --- |
| Optimized kernel | 0.992 × RBF(length scale = 0.10) + WhiteKernel(noise level = 0.02) |
| Training RMSE (eV) | 0.33 |
| Training R² | 0.98 |

*The GPR interpolation model yielded a training-fit R2 of 0.98 and a training RMSE of 0.33 eV. These values are reported only as fitting diagnostics for the interpolation model, not as independent predictive performance metrics.