Figure S1. FTIR spectra of adsorbents A–H corresponding to: (A) B5, (B) B10, (C) B20, (D) B40, (E) OM4, (F) OM8, (G) MRM, and (H) PM199.

The spectra show typical clay mineral bands, including O–H stretching (~3400 cm⁻¹), H–O–H bending (~1630 cm⁻¹), and Si–O stretching (~1000–1030 cm⁻¹), as well as C–H stretching bands (2920–2850 cm⁻¹) indicative of organic functionalization.

| Table S1. Physicochemical properties of the selected antibiotics. |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
|  | Structure | Molecular Mass (g/mol) | Molecular formula | pKa | Log Kw |
| AMX |  | 356.4 | C16H19N3O5S | 2.4 (carboxyl) 7.4 (amino) 9.6 (phenolic) | 0.87 |
| TMP |  | 290.3 | C14H18N4O3 | 7.12 | 0.91 |
| OFL |  | 361.4 | C18H20FN3O4 | 5.97 (carboxylic acid) 9.28 (piperizinyl ring) | -0.39 |
| CIP |  | 331.3 | C17H18FN3O3 | 6.09 (carboxylic acid group) 8.74 (nitrogen on piperazinyl ring) | 0.28 |
| TCN |  | 444.4 | C22H24N2O8 | 3.3 (enolic group) 7.7 (phenolic group) 9.7 (dimethylamino group) | -1.37 |
| SMZ |  | 253.3 | C10H11N3O3S | 1.6 (aniline group) 5.7 (sulfonamide group) | 0.89 |
| CLDM |  | 425.0 | C18H33ClN2O5S | 7.6 (amino group) | 2.16 |
| AZM |  | 749.0 | C38H72N2O12 | 8.5 (dimethylamino group) 9.5 (amine on desonamine group) | 4.02 |

| Table S2A. Chromatographic conditions for UHPLC analysis. |  |
| --- | --- |
| Parameter | Condition |
| Column | HILIC, HSS T3 (1.8 µm, 2.1 x 100 mm) |
| Column temperature | 40 °C |
| Injection volume | 10 µL |
| Flow rate | 0.25 mL min⁻¹ |
| Mobile phase A | Water + 0.2% formic acid |
| Mobile phase B | Methanol |
| Gradient program | 70% A (0–1.5 min), 60% A (3.0 min), 15% A (4.0 min), 0% A (8.0 min), returned to initial conditions (70% A) at 8.1 min and maintained until 10 min for column re-equilibration |
| Run time | 10 min |

Table S2B. Retention times, monitored ions and validation parameters of the UHPLC–MS analytical method.

|  | SIM ion (m/z) | Retention time (min) | Calibration range (mg L-1) | Regression equation | R² | LOD (mg L-1) | LOQ (mg L-1) |
| --- | --- | --- | --- | --- | --- | --- | --- |
| AMX | 349 | 1.54 | 1–10 | y = 0.0909x − 0.0294 | 0.994 | 0.05 | 0.20 |
| TMP | 291 | 2.16 | 0.1-10 | y = 1.4437x + 0.0706 | 0.992 | 0.04 | 0.13 |
| OFL | 362 | 2.60 | 2-10 | y = 0.9622x + 0.0138 | 0.993 | 0.52 | 1.58 |
| TCN | 445 | 2.93 | 0.5-10 | y = 0.3995x – 0.0132 | 0.993 | 0.10 | 0.30 |
| CIP | 332 | 3.17 | 0.5-10 | y = 0.5505x – 0.0906 | 0.994 | 0.08 | 0.25 |
| SMZ | 254 | 3.65 | 0.5-10 | y = 0.2981x – 0.0284 | 0.994 | 0.17 | 0.52 |
| AZM | 375 | 5.93 | 0.1-5 | y = 2.1751x + 0.0158 | 0.989 | 0.50 | 1.54 |
| CLDM | 425 | 6.17 | 0.1-10 | y = 1.4874x – 0.0716 | 0.997 | 0.71 | 2.20 |
| CIN | 250 | 7.01 |  |  |  |  |  |

Table S3. Kinetic models applied to describe single-component adsorption experiments. Model; Non-linear equation; Parameters; Units; References. Pseudo-first-order (PFO); qt=qe1-e-k1t; qe, 𝑘1; qe (mg g⁻¹) 𝑘1 (min⁻¹); Tran et al., 2017 Wang and Guo, 2020 Musah et al., 2022 Revellame et al., 2020 Chu et al. 2025. Pseudo-second-order (PSO); qt=qe2⋅k2t1+qek2t; qe, 𝑘2; qe (mg g⁻¹) k2 (g mg⁻¹ min⁻¹). Mixed PFO - PSO; qt=qe11-e-k1t+qe22⋅k2t1+qe2k2t; qe1, 𝑘1 qe2, 𝑘2; qe1, qe2 (mg g⁻¹) 𝑘1 (min⁻¹) k2 (g mg⁻¹ min⁻¹). Weber-Morris (WM); qt=kit1/2+C; ki, C; ki (mg g⁻¹ min⁻½) C (mg g⁻¹). Elovich (E); qt=1βln (1+αβt); α, β; α (mg g⁻¹ min⁻¹), β (g mg⁻¹). Where: qt = amount of contaminant adsorbed per unit mass of adsorbent at time t; qe = amount adsorbed at equilibrium; qe1, qe2 = adsorption capacities at equilibrium corresponding to the pseudo-first-order and pseudo-second-order mechanisms, respectively; k1 = pseudo-first-order rate constant; k2= pseudo-second-order rate constant; ki = intraparticle diffusion rate constant; C = constant related to the boundary layer thickness; α = initial adsorption rate; β = Elovich desorption constant, related to the activation energy and surface coverage.

Table S4. Non-linear adsorption isotherm models applied in this study.

| Model | Non-linear equation | Parameters | Units | References |
| --- | --- | --- | --- | --- |
| Langmuir | qe=qmaxKLCe1+KLCe | qmax, KL, Ce | qmax: (mg g⁻¹), KL: (L mg⁻¹) Ce: (mg L-1) | Ayawei et al., 2017 Mozaffari Majd et al., 2022 Murphy et al., 2023 |
| Freundlich | qe=KF Ce1/n | KF, Ce, n | KF: (mg g⁻¹) (L mg⁻¹)1/n Ce: (mg L-1) n: dimensionless |  |
| Sips (Langmuir-Freundlich) | qe=qmax(KSCe)n1+(KSCe)n | qmax, KS, n | qmax: mg g⁻¹, KS: (L mg⁻¹) n: dimensionless |  |

Where: qe = amount of contaminant adsorbed per unit mass of adsorbent at equilibrium; Ce = equilibrium concentration of the contaminant in solution; qmax = maximum adsorption capacity; KL = Langmuir constant related to the affinity of binding sites; KF = Freundlich constant related to adsorption capacity; n = heterogeneity factor; KS = Sips constant.

Table S5. Mathematical expressions of selected adsorption isotherm models applied in this study.

| Model | Mathematical expressions | References |
| --- | --- | --- |
| Original SRS model (Sheindorf–Rebhun–Sheintuch) |  | Sheindorf et al., 1981 Amrutha et al., 2023 |
| Global Freundlich model |  | Cela-Dablanca et al., 2025 |

Where:

qe,i = equilibrium adsorption capacity of component 𝑖

𝐶𝑒,i = equilibrium concentration of component 𝑖

𝐾𝐹,i = Freundlich adsorption constant for component 𝑖

𝑛i, n = heterogeneity parameter (dimensionless)

αi,𝑗  = interaction coefficient between solutes i and 𝑗, (αi,i = 1; αj,i = 1/αi,j)

𝑄𝑒,𝑇   = total adsorbed amount

𝐶𝑒,𝑇 = total equilibrium concentration

m = number of components in the system