Supplementary Information for “Constraint-aware online coarse-to-fine optimisation of crystalline silicon photovoltaic devices”

Aliaa Nabila Abdul Mutaali1, Joungha Lee1*, and Seung Beop Lee1,2,3,4*

1Department of Physical AI, Jeonbuk National University, Jeonju 54896, Republic of Korea

2School of International Engineering and Science, Jeonbuk National University, Jeonju 54896, Republic of Korea

3Institute of Applied Statistics, Jeonbuk National University, Jeonju 54896, Republic of Korea

4JBNU-Purdue Research Institute (JPRI), Jeonbuk National University, Jeonju 54896, Republic of Korea

OFAT sampling and Pearson-correlation procedure

The Pearson correlation coefficients reported in Table 1 of the main manuscript were obtained using a one-factor-at-a-time (OFAT) sensitivity analysis performed with the automated PC1D simulation framework.

For each of the nine candidate design parameters, 100 simulation cases were generated by varying only the selected parameter over its predefined screening range, while all remaining parameters were maintained at their baseline values. The resulting open-circuit voltage (Voc), short-circuit current density (Jsc), and fill factor (FF) were extracted from each simulation.

For each parameter, the Pearson correlation coefficients between the sampled parameter values and the corresponding photovoltaic performance metrics were then calculated using the standard Pearson correlation formula. This procedure was repeated independently for each candidate parameter. The resulting correlation coefficients were subsequently used to compute the joint-sensitivity score Sp according to Eq. (1) in the main manuscript.

Supplementary Table S1. Baseline device-model parameters and simulation settings used for virtual-device construction.

| Baseline device and simulation parameters | Baseline value | Unit |
| --- | --- | --- |
| Device Area | 1 | cm2 |
| Front Surface Charge | 10.0×1012 | cm-2 |
| Front Surface Coat Thickness | 75 | nm |
| Front Surface Coat Index | 2.01 | - |
| Emitter Distance | 0.3 | µm |
| Front Texture Angle | 54.74 | º (degrees) |
| Device Base Contact | 0.5 | Ω |
| Device Internal Conductor | 10.0×10-5 | S |
| Front Texture Depth | 3 | µm |
| Dielectric Constant | 11.9 | - |
| Band Gap | 1.124 | eV |
| Free Carrier Absorption | Enabled | - |
| Intrinsic carrier concentration at 300 K | 1.0E10 | cm-3 |
| Diffusion Length | 56 | µm |
| Base Thickness | 56 | µm |
| Substrate Thickness | 500 | µm |
| Front Surface Recombination Velocity | 1.0×105 | cm/s |
| Rear Surface Recombination Velocity | 1.0×105 | cm/s |
| Base Bulk Recombination | 1000 | µs |
| Excitation Mode | One-sun transient simulation with 16 time steps | - |
| Base Circuit sweep | Sweep from -0.8 to 0.8 V | - |
| Internal/External optical reflectance | 10 | % |
| Collector Circuit | Zero | - |
| Constant Intensity | 0.1 | W/cm² |
| Spectrum | AM 1.5G | - |
| Temperature | 25 | °C |
| Background Doping Concentration | 6.0×1016 | cm-3 |

Supplementary Table S2. Exact sampled values used in the PC1D coarse-grid search, local refinement, and one-dimensional sweeps.

Panel A. PC1D coarse-grid values

| Variable | Exact coarse-grid values | Number of levels |
| --- | --- | --- |
| t | 30, 40, 50, 60, 70, 80, 90, 100, 110, 120 μm | 10 |
| T | 285, 290, 295, 300, 305, 310, 315, 320, 325, 330 K | 10 |
| ND | 5.0, 5.2, 5.4, 5.6, 5.8, 6.0, 6.2, 6.4, 6.6, 6.8 ×1016 cm−3 | 10 |
| Sf | 500, 900.824, 1622.968, 2924.018, 5268.051, 9491.175, 17099.759, 30807.751, 55504.731, 100000 cm/s | 10 |
| Sr | 500, 900.824, 1622.968, 2924.018, 5268.051, 9491.175, 17099.759, 30807.751, 55504.731, 100000 cm/s | 10 |

Panel B. PC1D local-refinement values

| Variable | Local-refinement levels |
| --- | --- |
| t | 30, 33, 36 μm |
| T | 285, 286, 287 K |
| ND | 6.70, 6.75, 6.80 ×1016 cm−3 |
| Sf | 500, 600, 700 cm/s |
| Sr | 500, 600, 700 cm/s |

Panel C. One-dimensional sweep settings

| Variable | Lower bound | Upper bound | Interval or spacing | Number of points |
| --- | --- | --- | --- | --- |
| t | 3 μm | 75 μm | 3 μm | 25 |
| T | 270 K | 298 K | 1 K | 29 |
| ND | 6.0×1016 cm−3 | 7.5×1016 cm−3 | 5.0×1014 cm−3 | 31 |
| Sf | 1 cm/s | 1.0×104 cm/s | Piecewise logarithmic | 25 |
| Sr | 1 cm/s | 1.0×104 cm/s | Piecewise logarithmic | 25 |

For Sf and Sr, each sweep combines 13 logarithmically spaced points from 1 to 500 and 13 from 500 to 10,000 cm/s, with the shared value of 500 counted once, giving 25 points.

Supplementary Table S3. Representative local PC1D refinement configurations used to identify the refined optimal case.

| Case | Design Variables |  |  |  |  | Performances |  |  | Objective Function |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | t [µm] | T [K] | ND [cm-3] | Sf [cm/s] | Sr [cm/s] | Voc [V] | Jsc [mA/cm2] | FF | η [%] |
| H-1 | 30 | 285 | 6.70E16 | 500 | 500 | 0.6661 | 32.0721 | 0.8193 | 17.5043 |
| H-2 | 30 | 285 | 6.70E16 | 500 | 600 | 0.6661 | 32.0682 | 0.8193 | 17.5002 |
| H-3 | 30 | 285 | 6.70E16 | 500 | 700 | 0.6660 | 32.0642 | 0.8193 | 17.4961 |
| : | : | : | : | : | : | : | : | : | : |
| H-89 | 33 | 285 | 6.70E16 | 700 | 600 | 0.6646 | 32.1480 | 0.8191 | 17.5012 |
| H-90 | 33 | 285 | 6.70E16 | 700 | 700 | 0.6645 | 32.1440 | 0.8191 | 17.4973 |
| H-91* | 33 | 285 | 6.75E16 | 500 | 500 | 0.6649 | 32.1566 | 0.8196 | 17.5249 |
| H-92 | 33 | 285 | 6.75E16 | 500 | 600 | 0.6649 | 32.1526 | 0.8196 | 17.5209 |
| H-93 | 33 | 285 | 6.75E16 | 500 | 700 | 0.6648 | 32.1487 | 0.8196 | 17.5169 |
| : | : | : | : | : | : | : | : | : | : |
| H-241 | 36 | 287 | 6.80E16 | 700 | 500 | 0.6594 | 32.2099 | 0.8175 | 17.3642 |
| H-242 | 36 | 287 | 6.80E16 | 700 | 600 | 0.6594 | 32.2059 | 0.8175 | 17.3604 |
| H-243 | 36 | 287 | 6.80E16 | 700 | 700 | 0.6593 | 32.2020 | 0.8175 | 17.3566 |

*Refined optimal configuration identified by local high-resolution refinement. Blue entries indicate configurations satisfying all imposed constraints

Case representation and decision rules

Each simulation case k is represented by the following structured case record:

where

is the design-variable vector,

is the corresponding performance vector, and

After the first feasible case has been identified, the current best feasible design following k evaluations is updated as

Each component of xk is constrained to the corresponding admissible range specified in Table 2 of the main manuscript.

The optimization workflow applies the following decision rules throughout the design exploration process:

- The joint-sensitivity score Sp is computed for each candidate parameter using Eq. (1) in the main manuscript.

- A candidate parameter is retained as an effective design variable only when Sp ≥ 0.90, indicating that its absolute Pearson correlation coefficient is at least 0.90 for each of Voc, Jsc and FF.

- Parameters that do not satisfy the criterion are not retained as effective design variables and are maintained at their baseline values throughout the subsequent search.

- The retained design variables are explored using the hierarchical coarse-to-fine sampling strategy described in the main manuscript.

- The SCAPS-1D assessment independently performs reduced-resolution coarse exploration and constraint-enforced local refinement, after which the independently derived refined configuration is compared with the PC1D-derived refined configuration.

Computational-cost estimation

The full-domain comparison grid retained the local linear increments for t, T, and ND and used 32 logarithmically spaced levels for each of Sf and Sr. The surface-recombination grids were specified for computational-cost estimation and do not represent an exact extension of the local additive sampling intervals. The resulting full-domain variable-specific discretization scheme is summarized in Supplementary Table S5. The corresponding measured and estimated computation times are summarized in Supplementary Table S4. Under these assumptions, the total number of possible design configurations is obtained from Eq. (10) in the main manuscript. The estimated execution time was calculated using the measured average PC1D simulation time of approximately 1.1 s per case, assuming sequential execution without parallel processing.

Supplementary Table S4. Measured and estimated computation times for the implemented searches and hypothetical full-domain fine-grid scenarios.

| Search or assessment | Number of configurations | Average time per case | Total serial computation time | Basis |
| --- | --- | --- | --- | --- |
| Implemented PC1D coarse-to-fine search | 100,243 | 1.1 s | 110,267 s, approximately 30.6 h | Measured |
| Implemented SCAPS-1D coarse and refined search | 1,011 | 60 s | 60,660 s, approximately 16.9 h | Measured |
| Illustrative 20-level full-domain grid | 3,200,000 | 1.1 s | 3.52×106 s, approximately 40.7 days | Estimated |
| Full-domain variable-specific fine-sampling extrapolation | 54,028,288 | 1.1 s | 5.94×107 s, approximately 687.9 days | Estimated |

The hypothetical full-domain searches were not executed. The assumed per-case time was set equal to the measured average PC1D serial execution time. All estimates assume sequential execution without parallel processing.

Supplementary Table S5. Full-domain variable-specific fine-sampling definitions used for computational-cost extrapolation.

| Design variable | Full admissible range | Sampling definition | Number of levels |
| --- | --- | --- | --- |
| t | 30–120 μm | Δt=3 μm | 31 |
| T | 285–330 K | ΔT=1 K | 46 |
| ND | 5.0×1016 cm−3–6.8×1016 cm−3 | Δ ND =5.0×1014 cm−3 | 37 |
| Sf | 500–100000 cm/s | Logarithmic spacing | 32 |
| Sr | 500–100000 cm/s | Logarithmic spacing | 32 |

Both lower and upper bounds are included. The resulting full-factorial grid contains 31×46×37×32×32=54,028,288 configurations

Supplementary Algorithm S1. Automated PC1D-based coarse-to-fine optimization workflow

The proposed workflow consists of a preliminary variable-selection stage followed by an automated PC1D-based hierarchical optimization procedure. Variable selection is performed before the PC1D optimisation loop, whereas the SCAPS-1D cross-solver assessment is performed independently afterwards. The complete procedure is summarized in Algorithm S1.

1. Input: Candidate design variable set Parameter bounds PC1D device model Performance constraints Objective function 2. Step 1: Joint-sensitivity screening FOR each candidate parameter Vary the selected parameter Keep remaining parameters at baseline values Perform PC1D simulations Extract Voc, Jsc and FF Calculate Pearson correlation coefficients Calculate joint-sensitivity score Sp END FOR Retain each parameter satisfying Sp ≥ 0.90 (threshold) Fix remaining parameters at baseline values 3. Step 2-1: Global coarse-grid search Generate all combinations of selected design variables Initialize candidate optimal case FOR each generated design case Assign design variable values Construct PC1D device model Execute PC1D simulation Extract performance indicators Evaluate objective function Check design constraints IF case satisfies constraints Store case in feasible dataset IF objective value improves Update candidate optimal case END IF ELSE Store case in infeasible dataset END IF END FOR

4. Step 2-2: Local high-resolution refinement Define refined search region around candidate optimal case Generate high-resolution design combinations Repeat PC1D evaluation and constraint handling Identify and store the PC1D-derived refined optimal case 5. Step 3: Independent SCAPS-1D cross-solver assessment Generate the reduced-resolution SCAPS-1D coarse grid Evaluate all coarse cases and record their feasibility status Select the highest-efficiency coarse case as the refinement reference, irrespective of its feasibility status Generate a local refined grid around the coarse reference case Evaluate all refined SCAPS-1D cases Identify the highest-efficiency feasible case as the SCAPS-derived refined optimal case Compare the SCAPS- and PC1D-derived refined configurations 6. Output/Return: PC1D-derived refined optimal case SCAPS-derived refined optimal case Cross-solver comparison of design-variable settings and performance indicators