Iridium-Ruthenium Oxide for the Oxygen Evolution Reaction: Correlation between Calcination Temperature–Morphology–Activity Interplay

Claudelle Sybilline Anensong Djadock a*, Anele Nzimeni a, Shawn Gouws a*

a Department of Chemistry, Nelson Mandela University, Summerstrand, Gqeberha, 6001, South Africa

Corresponding author: shawn.gouws@mandela.ac.za

Figure S1. Powder XRD patterns of IrRuOx samples. Phase indices are shown for the rutile unit cell.

Figure S2. SEM images of catalyst@350

Figure S3. SEM images of catalyst@400

Figure S4. SEM images of catalyst@450

Figure S5. SEM images of catalyst@500

Figure S6. SEM images of catalyst@520

(a)

(b)

Figure S7. EDS elemental mapping images of IrRuOx at 350 °C (a) and 450 °C (b)

Figure S8. Cyclic voltammograms of IrRuOx@350 °C (1) and IrRuOx@400 °C (2), IrRuOx@450 °C (3), IrRuOx@500 °C (4), and IrRuOx@520 °C (5) in 0.5 M H2SO4 under N2 atmosphere at a scan rate of 50-600 mV/s

Table S1: Electrochemical data of IrRuOx@T recorded at a scan rate of 5 mV/s in 0.5 M H2SO4.

| Electrocatalysts | Means of crystalline sizes (nm) | ɳ@10 (mV vs RHE | Tafel Potential (mV/dec) | Cdl (F/cm2) | ECSA (cm2) | Mass loading (g) |
| --- | --- | --- | --- | --- | --- | --- |
| IrRuOx@350 oC | 16.3 | 251 | 68.97 | 2.75 | 78.57 | 0.0035±0.001 |
| IrRuOx@400 oC | 18.09 | 242 | 45.47 | 20.03 | 572.29 | 0.0010±0 |
| IrRuOx@450 oC | 20.7 | 335 | 58.60 | 32.23 | 920 | 0.0019±0.0001 |
| IrRuOx@500 oC | 22.25 | 220 | 24.41 | 31.63 | 903.71 | 0.0038±0.001 |
| IrRuOx@520oC | 16.04 | 254 | 42.70 | 0.63 | 18 | 0.0041±0.001 |

Figure S9. Before and after LSV curves of IrRuOx@350 °C (1) and IrRuOx@400 °C (2), IrRuOx@450 °C (3), IrRuOx@500 °C (4), and IrRuOx@520 °C (5) in 0.5 M H2SO4 under N2 atmosphere at a scan rate of 5 mV/s