Table S1. Measured density, theoretical density, and measured-to-theoretical density ratio of the L-DED Al–7Mg-based alloys.
	Alloys 
	Measured density 
(g/cm3)
	Theoretical density
(g/cm3)
	Measured density / Theoretical density

	 Al-7Mg
	2.576±0.022
	2.624
	0.982

	 Al-7Mg-0.2Sc-0.5Zr
	2.643±0.004
	2.638
	1.002

	 Al-7Mg-0.4Sc-0.5Zr
	2.649±0.006
	2.631
	1.006

	 Al-7Mg-2Zn-0.5Zr
	2.660±0.015
	2.651
	1.003

	 Al-7Mg-4Zn-0.5Zr
	2.683±0.012
	2.672
	1.004
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