Table S1. Measured density, theoretical density, and measured-to-theoretical density ratio of the L-DED Al–7Mg-based alloys.

| Alloys | Measured density (g/cm3) | Theoretical density (g/cm3) | Measured density / Theoretical density |
| --- | --- | --- | --- |
| Al-7Mg | 2.576±0.022 | 2.624 | 0.982 |
| Al-7Mg-0.2Sc-0.5Zr | 2.643±0.004 | 2.638 | 1.002 |
| Al-7Mg-0.4Sc-0.5Zr | 2.649±0.006 | 2.631 | 1.006 |
| Al-7Mg-2Zn-0.5Zr | 2.660±0.015 | 2.651 | 1.003 |
| Al-7Mg-4Zn-0.5Zr | 2.683±0.012 | 2.672 | 1.004 |