Bridging Chemically Distinct Coating Systems: Cross-System Transfer Learning Enables Discovery of Ultralow-Thermal-Conductivity Ferroelastic Tantalates

Yiwei Wei1, 2, 3, Jingjin He1, 2, 3,*, Yang Lin1, 2, 3, Shun-Li Shang4, Fuyang Tian5, Zulai Li1, 2, 3, Yehua Jiang1, 2, 3, Zi-Kui Liu4, Jing Feng1, 2, 3, Xiaoyu Chong1, 2, 3,*

1Faculty of Materials Science and Engineering, Kunming University of Science and Technology, Kunming 650093, China

2National-Local Joint Engineering Research Center for Technology of Advanced Metallic Solidification Forming and Equipment, Kunming 650093, China

3Yunnan Provincial Key Laboratory of Intelligent Technology for New Materials, Kunming 650093, China

4Department of Materials Science and Engineering, The Pennsylvania State University, University Park, PA 16802, USA

5Institute for Applied Physics, University of Science and Technology Beijing, Beijing 100083, China

*Corresponding authors, E-mail: hejingjin@kust.edu.cn (Jingjin He);

xiaoyuchong@kust.edu.cn (Xiaoyu Chong)

Figure S1. (a) Components distribution of RETaO₄ dataset. (b)Elements distribution of RETaO₄ dataset.

Figure S2. Heatmap of features correlation.

Figure S3. Scatter plot of each feature against target variable (a)m*, (b)r*, (c)MP, (d)rA/rB, (e)Z-eff-C, (f)FIE, (g)B, (h)IA-B

Figure S4. Comparison of model performance (a)GBRT, (b)Xgboost, (c)SVR, (d)RF, (e)LR, (f)RR, (g)Adaboost, (h)LASSO, (i)Bar chart of model performance comparison

Figure S5. Thermal conductivity distribution characteristics of multi-system data sets (a) Distribution of thermal conductivity for different systems at 900°C (b) Histogram of thermal conductivity distribution (c) Thermal conductivity-temperature distribution plot.

Figure S6. Comparison of pre-training performance across different source-domain models. (a)-(c) Cross-validation performance of 3-, 4-, and 5-layer source-domain models; (d)-(f) Direct prediction performance of the source-domain models on the RETaO4 test set.

Figure S7. Comparison of performance across different transfer learning fine-tuning strategies. (a)-(c) Cross-validation performance of PFT, BFT, and LFT models; (d)-(f) Prediction performance of the transfer learning models on the RETaO4 test set.

Figure S8. (a) 10-fold cross-validation performance of a 4-layer deep neural network model trained directly using the of a RETaO4 small dataset (b) Performance on an independent test set.

Figure S9. XRD refinement patterns and XPS high-resolution spectra of 5–8RE. XRD refinement pattern of (a) 5RE; (b) 6RE; (c) 7RE; (d) 8RE (e) XPS survey spectrum (f) High-resolution XPS O 1s spectra.

Figure S10. SEM-EDS patterns of 5RE–8RE.

Figure S11. XRD patterns of 5RE_eq – 8RE_eq.

Figure S12. Coefficient of Thermal Expansion of the Sample in This Work.

Table S1. A brief description of features and symbols.

| Features | Symbols |
| --- | --- |
| Temperature | T |
| Atomic number | N |
| Atomic weight | W |
| Row | R |
| Column | C |
| Density | ρ |
| Melting Point | MP |
| Bulk modulus | B |
| Mass disorder parameter | m* |
| Electronegativity (Pauling) | χp |
| Electronegativity (Alfred & Rochow) | χar |
| Electronegativity (Martynov & Batsanov) | χmb |
| First ionization energy | FIE |
| Electron affinity | Ea |
| Effective nuclear charge (Clementi) | Z-eff-C |
| Effective nuclear charge (Slater) | Z-eff-S |
| Charge radius ratio | z/r |
| Ionic bond strength | IA-B |
| The radius of cations in RE/Ta site | rA/rB |
| Radius disorder parameter | r* |
| Covalent Radius | CR |

Table S2. Nine groups of highly correlated descriptors and the ones retained.

| Highly correlated features | Retained |
| --- | --- |
| N, W, R, ρ, m*, χmb | m* |
| C, CR, z/r, r*, Z-eff-S | r* |
| Ea, FIE | FIE |
| rA/rB, χar | rA/rB |
| IA-B, χp | IA-B |
| Z-eff-C | Z-eff-C |
| MP | MP |
| B | B |
| T | T |

Table S3. Thermal conductivity distribution characteristics of multi-system data sets

| Total Data | Material Types | Thermal Conductivity Range (W·m⁻¹·K⁻¹) | Temperature Range (℃) |
| --- | --- | --- | --- |
| 872 | 95 | 0.905~3.962 | 25~1500 |

Table S4. Performance Comparison of Different Machine Learning Modeling Strategies

| Modeling Strategy | Description | Cross-Validation R² | Independent Test Set R2 |
| --- | --- | --- | --- |
| GBRT | Trained a GBRT model based on the RETaO4 dataset. | 0.950 | 0.832 |
| Source Domain Model | Modeled based on multi-material system datasets and directly predicted the RETaO4 independent test set. | 0.823 | 0.420 |
| DNN | Trained a deep neural network model based on the RETaO4 dataset. | 0.942 | 0.870 |
| PFT | Froze the bottom layer of source domain model and fine-tuned the other layers. | 0.947 | 0.904 |
| BFT | Froze the first two layers of source domain model and fine-tuned the other layers. | 0.942 | 0.909 |
| LFT | Froze the first three layers of source domain model and fine-tuned the last layer. | 0.917 | 0.896 |

Table S5. Details of the Composition Space

| Number of Components | Count |
| --- | --- |
| 5 | 99792 |
| 6 | 116424 |
| 7 | 66528 |
| 8 | 17820 |
| Total | 300,564 |

Table S6. Comparison of feature ranges for the RETaO₄ dataset, composition space, and multi-system dataset.

|  | Range of Z-eff-C | Range of IA-B |
| --- | --- | --- |
| RETaO4 Dataset | 5.265-5.497 | 0.657-0.677 |
| Composition Space | 5.248-5.586 | 0.655-0.678 |
| Multi-system Dataset | 4.823-6.237 | 0.556-0.736 |

Table S7. Lattice constants (a, b and c), β, volumes (V) and theoretical densities (ρcal) of 5RE, 6RE, 7RE and 8RE obtained from Rietveld refinement results.

| Samples | a (Å) | b (Å) | c (Å) | β (°) | V (Å3) | ρcal (g/cm3) |
| --- | --- | --- | --- | --- | --- | --- |
| 5RE | 5.3958 | 11.0563 | 5.0765 | 95.4801 | 301.4651 | 7.3547 |
| 6RE | 5.3996 | 11.0593 | 5.0769 | 95.5111 | 301.7676 | 7.3473 |
| 7RE | 5.3802 | 11.0292 | 5.0713 | 95.4522 | 299.5627 | 7.4014 |
| 8RE | 5.3781 | 11.0235 | 5.0685 | 95.4749 | 299.1177 | 7.4124 |

Table S8. Mean acoustic velocity (vm/m·s−1), Young’s modulus (E/GPa), Bulk modulus (B/GPa), shear modulus (G/GPa), Grüneisen parameter (γ), Poisson ratio (σ) and Debye temperature (θD/K) of 5RE – 8RE.

| Samples | vl | vt | vm | E | B | G | G/B | γ | σ | θD |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 5RE | 4553 | 2469 | 2755 | 116 | 93 | 45 | 0.48 | 1.72 | 0.29 | 354 |
| 6RE | 4637 | 2367 | 2651 | 108 | 103 | 41 | 0.40 | 1.93 | 0.32 | 339 |
| 7RE | 4553 | 2430 | 2714 | 111 | 93 | 43 | 0.46 | 1.78 | 0.30 | 348 |
| 8RE | 4933 | 2631 | 2939 | 133 | 112 | 51 | 0.46 | 1.78 | 0.30 | 377 |

Table S9. Comparison of thermal conductivity between samples in this work and previously reported works

| Samples | Thermal conductivity at 900 °C (W·m-1·K-1) |
| --- | --- |
| Y0.40Ce0.10Sm0.30Gd0.10Er0.10TaO4 - This work | 1.276 |
| Sm0.4Eu0.4Tb0.4Dy0.4Lu0.4ZrCeO7 | 1.305 |
| Y0.30Ce0.10Sm0.10Eu0.10Gd0.10Dy0.10Ho0.10Yb0.10TaO4 - This work | 1.307 |
| Y0.1Nd0.1Sm0.1Gd0.1Dy0.1Ho0.1Er0.1Tm0.1Yb0.1Lu0.1TaO4 | 1.322 |
| Y0.40Ce0.10Sm0.10Eu0.10Gd0.10Dy0.10Yb0.10TaO4 - This work | 1.341 |
| Y0.5Gd0.5TaO4 | 1.388 |
| Y1/8Ce1/8Sm1/8Eu1/8Gd1/8Dy1/8Ho1/8Yb1/8TaO4 - 8RE_eq | 1.433 |
| Sm1/8Dy1/8Ho1/8Er1/8Yb1/8Lu1/8Gd1/8Tm1/8Nb0.5Ta0.5O4 | 1.470 |
| Y0.40Ce0.10Sm0.20Eu0.10Gd0.10Dy0.10TaO4-This work | 1.470 |
| Y1/5Ce1/5Sm1/5Gd1/5Er1/5TaO4 - 5RE_eq | 1.491 |
| Y0.5Yb0.5TaO4 | 1.514 |
| YTa0.5Nb0.5O4 | 1.575 |
| La0.4Nd0.4Sm0.4Eu0.4Gd0.4Zr2O7 | 1.671 |
| Y1/6Ce1/6Sm1/6Eu1/6Gd1/6Dy1/6TaO4 - 6RE_eq | 1.680 |
| Y0.2Dy0.2Sm0.2Yb0.2Er0.2TaO4 | 1.689 |
| SmTaO4 | 1.698 |
| Y1/7Ce1/7Sm1/7Eu1/7Gd1/7Dy1/7Yb1/7TaO4 - 7RE_eq | 1.706 |
| La2Zr2O7 | 1.733 |
| YTaO4 | 1.793 |
| Sm0.2Dy0.2Ho0.2Er0.2Yb0.2NbO4 | 1.812 |
| Nd0.2Sm0.2Eu0.2Gd0.2Dy0.2TaO4 | 1.812 |
| DyTaO4 | 1.834 |
| Nd1/6Sm1/6Eu1/6Gd1/6Dy1/6Ho1/6TaO4 | 1.887 |
| MgTa2O6 | 1.912 |
| Dy2FeTaO7 | 1.927 |
| Sm1/7Dy1/7Ho1/7Er1/7Yb1/7Lu1/7Gd1/7TaO4 | 2.016 |
| Sm1/8Dy1/8Ho1/8Er1/8Yb1/8Lu1/8Gd1/8Tm1/8TaO4 | 2.087 |
| AlTaO4 | 2.352 |

Table S10. Key parameters of 5RE for Debye-Callaway modeling

| Parameters | Notes | Values |
| --- | --- | --- |
| θD | Acoustic mode Debye temperature | 354 K |
| V | Average atomic volume | 6.28 × 10-30 m3 |
| M | Average atomic mass | 1.10 × 10-25 kg |
| γ | Grüneisen parameter | 1.72 |
| dGB | Grain size | 29.4 μm |
| dDB | Domain boundary width | 25.4 nm |
| A | Domain boundary fitting parameter | 0.1 |
| Γ | Point defect scattering parameter | 0.29 |
| ND | Dislocation density | 1.04 × 1010 cm-2 |
| BD | Magnitude of Burgers vector | 0.47 nm |
|  | Poisson's ratio | 0.34 |
| vL | Longitudinal sound velocity | 4553 m/s |
| νT | Transverse sound velocity | 2469 m/s |
| ν | Average speed of sound | 2755 m/s |
| D | Mass density | 7315 kg/m3 |