Figure S1: Temperature and Energy Fluctuation profiles

Figure S2: Blending Analysis Mixing Energy:

Figure S3: Mesodyne mesoscopic simulated cell for miscible and immiscible polymer composition for as per density distribution

Table S1:

Computed Florry Huggins Interaction parameter at 298K temperature for various polymer compositions and simulated densities

| Simulations Run case. | Polymer-chain Composition in cell | SMA % wt.wt | Density g/cm3 | Chi Parameter Xi at 298K | Compatibility |
| --- | --- | --- | --- | --- | --- |
| 1 | 1PSMA chain | 100 | 1.086 | N/A | N/A |
| 2 | 12:88 (PSF:PSMA) | 88 | 1.079 | 11.146 | Incompatible |
| 3 | 25:75 (PSF:PSMA) | 75 | 1.086 | 12.203 | Incompatible |
| 4 | 34:66 (PSF:PSMA) | 66 | 1.095 | -4.460 | Compatible |
| 5 | 50:50 (PSF:PSMA) | 50 | 1.185 | 5.014 | Incompatible |
| 6 | 66:34 (PSF:PSMA) | 34 | 1.204 | 13.874 | Incompatible |
| 7 | 75:25 (PSF:PSMA) | 25 | 1.210 | 49.945 | Incompatible |
| 8 | 88:12 (PSF:PSMA) | 12 | 1.22 | 29.740 | Incompatible |
| 9 | 1 PSF chain | 0 | 1.25 | N/A | N/A |

Using Schneier Equation; - Polymers compatibility prediction

Table and figures are showing in summary for other polymers compatibility state with SMA and PMMA additives respectively using Schneier Enthalpy of mixing theory at 298K

Table S2: Compatibility of other polymers with SMA and PMMA by theories

| POLYMER | POLYMER PROPERTIES |  |  | SMA | PMMA |
| --- | --- | --- | --- | --- | --- |
|  | Density (g/ml) | Mol. Weight (g/mol) | Sol. Param.(cal/cm3) | COMPATIBILITY | COMPATIBILITY |
| PMMA | 1.18 | 100.12 | 9.29 | Compatible | - |
| SMA | 1.08 | 202.212 | 9.4 | - | Compatible |
| PSF | 1.24 | 442.52 | 9.63 | Compatible | Compatible |
| SPSF | 1.1 | 462 | 10.1219 | Compatible < 20% | Incompatible |
| PVDF | 1.78 | 64.034 | 9.02 | Partially Compatible | Compatible |
| PVDF-2* | 1.78 | 64.034 | 11.4 | Incompatible | Incompatible |
| PVA | 1.26 | 44.053 | 12.64 | Incompatible | Incompatible |
| PVA-2* | 1.3 | 44.053 | 15.2 | Incompatible | Incompatible |
| PES | 1.37 | 232.25 | 11.306 | Compatible <10% | Compatible <18% |
| PVC | 1.38 | 62.5 | 9.5 | Compatible | Compatible |
| PEEK | 1.26 | 288.31 | 10.71 | Compatible < 20% | Incompatible |
| NYLON 6,6 | 1.14 | 226.3 | 13.7 | Incompatible | Incompatible |
| EVOH 27 | 1.2 | 46.87 | 11.29 | Compatible < 15% | Incompatible |
| EVOH32 | 1.19 | 72.107 | 11.052 | Compatible < 9% | Incompatible |
| EVOH38 | 1.17 | 72.107 | 10.759 | Compatible < 20% | Incompatible |
| EVOH 44 | 1.14 | 60.09 | 10.46 | Compatible < 30% | Incompatible |

-2* - Change in solubility parameter of the polymer depend on manufacturer set

SPSF/SMA					SPSF/PMMA

PVDF / SMA					PVDF / PMMA

PVDF-2*/SMA				PVDF-2*/PMMA

PVA / SMA					PVA / PMMA

PVA-2*/SMA					PVA-2*/PMMA

PES / SMA					PES / PMMA

PVC / SMA					PVC / PMMA

PEEK / SMA					PEEK / PMMA

Nylon 6,6 / SMA				Nylon 6,6 / PMMA

EVOH 27/SMA					EVOH 27/PMMA

EVOH 32/ SMA				EVOH 32/ PMMA

EVOH 38/ SMA				EVOH 38/ PMMA

EVOH 44/ SMA					EVOH 44/ PMMA