Supporting Information

Solvothermal Engineering: A Universal Route to High-Performance Free-standing PEDOT:PSS Thick Films

Jiawei Wu,a Wanying Zhang,a,b Zhen Su,*a Tao Chen,a Wentao Wang,*b Jiayi Zeng,a Yingzhi Jin,a Jiaxing Song,a Lin Hu,a Xinxing Yin,a Erjun Zhou,a Zaifang Li*a

The following files including:

Table S1 The polarity, boiling point, and Hansen solubility parameters of MeOH, DMF, and DMSO

Table S2 The reaction time and pressure of sample treated with MeOH

Table S3 The reaction time and pressure of sample treated with DMF

Table S4 The reaction time and pressure of sample treated with DMSO

Table S5 The thickness, sheet resistance, and conductivity of MeOH-30, MeOH-50, MeOH-60, and MeOH-80

Table S6 The thickness, sheet resistance, and conductivity of DMF-80, DMF-100, DMF-120, and DMF-140

Table S7 The thickness, sheet resistance, and conductivity of DMSO-80, DMSO-100, DMSO-120, and DMSO-140

Figure S1 The correlation plot of pressure vs. conductivity

Figure S2 Cross-sectional images of (a) untreated PEDOT:PSS films, (b) MeOH-80, (c) DMF-100, and (d) DMSO-100

Figure S3 AFM images of PH1000, MeOH-80, DMF-100, and DMSO-100

Figure S4 Specific capacitances at different scan rates of our electrodes compared with previously reported PEDOT:PSS electrodes.

Table S1 The polarity, boiling point, and Hansen solubility parameters of MeOH, DMF, and DMSO.

| Materials | Boiling Point | Polarity | Hansen solubility parameters | Matching Degree (with PEDOT:PSS) |
| --- | --- | --- | --- | --- |
| MeOH | 64.7 | 32.6 | δd=15.1 | Poor |
|  |  |  | δp=12.3 |  |
|  |  |  | δh=22.3 |  |
| DMF | 153 | 38.3 | δd=17.4 | Good |
|  |  |  | δp=13.7 |  |
|  |  |  | δh=11.3 |  |
| DMSO | 189 | 46.7 | δd=18.4 | Excellent |
|  |  |  | δp=16.4 |  |
|  |  |  | δh=10.2 |  |
| PEDOT:PSS | / | 10-15 | δd=18.0 | / |
|  |  |  | δp=16.0 |  |
|  |  |  | δh=10.0 |  |

Table S2 The reaction time and pressure of sample treated with MeOH.

| Sample | MeOH-30 | MeOH-50 | MeOH-60 | MeOH-80 |
| --- | --- | --- | --- | --- |
| Time (h) | 6 | 6 | 6 | 6 |
| Pressure (MPa) | 0.020 | 0.025 | 0.03 | 0.04 |

Table S3 The reaction time and pressure of sample treated with DMF.

| Sample | DMF-80 | DMF-100 | DMF-120 | DMF-140 |
| --- | --- | --- | --- | --- |
| Time (h) | 6 | 6 | 6 | 6 |
| Pressure (MPa) | 0.020 | 0.025 | 0.040 | 0.065 |

Table S4 The reaction time and pressure of sample treated with DMSO.

| Sample | DMSO-80 | DMSO-100 | DMSO-120 | DMSO-140 |
| --- | --- | --- | --- | --- |
| Time (h) | 6 | 6 | 6 | 6 |
| Pressure (MPa) | 0.020 | 0.023 | 0.025 | 0.026 |

Table S5 The thickness, sheet resistance, and conductivity of MeOH-30, MeOH-50, MeOH-60, and MeOH-80.

| Sample | Thickness (μm) | Rsq (Ω sq-1) | Conductivity (S cm-1) |
| --- | --- | --- | --- |
| MeOH-30 | 3.60±0.03 | 1.18±0.10 | 2352±5 |
| MeOH-50 | 3.641±0.03 | 1.09±0.11 | 2635±110 |
| MeOH-60 | 3.691±0.04 | 1.12±0.13 | 2570±149 |
| MeOH-80 | 3.637±0.06 | 1.02±0.09 | 2698±260 |

Table S6 The thickness, sheet resistance, and conductivity of DMF-80, DMF-100, DMF-120, and DMF-140.

| Sample | Thickness (μm) | Rsq (Ω sq-1) | Conductivity (S cm-1) |
| --- | --- | --- | --- |
| DMF-80 | 3.715±0.04 | 1.40±0.02 | 1850±48 |
| DMF-100 | 3.770±0.02 | 1.30±0.03 | 2150±350 |
| DMF-120 | 3.708±0.05 | 1.60±0.05 | 1580±13 |
| DMF-140 | 3.705±0.02 | 1.68±0.02 | 1558±31 |

Table S7 The thickness, sheet resistance, and conductivity of DMSO-80, DMSO-100, DMSO-120, and DMSO-140.

| Sample | Thickness (μm) | Rsq (Ω sq-1) | Conductivity (S cm-1) |
| --- | --- | --- | --- |
| DMSO-80 | 3.959±0.04 | 1.17±0.02 | 2188±29 |
| DMSO-100 | 3.523±0.02 | 1.27±0.11 | 2294±144 |
| DMSO-120 | 3.681±0.04 | 1.51±0.07 | 1805±88 |
| DMSO-140 | 3.741±0.03 | 45.67±7.77 | 56±3 |

Figure S1 The correlation plot of pressure vs. conductivity.

Figure S2 Cross-sectional images of (a) untreated PEDOT:PSS films, (b) MeOH-80, (c) DMF-100, and (d) DMSO-100.

Figure S3 AFM images of PH1000, MeOH-80, DMF-100, and DMSO-100.

Figure S4 Specific capacitances at different scan rates of DMSO-treated samples compared with previous reported PEDOT:PSS electrodes.