Hierarchical carbon-encapsulated FeCo Alloy nanoparticles bridging N-doped graphene nanoribbons for efficient bifunctional oxygen electrocatalysis and rechargeable Zn-air batteries

Chao Cheng1,2, Yongqiang Ming3, Luping Liu2,, Yunjian Liu1,,Juan Yang 1,

1 Zhejiang New Era Zhongneng Technology Co., Ltd, Shaoxing 312000, China

2 School of Materials Science and Engineering, Jiangsu University, 301 Xuefu Road, Zhenjiang 212013, China

3 Changzhou Vocational Institute of Textile and Garment, 53 Gehu Middle Road, Wujin District, Changzhou 213164, China

Fig. S1. The XRD pattern of N-GNRs

Fig. S2. TEM images for Co@C (a, b) and FeCo@C (c, d)

Fig. S3. CV curves for prepared samples (a-e) and commercial Pt/C (f)

Fig. S4. LSV curves at diverse speeds (a, c, e and g) and corresponding K–L plots (b, d, f and h)

Fig. S5. the comparison of overpotential and tafel slope for OER catalysts

Fig. S6. CV curves of all catalysts in non-faradaic region region at different scan rates

Table S1. Product parameters of liquid Znair battery.

| Project | Parameter |
| --- | --- |
| Mold material | Polymethyl methacrylate |
| Width | 7 cm |
| Height | 6 cm |
| Distance between positive and negative poles | 1.4 cm |
| Sealing performance | Leakage-free |
| Reaction area | 1 cm2 |

Table S2. ORR parameters of prepared catalysts

| Catalysts | Eo （V） | E1/2 （V） | JL （mA cm-2） | Tafel slope （mV/dec） | n |
| --- | --- | --- | --- | --- | --- |
| N-GNRs | 0.921 | 0.751 | -4.78 | 92.6 | 3.74 |
| Co@C | 0.874 | 0.779 | -3.75 | 86.7 | 3.52 |
| FeCo@C | 0.877 | 0.807 | -5.45 | 60.1 | 3.91 |
| FeCo@C/N-GNRs | 0.922 | 0.830 | -5.34 | 83.2 | 4.00 |
| Pt/C | 0.938 | 0.840 | -5.78 | 83.8 | 4.00 |

Table S3 OER parameters of prepared catalysts

| Catalysts | E10 （V） | Overpotential（mV） | Tafel slope （mV/dec） |
| --- | --- | --- | --- |
| N-GNRs | 1.659 | 429 | 132.8 |
| Co@C | 1.609 | 379 | 111.1 |
| FeCo@C | 1.575 | 345 | 94.5 |
| FeCo@C/N-GNRs | 1.530 | 300 | 63.6 |
| IrO2 | 1.592 | 362 | 91.1 |

Table S4. Comparison of ORR and OER activity parameters for reported bifunctional catalysts.

| Catalyst | E1/2 (V) | E10 (V) | ΔE (V) | Ref. |
| --- | --- | --- | --- | --- |
| Zn1Co4@NC | 0.840 | 1.567 | 0.727 | [1] Journal of Power Sources 696 (2026) 241451. |
| N-GNRs/CoO | 0.825 | 1.554 | 0.729 | [2] Rare Met. 43 (2024) 1524–1536 |
| FePc-CoFe2O4/CNT | 0.870 | 1.690 | 0.820 | [3] ACS Appl. Mater. Interfaces 18 (2026) 1874-1884 |
| FeCo@CNTs-60 | 0.95 | 1.810 | 0.810 | [4] Appl. Catal. B Environ. 341 (2024) 123346 |
| FeCo-MI@TAP-900 | 0.865 | 1.615 | 0.75 | [5] Energy Storage Mater. 65 (2024) 103106 |
| Fe/SNCFs-NH3 | 0.89 | ~1.7 | ~0.81 | [6] Adv. Mater. 34 (2022) 2105410 |
| SA-Fe-SNC@900 | 0.876 | 1.632 | 0.756 | [7] Adv. Mater. 35 (2023) 2209948 |
| FeN/ZnSe/Fe-NC | 0.830 | 1.590 | 0.760 | [8] Energy Fuels 38 (2024) 12172-12181 |
| CoPx@CNS | 0.76 | 1.54 | 0.78 | [9] Angew. Chem. Int. Ed. 59 2020 21360-21366 |
| FeCoNiFCNFs | 0.92 | 1.64 | 0.72 | [10] Chem. Eng. J. 479 2024 147648 |
| ES-Co/Zn-CNZIF | 0.857 | 1.692 | 0.835 | [11] J. Energy Chem. 83 2023 138-149 |
| CoS2/Cu2S-NF | 0.8 | 1.53 | 0.73 | [12] Appl. Catal. B-Environ. 303 (2022) 120849 |
| Fe NPs@PC-700 | 0.786 | 1.550 | 0.764 | [13] Small Sci. 6 (2026) e202500448 |
| Pt/C+IrO2 | 0.840 | 1.592 | 0.752 | This work |
| FeCo@C/N-GNRs | 0.830 | 1.530 | 0.700 | This work |

Corresponding author.

E-mail: sarsasds@163.com (L.P. Liu), lyjian122331@ujs.edu.cn(Y.J. Liu), yangjuan6347@ujs.edu.cn (J. Yang).