Supporting Information

Cellulose-g-tetraethylenepentamine dual-function imprinted polymers selectively and effectively adsorb and remove 4-Nitrophenol and Cr(VI)

Daning Lang · Xia Xu · Ronglan Wu () · Wei Wang () · Ming Shi · Ke Jia · Shifei Chen · Jide Wang

D. Lang · X. Xu ·R. Wu · M. Shi · K. Jia · S. Chen · J. Wang

Key Laboratory of Oil & Gas Fine Chemicals, School of Chemical Engineering, Xinjiang University, Urumqi 830046, China

W. Wang

Institute of Chemistry & Center for Pharmacy, University of Bergen, Bergen 5020, Norway

X. Xu

School of Pharmaceutical & Environmental Engineering, College of Sichuan Chemical Vocational and Technical, Sichuan 646300, China

R Wu ()

e-mail: (wuronglan@163.com)

W. Wang ()

e-mail: wei.wang@uib.no

Adsorption tests.

Equilibrium adsorption isotherm

C-TEPA-MIP (10 mg) was added to the solutions (25 mL) with various initial concentrations of 4-NP (in the range of 20-800 mg/L) or Cr(VI) (in the range of 50-600 mg/L). The solutions were left for 12 h to achieve adsorption equilibrium at different temperatures (25oC, 35oC, and 45oC). The same amount of C-TEPA-NIP was added to the above solutions of 4-NP or Cr(VI), under the same conditions as described above. The concentrations of 4-NP and Cr(VI) in the residue were determined by UV-Vis spectroscopy. The adsorption capacity was calculated using the following Eq. (1):

(1)

where Qt (mg/g) is the adsorption capacity at time t (second), V (mL) is the volume of solution, W (mg) is the weight of the C-TEPA-MIP or C-TEPA-NIP, and C0 and Ce (mg/L) are the initial concentration of adsorbates and the equilibrium concentration of the adsorbates, respectively. All the experiments were repeated 3 times.

For elucidating the adsorption behavior, Langmuir model with monolayer homogeneous adsorption and Freundlich model with multilayer heterogeneous adsorption were used to study the adsorption isotherms of 4-NP and Cr(VI) on C-TEPA-MIP and C-TEPA-NIP. Eq. (2) and (3)(Zhang et al. 2020) were fitted to the experimental data:

Langmuir model:

(2)

Freundlich model:

(3)

where Qe is the adsorption capacity at equilibrium, Qm is the adsorption capacity when the adsorption in the monolayer reaches saturation (it is a theoretical adsorption capacity in the Langmuir model), KL is Langmuir constant, KF is the Freundlich constant and n is a fitting parameter.

Based on the adsorption constants at equilibrium, the thermodynamic parameters were calculated from Eq. (4) and (5) as follows(Wang et al. 2018):

（4）

（5）

where ko is a dimensionless thermodynamic equilibrium constant, ∆Go (kJ/mol), ∆Ho (kJ/mol) and ∆So (J/mol k) are Gibbs free energy change, enthalpy change and entropy change, respectively. R and T are the universal gas constant and the temperature, respectively.

Kinetic study

The kinetic studies were carried out with the initial concentration of 4-NP at 800 mg/L and the initial concentration of Cr(VI) at 600 mg/L. The solutions were kept at 25oC during the experiments. All experiments were repeated 3 times. In order to determine the adsorption mechanism of pollutants to the adsorbent, the following pseudo-first-order (6) and the pseudo-second-order (7) kinetic models were fitted to the experimental data(Manippady et al. 2020) .

(6)

(7)

where k1 and k2 are the rate constants for the first-order adsorption and the second-order adsorption, respectively, and t (second) is time.

Fig. S1. (a) The adsorption isotherms for adsorption of 4-nitrophenol (4-NP) and Cr(VI) on C-TEPA-MIP and C-TEPA-NIP; (b, e) fitting of Freundlich model of adsorption to the data; (c, f) fitting of Langmuir model of adsorption to the data.

The Langmuir and Freundlich isotherm models were used to analyze the adsorption isotherms of 4-NP and Cr(VI) on C-TEPA-MIP and C-TEPA-NIP adsorbents at 25oC, 35oC and 45oC. In Fig. S1, it is observed that the higher the initial concentration, the greater the adsorption capacity. This happened, because a higher concentration of contaminants meant a higher number of contaminants per unit volume, thus a greater chance for contacts with C-TEPA-MIP. Besides, the adsorption capacities of C-TEPA-MIP and C-TEPA-NIP for 4-NP and Cr(VI) decreased with an increase in the temperature, indicating that the adsorption was an exothermic process. Furthermore, the analysis using Langmuir and Freundlich isotherms revealed that the adsorption of the two pollutants more closely followed the Langmuir model (R2 > 0.99) than the Freundlich model. Thus, the maximum adsorption capacity (Qm) calculated using the Langmuir model is deemed reliable. At 25oC, the adsorption of the adsorbent reached a maximum. The adsorption capacity of C-TEPA-MIP for 4-NP was 181.82 mg/g, which was about 1.7 times higher than that of C-TEPA-NIP (104.17 mg/g), and the adsorption capacity for Cr(VI) was 134.41 mg/g, which was about 1.5 times higher than that of C-TEPA-NIP (88.72 mg/g). These results indicate that MIT could effectively improve the adsorption capacity of the adsorbent. We should point out that the value of 1/n in Freundlich model lies between 0 and 1, which further indicated that the adsorption was favorable.

Table S1. Freundlich isotherm and Langmuir isotherm fitting parameters for 4-NP and Cr(VI) adsorption on C-TEPA-MIP and C-TEPA-NIP.

| Absorbents |  | Freundlich isotherm |  |  | Langmuir isotherm |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | Temp. (oC) | 1/n | kF (L/mg) | R2 | Qm (mg/g) | kL10−2 (L/mg) | R2 |  | ∆Go (kJ/mol) | ∆Ho (kJ/mol) | ∆So (J/mol K) |
| C-TEPA-MIP 4-NP | 25 | 0.657 | 1.773 | 0.978 | 181.82 | 0.280 | 0.991 |  | -17.74 | -9.00 | 29.30 |
|  | 35 | 0.698 | 1.212 | 0.979 | 166.67 | 0.260 | 0.995 |  | -17.97 |  |  |
|  | 45 | 0.703 | 1.054 | 0.982 | 155.52 | 0.241 | 0.994 |  | -18.33 |  |  |
| C-TEPA-NIP 4-NP | 25 | 0.552 | 2.048 | 0.986 | 104.17 | 0.353 | 0.990 |  | -16.49 | -2.16 | 48.10 |
|  | 35 | 0.571 | 1.729 | 0.981 | 103.73 | 0.325 | 0.991 |  | -16.98 |  |  |
|  | 45 | 0.578 | 1.565 | 0.987 | 104.60 | 0.299 | 0.990 |  | -17.45 |  |  |
| C-TEPA-MIP Cr(VI) | 25 | 0.127 | 0.252 | 0.786 | 134.41 | 0.616 | 0.999 |  | -20.52 | -3.18 | 58.18 |
|  | 35 | 0.200 | 0.200 | 0.872 | 133.87 | 0.372 | 0.999 |  | -21.11 |  |  |
|  | 45 | 0.212 | 0.188 | 0.876 | 129.37 | 0.330 | 0.998 |  | -21.68 |  |  |
| C-TEPA-NIP Cr(VI) | 25 | 0.224 | 0.120 | 0.815 | 88.72 | 0.263 | 0.992 |  | -19.29 | -6.80 | 41.90 |
|  | 35 | 0.320 | 0.018 | 0.925 | 83.33 | 0.161 | 0.994 |  | -19.67 |  |  |
|  | 45 | 0.262 | 0.055 | 0.949 | 76.05 | 0.179 | 0.991 |  | -20.13 |  |  |

Based on the adsorption at equilibrium, the thermodynamic parameters were calculated (Table S1). In Table S1, it can be seen that the thermodynamic parameters of C-TEPA-MIP and C-TEPA-NIP for 4-NP and Cr(VI) followed the same pattern, meaning that their ∆Go was less than 0, which indicates that the adsorption was spontaneous and could reach equilibrium spontaneously at a certain temperature. ∆Ho was always less than 0, indicating that the adsorption reaction was exothermic, and the higher the temperature, the more unfavorable the adsorption was, which was consistent with the experimental results.

Fig. S2. (a) Adsorption capacity of 4-NP with time; Fitting 4-NP adsorption data with (b) pseudo-first order kinetic model and (c) pseudo-second order kinetic model; (d) Adsorption capacity of Cr(VI) with time; Fitting Cr(VI) adsorption data with (e) pseudo-first order kinetic model and (f) pseudo-second order kinetic model.

Based on the data in Fig. S1a and d, we selected concentrations of 800 mg/L of 4-NP and 600 mg/L of Cr(VI) for the kinetic tests. The removal of 4-NP by C-TEPA-MIP was very fast in the first 1 h, and reached the adsorption equilibrium in about 6 h (Fig. S2a). The removal of Cr(VI) by C-TEPA-MIP was very fast in the first 30 min, where afterwards the adsorption slowed, and reached the adsorption equilibrium in about 1 h (Fig. S2d). The adsorption rate was fast, because the adsorption occurred on the surface of the adsorbent rather than to its interior parts. The equilibrium time of the adsorption for 4-NP was longer than that of Cr(VI), because the imprinted pores of 4-NP were predominantly located in the interior of C-TEPA-MIP. During the adsorption of 4-NP, 4-NP molecules first reached the surface of C-TEPA-MIP, and then diffused through the imprinted sites.

Table S2. Kinetic constants for 4-NP and Cr6+ adsorption on the C-TEPA-MIP and C-TEPA-NIP

| Absorbents | Adsorbate |  | Pseudo first order |  |  |  |  |  |  | Pseudo second order |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  | Qe (mg/g) | Qe cal (mg/g) |  | k1 (1/min) |  | R2 |  | Qe cal (mg/g) |  | k210−2 (g/mg min) |  | R2 |  |
| C-TEPA-MIP |  | 4-NP | 126.34 | 111.06 | 0.015 |  | 0.933 |  | 139.86 |  | 0.017 |  | 0.999 |  |
| C-TEPA-NIP |  |  | 80.27 | 65.72 | 0.012 |  | 0.943 |  | 89.69 |  | 0.037 |  | 0.998 |  |
| C-TEPA-MIP |  | Cr(VI) | 136.75 | 53.72 | 0.036 |  | 0.901 |  | 139.47 |  | 0.287 |  | 0.997 |  |
| C-TEPA-NIP |  |  | 81.50 | 13.12 | 0.037 |  | 0.719 |  | 81.57 |  | 1.422 |  | 0.981 |  |

The values obtained for the parameters of pseudo-first-order and pseudo-second-order kinetics are summarized in Table S2. The results showed that the pseudo-second-order kinetics had a high correlation coefficient (R2 > 0.98), which well described the adsorption process. Also, the values of the calculated equilibrium adsorption capacity (Qe, cal) were closer to the experimental values for pseudo-second-order kinetics.

Fig. S3. BET Curves of 4-NP and Cr(VI) Adsorbed on C-TEPA-MIP

Table S3. BET Parameters of C-TEPA-MIP before and after Adsorption of 4-NP and Cr(VI)

| Samples | Surface area (m2/g) | Pore width (nm) | Pore volum (cm3/g) |
| --- | --- | --- | --- |
| C-TEPA-MIP | 118.090 | 1.478 | 0.319 |
| C-TEPA-MIP 4-NP | 107.711 | 8.227 | 0.345 |
| C-TEPA-MIP Cr(VI) | 171.734 | 1.478 | 0.464 |

References

Manippady SR, Singh A, Basavaraja BM, Samal AK, Srivastava S, Saxena M (2020) Iron–carbon hybrid magnetic nanosheets for adsorption-removal of organic dyes and 4-nitrophenol from aqueous solution. ACS Appl Nano Mater 3:1571-1582. https://doi.org/10.1021/acsanm.9b02348

Wang Y, Zhao L, Hou J, Peng H, Wu J, Liu Z, Guo X (2018) Kinetic, isotherm, and thermodynamic studies of the adsorption of dyes from aqueous solution by cellulose-based adsorbents. Water Sci Technol 77:2699-2708. https://doi.org/10.2166/wst. 2018.229

Zhang X, Li Z, Lin S, Theato P (2020) Fibrous materials based on polymeric salicyl active esters as efficient adsorbents for selective removal of anionic dye. ACS Appl Mater  Inter 12:21100-21113. https://doi.org/10.1021/acsami.0c03039