Supplementary Information

Dynamic adsorption and regeneration of gaseous ammonia on oxalic acid-modified corn-straw biochar

Supplementary Table S1. Experimental parameters used to prepare pristine corn-straw biochars by pyrolysis.

| Sample | Pyrolysis temperature (℃) | Holding time (h) | Sample | Pyrolysis temperature (℃) | Holding time (h) |
| --- | --- | --- | --- | --- | --- |
| C-400-2 | 400 | 2 | C-600-2 | 600 | 2 |
| C-400-3 | 400 | 3 | C-600-3 | 600 | 3 |
| C-400-4 | 400 | 4 | C-600-4 | 600 | 4 |
| C-400-5 | 400 | 5 | C-600-5 | 600 | 5 |
| C-500-2 | 500 | 2 | C-700-2 | 700 | 2 |
| C-500-3 | 500 | 3 | C-700-3 | 700 | 3 |
| C-500-4 | 500 | 4 | C-700-4 | 700 | 4 |
| C-500-5 | 500 | 5 | C-700-5 | 700 | 5 |

Note: The sample codes indicate pyrolysis temperature and holding time.

Supplementary Table S2. Orthogonal-test results for NH₃ adsorption by oxalic acid-modified corn-straw biochars prepared under different conditions.

| Sample | Run | Factor |  |  | Breakthrough time (min) |
| --- | --- | --- | --- | --- | --- |
|  |  | A (℃) | B (h) | C (mol L-1) |  |
| CC-0.1-400-2 | 1 | 400 | 2 | 0.1 | 23 |
| CC-0.2-400-3 | 2 | 400 | 3 | 0.2 | 29 |
| CC-0.3-400-4 | 3 | 400 | 4 | 0.3 | 28 |
| CC-0.4-400-5 | 4 | 400 | 5 | 0.4 | 26 |
| CC-0.2-500-2 | 5 | 500 | 2 | 0.2 | 31 |
| CC-0.1-500-3 | 6 | 500 | 3 | 0.1 | 24 |
| CC-0.4-500-4 | 7 | 500 | 4 | 0.4 | 37 |
| CC-0.3-500-5 | 8 | 500 | 5 | 0.3 | 29 |
| CC-0.3-600-2 | 9 | 600 | 2 | 0.3 | 21 |
| CC-0.4-600-3 | 10 | 600 | 3 | 0.4 | 21 |
| CC-0.1-600-4 | 11 | 600 | 4 | 0.1 | 22 |
| CC-0.2-600-5 | 12 | 600 | 5 | 0.2 | 23 |
| CC-0.4-700-2 | 13 | 700 | 2 | 0.4 | 25 |
| CC-0.3-700-3 | 14 | 700 | 3 | 0.3 | 26 |
| CC-0.2-700-4 | 15 | 700 | 4 | 0.2 | 25 |
| CC-0.1-700-5 | 16 | 700 | 5 | 0.1 | 15 |

Note: A, pyrolysis temperature; B, holding time; C, oxalic acid concentration. Breakthrough time was defined at an outlet NH3 concentration of 10 ppm.

Supplementary Table S3. Relative peak areas of oxygen-containing components in CC-0.4-500-4 before and after NH₃ adsorption, obtained by deconvolution of O 1s XPS spectra (%).

| Sample | State | C-O/C-OH | C=O | O-C=O |
| --- | --- | --- | --- | --- |
| CC-0.4-500-4 | Before adsorption | 69.95 | 23.37 | 6.68 |
|  | After adsorption | 71.10 | 22.26 | 6.64 |

Supplementary Table S4. BET specific surface area and pore-structure parameters of CC-0.4-500-4 before and after two regeneration cycles with water or ethanol.

| State |  | Sample | BET surface area (m2 g-1) | Total pore volume (cm3 g-1) | Micropore volume (cm3 g-1) (fraction, x%) | Mesopore volume (cm3 g-1) (fraction, x%) | Macropore volume (cm3 g-1) (fraction, x%) |
| --- | --- | --- | --- | --- | --- | --- | --- |
| CC-0.4-500-4 | Fresh |  | 27.35 | 0.0226 | 0.00171 (7.57%) | 0.0187 (82.74%) | 0.00217 (9.69%) |
|  | Water-washing regeneration (second cycle) |  | 11.32 | 0.0104 | 0.000036 (0.35%) | 0.0085 (82.69%) | 0.00186 (16.96%) |
|  | Ethanol regeneration (second cycle) |  | 9.95 | 0.00926 | 0 | 0.0070 (75.59%) | 0.00226 (24.41%) |

Note: Values in parentheses indicate the fraction of total pore volume.