Bio-based benzoxazine electrically conductive adhesives for sustainable and epoxy-free hybrid printed electronics.

Petsagkourakis I.1 , Hagel O.J. 1, Sawatdee A. 1, Carniello S.2, Schwarz-Funder E.2, Gasslander A.3, Strandberg J. 1, Alvi N.H. 1, Makhinia A.1, Beni V. 1 and Sandberg M. 1*

1RISE Research Institutes of Sweden, Unit of Printed and Organic Electronics, Södra Grytsgatan 4, 602 23,  Norrköping, Sweden

2Joanneum Research Forschungsgesellschaft mbH, Institute for Climate, Energy Systems, and Society, 8010 Graz, Austria

3RISE Research Institutes of Sweden, Unit of Advanced Electronics, Group "Electronics Reliability", Argongatan 30, 431 53, Mölndal, Sweden

* Corresponding author: mats.sandberg@ri.se

Section S1 : Nuclear Magnetic Resonance

Figure S1: The 1H NMR for the DPA starting material (up) and the DPA-Bz Crude product (down)

Figure S2: The 13C NMR for the DPA-Bz crude product

Section S2: Anisotropicity

Figure S3: (left) A schematic representation of the directions for the bond ; (right) A photographic depiction of a test sample that was used for the Isotropic Conductive Adhesive investigation (measurement in xy direction)

Section S3 : ACA Process engineering, electromechanical testing and assembly

Table S1: The engineered conditions of the bonding with the thermode

| Thermode Temperature T(oC) | Post annealing (150C , 1h) | Post annealing M (g) | Is it conductive ? | Does it stick ? |
| --- | --- | --- | --- | --- |
| 25oC | Yes | 500 | Yes | Yes |
| 25oC | Yes | 0 | No | No |
| 25oC | No | 0 | Yes | No |
| 150oC | Yes | 500 | Yes | Yes |
| 150oC | Yes | 0 | No | No |
| 150oC | No | 0 | Yes | No |
| 200oC | Yes | 500 | Yes | Yes |
| 200oC | Yes | 0 | Yes | Yes |
| 200oC | No | 0 | Yes | No |

Figure S4: The Stress vs Displacement plots for representative ACAs of various concentrations in the conductive filler

FigureS5: The updated process for the QFN SMD process

FigureS6: The 4-probe resistance of the SMD components on XD200 paper for the various concentrations of the ACA

Figure S7 : The mechanical performance of an SMD component mounted on the Kapton foil

Section S4 : LCA Inventories

Table S2 : The LCA inventory for the Cu ACA

| Cu ACA | Amount (g/FU, Wh/FU) | LCI unit process, source |
| --- | --- | --- |
| Cu extraction and processing - primary | 0.02205 | IEA estimation of GWP1 |
| Cu extraction and processing - secondary | 0 | IEA estimation of GWP1 |
| Polymeric matrix (DPA Bz + DIADO) | 0.02457 | Stoichiometric model base on RISE information, integrated with Ningbo patent. DIADO approximated hexamethylenediamine |
| Solvent (Benzyl acetone) | 0.01638 | Stoichiometric model base on Kuhn et al.2 |
| Storage | NA | Storage at room temperature possible |
| Curing | 1.33 | Primary data, EU electricity mix (EEA)3 |

Table S3 : The LCA inventory for the Ni ACA

| Ni ACA | Amount (g/FU, Wh/FU) | LCI unit process, source |
| --- | --- | --- |
| Ni extraction and processing - primary | 0.01325 | IEA estimation of GWP |
| Ni extraction and processing - secondary | 0 | IEA estimation of GWP |
| Polymeric matrix (epoxy resin + Bisphenol A) | 0.03975 | Composition extrapolated from datasheet |
| solvent | NA |  |
| Storage | 0.1 | 6 months storage in small lab fridge. Primary data, EU electricity mix (EEA)3 |
| Curing | 1.33 | Primary data, EU electricity mix (EEA)3 |

Table S4 : The LCA inventory for the GWP

|  | Ni-ACA |  |  | Cu-ACA |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| contribution | worst case | market ave | best case | worst case | market ave | best case |
| primary metal | 0.133 | 0.111 | 0.000 | 0.138 | 0.062 | 0.000 |
| secondary metal | 0.000 | 0.003 | 0.020 | 0.000 | 0.019 | 0.034 |
| matrix | 0.200 | 0.200 | 0.200 | 0.130 | 0.130 | 0.130 |
| solvent | 0.000 | 0.000 | 0.000 | 0.078 | 0.078 | 0.078 |
| storage energy | 0.019 | 0.019 | 0.019 | 0.000 | 0.000 | 0.000 |
| curing energy | 0.249 | 0.249 | 0.249 | 0.249 | 0.249 | 0.249 |

References

1.	Recycling of Critical Minerals, strategies to scale up recycling and urban mining. A World Energy Outlook Special Report; International Energy Agency: 2024.

2.	Senft, W. K. H.-U. F. G. Process for the preparation of benzylacetone. 2001.

3.	Greenhouse gas emission intensity of electricity generation in Europe. https://www.eea.europa.eu/en/analysis/indicators/greenhouse-gas-emission-intensity-of-1?activeAccordion=309c5ef9-de09-4759-bc02-802370dfa366.