Supplement to: A Simple, Modular Pipeline for Automated EIS Equivalent-Circuit Fitting via PCA-Space Nearest-Neighbour Matching, Validated Against Manual Fitting

Reference spectra

Table S1. Equivalent-circuit parameters and reduced χ² obtained from manual CNLS fitting (PSTrace) of the five reference measured spectra, one per equivalent-circuit topology studied. These values were used as the seed parameter sets for the synthetic reference database.

| Parameter | 1TC MANUAL | 2TC SER MANUAL | 2TC PAR MANUAL | 3TC SER MANUAL | 3TC PAR MANUAL |
| --- | --- | --- | --- | --- | --- |
| L (H) | 3.27×10-7 | 1.93×10-6 | 1.84×10-6 | 2.33×10-6 | 2.16×10-6 |
| Rs (Ω) | 5.459 | 19.05 | 19.23 | 12.07 | 12.26 |
| Q1 (S·sⁿ) | 1.10×10-4 | 2.70×10-4 | 5.42×10-5 | 6.09×10-4 | 2.47×10-4 |
| n1 | 0.871 | 1 | 0.95 | 0.689 | 0.655 |
| R1 (Ω) | 1.52×105 | 63.26 | 829.3 | 2.904 | 30.92 |
| Q2 (S·sⁿ) | – | 8.79×10-5 | 3.78×10-5 | 9.34×10-4 | 2.39×10-4 |
| n2 | – | 0.899 | 0.795 | 0.566 | 0.649 |
| R2 (Ω) | – | 2.20×104 | 2.17×104 | 741.6 | 1461 |
| Q3 (S·sⁿ) | – | – | – | 9.10×10-4 | 2.27×10-4 |
| n3 | – | – | – | 0.786 | 0.792 |
| R3 (Ω) | – | – | – | 5678 | 5764 |
| 2 | 0.0008 | 0.0012 | 0.0009 | 0.0002 | 0.0004 |

Table S2. Jacobian-based parameter uncertainty (% error) for the manual CNLS fits reported in Table S1.

| Parameter | Error% |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
|  | 1TC MANUAL | 2TC SER MANUAL | 2TC PAR MANUAL | 3TC SER MANUAL | 3TC PAR MANUAL |
| L (H) | 56.01 | 44.36 | 39.41 | 12.25 | 18.96 |
| Rs (Ω) | 0.867 | 1.018 | 0.909 | 1.391 | 2.609 |
| Q1 (S·sⁿ) | 0.804 | 39.09 | 11.36 | 159.3 | 125.5 |
| n1 | 0.202 | 11.27 | 1.7 | 27.34 | 17.76 |
| R1 (Ω) | 5.49 | 60.41 | 39.48 | 69.15 | 121.3 |
| Q2 (S·sⁿ) | - | 1.511 | 15.86 | 9.769 | 134.4 |
| n2 | - | 1.304 | 2.625 | 2.545 | 17.58 |
| R2 (Ω) | - | 2.445 | 3.195 | 40.35 | 53.58 |
| Q3 (S·sⁿ) | - | - | - | 13.64 | 24.82 |
| n3 | - | - | - | 4.063 | 15.18 |
| R3 (Ω) | - | - | - | 8.088 | 11.16 |

Known spectra

Table S3. Automated NN+CNLS fit for the measured 1TC spectrum, automatically identified by the pipeline as the winning topology. For each parameter, the CNLS fit value and the χ²-scaled % error are given for both topologies, alongside the overall reduced χ², RMSPE, and PCA distance for each fit. Excluding L, whose 100-fold difference from the manual fit reflects its fundamentally weak determination rather than a fitting discrepancy (see main text), the automated and manual fits agree within 0.4% for every parameter.

| Parameter | Fit value | χ²-scaled % error |
| --- | --- | --- |
| Parameter | 1TC (winner) |  |
| L | 3.07385×10⁻⁹ | 608.88 |
| Rs | 5.46714 | 0.09 |
| Q1 | 1.09578×10⁻⁴ | 0.08 |
| n1 | 0.870987 | 0.02 |
| R1 | 151665 | 0.39 |
| χ² | 0.000008 |  |
| RMSPE (%) | 0.37 |  |
| PCA distance | 0.006099 |  |

Table S4. Comparison of the 2TC_PAR fit, automatically identified by the pipeline as the winning topology, against the runner-up topology, 2TC_SER, for the same measured 2TC spectrum. For each parameter, the CNLS fit value and the χ²-scaled % error are given for both topologies, alongside the overall reduced χ², RMSPE, and PCA distance for each fit. The winning automated fit agrees with the manual fit within 0.7% for every parameter, with no individual parameter poorly determined in either fit.

|  | Fit value | χ²-scaled % error | Fit value | χ²-scaled % error |
| --- | --- | --- | --- | --- |
| Parameter | 2TC_PAR (winner) |  | 2TC_SER |  |
| L | 1.84055×10⁻⁶ | 25.89 | 1.93259×10⁻⁶ | 27.89 |
| Rs | 19.2321 | 0.60 | 19.0533 | 0.64 |
| Q1 | 5.41565×10⁻⁵ | 7.44 | 2.89254×10⁻⁴ | 24.03 |
| n1 | 0.949742 | 1.11 | 1.0 | 7.66 |
| R1 | 835.102 | 25.93 | 72.1143 | 41.68 |
| Q2 | 3.7672×10⁻⁵ | 10.43 | 8.77463×10⁻⁵ | 0.96 |
| n2 | 0.794845 | 1.73 | 0.901172 | 0.88 |
| R2 | 21725.5 | 2.10 | 21936.8 | 1.57 |
| χ² |  | 0.000380 |  | 0.000488 |
| RMSPE (%) |  | 2.20% |  | 2.52 |
| PCA distance |  | 0.097908 |  | 0.113464 |

Table S5. Comparison of the 3TC_SER fit, automatically identified by the pipeline as the winning topology, against the runner-up topology, 3TC_PAR, for the same measured 3TC spectrum. For each parameter, the CNLS fit value and the χ²-scaled % error are given for both topologies, alongside the overall reduced χ², RMSPE, and PCA distance for each fit. The winning automated fit agrees with the manual fit within 0.9% for every parameter, including R1 and Q1, which are poorly determined in the automated fit individually (43.19% and 100.17%, respectively) yet converge to essentially the same value as the manual fit in both cases.

| Parameter | Fit value | χ²-scaled % error | Fit value | χ²-scaled % error |
| --- | --- | --- | --- | --- |
| Topology | 3TC_PAR |  | 3TC_SER (winner) |  |
| L | 2.1657×10⁻⁶ | 11.90 | 2.3281×10⁻⁶ | 7.68 |
| Rs | 12.2572 | 1.64 | 12.0692 | 0.87 |
| Q1 | 2.47234×10⁻⁴ | 78.89 | 6.03827×10⁻⁴ | 100.17 |
| n1 | 0.654978 | 11.17 | 0.68982 | 17.18 |
| R1 | 30.9068 | 76.27 | 2.88346 | 43.19 |
| Q2 | 2.38662×10⁻⁴ | 84.44 | 9.30647×10⁻⁴ | 6.13 |
| n2 | 0.64822 | 11.04 | 0.565535 | 1.58 |
| R2 | 1469.63 | 33.50 | 748.022 | 25.29 |
| Q3 | 2.25886×10⁻⁴ | 15.55 | 910618×10⁻⁴ | 8.61 |
| n3 | 0.793057 | 9.54 | 0.786758 | 2.56 |
| R3 | 5757.78 | 7.01 | 5669.78 | 5.11 |
| χ² |  | 0.000158 |  | 0.000088 |
| RMSPE (%) |  | 1.15 |  | 0.93 |
| PCA distance |  | 0.020400 |  | 0.019018 |

Unknown spectra

Table S6. Comparison of the manual CNLS fit against the automated NN+CNLS fit of the same measured 2TC_SER spectrum. The two fits agree within 1% for every parameter, including R2, which is poorly determined in both fits individually (manual error 48.81%, automated error 32.32%) yet converges to essentially the same value (4.28×10⁶ vs. 4.237×10⁶ Ω) in both cases. The automated fit achieved a lower reduced χ² and χ²-scaled % error.

| Parameter | Manual CNLS fit |  | Automated NN+CNLS fit |  |
| --- | --- | --- | --- | --- |
|  | Fit value | χ²-scaled % error | Fit value | χ²-scaled % error |
| Topology | 2TC_SER |  | 2TC_SER |  |
| L (H) | 2.49×10⁻⁶ | 13.91 | 2.48924×10⁻⁶ | 9.28 |
| Rs (Ω) | 15.73 | 0.685 | 15.7275 | 0.46 |
| Q1 (S·sⁿ) | 2.49×10⁻⁴ | 11.68 | 2.49261×10⁻⁴ | 7.78 |
| n1 | 0.752 | 2.223 | 0.751292 | 1.48 |
| R1 (Ω) | 107 | 13.47 | 107.738 | 9.01 |
| Q2 (S·sⁿ) | 7.12×10⁻⁵ | 0.481 | 7.10891×10⁻⁵ | 0.32 |
| n2 | 0.836 | 0.353 | 0.835941 | 0.24 |
| R2 (Ω) | 4.28×10⁶ | 48.81 | 4.23729×10⁶ | 32.32 |
| χ² | 0.0003 |  | 0.000130 |  |
| RMSPE (%) |  |  | 1.28 |  |
| PCA distance |  |  | 0.412248 |  |

Table S7. Comparison of the manual CNLS fit against the automated NN+CNLS fit of the same measured 3TC_PAR spectrum. The two fits agree within 0.74% for every parameter, including R1, which is poorly determined in both fits individually (manual error 34.3%, automated error 21.89%) yet converges to essentially the same value (192.5 vs. 193.92 Ω) in both cases. The automated fit achieved a lower reduced χ² and χ²-scaled % error.

| Parameter | Manual CNLS fit |  | Automated NN+CNLS fit |  |
| --- | --- | --- | --- | --- |
|  | Fit value | χ²-scaled % error | Fit value | χ²-scaled % error |
| Topology | 3TC_PAR |  | 3TC_PAR |  |
| L (H) | 1.38×10⁻⁶ | 26.34 | 1.378×10⁻⁶ | 16.82 |
| Rs (Ω) | 18.71 | 0.664 | 18.7075 | 0.42 |
| Q1 (S·sⁿ) | 1.01×10⁻⁵ | 18.06 | 1.01513×10⁻⁵ | 11.51 |
| n1 | 0.942 | 1.974 | 0.941711 | 1.26 |
| R1 (Ω) | 192.5 | 34.3 | 193.92 | 21.89 |
| Q2 (S·sⁿ) | 5.84×10⁻⁵ | 14.99 | 5.81696×10⁻⁵ | 9.64 |
| n2 | 0.622 | 4.503 | 0.622627 | 2.90 |
| R2 (Ω) | 5334 | 20.08 | 5325.44 | 12.87 |
| Q3 (S·sⁿ) | 2.44×10⁻⁴ | 14.96 | 2.43622×10⁻⁴ | 9.55 |
| n3 | 0.586 | 10.05 | 0.586133 | 6.43 |
| R3 (Ω) | 1.34×10⁴ | 14.9 | 13412.4 | 9.53 |
| χ² | 0.0002 |  | 0.000093 |  |
| RMSPE (%) |  |  | 2.19 |  |
| PCA distance |  |  | 0.110120 |  |

Genuinely unknown spectra

Table S8. Comparison of a manual CNLS fit against the automated NN+CNLS fit of the genuinely unknown spectrum shown in Figure 8a. Both fits use the 3TC_PAR topology without an inductive element. R3 was held fixed in the manual fit at 8.00×10⁵ Ω, the smallest value found to leave the reduced χ² unchanged. PSTrace does not report parameter uncertainties when any parameter is held fixed, so the manual fit's χ²-scaled % error column is left blank The automated fit, refining R3 freely, converged to a larger value (2.88×10⁶ Ω) with a correspondingly large relative uncertainty (803.52%), consistent with this parameter being only weakly bounded from below by the data. This difference in R3 propagates to the correlated parameters Rs, n1, and R1, which differ by up to a factor of 2.5 between the two fits, while the remaining parameters (Q1, Q2, Q3, n2, n3) agree within 10%. The automated fit achieved a lower reduced χ² (0.000302 vs. 0.0007).

| Fit type | Manual CNLS fit |  | Automated NN+CNLS fit |  |
| --- | --- | --- | --- | --- |
| Parameter | Fit value | χ²-scaled % error | Fit value | χ²-scaled % error |
| Topology | 3TC_PAR |  | 3TC_PAR |  |
| Rs (Ω) | 311.2 | - | 123.056 | 135.75 |
| Q1 (S·sⁿ) | 1.27×10⁻5 | - | 1.16645×10⁻5 | 29.63 |
| n1 | 0.519 | - | 0.337576 | 30.88 |
| R1 (Ω) | 127 | - | 305.989 | 57.16 |
| Q2 (S·sⁿ) | 1.15×10⁻5 | - | 1.56672×10⁻5 | 7.57 |
| n2 | 0.769 | - | 0.743021 | 1.21 |
| R2 (Ω) | 3.82×104 | - | 4.43655×104 | 18.51 |
| Q3 (S·sⁿ) | 4.07×10-4 | - | 3.81781×10⁻4 | 18.07 |
| n3 | 0.915 | - | 0.950834 | 10.04 |
| R3 (Ω) | 8.00E+05 | - | 2.88197×106 | 803.52 |
| Chi² reduced | 0.0007 |  | 0.000302 |  |
| RMSPE (%) |  |  | 1.16 |  |
| PCA distance |  |  | 1.140782 |  |

Table S9. Comparison of a manual CNLS fit against the automated NN+CNLS fit of the same genuinely unknown spectrum shown in Figure 8b. The two fits agree within 0.51% for every parameter. Both fitting procedures identify 3TC_PAR as the topology with the lowest χ². The automated fit achieved a lower reduced χ² (0.000302 vs. 0.0008) and lower parameter errors overall.

| Fit type | Manual CNLS fit |  | Automated NN+CNLS fit |  |
| --- | --- | --- | --- | --- |
| Parameter | Fit value | χ²-scaled % error | Fit value | χ²-scaled % error |
| Topology | 3TC_PAR |  | 3TC_PAR |  |
| L (H) | 6.50×10⁻⁶ | 27.65 | 6.53307×10⁻⁶ | 17.31 |
| Rs (Ω) | 43.93 | 1.755 | 43.9176 | 1.11 |
| Q1 (S·sⁿ) | 1.58×10⁻⁶ | 18.74 | 1.58059×10⁻6 | 11.80 |
| n1 | 0.884 | 2.086 | 0.883996 | 1.31 |
| R1 (Ω) | 299.7 | 6.282 | 300.034 | 3.96 |
| Q2 (S·sⁿ) | 7.27×10⁻5 | 9.442 | 7.2621×10⁻⁵ | 5.96 |
| n2 | 0.62 | 3.13 | 0.620169 | 1.98 |
| R2 (Ω) | 2.77×104 | 63.29 | 27558.9 | 39.87 |
| Q3 (S·sⁿ) | 2.16×10⁻5 | 38.42 | 2.15583×10⁻5 | 24.20% |
| n3 | 0.94 | 21.44 | 0.938928 | 13.48% |
| R3 (Ω) | 1.66×105 | 15.18 | 165372 | 9.54% |
| Chi² reduced | 0.0008 |  | 0.000302 |  |
| RMSPE (%) |  |  | 1.80 |  |
| PCA distance |  |  | 0.523631 |  |

Out-of-envelope spectrum

Table S10. Comparison of a manual CNLS fit against the automated NN+CNLS fit of the same measured, out-of-envelope 2TC_PAR spectrum. The two fits agree within 2.3% for every parameter except Rs, which is statistically undetermined in both fits (manual: Inf; automated: undeterm.), consistent with the negligible solution resistance expected for a coating-dominated system; even so, the two Rs point estimates differ by only 20% in absolute terms (1.00×10⁻⁶ Ω vs. 8×10⁻⁷ Ω). The automated fit achieved a lower reduced χ² (0.000265 vs. 0.0007).

| Parameter | Manual CNLS fit |  | Automated NN+CNLS fit |  |
| --- | --- | --- | --- | --- |
|  | Fit value | χ²-scaled % error | Fit value | χ²-scaled % error |
| Topology | 2TC_PAR |  | 2TC_PAR |  |
| L (H) | - | - | - | - |
| Rs (Ω) | 1.00E-06 | Inf | 8×10⁻7 | undeterm. |
| Q1 (S·sⁿ) | 7.37E-10 | 1.753 | 7.35×10⁻10 | 1.45 |
| n1 | 0.933 | 0.197 | 0.933 | 0.14 |
| R1 (Ω) | 2.23E+08 | 20.36 | 2.18×108 | 14.73 |
| Q2 (S·sⁿ) | 1.08E-09 | 7.962 | 1.07×10⁻9 | 5.71 |
| n2 | 0.547 | 6.496 | 0.545 | 4.45 |
| R2 (Ω) | 1.61E+09 | 7.179 | 1.62e+09 | 4.93 |
| χ² | 0.0007 |  | 0.000265 |  |
| RMSPE (%) |  |  | 1.84 |  |
| PCA distance |  |  | 0.030248 |  |