Table S1. Mechanical and Optical Properties of GM/RGM Modified UV-Cured Specimens under 365 nm UV Irradiation

| Experiment No. | Amount of GM/RGM (g, weighing error ±1%) | Ambient temperature(℃) | Mechanical Properties |  |  |  | Optical Properties |  |  | Varnish Dosage(mL) | Coating Thickness(μm) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  | Mold irradiation duration(min) | Mold heating duration(min) | PTF(N) | Elong.(mm) | Glass plate irradiation duration(min) | Glass plate heating duration(min) | Hz(%) / T(%) |  |  |
| #1 | RGM 0.200 | 25 | 30 | 30 | 13 | / | 10 | 10 | Hz:0.41/T:100.0 | 5.0 | 50 |
| #2 | RGM 0.300 |  |  |  | 12 | / |  |  | Hz:1.42/T:100.0 |  |  |
| #3 | RGM 0.400 |  |  |  | 17 | / |  |  | Hz:2.82/T:100.0 |  |  |
| #4 | RGM 0.500 |  |  |  | 14 | / |  |  | Hz:4.21/T:100.0 |  |  |
| #5 | RGM 0.200 |  |  |  | 9 | / |  |  | Hz:0.31/T:99.9 |  |  |
| #6 | RGM 0.300 |  |  |  | 10 | / |  |  | Hz:0.76/T:100.0 |  |  |
| #7 | RGM 0.400 |  |  |  | 13 | / |  |  | Hz:2.36/T:100.0 |  |  |
| #8 | RGM 0.500 |  |  |  | 27 | / |  |  | Hz:2.89/T:99.6 |  |  |
| #9 | RGM 0.100+ RGM 0.100 |  |  |  | 21 | / |  |  | Hz:1.04/T:98.5 |  |  |
| #10 | RGM 0.150+ RGM 0.150 |  |  |  | 29 | / |  |  | Hz:1.25/T:100.0 |  |  |
| #11 | RGM 0.200+ RGM 0.200 |  |  |  | 18 | / |  |  | Hz:2.10/T:100.0 |  |  |
| #12 | RGM 0.250+ RGM 0.250 |  |  |  | 16 | / |  |  | Hz:2.62/T:99.9 |  |  |
| #13 | RGM 0.600 |  |  |  | 38 | / | 5 | 5 | Hz:9.76/T:99.3 |  |  |
| #14 | RGM 0.700 |  |  |  | 19 | / |  |  | Hz:25.8/T:98.5 |  |  |
| #15 | RGM 0.800 |  |  |  | 13 | / |  |  | Hz:30.4/T:98.0 |  |  |
| #16 | RGM 0.900 |  |  |  | 20 | / |  |  | Hz:65.7/T:94.7 |  |  |
| #17 | RGM 0.600 |  |  |  | 24 | / |  |  | Hz:7.27/T:98.4 |  |  |
| #18 | RGM 0.700 |  |  |  | 25 | / |  |  | Hz:13.3/T:98.3 |  |  |
| #19 | RGM 0.800 |  |  |  | 9 | / |  |  | Hz:23.7/T:96.0 |  |  |
| #20 | RGM 0.900 |  |  |  | 11 | / |  |  | Hz:16.2/T:83.5 |  |  |
| #21 | RGM 0.300+ RGM 0.300 |  |  |  | 13 | / |  |  | Hz:17.3/T:98.6 |  |  |
| #22 | RGM 0.350+ RGM 0.350 |  |  |  | 22 | / |  |  | Hz:19.2/T:98.2 |  |  |
| #23 | RGM 0.400+ RGM 0.400 |  |  |  | 21 | / |  |  | Hz:22.9/T:97.1 |  |  |
| #24 | RGM 0.450+ RGM 0.450 |  |  |  | 22 | / |  |  | Hz:25.3/T:96.5 |  |  |
| #25 | RGM 0.200 | 50 | 30 | 30 | 7 | / | 10 | 10 | Hz:0.63/T:100.0 |  |  |
| #26 | RGM 0.300 |  |  |  | 16 | / |  |  | Hz:2.70/T:99.4 |  |  |
| #27 | RGM 0.400 |  |  |  | 10 | / |  |  | Hz:4.18/T:100.0 |  |  |
| #28 | RGM 0.500 |  |  |  | 10 | / |  |  | Hz:6.08/T:100.0 |  |  |
| #29 | RGM 0.200 |  |  |  | 15 | / |  |  | Hz:0.38/T:100.0 |  |  |
| #30 | RGM 0.300 |  |  |  | 14 | / |  |  | Hz:0.95/T:100.0 |  |  |
| #31 | RGM 0.400 |  |  |  | 12 | / |  |  | Hz:0.97/T:100.0 |  |  |
| #32 | RGM 0.500 |  |  |  | 17 | / |  |  | Hz:2.91/T:100.0 |  |  |
| #33 | RGM 0.100+ RGM 0.100 |  |  |  | 23 | / |  |  | Hz:0.76/T:100.0 |  |  |
| #34 | RGM 0.150+ RGM 0.150 |  |  |  | 21 | / |  |  | Hz:1.79/T:100.0 |  |  |
| #35 | RGM 0.200+ RGM 0.200 |  |  |  | 10 | / |  |  | Hz:2.83/T:99.6 |  |  |
| #36 | RGM 0.250+ RGM 0.250 |  |  |  | 12 | / |  |  | Hz:11.5/T:99.3 |  |  |
| #37 | RGM 0.600 |  | 20 | 5 | 15 | 1.8 | 5 | 5 | Hz:16.4/T:99.0 |  |  |
| #38 | RGM 0.700 |  |  |  | 12 | 0.8 |  |  | Hz:25.1/T:97.8 |  |  |
| #39 | RGM 0.800 |  |  |  | / | / |  |  | Hz:17.7/T:98.2 |  |  |
| #40 | RGM 0.900 |  |  |  | 0 | 1.0 |  |  | Hz:26.4/T:93.4 |  |  |
| #41 | RGM 0.600 |  |  |  | 20 | 1.8 |  |  | Hz:28.9/T:97.1 |  |  |
| #42 | RGM 0.700 |  |  |  | 25 | 1.9 |  |  | Hz:36.5/T:96.2 |  |  |
| #43 | RGM 0.800 |  |  |  | 0 | 1.0 |  |  | Hz:29.7/T:97.9 |  |  |
| #44 | RGM 0.900 |  |  |  | 14 | 0.5 |  |  | Hz:38.4/T:77.2 |  |  |
| #45 | RGM 0.300+ RGM 0.300 |  |  |  | 23 | 2.0 |  |  | Hz:22.1/T:99.1 |  |  |
| #46 | RGM 0.350+ RGM 0.350 |  |  |  | 45 | 0.2 |  |  | Hz:28.5/T:98.2 |  |  |
| #47 | RGM 0.400+ RGM 0.400 |  |  |  | 12 | 0.7 |  |  | Hz:34.9/T:98.1 |  |  |
| #48 | RGM 0.450+ RGM 0.450 |  |  |  | 10 | 0.5 |  |  | Hz:26.1/T:90.1 |  |  |
| #49 | RGM 0.200 | 55 | 30 | 5 | 9 | 1.2 | 5 | 5 | Hz:1.54/T:99.9 |  |  |
| #50 | RGM 0.300 |  |  |  | / | / |  |  | Hz:2.88/T:99.8 |  |  |
| #51 | RGM 0.400 |  |  |  | / | / |  |  | Hz:7.49/T:99.9 |  |  |
| #52 | RGM 0.500 |  |  |  | / | / |  |  | Hz:15.1/T:99.5 |  |  |
| #53 | RGM 0.200 |  | 25 |  | 9 | 1.0 |  |  | Hz:0.92/T:99.7 |  |  |
| #54 | RGM 0.300 |  |  |  | 9 | 0.9 |  |  | Hz:1.54/T:99.6 |  |  |
| #55 | RGM 0.400 |  |  |  | 12 | 1.2 |  |  | Hz:5.31/T:100.0 |  |  |
| #56 | RGM 0.500 |  |  |  | 12 | 0.8 |  |  | Hz:6.32/T:99.9 |  |  |
| #57 | RGM 0.100+ RGM 0.100 |  |  |  | 16 | 0.7 |  |  | Hz:0.67/T:100.0 |  |  |
| #58 | RGM 0.150+ RGM 0.150 |  |  |  | 10 | 0.5 |  |  | Hz:1.54/T:99.7 |  |  |
| #59 | RGM 0.200+ RGM 0.200 |  |  |  | / | / |  |  | Hz:3.46/T:99.4 |  |  |
| #60 | RGM 0.250+ RGM 0.250 |  |  |  | 17 | 0.8 |  |  | Hz:6.19/T:99.8 |  |  |
| #61 | RGM 0.600 |  |  |  | 5 | 0.5 |  |  | Hz:1.96/T:100.0 |  |  |
| #62 | RGM 0.700 |  |  |  | 14 | 1.2 |  |  | Hz:38.4/T:98.0 |  |  |
| #63 | RGM 0.800 |  |  |  | / | / |  |  | Hz:35.8/T:98.0 |  |  |
| #64 | RGM 0.900 |  |  |  | 16 | 1.0 |  |  | Hz:42.2/T:96.7 |  |  |
| #65 | RGM 0.600 |  |  |  | 9 | 1.1 |  |  | Hz:8.13/T:99.1 |  |  |
| #66 | RGM 0.700 |  |  |  | 0 | 0.1 |  |  | Hz:11.5/T:98.4 |  |  |
| #67 | RGM 0.800 |  |  |  | 13 | 1.0 |  |  | Hz:35.7/T:97.4 |  |  |
| #68 | RGM 0.900 |  |  |  | / | / |  |  | Hz:34.2/T:97.3 |  |  |
| #69 | RGM 0.300+ RGM 0.300 |  |  |  | / | / |  |  | Hz:16.0/T:98.4 |  |  |
| #70 | RGM 0.350+ RGM 0.350 |  |  |  | 9 | 1.0 |  |  | Hz:21.6/T:97.0 |  |  |
| #71 | RGM 0.400+ RGM 0.400 |  |  |  | 8 | 0.8 |  |  | Hz:33.6/T:96.2 |  |  |
| #72 | RGM 0.450+ RGM 0.450 |  |  |  | / | / |  |  | Hz:40.7/T:92.1 |  |  |
| #73 | RGM 0.200 | 60 | 25 | 5 | 19 | 0.8 | 5 | 5 | Hz:5.29/T:99.4 |  |  |
| #74 | RGM 0.300 |  |  |  | / | / |  |  | Hz:8.19/T:97.8 |  |  |
| #75 | RGM 0.400 |  |  |  | / | / |  |  | Hz:10.6/T:97.6 |  |  |
| #76 | RGM 0.500 |  |  |  | 14 | 0.2 |  |  | Hz:13.8/T:98.1 |  |  |
| #77 | RGM 0.200 |  | 27 |  | 0 | 0.2 |  |  | Hz:5.42/T:100.0 |  |  |
| #78 | RGM 0.300 |  |  |  | / | / |  |  | Hz:7.26/T:99.5 |  |  |
| #79 | RGM 0.400 |  |  |  | / | / |  |  | Hz:11.6/T:99.3 |  |  |
| #80 | RGM 0.500 |  |  |  | 0 | 0.2 |  |  | Hz:31.9/T:97.8 |  |  |
| #81 | RGM 0.100+ RGM 0.100 |  | 25 |  | 0 | 1.2 |  |  | Hz:1.19/T:100.0 |  |  |
| #82 | RGM 0.150+ RGM 0.150 |  |  |  | 12 | 1.1 |  |  | Hz:2.09/T:99.5 |  |  |
| #83 | RGM 0.200+ RGM 0.200 |  |  |  | / | / |  |  | Hz:2.33/T:99.5 |  |  |
| #84 | RGM 0.250(+ RGM 0.250 |  |  |  | 9 | 1.0 |  |  | Hz:3.81/T:98.8 |  |  |
| #85 | RGM 0.600 |  |  |  | / | / |  |  | Hz:1.34/T:100.0 |  |  |
| #86 | RGM 0.700 |  |  |  | 21 | 1.2 |  |  | Hz:2.53/T:100.0 |  |  |
| #87 | RGM 0.800 |  |  |  | / | / |  |  | Hz:5.91/T:100.0 |  |  |
| #88 | RGM 0.900 |  |  |  | 21 | 1.8 |  |  | Hz:13.4/T:99.0 |  |  |
| #89 | RGM 0.600 |  | 25 | 10 | / | / |  |  | Hz:3.04/T:99.9 |  |  |
| #90 | RGM 0.700 |  |  |  | / | / |  |  | Hz:24.2/T:98.4 |  |  |
| #91 | RGM 0.800 |  |  |  | / | / |  |  | Hz:26.5/T:98.4 |  |  |
| #92 | RGM 0.900 |  |  |  | / | / |  |  | Hz:26.6/T:98.4 |  |  |
| #93 | RGM 0.300+ RGM 0.300 |  | 20 | 5 | / | / |  |  | Hz:11.6/T:99.6 |  |  |
| #94 | RGM 0.350+ RGM 0.350 |  |  |  | 14 | 0.8 |  |  | Hz:17.8/T:97.8 |  |  |
| #95 | RGM 0.400+ RGM 0.400 |  |  |  | / | / |  |  | Hz:27.5/T:97.1 |  |  |
| #96 | RGM 0.450+ RGM 0.450 |  |  |  | 10 | 1.0 |  |  | Hz:18.1/T:91.4 |  |  |

Abbreviations: GM = glass microsphere, RGM = reflective glass microsphere,PTF = peak tensile force, Elong. = elongation, Hz = haze, T = transmittance, UV = ultraviolet.

* All specimens (both mechanical and optical) were fabricated from the same oscillated mixture of UV-curable varnish with either single glass microspheres (GM or RGM) or hybrid GM+RGM. Mechanical tensile tests (PTF, Elong.) were performed on dumbbell-shaped specimens (width: 25.0 mm, length: 114.5 mm) prepared via in-situ UV irradiation and heating. Optical performance tests (Hz, T) were conducted on coatings applied onto optically clear glass plates, cured under the same in-situ UV irradiation and heating conditions. A slash (/) in the mechanical data columns indicates that the specimen experienced chain scission or fracture failure after process completion, resulting in no valid mechanical measurement being obtained.

Table S2. Mechanical and Optical Properties of GM/RGM Modified UV-Cured Specimens under 395 nm UV Irradiation

| Experiment No. | Amount of GM/RGM (g, weighing error ±1%) | Ambient temperature(℃) | Mechanical Properties |  |  |  | Optical Properties |  |  | Coating Thickness(μm) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  | Mold irradiation duration(min) | Mold heating duration(min) | PTF(N) | Elong.(mm) | Glass plate irradiation duration(min) | Glass plate heating duration(min) | Hz(%) / T(%) |  |
| #97 | RGM 0.200 | 25 | 20 | 0 | 10 | 0.8 | 5 | 0 | Hz:0.73/T:100.0 | 50 |
| #98 | RGM 0.300 |  |  |  | 12 | 1.6 |  |  | Hz:2.43/T:99.9 |  |
| #99 | RGM 0.400 |  |  |  | 14 | 1.0 |  |  | Hz:8.18/T:99.1 |  |
| #100 | RGM 0.500 |  |  |  | / | / |  |  | Hz:41.7/T:54.5 |  |
| #101 | GM 0.200 |  |  |  | 14 | 1.8 |  |  | Hz:3.04/T:100.0 |  |
| #102 | GM 0.300 |  |  |  | 0 | 0.2 |  |  | Hz:7.35/T:100.0 |  |
| #103 | GM 0.400 |  |  |  | / | / |  |  | Hz:37.0/T:96.6 |  |
| #104 | GM 0.500 |  |  |  | 0 | 0.2 |  |  | Hz:20.2/T:80.1 |  |
| #105 | RGM 0.100+ GM 0.100 |  |  |  | 19 | 1.9 |  |  | Hz:6.54/T:99.7 |  |
| #106 | RGM 0.150+ GM 0.150 |  |  |  | 25 | 0.9 |  |  | Hz:12.2/T:99.8 |  |
| #107 | RGM 0.200+ GM 0.200 |  |  |  | / | / |  |  | Hz:14.3/T:98.1 |  |
| #108 | RGM 0.250+ GM 0.250 |  |  |  | / | / |  |  | Hz:23.1/T:69.0 |  |
| #109 | RGM 0.600 |  |  |  | 12 | 1.0 |  |  | Hz:23.4/T:98.0 |  |
| #110 | RGM 0.700 |  |  |  | 16 | 1.8 |  |  | Hz:27.5/T:98.2 |  |
| #111 | RGM 0.800 |  |  |  | 20 | 0.2 |  |  | Hz:37.7/T:94.9 |  |
| #112 | RGM 0.900 |  |  |  | 16 | 0.2 |  |  | Hz:65.5/T:55.4 |  |
| #113 | GM 0.600 |  |  |  | / | / |  |  | Hz:37.3/T:96.8 |  |
| #114 | GM 0.700 |  |  |  | 11 | 1.5 |  |  | Hz:42.1/T:96.7 |  |
| #115 | GM 0.800 |  |  |  | 17 | 1.5 |  |  | Hz:35.0/T:97.7 |  |
| #116 | GM 0.900 |  |  |  | 12 | 1.0 |  |  | Hz:41.1/T:87.7 |  |
| #117 | RGM 0.300+ GM 0.300 |  |  |  | 13 | 0.9 |  |  | Hz:15.7/T:91.6 |  |
| #118 | RGM 0.350+ GM 0.350 |  |  |  | 12 | 1.1 |  |  | Hz:20.5/T:91.5 |  |
| #119 | RGM 0.400+ GM 0.400 |  |  |  | / | / |  |  | Hz:26.6/T:91.1 |  |
| #120 | RGM 0.450+ GM 0.450 |  |  |  | 15 | 1.0 |  |  | Hz:30.3/T:83.1 |  |
| #121 | RGM 0.200 | 50 | 20 | 4 | 11 | 1.8 | 5 | 5 | Hz:5.21T:91.8 |  |
| #122 | RGM 0.300 |  |  |  | 15 | 0.4 |  |  | Hz:9.97/T:92.5 |  |
| #123 | RGM 0.400 |  |  |  | 9 | 0.2 |  |  | Hz:20.4/T:91.6 |  |
| #124 | RGM 0.500 |  |  |  | 15 | 1.5 |  |  | Hz:26.5/T:91.1 |  |
| #125 | GM 0.200 |  |  | 3 | / | / |  |  | Hz:11.0/T:94.3 |  |
| #126 | GM 0.300 |  |  |  | / | / |  |  | Hz:12.5/T:98.8 |  |
| #127 | GM 0.400 |  |  |  | 11 | 1.8 |  |  | Hz:27.4/T:97.7 |  |
| #128 | GM 0.500 |  |  |  | 18 | 0.5 |  |  | Hz:24.4./T:91.3 |  |
| #129 | RGM 0.100+ GM 0.100 |  |  | 5 | 9 | 0.6 |  |  | Hz:1.38/T:99.7 |  |
| #130 | RGM 0.150+ GM 0.150 |  |  |  | 13 | 0.9 |  |  | Hz:6.54/T:99.5 |  |
| #131 | RGM 0.200+ GM 0.200 |  |  |  | / | / |  |  | Hz:10.36/T:98.5 |  |
| #132 | RGM 0.250+ GM 0.250 |  |  |  | / | / |  |  | Hz:15.96/T:90.1 |  |
| #133 | RGM 0.600 |  |  |  | 12 | 0.8 |  |  | Hz:4.48/T:99.1 |  |
| #134 | RGM 0.700 |  |  |  | 14 | 0.6 |  |  | Hz:7.27/T:99.9 |  |
| #135 | RGM 0.800 |  |  |  | / | / |  |  | Hz:8.04/T:99.1 |  |
| #136 | RGM 0.900 |  |  |  | / | / |  |  | Hz:15.7/T:99.2 |  |
| #137 | GM 0.600 |  |  | 3 | 9 | 0.8 |  |  | Hz:14.5/T:99.0 |  |
| #138 | GM 0.700 |  |  |  | 15 | 0.9 |  |  | Hz:17.4/T:99.0 |  |
| #139 | GM 0.800 |  |  |  | 0 | 0.1 |  |  | Hz:19.8/T:98.5 |  |
| #140 | GM 0.900 |  |  |  | 0 | 0.1 |  |  | Hz:28.5/T:95.5 |  |
| #141 | RGM 0.300+ GM 0.300 |  |  |  | 11 | 1.0 |  |  | Hz:33.5/T:98.5 |  |
| #142 | RGM 0.350+ GM 0.350 |  |  |  | 15 | 0.3 |  |  | Hz:49.7/T:96.0 |  |
| #143 | RGM 0.400+ GM 0.400 |  |  |  | 11 | 0.5 |  |  | Hz:43.7/T:89.1 |  |
| #144 | RGM 0.450+ GM 0.450 |  |  |  | / | / |  |  | Hz:43.7/T:70.7 |  |
| #145 | RGM 0.200 | 55 | 15 | 3 | 0 | 0.5 | 3 | 3 | Hz:7.88/T:92.1 |  |
| #146 | RGM 0.300 |  |  |  | 12 | 0.5 |  |  | Hz:13.1/T:92.5 |  |
| #147 | RGM 0.400 |  |  |  | 13 | 1.8 |  |  | Hz:14.3/T:92.5 |  |
| #148 | RGM 0.500 |  |  |  | 14 | 1.0 |  |  | Hz:29.9/T:84.2 |  |
| #149 | GM 0.200 |  |  |  | 12 | 1.0 |  |  | Hz:5.91/T:91.0 |  |
| #150 | GM 0.300 |  |  |  | 11 | 1.5 |  |  | Hz:12.4/T:89.8 |  |
| #151 | GM 0.400 |  |  |  | 0 | 2.0 |  |  | Hz:25.2/T:90.2 |  |
| #152 | GM 0.500 |  |  |  | 0 | 0.8 |  |  | Hz:43.1/T:30.5 |  |
| #153 | RGM 0.100+ GM 0.100 |  | 25 |  | 19 | 1.0 |  |  | Hz:4.85/T:92.8 |  |
| #154 | RGM 0.150+ GM 0.150 |  |  |  | 20 | 1.1 |  |  | Hz:9.12/T:92.6 |  |
| #155 | RGM 0.200+ GM 0.200 |  |  |  | 14 | 0.5 |  |  | Hz:14.3/T:86.4 |  |
| #156 | RGM 0.250+ GM 0.250 |  |  |  | 22 | 0.7 |  |  | Hz:20.7/T:78.8 |  |
| #157 | RGM 0.600 |  |  |  | 14 | 0.3 |  |  | Hz:30.3/T:99.1 |  |
| #158 | RGM 0.700 |  |  |  | 13 | 1.0 |  |  | Hz:31.1/T:98.8 |  |
| #159 | RGM 0.800 |  |  |  | 19 | 0.7 |  |  | Hz:36.9/T:97.8 |  |
| #160 | RGM 0.900 |  |  |  | 15 | 0.4 |  |  | Hz:40.1/T:75.8 |  |
| #161 | GM 0.600 |  | 20 |  | 10 | 1.8 |  |  | Hz:20.5/T:92.8 |  |
| #162 | GM 0.700 |  |  |  | / | / |  |  | Hz:27.1/T:92.9 |  |
| #163 | GM 0.800 |  |  |  | 10 | 1.0 |  |  | Hz:43.1/T:92.8 |  |
| #164 | GM 0.900 |  |  |  | / | / |  |  | Hz:32.2/T:91.3 |  |
| #165 | RGM 0.300+ GM 0.300 |  | 17 |  | 15 | 1.3 |  |  | Hz:21.5/T:98.2 |  |
| #166 | RGM 0.350+ GM 0.350 |  |  |  | 12 | 0.8 |  |  | Hz:25.0/T:98.1 |  |
| #167 | RGM 0.400+ GM 0.400 |  |  |  | 12 | 1.0 |  |  | Hz:28.6/T:98.5 |  |
| #168 | RGM 0.450+ GM 0.450 |  |  |  | 14 | 0.5 |  |  | Hz:32.4/T:94.1 |  |
| #169 | RGM 0.200 | 60 | 20 | 3 | 16 | 1.0 | 3 | 3 | Hz:3.93/T:99.9 |  |
| #170 | RGM 0.300 |  |  |  | 13 | 0.6 |  |  | Hz:6.80/T:100.0 |  |
| #171 | RGM 0.400 |  |  |  | 21 | 1.0 |  |  | Hz:16.0/T:98.8 |  |
| #172 | RGM 0.500 |  |  |  | 18 | 0.9 |  |  | Hz:23.1/T:80.2 |  |
| #173 | GM 0.200 |  |  |  | 12 | 0.8 |  |  | Hz:3.62/T:99.5 |  |
| #174 | GM 0.300 |  |  |  | 17 | 0.8 |  |  | Hz:7.66/T:98.6 |  |
| #175 | GM 0.400 |  |  |  | 15 | 1.0 |  |  | Hz:14.7/T:99.9 |  |
| #176 | GM 0.500 |  |  |  | 17 | 0.9 |  |  | Hz:22.2/T:81.5 |  |
| #177 | RGM 0.100+ GM 0.100 |  | 17 |  | / | / |  |  | Hz:4.28/T:100.0 |  |
| #178 | RGM 0.150+ GM 0.150 |  |  |  | / | / |  |  | Hz:8.52/T:99.4 |  |
| #179 | RGM 0.200+ GM 0.200 |  |  |  | 16 | 0.8 |  |  | Hz:14.3/T:98.5 |  |
| #180 | RGM 0.250+ GM 0.250 |  |  |  | 11 | 1.0 |  |  | Hz:23.1/T:74.7 |  |
| #181 | RGM 0.600 |  |  |  | / | / |  |  | Hz:15.6/T:98.0 |  |
| #182 | RGM 0.700 |  |  |  | / | / |  |  | Hz:17.7/T:98.4 |  |
| #183 | RGM 0.800 |  |  |  | / | / |  |  | Hz:29.4/T:96.2 |  |
| #184 | RGM 0.900 |  |  |  | 0 | 0.8 |  |  | Hz:41.6/T:96.1 |  |
| #185 | GM 0.600 |  |  |  | 17 | 1.9 |  |  | Hz:22.9/T:99.4 |  |
| #186 | GM 0.700 |  |  |  | 9 | 0.7 |  |  | Hz:27.8/T:96.1 |  |
| #187 | GM 0.800 |  |  |  | / | / |  |  | Hz:36.2/T:97.7 |  |
| #188 | GM 0.900 |  |  |  | / | / |  |  | Hz:37.2/T:90.8 |  |
| #189 | RGM 0.300+ GM 0.300 |  |  |  | 18 | / |  |  | Hz:21.7/T:98.0 |  |
| #190 | RGM 0.350+ GM 0.350 |  |  |  | / | / |  |  | Hz:30.7/T:97.8 |  |
| #191 | RGM 0.400+ GM 0.400 |  |  |  | / | / |  |  | Hz:33.3/T:98.0 |  |
| #192 | RGM 0.450+ GM 0.450 |  |  |  | / | / |  |  | Hz:40.9/T:82.7 |  |

Table S3. Mechanical and Optical Properties of Unmodified UV-Cured Specimens (No GM/RGM)

| Experiment No. | Ambient temperature(℃) | UV Wavelength(nm) | Mold irradiation duration((min) | Mold heating duration(min) | Mold irradiation duration(min) | Mold heating duration(min) | Hz(%) | T(%) | PTF(N) | Elong.(mm) | Varnish Dosage(mL) | Coating Thickness(µm) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | 25 | 365 | 20 | 0 | 3 | 3 | 0.00 | 99.9 | 27 | 2.0 | 4 | 50 |
| 2 |  | 395 |  |  |  |  |  | 99.8 | 24 | 2.4 |  |  |
| 3 | 50 | 365 |  | 3 |  |  |  | 100.0 | 33 | 1.0 |  |  |
| 4 |  | 395 |  |  |  |  |  | 99.8 | 21 | 1.8 |  |  |
| 5 | 55 | 365 |  |  |  |  |  | 99.9 | 11 | 0.1 |  |  |
| 6 |  | 395 |  |  |  |  |  | 99.6 | 20 | 1.8 |  |  |
| 7 | 60 | 365 |  |  |  |  |  | 100.0 | 16 | 1.5 |  |  |
| 8 |  | 395 |  |  |  |  |  | 99.9 | 38 | 3.9 |  |  |

Table S4. Mechanical and Optical Properties of GM/RGM Modified UV-Cured Specimens under 365 nm UV Irradiation (Unique Dataset)

| Experiment No. | Amount of GM/RGM (g, weighing error ±1%) | Ambient temperature(℃) | Mechanical Properties |  |  |  | Optical Properties |  |  | Varnish Dosage(mL) | Coating Thickness(μm) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  | Mold irradiation duration(min) | Mold heating duration(min) | PTF(N) | Elong.(mm) | Glass plate irradiation duration(min) | Glass plate heating duration(min) | Hz(%) / T(%) |  |  |
| #1 | RGM 0 | 25 | 20 | 20 | 15 | / | 10 | 10 | Hz:0.00/T:99.9 | 4.0 | 50 |
| #2 | RGM 0.100 |  |  |  | 16 | / |  |  | Hz:0.00/T:99.6 |  |  |
| #3 | RGM 0.125 |  |  |  | 10 | / |  |  | Hz:0.27/T:99.7 |  |  |
| #4 | RGM 0.150 |  |  |  | 11 | / |  |  | Hz:0.87/T:98.3 |  |  |
| #5 | GM 0.050 |  |  |  | 14 | / |  |  | Hz:0.00/T:99.9 | 5.0 |  |
| #6 | GM 0.100 |  |  |  | 14 | / |  |  | Hz:0.00/T:100.0 |  |  |
| #7 | GM 0.125 |  |  |  | 17 | / |  |  | Hz:0.00/T:99.9 |  |  |
| #8 | GM 0.150 |  |  |  | 9 | / |  |  | Hz:0.00/T:99.8 |  |  |
| #9 | RGM 0.050+ GM 0.050 |  | 30 | 30 | 28 | / |  |  | Hz:0.00/T:99.6 |  |  |
| #10 | RGM 0.075+ GM 0.075 |  |  |  | 13 | / |  |  | Hz:0.00/T:99.5 |  |  |
| #11 | RGM 0.100+ GM 0.100 |  |  |  | 10 | / |  |  | Hz:0.00/T:99.8 |  |  |
| #12 | RGM 0.200+ GM 0.200 |  |  |  | 12 | / |  |  | Hz:1.24/T:98.8 |  |  |
| #13 | RGM 0 | 50 | 30 | 30 | 11 | / | 10 | 10 | Hz:0.00/T:99.1 |  |  |
| #14 | RGM 0.100 |  |  |  | 30 | / |  |  | Hz:0.07/T:99.1 |  |  |
| #15 | RGM 0.125 |  |  |  | 19 | / |  |  | Hz:0.29/T:100.0 |  |  |
| #16 | RGM 0.150 |  |  |  | 18 | / |  |  | Hz:0.24/T:99.8 |  |  |
| #17 | GM 0.050 |  |  |  | 20 | / |  |  | Hz:0.15/T:99.9 |  |  |
| #18 | GM 0.100 |  |  |  | 20 | / |  |  | Hz:0.12/T:100.0 |  |  |
| #19 | GM 0.125 |  |  |  | 15 | / |  |  | Hz:0.19/T:99.9 |  |  |
| #20 | GM 0.150 |  |  |  | 15 | / |  |  | Hz:0.21/T:99.6 |  |  |
| #21 | RGM 0.050+ GM 0.050 |  |  |  | 10 | / |  |  | Hz:0.05/T:99.9 |  |  |
| #22 | RGM 0.075+ GM 0.075 |  |  |  | 13 | / |  |  | Hz:0.07/T:99.9 |  |  |
| #23 | RGM 0.100+ GM 0.100 |  |  |  | 15 | / |  |  | Hz:0.37/T:100.0 |  |  |
| #24 | RGM 0.200+ GM 0.200 |  |  |  | 14 | / |  |  | Hz:0.90/T:99.9 |  |  |
| #61 | RGM 0.100+ GM 0.100 | 70 | 30 | 30 | 13 | 2.0 | 5 | 5 | Hz:2.72/T:100.0 |  |  |
| #62 | RGM 0.150+ GM 0.150 |  |  |  | / | / |  |  | Hz:5.03/T:100.0 |  |  |
| #63 | RGM 0.200+ GM 0.200 |  |  |  | / | / |  |  | Hz:7.56/T:99.8 |  |  |
| #64 | RGM 0.250+ GM 0.250 |  |  |  | / | / |  |  | Hz:13.3/T:99.7 |  |  |
| #65 | RGM 0.200 |  |  |  | / | / |  |  | Hz:0.39/T:100.0 |  |  |
| #66 | RGM 0.300 |  |  |  | / | / |  |  | Hz:0.42/T:99.4 |  |  |
| #67 | RGM 0.400 |  |  |  | 18 | 1.0 |  |  | Hz:2.73/T:100.0 |  |  |
| #68 | RGM 0.500 |  |  |  | / | / |  |  | Hz:4.81/T:99.9 |  |  |
| #69 | GM 0.200 |  |  |  | / | / |  |  | Hz:1.25/T:99.4 |  |  |
| #70 | GM 0.300 |  |  |  | / | / |  |  | Hz:3.45/T:99.5 |  |  |
| #71 | GM 0.400 |  |  |  | / | / |  |  | Hz:3.98/T:99.4 |  |  |
| #72 | GM 0.500 |  |  |  | / | / |  |  | Hz:9.55/T:99.3 |  |  |
| #73 | RGM 0.600 |  | 10 | 10 | / | / |  |  | Hz:2.44/T:100.0 |  |  |
| #74 | RGM 0.700 |  |  |  | / | / |  |  | Hz:2.42/T:100.0 |  |  |
| #75 | RGM 0.800 |  |  |  | / | / |  |  | Hz:14.3/T:100.0 |  |  |
| #76 | RGM 0.900 |  |  |  | / | / |  |  | Hz:15.1/T:99.8 |  |  |