SUPPLEMENTRY INFORMATION MATERIAL

Influence of Chemical Activation on the Structural and Electrochemical Properties of Calophyllum inophyllum Shell-Derived Porous Carbon for Supercapacitor Application

Catherine V a, A.V Jhone Verjhula a*

Department of Physics, Ethiraj College for Women (Autonomous),

Affiliated to University of Madras, Chennai, Tamil Nadu, 600008, India.

*Corresponding author: verjhulajhone@gmail.com

Fig.S1. Schematic representation of the prepared BDC and BDAC

Table S1. Specific surface area, pore volume, and average pore diameter of the prepared carbon samples.

Fig. S2. Comparative XRD patterns of raw carbon (CA-1) and activated carbon samples: (a) CA-2 and CA-3, (b) CA-4 and CA-5, and (c) CA-6 and CA-7.

Fig. S3. EDX spectra and elemental composition analysis of (a) CA-1, (b) CA-2, (c) CA-3, (d) CA-4, (e) CA-5, (f) CA-6, and (g) CA-7.

Fig. S4. XPS surface chemical analysis of CA-1 (a–c), CA-2 (d–f), CA-3 (g–i), CA-4 (j–l), CA-5 (m–o), CA-6 (p–r), and CA-7 (s–u), showing the survey scan, high-resolution C 1s spectrum, and high-resolution O 1s spectrum for each sample.

Table S1. Specific surface area, pore volume, and average pore diameter of the prepared carbon samples.

| SAMPLE CODE | SURFACE AREA [m²/g] | PORE SIZE [ nm] | PORE VOLUME [cc/g] |  |  |
| --- | --- | --- | --- | --- | --- |
| CA-1 | 331.515 m²/g | 1.54nm | 0.539 |  |  |
| CA-2 | 328.823 m²/g | 1.688 nm | 0.151 |  |  |
| CA-3 | 225.250 m²/g | 1.55 nm | 0.426 |  |  |
| CA-4 | 588.993 m²/g | 1.23 nm | 0.235 |  |  |
| CA-5 | 609.700 m²/g | 1.23 nm | 0.249 |  |  |
| CA-6 | 479.753 m²/g | 1.23 nm | 0.214 |  |  |
| CA-7 | 1014.742 m²/g | 1.23 nm | 0.417 |  |  |