Modifying the Surface of Silica-Coated Magnesium Cobalt Ferrite with Curcumin to Eliminate Pb(II) and Cd(II) from

Different Environmental Water Samples

Hawar J. Sadiq Hawezy, Layth I. Abd Ali *

Department of Chemistry, Faculty of Science and Health, Koya University, Koya 44023, Kurdistan Region – F.R., Iraq

* Corresponding authors.

E-mail address:

layth.imad@koyauniversityorg (L. I. Abd Ali), ORCID: https://orcid.org/0000-0002-5948-2513

Table S1

The parameters obtained from XRD analysis.

| Samples | DXRD (nm) | d-spacing (Å) | Lattice Parameter (Å) | Vcell (Å) |
| --- | --- | --- | --- | --- |
| MgCoFe2O4 | 19.04 | 2.56 | 8.41 | 595 |
| MgCoFe2O4@SiO2-CPTMS-Cur | 13.03 | 2.53 | 8.36 | 584 |

Table S2

Ionic compositions for several real water samples (tap water, surface water and lake water)

| Types of ionic species | Tap water (mM) | Surface water (mM) | Lake water (mM) |
| --- | --- | --- | --- |
| Na+ | 0.90 | 0.38 | 0.68 |
| K+ | 0.09 | 0.07 | 0.40 |
| Ca2+ | 0.36 | 0.62 | 0.79 |
| Mg2+ | 0.51 | 0.28 | 0.71 |
| Cl− | 0.98 | 0.21 | 1.41 |
| Zn2+ | 0.01 | 0.05 | 0.28 |
| NO3− | — | 0.02 | 1.52 |
| SO4− | 0.04 | 0.08 | 1.29 |

Fig. S1: Pseudo-first-order model plots of adsorption kinetics for Pb(II) and Cd(II) metal ions for MgCF@SiO2-CPTMS-Cur adsorbent.

Fig. S2: Pseudo-second-order model plots of adsorption kinetics for Pb(II) and Cd(II) metal ions for MgCF@SiO2-CPTMS-Cur adsorbent.

Fig. S3: Elovich model plots of adsorption kinetics for Pb(II) and Cd(II) metal ions for MgCF@SiO2-CPTMS-Cur adsorbent.

Fig. S4: Langmuir model plots of adsorption isotherm for Pb(II) and Cd(II) metal ions for MgCF@SiO2-CPTMS-Cur adsorbent.

Fig. S5: Freundlich model plots of adsorption isotherm for Pb(II) and Cd(II) metal ions for MgCF@SiO2-CPTMS-Cur adsorbent.

Fig. S6: Temkin model plots of adsorption isotherm for Pb(II) and Cd(II) metal ions for MgCF@SiO2-CPTMS-Cur adsorbent.

a)

b)

c)

Fig. S8. Elemental maps of MgCF@SiO2-CPTMS-Cur (a) before adsorption (b) after Pb ion adsorption and (c) after Cd ion adsorption.