Supplementary information

Value-Oriented Design of Electrocatalytic PET Upcycling: Integrating Product Selection, Cathodic Pairing, and System Design

Seungwook Baek1,^, Yun Do Kim1,^, Yeeun Kim1,^, Sungjin Park1,2, and Byoung-Hoon Lee1,3*

1KU-KIST Graduate School of Converging Science and Technology, Korea University, Seoul 02481, Republic of Korea

2Department of Chemistry, Northwestern University, Evanston, IL 60208, USA

3Department of Integrative Energy Engineering, College of Engineering, Korea University, Seoul 02481, Republic of Korea

*Corresponding author. Email: bhlee90@korea.ac.kr

Table of Contents

Supplementary Table 1	3

Supplementary Table 2	4

References	5

| Electrocatalyst | Current density @ Potential (mA/cm2 @ V) | FE (%) | jglycolate (mA/cm2) | Coupled Cathodic Reaction | Reference |
| --- | --- | --- | --- | --- | --- |
| PdAg/NF | 10 @ 0.57 | 92 | 9.2 | HER | 1 |
| Pd─CuCo2O4 | 200 @ 0.8 | 92.6 | 185.2 | HER | 2 |
| PdB | 100 @ 0.65 | 93.8 | 93.8 | - | 3 |
| Pd/NiMoO4/NF | 100 @ 0.79 | 98.9 | 98.9 | HER | 4 |
| Pd-Ni(OH)2 | 600 @ 1.15 | 94.1 | 564.6 | HER | 5 |
| LM-PdCu | 10 @ 0.76 | 92 | 9.2 | - | 6 |
| Pd/NiOx | 300 @ 1.03 | 98.3 | 294.9 | HER | 7 |
| PdCuNiCoFe | 10 @ 0.59 | 98.6 | 9.9 | HER | 8 |
| Pt/SePC | 10 @ 0.65 | 84.4 | 8.44 | HER | 9 |
| Pt–Ni(OH)2/NF | 100 @ 0.69 | 93 | 93 | HER | 10 |
| Pt-Ni(OH)2 | 100 @ 0.61 | 90.1 | 90.1 | - | 11 |
| Pt@Ni(OH)2-x | 366.5 @ 0.9 | 95 | 348.1 | HER | 12 |
| Pt-Co3O4/CF | 100 @ 0.52 | 93.75 | 93.8 | HER | 13 |
| PtAgCuRhRu NWs | 50 @ 0.6 | 93.49 | 46.8 | HER | 14 |
| PtPd-Ni(OH)2 | 200 @ 0.69 | 90.38 | 180.8 | HER | 15 |

Supplementary Table 1. Reported electrocatalytic performance of Pd- and Pt-based catalysts for ethylene glycol oxidation to glycolate.

| Electrocatalyst | Current density @ Potential (mA/cm2 @ V) | FE (%) | Jformate (mA/cm2) | Coupled Cathodic Reaction | Reference |
| --- | --- | --- | --- | --- | --- |
| NiFe-sc-PBA | 500 @ 1.48 | 90 | 450 | HER | 16 |
| NiCo-OH | 100 @ 1.37 | 90 | 90 | HER | 17 |
| NiCu60s/NF | 100 @ 1.47 | 90 | 90 | HER | 18 |
| Ru-Co3O4 | 200 @ 1.34 | 90 | 180 | NO3RR | 19 |
| Vo-NiCo2O4/NF | 100 @ 1.26 | 90 | 90 | NO3RR | 20 |
| CoNiOOH-Ni3S2/NF | 100 @ 1.34 | 70 | 70 | HER | 21 |
| Ni(OH)2-Vo | 100 @ 1.45 | 90 | 90 | CO2RR | 22 |
| Ni0.9Mn0.1LDH | 10 @ 1.37 | 85.8 | 8.58 | HER | 23 |
| Ni-Co9O8 NSAs/NF | 100 @ 1.28 | 90 | 90 | HER | 24 |
| AC-NiO | 300 @ 1.39 | 90 | 270 | HER | 25 |
| Ni1Mn1-MOF-Se/NF | 100 @ 1.33 | 90 | 90 | 2e- ORR | 26 |
| CoNi0.25P | 300 @ 1.4 | 81.4 | 244.2 | HER | 27 |
| Ru,S-Ni(OH)2-Ov | 500 @ 1.42 | 85 | 425 | HER | 28 |
| Co2P-Ni2P/CC | 200 @ 1.35 | 95 | 190 | HER | 29 |
| UC-CoFeOx(OH)y/CFP | 600 @ 1.46 | 95 | 570 | HER | 30 |

Supplementary Table 2. Reported electrocatalytic performance of various catalysts for ethylene glycol oxidation to formate.

Reference

1	Si, D., Xiong, B., Chen, L. & Shi, J. Highly selective and efficient electrocatalytic synthesis of glycolic acid in coupling with hydrogen evolution. Chem Catalysis 1, 941–955 (2021).

2	Liu, K. et al. Energy‐saving hydrogen production by seawater splitting coupled with PET plastic upcycling. Advanced Energy Materials 14, 2304065 (2024).

3	Chen, J., Jiang, M., Zhang, F., Wang, L. & Yang, J. Interstitial boron atoms in Pd aerogel selectively switch the pathway for glycolic acid synthesis from waste plastics. Advanced Materials 36, 2401867 (2024).

4	Shi, K., Si, D., Teng, X., Chen, L. & Shi, J. Pd/NiMoO4/NF electrocatalysts for the efficient and ultra-stable synthesis and electrolyte-assisted extraction of glycolate. Nature Communications 15, 2899 (2024).

5	Liu, F. et al. Concerted and selective electrooxidation of polyethylene‐terephthalate‐derived alcohol to glycolic acid at an industry‐level current density over a Pd− Ni (OH) 2 catalyst. Angewandte Chemie International Edition 62, e202300094 (2023).

6	Han, S., Sun, L., Fan, D. & Liu, B. Pulsed electrosynthesis of glycolic acid through polyethylene terephthalate upcycling over a mesoporous PdCu catalyst. Nature Communications 16, 3426 (2025).

7	Wang, H. et al. Lattice-distortion-driven electron delocalization enables efficient electrosynthesis of glycolic acid and terephthalic acid from plastic wastes. Journal of the American Chemical Society 148, 1406–1418 (2026).

8	Huang, B. et al. Simultaneously Engineering the Amorphous Phase and Branch Morphology of High‐Entropy Alloy Nanomaterials for Enhanced Ethylene Glycol Oxidation. Advanced Materials 38, e73384 (2026).

9	Jang, D. et al. Structural Modification Effect of Se‐Doped Porous Carbon for Hydrogen Evolution Coupled Selective Electrooxidation of Ethylene Glycol to Value‐Added Glycolic Acid. Small 20, 2404540 (2024).

10	Liu, X. et al. Electro-reforming of PET plastic to C2 chemicals with concurrent generation of hydrogen and electric energy. Acs Catalysis 14, 5366–5376 (2024).

11	Li, Z. et al. Electrooxidation of Ethylene Glycol to Glycolic Acid with Pt‐Ni (OH) 2 Catalysts: High Efficiency and Selectivity for PET Plastics Upgrading. Chemistry–An Asian Journal 20, e202401843 (2025).

12	Ma, F. et al. Selectively steering the retention and cleavage of C–C bond in electrooxidation of PET plastic and biomass-derived alcohols by defective Ni (OH) 2–x-supported Pt. ACS Catalysis 15, 4759–4769 (2025).

13	Wu, H. et al. A Bioinspired OH-Sponge Catalyst Enables Ultrawide-Voltage and Durable Electrosynthesis of Glycolic Acid from Plastic Waste. Journal of the American Chemical Society (2026).

14	Liu, Y. et al. Multimetallic Pt-based alloy nanowires library as a platform for selective electrocatalytic oxidation of ethylene glycol. ACS nano 20, 9428–9439 (2026).

15	Lu, X. et al. Alloying Strategy for the Electro‐Upcycling of Polyethylene Terephthalate (PET) to C2 Products at Industrial‐Grade Current Density for over 700 h. Small 21, e05978 (2025).

16	Liu, J. K. et al. Stable Ni (II) sites in Prussian blue analogue for selective, ampere-level ethylene glycol electrooxidation. Nature Communications 16, 3458 (2025).

17	Zhao, X., Kuang, C., An, C. & Wang, M. Preparation of NiCo hydroxide by chloride corrosion for electrocatalytic upcycling of polyethylene terephthalate plastic waste. Chemical Engineering Journal 500, 157275 (2024).

18	Kang, H. et al. Cu promoted the dynamic evolution of Ni-based catalysts for polyethylene terephthalate plastic upcycling. Acs Catalysis 14, 5314 (2024).

19	Jiang, J. et al. Efficient Electrochemical‐Enzymatic Conversion of PET to Formate Coupled with Nitrate Reduction Over Ru‐Doped Co3O4 Catalysts. Angewandte Chemie 137, e202421240 (2025).

20	Guo, Y. et al. Oxygen-deficient NiCo2O4 porous nanowire for superior electrosynthesis of ammonia coupling with valorization of ethylene glycol. Chemical Engineering Journal 496, 154220 (2024).

21	Sun, J. et al. Promoted* OH adsorption facilitates C–C bond cleavage for efficient electrochemical upcycling of polyethylene terephthalate. Acs Catalysis 15, 529–542 (2025).

22	Ma, F. et al. Electrocatalytic waste-treating-waste strategy for concurrently upgrading of polyethylene terephthalate plastic and CO2 into value-added formic acid. ACS Catalysis 13, 14163–14172 (2023).

23	Wang, Z. et al. Facilitating formate selectivity via optimizing eg* band broadening in NiMn hydroxides for ethylene glycol electro‐oxidation. Angewandte Chemie 136, e202411517 (2024).

24	Ma, Y. et al. Electrochemical PET recycling to formate through ethylene glycol oxidation on Ni–Co–S nanosheet arrays. Journal of Materials Chemistry A 12, 33917–33925 (2024).

25	Ding, W. et al. Rapid surface reconstruction of amorphous‐crystalline NiO for industrial‐scale electrocatalytic PET upcycling. Angewandte Chemie International Edition 64, e202418640 (2025).

26	Qi, J. et al. Energy-saving and product-oriented hydrogen peroxide electrosynthesis enabled by electrochemistry pairing and product engineering. Nature Communications 14, 6263 (2023).

27	Zhou, H. et al. Electrocatalytic upcycling of polyethylene terephthalate to commodity chemicals and H2 fuel. Nature communications 12, 4679 (2021).

28	Li, Y. et al. Oxygen vacancy assisted Ru–Ni (OH) 2 for efficient ethylene glycol electrooxidation reaction. Inorganic Chemistry Frontiers 11, 6889–6897 (2024).

29	Zhang, J. et al. Plasma‐Constructed Co2P–Ni2P Heterointerface for Electro‑Upcycling of Polyethylene Terephthalate Plastic to Co‐Produce Hydrogen and Formate. Small 20, 2406767 (2024).

30	Lu, X. et al. An Oxygen‐Defect‐Induced Unsaturated Coordination Strategy Boosts High‐Selective PET Upcycling via Suppressing Oxygen Evolution. Angewandte Chemie International Edition, e3451583 (2026).