Supplementary Information

Hybridization–Ionicity Mapping for Descriptor-Guided Design of Amorphous Ge–Sb–Se Selector-Only Memory

Inchan Oh1, Won Hee Jeong1, Min Kyu Yang2, and Gun Hwan Kim1, 3

1Department of System Semiconductor Engineering, Yonsei University, Seoul 03722, Republic of Korea

2Department of AI Convergence, Sahmyook University, Seoul, 01795, Republic of Korea.

3Department of Materials Science and Engineering, Yonsei University, Seoul 03722, Republic of Korea

Corresponding author: Min Kyu Yang (dbrophd@syu.ac.kr), Gun Hwan Kim (kgh@yonsei.ac.kr)

Supplementary Material 1 | Electrical switching and compositional characterization of Ge–Sb–Se–Sn SOM devices based on hybridization–ionicity mapping.

Fig S1. Experimental validation of the hybridization–ionicity mapping framework using additional GeSbSeSn-based SOM compositions. a Hybridization–ionicity mapping of five Sb-containing GeSbSeSn compositions. b–f Ten consecutive PIV cycles and corresponding AES depth profiles of the fabricated devices. All five compositions exhibited reproducible SOM characteristics, further supporting the applicability of the proposed mapping framework to the Sb-based SOM region in Fig. 1

Supplementary Material 2 | Pulse measurement setup and write–read schemes for SOM electrical characterization.

Fig S2. Pulse schemes and measurement configuration used for the electrical characterization of SOM devices. a Write–read pulse sequence for evaluating the basic SOM characteristics and extracting Vth1 and Vth2 after positive and negative write pulses, respectively. b Schematic of the pulse measurement setup using an AFG and OSC. c Pulse sequence for evaluating Vth drift as a function of the delay time between the write and read pulses. d Pulse sequence for endurance measurements using repeated write operations followed by read pulses to monitor the programmed threshold states.

Supplementary Material 3 | Arrhenius analysis of the programmed states in GS and GSS1–3 SOM devices.

Fig S3. Arrhenius analysis of the programmed states in the GS and GSS SOM devices. Temperature-dependent ln(J/E) characteristics measured at fixed DC biases ranging from 0.3 to 0.8 V and corresponding Arrhenius plots of the Vth1 and Vth2 states for a GS, b GSS1, c GSS2, and d GSS3. The Ea for each programmed state was extracted from the linear fitting of ln(J/E) as a function of 1/(kBT).

Supplementary Material 4 | Poole–Frenkel analysis of the programmed states in GS and GSS1–3 SOM devices.

Fig S4. PF analysis of the programmed states in the GS and GSS SOM devices. Temperature-dependent DC I–V characteristics, corresponding ln(J/E) versus E1/2 plots, and temperature dependence of the extracted PF intercepts for the Vth1 and Vth2 states of a GS, b GSS1, c GSS2, and d GSS3. Measurements were performed at 25, 45, 65, and 85 °C. Φt were extracted from the linear fitting of the PF intercepts as a function of 1/(kBT).

Supplementary Material 5 | Electronic bandgap structure characterization of the GS and GSS1–3 SOM devices using UPS and UV–vis spectroscopy.

Fig S5. UPS spectra and Tauc plots for a GS, b GSS1, c GSS2, and d GSS3. The Ecut-off and EVBM were determined from linear fitting of the UPS spectra, while the Eg was extracted from the Tauc plots of (αhν)² versus hν.

Supplementary Material 6 | Ge 3d XPS spectra and peak deconvolution of GS and GSS1–3 films.

Fig S6. Ge 3d XPS spectra and peak deconvolution of the GS and GSS SOM devices. High-resolution Ge 3d spectra and corresponding fitted bonding components for a GS, b GSS1, c GSS2, and d GSS3, showing the evolution of Ge-related chemical bonding configurations with increasing Sb concentration.

Table S1. Calculated ionicity and hybridization values of previously reported SOM materials used for the hybridization–ionicity mapping in Fig. 1.

| Material composition | Ionicity | Hybridization |
| --- | --- | --- |
| Ge29Se30Te41 [17] | 0.085 | 2.140 |
| Ge36Sb21Se43 [18] | 0.178 | 2.278 |
| Ge24Sb21Se29Te26 [18] | 0.122 | 2.221 |
| Ge31Se38Sb3Te28 [19] | 0.109 | 2.174 |
| Ge32Se38Sb3Te27 [19] | 0.111 | 2.174 |
| Ge35Se35Sb3Te27 [19] | 0.107 | 2.171 |
| Ge37Se34Sb3Te26 [19] | 0.107 | 2.170 |
| Ge20Se42Te38 [26] | 0.098 | 2.154 |
| Ge34Se45Te21 [27] | 0.119 | 2.176 |
| Ge26Se23Te51 [27] | 0.070 | 2.125 |
| Ge20S7Se43Te30 [28] | 0.120 | 2.185 |
| In2(Ge22Sb3Se34Te41)98 [29] | 0.113 | 2.115 |
| In6(Ge22Sb3Se34Te41)94 [29] | 0.145 | 2.041 |
| Ge22Sb3Se34Te41 [29] | 0.095 | 2.161 |
| Se40(Si15Te34As42Ge9)60 [30, 31] | 0.052 | 2.474 |
| Se50(Si15Te34As42Ge9)50 [30, 31] | 0.063 | 2.489 |
| Se60(Si15Te34As42Ge9)40 [30, 31] | 0.072 | 2.502 |
| Ge20As30Se50 [32] | 0.106 | 2.451 |
| Ge56Se44 [33] | 0.160 | 2.222 |
| Ge29Se43Te28 [34] | 0.108 | 2.149 |
| Ge25Se38Te37 [34] | 0.095 | 2.128 |
| Ge22Se33Te45 [34] | 0.086 | 2.113 |
| Ge20Se30Te50 [34] | 0.079 | 2.101 |

Table S2. Relative bonding ratios extracted from the Se 3d and Sb 3d XPS spectra of the GS, GSS1, GSS2, and GSS3 devices shown in Fig. 6. The integrated area of each deconvoluted bonding component was normalized to the total fitted peak area of the corresponding core-level spectrum and expressed as a percentage.

| Bonding ratio (%) | GS | GSS1 | GSS2 | GSS3 |
| --- | --- | --- | --- | --- |
| Se-Ge | 71.97 | 49.20 | 43.21 | 37.41 |
| Se-Sb | X | 24.29 | 40.00 | 44.31 |
| Se-Se | 28.03 | 26.51 | 16.78 | 18.28 |

Se 3d

| Bonding ratio (%) | GS | GSS1 | GSS2 | GSS3 |
| --- | --- | --- | --- | --- |
| Sb-Se | X | 10.85 | 28.97 | 19.09 |
| Sb-Sb | X | 69.04 | 60.27 | 71.37 |
| SbOx | X | 20.11 | 10.76 | 9.54 |

Sb 3d