Table 1. Material Characteristics of Investigated Materials

| Parameter | 3Y-TZP Opaque | 5Y-PSZ Translucent | BioHPP |
| --- | --- | --- | --- |
| Manufacturer | Jyoti Ceramic Industries Pvt. Ltd., Maharashtra, India | Jyoti Ceramic Industries Pvt. Ltd., Maharashtra, India | Bredent GmbH & Co. KG, Senden, Germany, |
| Base Composition | Zirconia (ZrO₂) | Zirconia (ZrO₂) | PEEK-based polymer |
| Stabilizer | ~3 mol% Y₂O₃ | ~5 mol% Y₂O₃ | — |
| Approx.ZrO₂ Content | ~93% | ~96% | — |
| Phase Composition | Predominantly tetragonal | Increased cubic phase fraction | Semi-crystalline polymer |
| Reinforcement | — | — | ~20% ceramic fillers |
| Flexural Strength (Manufacturer) | ~1200 MPa | ~1100 MPa | ~150–180 MPa |
| Elastic Modulus | ~200 GPa | ~200 GPa | ~4 GPa |
| Specimen Form | CAD/CAM milled + sintered | CAD/CAM milled + sintered | Prefabricated discs |
| Dimensions Used | 8 mm × 2 mm | 8 mm × 2 mm | 8 mm × 2 mm |

Table 2. Descriptive statistics for weight loss of antagonist teeth and restorative discs (n = 4 per subgroup)

| Material | Aging | Tooth Weight Loss (Mean ± SD) | Disc Weight Loss (Mean ± SD) |
| --- | --- | --- | --- |
| TZ | Distilled water | 0.0010 ± 0.0000 | 0.00325 ± 0.00189 |
| TZ | APB | 0.0015 ± 0.0010 | 0.00700 ± 0.00216 |
| TZ | Saliva | 0.0035 ± 0.0010 | 0.00200 ± 0.00000 |
| OZ | Distilled water | 0.0030 ± 0.0020 | 0.00475 ± 0.00189 |
| OZ | APB | 0.00725 ± 0.00222 | 0.00425 ± 0.00150 |
| OZ | Saliva | 0.01025 ± 0.00263 | 0.00200 ± 0.00183 |
| BIOHPP | Distilled water | 0.0010 ± 0.00141 | 0.00125 ± 0.00050 |
| BIOHPP | APB | 0.0310 ± 0.05087 | 0.00550 ± 0.00289 |
| BIOHPP | Saliva | 0.0040 ± 0.00216 | 0.00175 ± 0.00096 |

Table 3. Two-way repeated measures ANOVA for antagonist tooth weight

| Source | df | F | p value |
| --- | --- | --- | --- |
| Time | 1, 27 | 5.982 | 0.021* |
| Time × Material | 2, 27 | 1.034 | 0.369 |
| Time × Aging | 2, 27 | 1.420 | 0.259 |
| Time × Material × Aging | 4, 27 | 1.275 | 0.304 |

* Significant at p < 0.05

Table 4. One-way ANOVA for Weight Loss Across Experimental Groups

(A) Antagonist Tooth Weight Loss

| Group | n | Mean (g) | SD | SE | p-value |
| --- | --- | --- | --- | --- | --- |
| TZ – Distilled Water | 4 | 0.0010 | 0.0000 | 0.0000 |  |
| TZ – APB | 4 | 0.0015 | 0.0010 | 0.0005 |  |
| TZ – Saliva | 4 | 0.0035 | 0.0010 | 0.0005 |  |
| OZ – Distilled Water | 4 | 0.0030 | 0.0020 | 0.0010 |  |
| OZ – APB | 4 | 0.0073 | 0.0022 | 0.0011 |  |
| OZ – Saliva | 4 | 0.0103 | 0.0026 | 0.0013 |  |
| BioHPP – Distilled Water | 4 | 0.0010 | 0.0014 | 0.0007 |  |
| BioHPP – APB | 4 | 0.0310 | 0.0509 | 0.0254 |  |
| BioHPP – Saliva | 4 | 0.0040 | 0.0022 | 0.0011 |  |
| Overall | 36 | 0.0069 | 0.0175 | 0.0029 | 0.309 |

B) Restorative Disc Weight Loss

| Group | n | Mean (g) | SD | SE | p-value |
| --- | --- | --- | --- | --- | --- |
| TZ – Distilled Water | 4 | 0.00325 | 0.00189 | 0.00095 |  |
| TZ – APB | 4 | 0.00700 | 0.00216 | 0.00108 |  |
| TZ – Saliva | 4 | 0.00200 | 0.00000 | 0.00000 |  |
| OZ – Distilled Water | 4 | 0.00475 | 0.00189 | 0.00095 |  |
| OZ – APB | 4 | 0.00425 | 0.00150 | 0.00075 |  |
| OZ – Saliva | 4 | 0.00200 | 0.00183 | 0.00091 |  |
| BioHPP – Distilled Water | 4 | 0.00125 | 0.00050 | 0.00025 |  |
| BioHPP – APB | 4 | 0.00550 | 0.00289 | 0.00144 |  |
| BioHPP – Saliva | 4 | 0.00175 | 0.00096 | 0.00048 |  |
| Overall | 36 | 0.00353 | 0.00242 | 0.00040 | <0.001* |

Table 5. Tukey Post Hoc Comparisons for Restorative Disc Weight Loss

| Comparison | Mean Difference | SE | p-value |
| --- | --- | --- | --- |
| TZ – Saliva | 0.0050* | 0.00122 | 0.009 |
| TZ – APB | −0.00575* | 0.00122 | 0.002 |
| TZ – Distilled Water | 0.00375 | 0.00122 | 0.095 |
| BioHPP – APB | −0.00425* | 0.00122 | 0.039 |
| BioHPP – Saliva | 0.00525* | 0.00122 | 0.005 |
| BioHPP – Distilled Water | 0.00425* | 0.00122 | 0.039 |
| OZ – Distilled Water | −0.0030 | 0.00122 | 0.297 |
| OZ – APB | −0.0030 | 0.00122 | 0.297 |
| OZ – Saliva | 0.0050* | 0.00122 | 0.009 |

*Statistically significant (p < 0.05)

Table 6. AFM Surface Roughness (Ra, nm)

| Group | Ra (nm) |
| --- | --- |
| TZ – APB | 203 |
| TZ – Saliva | 64.2 |
| TZ – Distilled Water | 8.77 |
| OZ – APB | 90.4 |
| OZ – Saliva | 139 |
| OZ – Distilled Water | 102 |
| BioHPP – APB | 180 |
| BioHPP – Saliva | 177 |
| BioHPP – Distilled Water | 124 |

Legends

Table 1. Material Characteristics of Investigated Materials

Table 2. Descriptive statistics for weight loss of antagonist teeth and restorative discs (n = 4 per subgroup)

Table 3. Two-way repeated measures ANOVA for antagonist tooth weight

Table 4. One-way ANOVA for Weight Loss Across Experimental Groups

Table 5. Tukey Post Hoc Comparisons for Restorative Disc Weight Loss

Table 6. AFM Surface Roughness (Ra, nm)