SUPPLEMENTARY INFORMATION

Carbon Support–Alkali Interplay Controls CO₂ Slip in Dual-Functional Materials for Direct Air Capture and Methanation

Victor Bordejéa, José María Conesab, María V. Moralesc, Antonio Guerrero-Ruizc,d, Inmaculada Rodríguez-Ramosb,d , Enrique García-Bordejéa

a Instituto de Carboquímica (ICB-CSIC), Miguel Luesma Castán 4, E-50018 Zaragoza, Spain,

b Instituto de Catálisis y Petroleoquímica (CSIC), 28049, Madrid, Spain

c Departamento de Química Inorgánica y Química Técnica, UNED, 28040, Madrid, Spain

d Grupo de Diseño y Aplicación de Catalizadores Heterogéneos, Unidad Asociada UNED-CSIC (ICP), Spain

Textural characterisation

Figure S1. N₂ adsorption-desorption isotherms (left panels, a and c) and pore-size distributions (right panels, b and d) for RuNa DFMs with different Na loadings: (a,b) HSAG-supported samples and bare HSAG; (c,d) AC Norit-supported samples and bare Norit AC.

Table S1. Textural properties of RuNa DFMs supported on HSAG and Norit AC, normalised to the support mass.

| Sample | Surface area | Pore Volume | Micropore Surface Area* (Smic) | Micr. Pore vol. * | Mesop Surface Area (Smes) | Meso Pore vol. | Percentage of support weight |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | m2g-1 | cm3 g-1 | m2 g-1 | cm3g-1 | m2g-1 | cm3g-1 | % |
| HSAG | 298 | 0,41 | n.d. | n.d. | 227 | 0,376 | 100 |
| RuNa(1:2.5)/H | 163 | 0,37 | n.d. | n.d. | 157,8 | 0,368 | 95,5 |
| RuNa(1:3.7)/H | 174 | 0.37 | n.d. | n.d. | 151 | 0,359 | 94,8 |
| RuNa(1:7.4)/H | 154 | 0.35 | n.d. | n.d. | 138 | 0,343 | 92,5 |
| RuNa(1:10)/H | 117 | 0.30 | n.d. | n.d. | 103 | 0,294 | 91 |
| RuNa(1:14.6)/H | 116 | 0.31 | n.d. | n.d. | 107 | 0,306 | 88,5 |
| Norit AC support | 935 | 0.77 | 615 | 0.24 | 320 | 0.53 | 100 |
| RuNa(1:3.7)/N | 826 | 0.68 | 528 | 0.21 | 298 | 0.47 | 94.8 |
| RuNa(1:7.4)/N | 800 | 0.69 | 446 | 0.17 | 354 | 0.52 | 92.5 |
| RuNa(1:10)/N | 776 | 0.67 | 466 | 0.18 | 310 | 0.49 | 91.0 |

*  calculated from the N2 adsorption isotherm using the t-plot method

n.d.: not reliably determined by the t-plot method because is below determination error

Figure S2. Representative HRTEM images and corresponding Ru particle-size distributions for (a) RuNa(1:3.7)/N, (b) RuNa(1:10)/N, (c) RuK(1:3.7)/N and (d) RuK(1:10)/N.

Figure S3. Representative HRTEM images and corresponding Ru particle-size distributions for (a) RuNa(1:3.7)/H, (b) RuNa(1:10)/H, (c) RuK(1:3.7)/H and (d) RuK(1:10)/H.

| a |  |  |  |
| --- | --- | --- | --- |
| b |  |  |  |
| c |  |  |  |
| d |  |  |  |

Figure S4. STEM images and EDS maps for (a) RuNa(1:3.7)/N, (b) RuNa(1:10)/N, (c) RuK(1:3.7)/N and (d) RuK(1:10)/N. Ru, Na and K are shown in green, orange and yellow, respectively

| a |  |  |  |
| --- | --- | --- | --- |
| b |  |  |  |
| c |  |  |  |
| d |  |  |  |

Figure S5. STEM images and EDS maps for (a) RuNa(1:3.7)/H, (b) RuNa(1:10)/H, (c) RuK(1:3.7)/H and (d) RuK(1:10)/H. Ru, Na and K are shown in green, orange and yellow, respectively.

XPS

The peak assignments used for XPS fitting are summarised below.

- Ru 3p fitting

Ru was analysed by ex situ XPS. Because Ru 3d overlaps the C 1s region near 284.6 eV, the Ru 3p3/2 region at 458-468 eV was used. Components at 461.2-461.6, 463.4-463.8 and 465.7-466.1 eV were assigned to Ru⁰, RuO₂ and hydrated RuO₂ or Ru oxyhydroxide, respectively [1,2].

- Na 1s fitting

The Na 1s spectra were fitted with components near 1071.6 and 1073.1 eV, assigned to carbonate/bicarbonate and oxide/hydroxide environments [3–6], respectively. A third component near 1075 eV appeared at high loading. This high-binding-energy component could not be assigned unambiguously and may reflect differential charging; it was therefore not used to identify a specific Na phase.

- K 2p fitting

The K 2p region contains the characteristic K 2p3/2-K 2p1/2 doublet. A K 2p3/2 component at 292.2 ± 0.1 eV was assigned to K₂CO₃ and KHCO₃ environments [7].

- O 1s fitting

The O 1s spectra were fitted using the following components:

- O1 (529-530.6 eV):  lattice inorganic oxygen from Na oxide or carbonates[8], and conjugated carbonyl oxygen, including quinone- and pyrone-like groups [9,10];

- O2 (531.4±0.4 eV): C=O type oxygen (carbonylic oxygen in esters and anhydrides)[11,12]

- O3 (532.5 ± 0.4 eV): C–O type oxygen (hydroxylic groups, non-carbonyl – ether type – oxygen atoms in esters and anhydrides)

- O4 (534.2 ± 0.4 eV): oxygen in acidic carboxyl groups [11,12]

- O5 (535.3 ± 0.4 eV): assigned to chemisorbed water and/or weakly bound oxygen-containing species [12].

- A Na KLL Auger feature was also observed near 536 eV [13].

XPS References

[1]	R. Chetty, W. Xia, S. Kundu, M. Bron, T. Reinecke, W. Schuhmann, M. Muhler, Effect of Reduction Temperature on the Preparation and Characterization of Pt−Ru Nanoparticles on Multiwalled Carbon Nanotubes, Langmuir 25 (2009) 3853–3860. https://doi.org/10.1021/la804039w.

[2]	S. Armenise, L. Roldán, Y. Marco, A. Monzón, E. García-Bordejé, Elucidation of Catalyst Support Effect for NH3 Decomposition Using Ru Nanoparticles on Nitrogen-Functionalized Carbon Nanofiber Monoliths, J. Phys. Chem. C 116 (2012) 26385–26395. https://doi.org/10.1021/jp308985x.

[3]	P.H. Citrin, High-Resolution X-Ray Photoemission from Sodium Metal and Its Hydroxide, Phys. Rev. B 8 (1973) 5545–5556. https://doi.org/10.1103/PhysRevB.8.5545.

[4]	A. Barrie, F.J. Street, An Auger and X-ray photoelectron spectroscopic study of sodium metal and sodium oxide, Journal of Electron Spectroscopy and Related Phenomena 7 (1975) 1–31. https://doi.org/10.1016/0368-2048(75)80052-1.

[5]	S.P. Kowalczyk, L. Ley, F.R. McFeely, R.A. Pollak, D.A. Shirley, X-Ray Photoemission from Sodium and Lithium, Physical Review. B. Solid State. 8 (1973) 3583–3585.

[6]	R.V. Siriwardane, J.M. Cook, Interactions of SO2 with sodium deposited on CaO, Journal of Colloid and Interface Science 114 (1986) 525–535. https://doi.org/10.1016/0021-9797(86)90438-8.

[7]	X. ‐L. Zhou, S.R. Coon, J.M. White, Potassium promoted decomposition of methyl bromide on Ag(111), J. Chem. Phys. 94 (1991) 1613–1625. https://doi.org/10.1063/1.459965.

[8]	X. Feng, D.F. Cox, Synthesis of a planar, multicomponent catalytic surface of Na2CO3/MnO, Surface Science 707 (2021) 121807. https://doi.org/10.1016/j.susc.2021.121807.

[9]	M.E. Schuster, M. Hävecker, R. Arrigo, R. Blume, M. Knauer, N.P. Ivleva, D.S. Su, R. Niessner, R. Schlögl, Surface Sensitive Study To Determine the Reactivity of Soot with the Focus on the European Emission Standards IV and VI, The Journal of Physical Chemistry A 115 (2011) 2568–2580. https://doi.org/10.1021/jp1088417.

[10]	J.R. Pels, F. Kapteijn, J.A. Moulijn, Q. Zhu, K.M. Thomas, Evolution of nitrogen functionalities in carbonaceous materials during pyrolysis, Carbon 33 (1995) 1641–1653. https://doi.org/10.1016/0008-6223(95)00154-6.

[11]	A.B. Dongil, B. Bachiller-Baeza, A. Guerrero-Ruiz, I. Rodríguez-Ramos, A. Martínez-Alonso, J.M.D. Tascón, Surface chemical modifications induced on high surface area graphite and carbon nanofibers using different oxidation and functionalization treatments, Journal of Colloid and Interface Science 355 (2011) 179–189. https://doi.org/10.1016/j.jcis.2010.11.066.

[12]	M.R. Cuervo, E. Asedegbega-Nieto, E. Díaz, S. Ordóñez, A. Vega, A.B. Dongil, I. Rodríguez-Ramos, Modification of the adsorption properties of high surface area graphites by oxygen functional groups, Carbon 46 (2008) 2096–2106. https://doi.org/10.1016/j.carbon.2008.08.025.

[13]	https://xpsdatabase.net/sodium-na-z11/, (n.d.).

Figure S6. Fits of the O 1s XPS spectra of RuNa DFMs with different Na loadings on (a) HSAG and (b) AC Norit, and RuK DFMs with different K loadings on (c) HSAG and (d) AC Norit.

Figure S7. Fits of the Ru 3p XPS spectra of RuNa DFMs with different Na loadings on (a) HSAG and (b) AC Norit, and RuK DFMs with different K loadings on (c) HSAG and (d) AC Norit.

Table S2. CH₄ onset temperature, apparent initial CH₄ production rate and total CH₄ yield for RuK(1:2.5)/H and RuNa(1:2.5)/H at different regeneration temperatures.

| Regeneration temperature | RuK(1:2.5)/H |  |  | RuNa(1:2.5)/H |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | CH4 onset | Apparent initial rate* | Total CH4 yield | CH4 onset | Apparent initial rate* | Total CH4 yield |
| ºC | ºC | µmol g-1 s-1 | µmol g-1 | ºC | µmol g-1 s-1 | µmol g-1 |
| 200 | 171 | 0.03 | 61 | 157 | 0.13 | 100 |
| 250 | 172 | 0.30 | 165 | 173 | 0.21 | 111 |
| 300 | 171 | 0.40 | 193 | 173 | 0.22 | 159 |

* These values therefore reflect both reaction and release during a non-isothermal experiment and should not be interpreted as intrinsic kinetic constants.

Table S3. CH₄ onset and peak temperatures, apparent initial CH₄ production rate and total CH₄ yield for RuNa and RuK supported on HSAG.

| DFM | CH4 peak onset | CH4 peak maximum | Initial CH4 rate | Total CH4 yield |
| --- | --- | --- | --- | --- |
|  | ºC | ºC | µmol g-1 s-1 | µmol g-1 |
| RuNa(1:2.5)/H | 177 | 218-291 | 0.15 | 153 |
| RuNa(1:3.7)/H | 199 | 250-291 | 0.17 | 128 |
| RuNa(1:7.4)/H | 181 | 220-293 | 0.14 | 133 |
| RuNa(1:10)/H | 191 | 241-294 | 0.15 | 107 |
| RuNa(1:14.6)/H | 200 | 254-281 | 0.17 | 116 |
| RuK(1:2.5)/H | 199 | 263 | 0.37 | 195 |
| RuK(1:3.7)/H | 251 | 296 | 0.34 | 205 |
| RuK(1:7.4)/H | 226 | 291 | 0.46 | 220 |
| RuK(1:10)/H | 270 | 300 | 0.13 | 168 |
| RuK(1:14.6)/H | 264 | 300 | 0.21 | 145 |

Table S4. CH₄ onset and peak temperatures, apparent initial CH₄ production rate and total CH₄ yield for RuNa and RuK supported on Norit AC.

| DFM | CH4 peak onset | CH4 peak maximum | Initial CH4 rate | Total CH4 yield |
| --- | --- | --- | --- | --- |
|  | ºC | ºC | µmol g-1 s-1 | µmol g-1 |
| RuNa(1:2.5)/N | 194 | 233 | 0.28 | 176 |
| RuNa(1:3.7)/N | 160 | 202 | 0.33 | 275 |
| RuNa(1:7.4)/N | 179 | 250 | 0.46 | 346 |
| RuNa(1:10)/N | 160 | 219 | 0.50 | 382 |
| RuNa(1:12.5)/N | 179 | 216 | 0.52 | 386 |
| RuK(1:2.5)/N | 263 | 300 | 0.55 | 277 |
| RuK(1:3.7)/N | 224 | 296 | 0.86 | 379 |
| RuK(1:7.4)/N | 247 | 300 | 0.64 | 401 |
| RuK(1:10)/N | 238 | 296 | 0.95 | 398 |
| RuK(1:12.5)/N | 276 | 300 | 0.28 | 402 |

Table S5. Comparison of DFMs operated under isothermal direct-air-capture and conversion conditions.

| Reference | DFM composition | Capture T | Regeneration T | CO2 captured | CO2 conversion | CH4 selectivity | CO2 slip during purge/heating |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | ºC | ºC | µmol*g-1 | % | % | % |
| [28] Jeong-Potter et al. | 0.5 wt% Ru+6.1 wt% Na₂O/γ-Al₂O₃ | 320 | 320 | 200 | 75 | 100 | 25 |
| [43] Tayyab et al. | LaCoO3 perovskite derived material (Co/LCO) | 300 | 300 | 36 (dry) | <100 | 100 | 0 |
|  |  | 450 | 450 | 48.9 (dry) | n.r. | 0 (CO) | n.r |
| [29] Tatsumichi et al. | 10 wt% Ni + 15 wt% La en Al2O3 | 350 | 350 | 129 | 97 | 99 | 3 |
|  | 10 wt% Ni + 4 wt% Ca en Al2O3 | 350 | 350 | 118 | 99 | 99 | 1 |
|  | 10 wt% Ni + 3 wt% Na en Al2O3 | 350 | 350 | 161 | 99 | 89 | 1 |

Table S6. Comparison of DFMs operated under isothermal direct-air-capture and conversion conditions.

| Reference | DFM composition | Capture T | Regeneration T | CO2 captured |  | CO2 conversion | CH4 selectivity | CO2 slip during purge/heating* |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | ºC | ºC | µmol*g-1 |  | % | % | % |
| [30] McNeary et al. | Diaminosilane- 5 wt% Ru/TiO₂ | 50 | 200 | 62 |  | <5 | 100 | >95 |
| [15] Crawford et al. | 1 wt% Ru + ~20 wt% Na/ FAU zeolite | 50 | 300 | 281 |  | 100 | 100 | 0 |
| [24] Jeong-Potter et al. | 1 wt% Ru + 10 wt% Na₂O /γ-Al₂O₃ | 25 | 300 | 1300 (humid) |  | 79 | 100 | 21 |
| [19] Kosaka et al. | 10 wt% Ni + 15 wt% Na₂CO₃/γ-Al₂O₃ | 20-25 | 450 | 168 (at 0.9 MPa) |  | 97 | 98 | 0-2 |
| [44] Martínez-López et al. | 15 wt% MgO + 20 wt% NiO-CeO₂ on β-zeolite | 35 | 350 | 568 |  | 45 | 100 | 32 |
| [34] Karaçoban et al. | 1.7 wt% Ru + 10 wt% K2CO3 on CNF | 30 | 225 | 410 (humid) |  | 56 | 87 | 44 |
| [45] Lin et al. | 0.25 wt% Ru + 10 wt% Na2CO3 on Al2O3 | 40 | 300 | 811 (humid) |  | 37 | - | 49 |
| [35] Karaçoban et al. | 1.6 wt% Ru + 10 wt% K2CO3 on CNF | 30 | 250 | 310 |  | 58 | - | 42 |
| [46] Zhang et al. | 1.6 wt% Ru + 5 wt% Na2CO3 on Al2O3 | 25 | 350 | 87 |  | 21 | 21 | 79 |
|  | 1.6 wt% Ru + 15 wt% Na2CO3 on Al2O3 | 25 | 350 | 432 |  | 64 | 66 | 36 |
|  | 1.6 wt% Ru + 25 wt% Na2CO3 on Al2O3 | 25 | 350 | 570 |  | 81 | 89 | 19 |
|  | 1.6 wt% Ru + 25 wt% Na2CO3 on Al2O3 | 25 | 350 | 2055 (humid) |  | 64 | 65 | 36 |
|  | 1.6 wt% Ru + 35 wt% Na2CO3 on Al2O3 | 25 | 350 | 582 |  | 90 | 99 | 10 |
| [31] Moral-Pombo et al. | 4 wt% Ru + 5.4 wt% Ba on HSGA | 40 | 300 | 110 (humid) |  | 100 | 100 | 0 |
|  | 4 wt% Ru + 10 wt% Cs on HSGA | 40 | 300 | 440 (humid) |  | 93 | 100 | 7 |
| [32] García-Bordejé et al. | 3 wt% Ru + 6.8 wt% NaNO3 on Al₂O₃ | 40 | 300 | 740 (humid) | 96 |  | 100 | 4 |
|  | 3 wt% Ru + 11.6 wt% KNO3 on Al₂O₃ | 40 | 300 | 440 (humid) | 75 |  | 100 | 25 |
| [47] Wu et al. | Ni0.7Ce0.3Ox (molar ratio) | 25 | 230 | 1050 (humid) | 84 |  | 100 | 16 |
| [26] Lin et al. | 0.25 wt% Ru + 6.1 wt% Na2O + γ-Al₂O₃ on monolith | 25 | 280 | 800 (humid) | 50 |  | 100 | 50 |
| [25] Abdallah et al. | 1 wt% Ru + 10 wt% Na2O + γ-Al₂O₃ on monolith | 0 | 300 | 368 (humid) | 42 |  | 100 | 58 |
|  |  | 25 | 300 | 1030 (humid) | 56 |  | 100 | 44 |
|  |  | 40 | 300 | 745 (humid) | 52 |  | 100 | 48 |
| [48] Feng et al. | 10 wt% NiCa | 25 | 450 | 8960 | 96 |  | 100 | 4 |
|  | 10 wt% NiCa9Mg | 25 | 450 | 8370 | 96 |  | 100 | 4 |
|  | 10 wt% NiCa9Ce | 25 | 450 | 7930 | 95 |  | 100 | 5 |
|  | 10 wt% NiCa9Zr | 25 | 450 | 7420 | 97 |  | 100 | 3 |
| [49] Lee et al. | 5 wt% Ru + 40 wt% K2CO3 on K-β″ Alumina | 30 | 300 | 209 (humid) | 69 |  | 99 | 31 |
| [27] Kim et al. | 10 wt% Ni + 30 wt% K2CO3 on Al2O3 | 30 | 320 | 2150 (humid) | 32 |  | 87 | 65 |
| This work | 3 wt% Ru+6.8 wt% Na on AC | 40 | 300 | 380 (humid) | 98.6 |  | 100 | 1.4 |

* When CO₂ slip was not reported, it was estimated from the reported CO₂ conversion by assuming that unconverted carbon was released as CO₂.