Supporting Information

Role of Cu-O-Ce Interface on Low-Temperature CO Oxidation over CuO/CeO2

Fuka Takahashi, Takeshi Ohtsu, Atsushi Satsuma*

Department of Materials Chemistry, Graduate School of Engineering, Nagoya University, Furo-cho, Chikusa-ku, Nagoya 464-8603, Japan

*Correspondence should be addressed: satsuma@chembio.nagoya-u.ac.jp

Fig. S1 XRD patterns of 0.5wt% M/CeO2 (M = Ru, Cu, Pt, Co, and Ni).

Fig. S2 CO conversion on 0.5wt% M/CeO2 (M = Ru, Cu, Pt, Co, and Ni) as a function of reaction temperature. Reaction conditions: 0.3%CO, 10%O2, N2 balance, catalyst 25 mg, total flow rate 100 mL/min.

Fig. S3 Effect of calcination temperature of CeO2 support on CO conversion of 0.5wt% Cu/CeO2. Reaction conditions: 0.3% CO, 10% O2, N2 balance; catalyst 25 mg; total flow rate 100 mL/min.

Fig. S4 Comparison of TOF of CO oxidation over Cu/CeO2 catalysts as a function of Cu content. The numbers indicate the reference number.

Table S1 Cu content, reaction conditions, and catalytic activity of CO oxidation at 60 ºC over Cu/CeO2 catalysts.

| Catalyst | Cu (wt%) | SV (mL/gcat·h) | CO conc. (%) | CO conv.* (%) | TOF* h-1 | Ref. |
| --- | --- | --- | --- | --- | --- | --- |
| Cu/CeO2 | 0.5 | 240,000 | 0.3 | 8.20 | 27.2 | This study |
| CuO-CeO2 nanosheet | 14.7 | 54,000 | 0.4 | 39.0 | 3.33 | 24 |
| Cu0.3Ce0.7-T | 12.56 | 54,000 | 1 | 21.0 | 2.10 | 25 |
| Cu0.1Ce0.9-T | 4.18 | 54,000 | 1 | 4.5 | 1.35 | 25 |
| CuO/CeO2 20-CC | 9.7 | 18,000 | 1 | 34.0 | 1.47 | 26 |
| CuO/CeO2 5-CC | 2.4 | 18,000 | 1 | 20.0 | 3.49 | 26 |
| CuO-CeO2 | 14 | 60,000 | 1 | 10.0 | 1.00 | 27 |
| Cu0.1Ce0.9O2 | 4.18 | 30,000 | 1 | 12.0 | 2.00 | 28 |
| 0.15Cu/CeO2 nanorod | 6.27 | 30,000 | 3 | 17.0 | 5.67 | 29 |
| 0.05Cu/CeO2 nanorod | 2.09 | 30,000 | 3 | 5.0 | 5.00 | 29 |
| CuO-CeO2 450-CC | 8.37 | 18,000 | 1 | 36.5 | 1.82 | 30 |
| Cu/CeO2 nanorod | 12.34 | 7,200 | 1 | 100.0 | 1.36 | 31 |

* at 60 ºC

Table S2 Comparison of TOF at 70 ºC with after treated CuCe catalysts reported by Tian et al. [33].

| Catalyst | Cu (wt%) | Treatment | TOF (10-2 s-1) | Ref. |
| --- | --- | --- | --- | --- |
| 0.5 wt% Cu/CeO2 | 0.5 | 10%O2/N2 at 300 °C | 1.0 | This study |
| CuCe-Red | 5.0 | 1% CO/Ar at 200 °C | 40 | 33 |
| CuCe-Rex |  | %CO/20%O2/Ar at 200 °C | 1.9 |  |
| CuCe-Ox |  | 20%O2/Ar at 200 °C | 1.5 |  |

Reaction conditions

This study: 0.3%CO/10%O2/N2, SV = 240,000 mL/gcat·h

Reference 34: 1%CO/20%O2/Ar, SV = 60,000 mL/gcat·h

Fig. S5 Distribution of particle size of Cu species on 0.5wt% Cu/CeO2 and 2wt% Cu/CeO2.

Fig. S6 Schematic model of periphery in CuO monolayer island