SUPPORTING INFORMATION

CORRELATING CHARGE-STORAGE KINETICS, QUANTUM CAPACITANCE, AND SURFACE CHARGE DENSITY IN Bi2O2S: AN EXPERIMENTAL-DFT STUDY

Ismail Adegbola Akintayo, Rasik Manve, Jatis Kumar Dash*, Sabyasachi Mukhopadhyay*

Department of Physics, SRM University-AP, Amaravati, Andhra Pradesh-522240, India

*Corresponding author: jatis.d@srmap.edu.in, sabyasachi.m@srmap.edu.in

PART A: EXPERIMENTAL

S1:	Synthesis Procedure

Fig. S1: Photographs showing synthesis procedure of Bi2O2S at different stages of the reaction

S2:	XRD Peaking Index Table

Table S1: XRD peak positions and crystallographic indexing of Bi2O2S

| Peak | 2θ (°) | Miller index (hkl) | Intensity (a.u.) |
| --- | --- | --- | --- |
| 1 | 24.723 | (110) | 1375 |
| 2 | 29.647 | (040) | 857 |
| 3 | 33.152 | (031) | 3521 |
| 4 | 44.983 | (141) | 936 |
| 5 | 47.517 | (002) | 1505 |
| 6 | 54.122 | (112) | 796 |
| 7 | 55.474 | (221) | 962 |
| 8 | 58.599 | (132) | 1082 |
| 9 | 69.116 | (212) | 558 |
| 10 | 78.662 | (172) | 744 |

Using Scherer equation:

D=kλβcosθ

k = 0.94, λ = 1.5406 Å, θ is obtained from 2θ/2 and is in degrees used for calculation of cosθ and FWHM (β) obtained in degrees which were converted to radians before substitution into the Scherrer equation using

βrad=β(∘×π180

The term βcosθ is then calculated as:

βcosθ=βrad×cosθ

Table S2: XRD peak parameters and crystallite sizes of Bi2O2S calculated using Scherrer equation

| Miller Index (hkl) | 2θ (°) | θ (°) | FWHM β (°) | β (rad) | βcosθ | D (nm) |
| --- | --- | --- | --- | --- | --- | --- |
| (110) | 24.70 | 12.35 | 0.74754 | 0.013047 | 0.012745 | 11.36 |
| (101) | 33.03 | 16.52 | 0.99305 | 0.017332 | 0.016620 | 8.71 |
| (141) | 45.30 | 22.65 | 1.58874 | 0.027728 | 0.025592 | 5.66 |
| (002) | 47.66 | 23.83 | 0.73216 | 0.012778 | 0.011694 | 12.39 |
| (132) | 58.35 | 29.18 | 0.98534 | 0.017198 | 0.015013 | 9.65 |
| (212) | 69.13 | 34.57 | 0.95877 | 0.016734 | 0.013780 | 10.50 |
| (172) | 78.67 | 39.34 | 1.06328 | 0.018558 | 0.014352 | 10.08 |

Table S3: Deviations for Bi2O2S obtained from XRD analysis.

| Miller Index | Crystallite Size, (Di) (nm) | Di-D | Di-D2 |
| --- | --- | --- | --- |
| (110) | 11.36 | 1.60 | 2.56 |
| (101) | 8.71 | −1.05 | 1.10 |
| (141) | 5.66 | −4.10 | 16.81 |
| (002) | 12.39 | 2.63 | 6.92 |
| (132) | 9.65 | −0.11 | 0.01 |
| (212) | 10.50 | 0.74 | 0.55 |
| (172) | 10.08 | 0.32 | 0.10 |
| Total | 68.35 | — | 28.05 |

Mean crystallite size

D=Din=68.357=9.76 nm

For experimental data, the sample standard deviation:

SD=(Di-D)2n-1 =28.056=4.675

SD=2.16 nm

Average crystallite size, Davg=9.76±2.16 nm

Fig. S2: (a) XRD pattern of Synthesized Bi2O2S (b) Crystallite-size distribution determined using the Scherrer equation (average crystallite size: 9.76 ± 2.16 nm)

Fig. S3: Elemental maps of (a) Bi O S (b) Bi, (c) S, and (d) O, indicating the uniform spatial distribution of the constituent elements across the sample (e) BET linear plot used for the determination of the specific surface area and BET constant (f) XPS (d) survey spectrum (g) UV-Vis. absorption spectrum of Bi2O2S with the corresponding Tauc plot (inset) showing the estimated optical band gap.

S3:	BET Parameters Table

Table S4: BET parameters table

| Parameter | Value |
| --- | --- |
| BET surface area (m² g⁻¹) | 48.91 |
| BET constant (C) | 51.04 |
| Correlation coefficient (R²) | 0.9998 |
| Average pore diameter (nm) | 24.0 (BJH average) |
| Total pore volume (cm³ g⁻¹) | 0.2399 |
| Isotherm type | Type IV |
| Hysteresis loop | H3 |

S4:	Impedance Fitting Parameters

Table S5: EIS fitting parameters

| Cycle | Rs (Ω) | Q (F·sα−1) | α | Rct (Ω) | σ (Ω·s⁻¹ᐟ²) |
| --- | --- | --- | --- | --- | --- |
| 1 | 1.010 | 0.0196 | 0.649 | 29.11 | 15.77 |
| 2 | 1.016 | 0.0188 | 0.656 | 28.28 | 17.20 |

S6:	Cyclic Voltammetry Data

Table S6: CV-derived specific capacitance data.

| Scan rate (mV/s) | CV plot area | Δm (g) | ΔV (V) | Specific capacitance, Cₚ (F/g) |
| --- | --- | --- | --- | --- |
| 10 | 10.19868 | 0.002 | 0.6 | 424.9448 |
| 20 | 17.89676 | 0.002 | 0.6 | 372.8492 |
| 30 | 22.95629 | 0.002 | 0.6 | 318.8373 |
| 40 | 26.50157 | 0.002 | 0.6 | 276.0581 |
| 50 | 29.00025 | 0.002 | 0.6 | 241.6687 |
| 60 | 30.85627 | 0.002 | 0.6 | 214.2797 |
| 70 | 32.28821 | 0.002 | 0.6 | 192.1917 |
| 80 | 33.43136 | 0.002 | 0.6 | 174.1217 |
| 90 | 34.41156 | 0.002 | 0.6 | 159.3128 |
| 100 | 35.23061 | 0.002 | 0.6 | 146.7942 |

Table S7: Kinetic analysis of the Bi2O2S electrode from CV data.

| Scan rate, v (mV s⁻¹) | Peak current, iₚ (mA) | v¹ᐟ² (mV s⁻¹)¹ᐟ² | iₚ / v¹ᐟ² | Capacitive contribution, k₁v | Diffusion contribution, k₂v¹ᐟ² | iₜₒₜ(v²) = k₁v + k₂v¹ᐟ² | Percentage capacitive contribution (%) | Percentage diffusion contribution (%) | log scan rate | log peak current |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 10 | 34.80 | 3.162278 | 11.00473 | 4.0788 | 34.56316 | 38.64196 | 10.55537 | 89.44463 | 1.00000 | 1.541579 |
| 20 | 57.80 | 4.472136 | 12.92447 | 8.1576 | 48.87969 | 57.03729 | 14.30222 | 85.69778 | 1.30103 | 1.761928 |
| 30 | 75.89 | 5.477226 | 13.85555 | 12.2364 | 59.86514 | 72.10154 | 16.97107 | 83.02893 | 1.477121 | 1.880185 |
| 40 | 89.30 | 6.324555 | 14.11957 | 16.3152 | 69.12635 | 85.44151 | 19.09517 | 80.90483 | 1.60206 | 1.950851 |
| 50 | 100.63 | 7.071068 | 14.23123 | 20.394 | 77.28557 | 97.67957 | 20.87847 | 79.12153 | 1.69897 | 2.002727 |
| 60 | 112.06 | 7.745967 | 14.46688 | 24.4728 | 84.6621 | 109.1349 | 22.42436 | 77.57564 | 1.778151 | 2.049451 |
| 70 | 120.68 | 8.366600 | 14.42402 | 28.5516 | 91.44552 | 119.9971 | 23.79357 | 76.20643 | 1.845098 | 2.081635 |
| 80 | 130.09 | 8.944272 | 14.54450 | 32.6304 | 97.75937 | 130.3898 | 25.02528 | 74.97472 | 1.90309 | 2.114244 |
| 90 | 137.13 | 9.486833 | 14.45477 | 36.7092 | 103.6895 | 140.3987 | 26.14640 | 73.8536 | 1.954243 | 2.137132 |
| 100 | 142.53 | 10.00000 | 14.25300 | 40.7880 | 109.2983 | 150.0863 | 27.17636 | 72.82364 | 2.00000 | 2.153906 |

S7:	GCD Data

Table S8: GCD-derived specific capacitance, energy density, and power density.

| Current density, id (A/g) | Discharging time, Δt (s) | Potential drop, ΔV (V) | Specific capacitance, Cₚ (F/g) | Energy density, Ed (Wh/kg) | Power density, Pd (W/kg) |
| --- | --- | --- | --- | --- | --- |
| 0.5 | 920 | 0.5 | 920 | 31.94444 | 125 |
| 1.0 | 433 | 0.5 | 866 | 30.06944 | 250 |
| 1.5 | 266 | 0.5 | 798 | 27.08333 | 375 |
| 2.0 | 183 | 0.5 | 732 | 25.41667 | 500 |
| 2.5 | 135 | 0.5 | 675 | 23.4375 | 625 |
| 3.0 | 101 | 0.5 | 606 | 21.04167 | 750 |
| 4.0 | 65 | 0.5 | 520 | 18.05556 | 1000 |
| 5.0 | 47 | 0.5 | 470 | 16.31944 | 1250 |

Fig. S4: (a) CV plots of Bi2O2S at scan rates (10-100 mVs-1) (b) GCD plots of Bi2O2S at current densities (0.5-5 A/g) (c) log(i) vs log(v) plot for determination of b-value (d)  Cp vs. Id plot (d)

PART B: COMPUTATIONAL STUDIES

S8: Computational Methodology

All first-principles calculations were carried out using the Vienna Ab initio Simulation Package (VASP). The interaction between ionic cores and valence electrons was described using the projector augmented wave (PAW) method. The exchange–correlation interaction was treated within the generalized gradient approximation (GGA) using the Perdew-Burke-Ernzerhof (PBE) functional. Long-range dispersion interactions were included through the Grimme DFT-D3 correction. Hybrid functional calculations were additionally employed for bulk Bi2O2S using the HSE06 functional to obtain improved electronic structures (bandgap). A plane-wave kinetic-energy cutoff of 520 eV was employed throughout the calculation. Structural optimization was continued until the total energy converged to 10⁻⁶ eV, while the residual force acting on each atom was below 0.01 eV Å⁻¹. Brillouin-zone integrations were performed using Monkhorst–Pack k-point meshes of 7 × 7 × 1 for geometry optimization and 15 × 15 × 1 for density-of-states calculations. A vacuum layer of approximately 17 Å was introduced along the surface normal to eliminate interactions between periodic images.

Table S9: Computational parameters used in this work.

| Parameter | Value / Description |
| --- | --- |
| DFT package | Vienna Ab Initio Simulation Package (VASP) |
| Electron–ion interaction | Projector Augmented Wave (PAW) method |
| Exchange–correlation functional | Generalized Gradient Approximation (GGA) using the Perdew–Burke–Ernzerhof (PBE) functional |
| Hybrid functional | Heyd–Scuseria–Ernzerhof (HSE06) |
| Dispersion correction | Grimme DFT-D3 method |
| Plane-wave energy cutoff | 520 eV |
| Electronic energy convergence criterion | 1 × 10⁻⁶ eV |
| Ionic force convergence criterion | 0.01 eV Å⁻¹ |
| Structural optimization | Full relaxation of atomic coordinates until convergence criteria were satisfied |
| van der Waals interaction | Included using the DFT-D3 dispersion correction |
| k-point mesh (geometry optimization) | 7 × 7 × 1 Monkhorst–Pack grid |
| k-point mesh (DOS calculations) | 15 × 15 × 1 Monkhorst–Pack grid |
| Periodic boundary condition | Two-dimensional periodic boundary condition |
| Vacuum thickness | >15 Å along the z-direction |
| Spin polarization | ISPIN = 2 |
| Spin–orbit coupling (SOC) | Included for electronic structure calculations using LSORBIT =. TRUE. |
| Smearing method | Gaussian smearing (ISMEAR = 0) |
| Smearing width | SIGMA = 0.05 eV |
| Precision | Accurate (PREC = Accurate) |
| Electronic minimization algorithm | Blocked Davidson algorithm |
| Surface model | Bi2O2S (001) slab |
| Adsorbates considered | K⁺ and OH⁻ |
| Calculated properties | Structural optimization, adsorption energy, band structure, DOS, PDOS, charge-density difference, surface charge density, and quantum capacitance |

S9:	Geometry Optimization

The Bi2O2S unit cell obtained from material project was fully relaxed before constructing the surface slab. During optimization, both lattice constants and atomic coordinates were allowed to relax until the convergence criteria described above were satisfied. The optimized Bi2O2S structure retained the layered orthorhombic framework of Bi2O2S after relaxation. The optimized lattice parameters are summarized in Table S8, while the relaxed crystal and slab models are shown in Fig. S6.

Table S10: Lattice Parameters of Bi2O2S unit cell before and after optimization

| Semiconductor | Before optimization |  |  |  |  |  | After optimization |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Lattice parameters | a | b | c | α | β | γ | a | b | c | α | β | γ |
| Bi2O2S | 3.84 | 3.88 | 11.96 | 90 | 90 | 90 | 3.84 | 3.88 | 11.96 | 90 | 90 | 90 |

Fig. S5: (a) Optimized crystal structure and (b) (001) slab of Bi2O2S.

S10:	Convergence Tests

To ensure the reliability of the calculations, convergence tests were performed for the plane-wave cutoff energy, k-point sampling, and vacuum thickness. The computational parameters adopted in the manuscript correspond to the point at which the total energy became nearly invariant with further increases in these parameters.

S10.1:	Plane-Wave Cutoff Energy

The total energy was calculated using several cutoff energies ranging from 250 to 600 eV. The energy variation became negligible beyond 500 eV, confirming that this cutoff provides sufficient numerical accuracy while maintaining computational efficiency.

Fig. S6: Total energy as a function of plane-wave cutoff energy.

S10.2:	K-point Convergence

Several Monkhorst–Pack meshes were tested to evaluate Brillouin-zone sampling. The total energy showed minimal variation beyond the 7 × 7 × 1 mesh, which was therefore selected for structural optimization.

Fig. S7: Total energy versus k-point mesh.

S11:	Optimized Structures

S11.1	Pristine Bi2O2S bulk

Figure S4 presents the initial structure in CIF format with POSCAR listed below and optimized one of bulk Bi2O2S as shown in Fig. S8(a-b) used for DOS and band structure calculations before slab formation.

Fig. S8: (a) Unrelaxed and (b) Relaxed bulk Bi2O2S.

POSCAR for Bulk

Bi4 S2 O4

1.0

3.8426029682         0.0000000000         0.0000000000

0.0000000000         3.8772959709         0.0000000000

0.0000000000         0.0000000000        11.9636888504

Bi    S    O

4    2    4

Cartesian

1.921301484         1.625895211        10.242363228

1.921301484         2.251400759         1.721325622

0.000000000         3.564543197         7.703170047

0.000000000         0.312752774         4.260518803

0.000000000         0.000000000         0.000000000

1.921301484         1.938647985         5.981844425

0.000000000         1.709876861         8.962101368

0.000000000         2.167419110         3.001587482

1.921301484         3.648524846         8.983431908

1.921301484         0.228771125         2.980256943

POSCAR for Bi2O2S(001) Slabs

Bi2SO2(001)

1.0

7.6852002144         0.0000000000         0.0000000000

0.0000000000         7.7546000481         0.0000000000

0.0000000000         0.0000000000        28.9834003448

Bi    S    O

12    8   12

Cartesian

1.921300054         1.625906992         7.262080790

0.000000000         3.564557004         4.722845086

0.000000000         0.312743020         1.280196793

5.763900161         1.625906992         7.262080790

3.842600107         3.564557004         4.722845086

3.842600107         0.312743020         1.280196793

1.921300054         5.503207016         7.262080790

0.000000000         7.441857028         4.722845086

0.000000000         4.190043044         1.280196793

5.763900161         5.503207016         7.262080790

3.842600107         7.441857028         4.722845086

3.842600107         4.190043044         1.280196793

0.000000000         0.000000000         8.983404937

1.921300054         1.938650012         3.001520940

3.842600107         0.000000000         8.983404937

5.763900161         1.938650012         3.001520940

0.000000000         3.877300024         8.983404937

1.921300054         5.815950036         3.001520940

3.842600107         3.877300024         8.983404937

5.763900161         5.815950036         3.001520940

0.000000000         1.709889311         5.981883997

0.000000000         2.167410713         0.021447716

1.921300054         3.648539323         6.003041879

3.842600107         1.709889311         5.981883997

3.842600107         2.167410713         0.021447716

5.763900161         3.648539323         6.003041879

0.000000000         5.587189335         5.981883997

0.000000000         6.044710737         0.021447716

1.921300054         7.525839347         6.003041879

3.842600107         5.587189335         5.981883997

3.842600107         6.044710737         0.021447716

5.763900161         7.525839347         6.003041879

S11.2:	Bi2O2S Slab: Pristine, K and OH Adsorption

Three possible adsorption configurations were considered, namely the top, bridge, hollow sites and OH at top sites. Geometry optimization indicates that the bridge site provides the lowest adsorption energy and therefore represents the most stable adsorption configuration for K⁺. Fig. S9 and S10 represent unoptimized and optimized configurations, respectively.

Fig. S9: Optimized atomic configurations of the Bi2O2S (001) slab: (a) pristine surface, (b) K adsorption at the top site, (c) K adsorption at the hollow site, (d) K adsorption at the bridge site, and (e) OH⁻ adsorption on the Bi2O2S (001) surface.

Fig. S10: Optimized atomic configurations of the Bi2O2S (001) slab: (a) pristine surface, (b) K adsorption at the top site, (c) K adsorption at the hollow site, (d) K adsorption at the bridge site, and (e) OH⁻ adsorption on the Bi2O2S (001) surface.

S12:	Adsorption Energy Calculations

Adsorption energies were evaluated using Eads= Eslab+ads- Eslab- Eadsorbate

Table S11: Adsorption energies.

| Adsorbate | Adsorption site | Adsorption energy, (Eads) (eV) | Relative interaction | Stability |
| --- | --- | --- | --- | --- |
| K+ | Top | −3.25 | Moderate | Stable |
| K+ | Hollow | −2.86 | Weakest | Stable |
| K+ | Bridge | −4.99 | Strong | Most stable K configuration |
| OH− | Surface site | −9.90 | Very strong | Most stable adsorption |

S12:	Electronic Structure

S12.1	Band Structure and Density of States of Bulk Bi2O2S

The band structure was only calculated for Bi2O2S unit cell to determine its band gap using both GGA (PBE) and hybrid functional (HSE06 plus SOC).

Top of Form

Fig. 11: Calculated TDOS/PDOS and band structures of Bi2O2S using PBE, HSE06, and HSE06+SOC methods. The corresponding band gaps are 0.83, 1.54, and 1.36 eV, respectively, with the Fermi level referenced to 0 eV.

INCAR USED

The incar settings used are listed below

SYSTEM = hsebos#soc

Starting parameters for this run:

NWRITE =      2    write-flag

ISTART =      1    job: 0-new, 1-cont, 2-samecut

ICHARG =      1    charge: 0-wave, 1-file, 2-atom, >10-const

INIWAV =      1    electr: 0-lowe 1-rand 2-diag

ISPIN =      1    spin-polarized or not:

LSCALAPACK=.FALSE.

Spin-Orbit Coupling, Noncollinear Magnetism

LSORBIT =. TRUE.

LNONCOLLINEAR =. TRUE.

#  MAGMOM = 2*2.5

SAXIS = 0 0 1

Electronic Relaxation:

PREC   = Accurate   low | medium | high

ENCUT = 500

#  ENAUG = 644.9

#  NGX    = 42; NGY = 56; NGZ = 90

#  NGXF   = 60; NGYF = 80; NGZF = 128

#  NELECT = 36

NELMDL =     -6    number of delayed ELM steps

NELM   =    150   number of ELM steps

EDIFF = 1E-06    energy stopping-criterion for ELM

LREAL =. FALSE.   real-space projection (. FALSE.,. TRUE., On, Auto)

IALGO = 38        algorithm (8=CG for small, 48=RMM for big systems)

#  NSIM   =      2    NSIM bands are optimized simultaneously (IALGO=48 only)

#  ROPT   =   3.75 2.80 2.20 Real-space Cutoff in Angstrom (Al, Sb, H)

#  IDIPOL = 3; DIPOL = 0.5 0.5 0.5; LDIPOL =. TRUE.

#  LAECHG =. TRUE.

LCHARG =. TRUE.

#   LVTOT =. FALSE.

LWAVE   =. TRUE.

#   LVDW   =. TRUE.

#   IVDW = 11

#   VDW_S6 = 0.75

Ionic Relaxation:

NSW    =     0    max number of geometry steps

IBRION =     2     ionic relax: 0-MD, 1-quasi-Newton, 2-CG, 3-Damped MD

EDIFFG =    -0.01   force (eV/A) stopping-criterion for geometry steps

ISIF   =     2 (1: force=y stress=trace only ions=y shape=n volume=n)

ISYM   =     0 (1-use symmetry, 0-no symmetry)

POTIM =     0.2   initial time step for geo-opt (increase for soft sys)

#   NFREE =     2

#  smass = 0.0

#  TEBEG = 400.0

DOS related values:

ISMEAR =   0 (-1-Fermi, 1-Methfessel/Paxton)

SIGMA =   0.05   broadening in eV

NEDOS = 1000

#  VOSKOWN = 1

Hybrid functional settings for HSE06

LHFCALC =. TRUE.

HFSCREEN = 0.2

AEXX = 0.25

ALGO = Damped

PRECFOCK = Fast

TIME = 0.4

Dispersion Correction in exchange and corellation functional:

#  LUSE_VDW =. TRUE.

#  AGGAC = 0.0000

#  GGA = MK

#  PARAM1 = 0.1234

#  PARAM2 = 1.0000

NPAR = 4

GGA = PE

Dispersion Correction in total energy:

#  LVDW =. TRUE.

#  VDW_C6 = 38*47.81

#  VDW_R0 = 38*1.497

Parallelization and R-Wigs flags:

LPLANE =. TRUE.

LORBIT = 11

#  RWIGS = .794 .794

Band-decomposed charge density:

#  LPARD =. TRUE.

#  LSEPB =. TRUE.

#  LSEPK =. TRUE.

#  IBAND = 1 2 3 4

#  KPUSE =

S12.2:	Density of States (DOS) of Bi2O2S Slabs

The total spin polarized DOS illustrates the electronic states available near the Fermi level.

Fig. S13: Spin-polarized total density of states (TDOS) and projected density of states (PDOS) of the pristine and adsorbate-modified Bi2O2S (001) surfaces.

S13:	Quantum Capacitance (QC) and Surface Charge Density (SCD) Calculations

After completion of the electronic structure calculations, the total density of states (DOS) obtained from DFT was used as the primary input for the quantum capacitance analysis. First, the optimized Bi2O2S slabs (pristine, K-adsorbed, and OH-adsorbed) were obtained using DFT calculations performed with VASP. The electronic structure was then evaluated by calculating DOS. Because DOS consists of discrete energy points, the data were interpolated using cubic spline functions to generate a continuous DOS profile, (D(E)). This continuous representation is required for numerical integration during the quantum capacitance calculation. To account for thermal broadening of the electronic states at room temperature (300 K), the derivative of the Fermi–Dirac distribution was introduced through the thermal broadening function

FT(E)=14kBTsec2E2kBT

where (kB) is the Boltzmann constant and (T) is the absolute temperature.

The quantum capacitance was subsequently evaluated as a function of electrochemical potential using

CQ=e2-∞+∞DOSEfT(E-eΦ)dE

where (e) is the elementary charge, (D(E)) is the electronic density of states, and (Φ) denotes the applied electrochemical potential. The integration was carried out numerically using a Python script employing the trapezoidal integration algorithm. The electrochemical potential was varied over the experimental operating window of 0.0–0.6 V, corresponding to the potential range used during cyclic voltammetry and galvanostatic charge–discharge measurements. After obtaining the potential-dependent quantum capacitance, the surface charge density was determined by integrating the quantum capacitance over the applied potential according to

σ(Φ)=0ΦCQdΦ

σ is the accumulated surface charge density.

The Python workflow generated both the CQ-potential an σ-potential datasets, which were subsequently imported into OriginPro for visualization and quantitative analysis. From these curves, the maximum quantum capacitance, maximum surface charge density, and their corresponding electrochemical potentials were extracted for comparison between the pristine and adsorbate-modified Bi2O2S surfaces. These values were further correlated with the experimentally measured specific capacitance to elucidate the influence of electronic structure modulation on the charge-storage mechanism.

Fig. S14: CQ of pristine and adsorbate-modified slabs as a function of applied potential (−0.60 to +0.60 V): (a) pristine slab, (b) K-bridge, (c) K-top, (d) K-hollow, (e) OH-top adsorption, and (f) comparison of the maximum and minimum CQ values.

Table S12: Total CQ values and their corresponding Cg values of pristine and adsorbate-modified Bi2O2S slabs

| Material | Max. CQ (μFcm⁻²) | Min. CQ (μFcm⁻²) | Max. CgDFT (F g⁻¹) | Min. CgDFT (F g⁻¹) |
| --- | --- | --- | --- | --- |
| Pure slab | 986.274 | 465.604 | 482.40 | 227.75 |
| OH-top site | 1277.508 | 497.530 | 624.85 | 243.37 |
| K-top site | 1207.658 | 409.256 | 590.69 | 200.18 |
| K-bridge site | 977.334 | 454.330 | 478.03 | 222.23 |
| K-hollow site | 1141.638 | 541.542 | 558.39 | 264.89 |

Table S13: Calculate σexp from GCD Measurements

| Id (A g⁻¹) | Cₚ (F g⁻¹) | σexp (μC cm⁻²) |
| --- | --- | --- |
| 0.5 | 920 | 940.5 |
| 1.0 | 866 | 885.3 |
| 1.5 | 798 | 815.8 |
| 2.0 | 732 | 748.3 |
| 2.5 | 675 | 690.1 |
| 3.0 | 606 | 619.5 |
| 4.0 | 520 | 531.6 |
| 5.0 | 470 | 480.5 |

Fig. S15: SCD of Bi2O2S(001) under an applied potential: (a) pristine slab, (b) K bridge-site adsorption, (c) K top-site adsorption, (d) K hollow-site adsorption, (e) OH top-site adsorption, and (f) comparison of the maximum SCD for all configurations.

S13: Additional Tables

Table S12. Selected bond lengths (Å) before and after structural relaxation for the Bi2O2S (001) slab and adsorbate configurations.

|  | Before relaxation |  |  |  |  | After relaxation |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Configuration | Bi–O | Bi–S | K–O | K–S | O–H | Bi–O | Bi–S | O–H | S–O / S–S | K–S |
| (a) Pristine slab | 2.6658 | 3.13291 | – | – | – | 2.6608 | 3.13291 | – | – | – |
| (b) K-top site | 2.6608 | 3.13291 | – | 3.79285 | – | 2.6608 | 3.13291 | – | – | 3.79285 |
| (c) K-hollow site | 2.6608 | 3.13291 | – | 3.75285 | – | 2.6608 | 3.13291 | – | – | 3.79285 |
| (d) K-bridge site | 2.6608 | 3.13291 | 3.02514 | 3.79285 | – | 2.6608 | 3.13291 | – | S–S = 2.20 | – |
| (e) OH⁻ adsorption | 2.6608 | 3.13291 | – | – | 1.20 | 2.6608 | 2.6608 | 1.20 | S–O = 1.80 | – |

Table S13: PAW datasets

| Calculation | Elements | PAW datasets used |
| --- | --- | --- |
| Pristine Bi2O2S | Bi, O, S | PAW_PBE/Bi, PAW_PBE/O, PAW_PBE/S |
| K adsorption | Bi, O, S, K | PAW_PBE/Bi, PAW_PBE/O, PAW_PBE/S, PAW_PBE/K_sv |
| OH adsorption | Bi, O, S, H | PAW_PBE/Bi, PAW_PBE/O, PAW_PBE/S, PAW_PBE/H |