Table 1

Mechanical properties of component materials.

| T800-12K carbon fiber |  |  |  | QY8911-IV bismaleimide resin |  |
| --- | --- | --- | --- | --- | --- |
| Parameter | Value | Parameter | Value | Parameter | Value |
| E11 (GPa) | 294 | ν12 | 0.3 | Em (GPa) | 4.16 |
| E22 (GPa) | 19.4 | ν23 | 0.4 | νm | 0.34 |
| G12 (GPa) | 15.0 | X11, T (MPa) | 5490 | Xm, T (MPa) | 68.44 |
| G23 (GPa) | 6.9 | X11, C (MPa) | 2689 | Xm, C (MPa) | 203.28 |

Note: E11 and E22 are the longitudinal elastic modulus and transverse elastic moduli; G12 and G23 are the shear moduli; ν12 and ν23 are the Poisson’s ratio in different directions, respectively. X11, T and X11, C are the strengths. ‘T’ and ‘C’ denote tension and compression, respectively. Em, νm, X m, T, and Xm, C are the elastic moduli, Poisson’s ratio, and strength of QY8911-IV bismaleimide resin, respectively.

Table 2

Static tensile test results.

| NO. | Tensile stiffness (GPa) | Average stiffness (GPa) | Coefficient of Variation (%) | Tensile strength (MPa) | Average strength (MPa) | Coefficient of Variation (%) |
| --- | --- | --- | --- | --- | --- | --- |
| H01 | 71.45 |  |  | 763.07 |  |  |
| H02 | 70.23 | 68.21 | 6.73 | 737.87 | 742.06 | 2.60 |
| H03 | 62.96 |  |  | 725.23 |  |  |
| P01 | 36.15 |  |  | 463.20 |  |  |
| P02 | 35.95 | 34.82 | 6.14 | 466.35 | 450.92 | 5.33 |
| P03 | 32.35 |  |  | 423.21 |  |  |

Table 3

Dwell tension-tension fatigue results for standard specimens.

| NO. | ST (%) | max (MPa) | Ndwell | Ndwell |
| --- | --- | --- | --- | --- |
| D01 | 90 | 668 | 870 | 1651 |
| D02 |  | 668 | 1274 |  |
| D03 |  | 668 | 2810 |  |
| D04 | 85 | 630 | 3005 | 2643 |
| D05 |  | 630 | 2280 |  |
| D06 | 82 | 610 | 4630 | 6555 |
| D07 |  | 610 | 11162 |  |
| D08 |  | 610 | 3872 |  |
| D09 | 80 | 593 | 12125 | 12125 |

Table 4

Dwell tension-tension fatigue results for open-hole specimens.

| NO. | ST (%) | max (MPa) | Ndwell | Ndwell |
| --- | --- | --- | --- | --- |
| H01 | 92 | 415 | 2080 | 3728 |
| H02 |  | 415 | 3080 |  |
| H03 |  | 415 | 6024 |  |
| H04 | 90 | 405 | 6661 | 5078 |
| H05 |  | 405 | 4683 |  |
| H06 |  | 405 | 3890 |  |
| H07 | 87 | 392 | 7455 | 12038 |
| H08 |  | 392 | 16621 |  |

Table 5

The results for the standard specimens under CTBF loading.

| NO. | ST (%) | max (MPa) | AH (mm) | NCCF | NCCF |
| --- | --- | --- | --- | --- | --- |
| CS01 | 77 | 570 | 0.3 | 9610 | 12301 |
| CS02 |  |  |  | 14992 |  |
| CS03 |  |  | 0.5 | 13210 | 9634 |
| CS04 |  |  |  | 6058 |  |
| CS05 |  |  | 0.8 | 8301 | 5771 |
| CS06 |  |  |  | 3241 |  |
| CS07 | 80 | 593 | 0.3 | 13023 | 8923 |
| CS08 |  |  |  | 3224 |  |
| CS09 |  |  |  | 10523 |  |
| CS10 |  |  | 0.5 | 7434 | 6815 |
| CS11 |  |  |  | 4690 |  |
| CS12 |  |  |  | 8321 |  |
| CS13 |  |  | 0.8 | 2471 | 3566 |
| CS14 |  |  |  | 241 |  |
| CS15 |  |  |  | 7985 |  |
| CS16 | 82 | 610 | 0.3 | 2014 | 5360 |
| CS17 |  |  |  | 8598 |  |
| CS18 |  |  | 0.5 | 1380 | 3077 |
| CS19 |  |  |  | 2229 |  |
| CS20 |  |  |  | 5623 |  |
| CS21 |  |  | 0.8 | 564 | 1275 |
| CS22 |  |  |  | 1985 |  |

Table 6

CTBF loading results for open-hole specimen.

| NO. | ST (%) | max (MPa) | AH (mm) | fB (Hz) | NCCF | NCCF |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| CH01 | 82 | 370 | 0.3 | 30 | 32085 | 28278 |  |
| CH02 |  |  |  |  | 24470 |  |  |
| CH03 |  |  |  | 50 | 17406 | 18848 |  |
| CH04 |  |  |  |  | 20289 |  |  |
| CH05 |  |  |  | 80 | 18977 | 16381 |  |
| CH06 |  |  |  |  | 13785 |  |  |
| CH07 |  |  | 0.5 | 30 | 20010 |  |  |
| CH08 |  |  |  |  | 15913 | 14944 |  |
| CH09 |  |  |  |  | 8909 |  |  |
| CH10 |  |  | 0.8 | 30 | 2263 |  |  |
| CH11 |  |  |  |  | 7953 | 5086 |  |
| CH12 |  |  |  |  | 5043 |  |  |
| CH13 | 87 | 392 | 0.3 | 30 | 7386 |  |  |
| CH14 |  |  |  |  | 6311 | 7904 |  |
| CH15 |  |  |  |  | 10014 |  |  |
| CH16 |  |  | 0.5 | 30 | 1219 |  |  |
| CH17 |  |  |  |  | 6234 | 5714 |  |
| CH18 |  |  |  |  | 9690 |  |  |
| CH19 |  |  | 0.8 | 30 | 968 | 1775 |  |
| CH20 |  |  |  |  | 2581 |  |  |
| CH21 | 90 | 405 | 0.3 | 30 | 1781 | 3046 |
| CH22 |  |  |  |  | 4311 |  |
| CH23 |  |  | 0.5 | 30 | 1219 |  |
| CH24 |  |  |  |  | 1706 | 1205 |
| CH25 |  |  |  |  | 690 |  |
| CH26 |  |  | 0.8 | 30 | 168 | 612 |
| CH27 |  |  |  |  | 1056 |  |

Table 7

Test results for standard specimens under CTBF loading at ST=80% and fB=30Hz.

| MF | Parameters | (%) |  |  |  | (%) |
| --- | --- | --- | --- | --- | --- | --- |
| Trapezoidal distribution | a=1.39 b=2.31 | 2.22 | 120 | 8923 | 7453 | 16.5 |
|  |  | 3.40 |  | 6815 | 5636 | 17.3 |
|  |  | 4.29 |  | 3566 | 3063 | 14.1 |
| Normal distribution | a=1.39 c=0.20 | 2.22 | 120 | 8923 | 7031 | 21.2 |  |
|  |  | 3.40 |  | 6815 | 5214 | 23.5 |  |
|  |  | 4.29 |  | 3566 | 2871 | 19.5 |  |
| Γ-type distribution | a=1.39 k=6.50 | 2.22 | 120 | 8923 | 8369 | 6.2 |  |
|  |  | 3.40 |  | 6815 | 6601 | 3.1 |  |
|  |  | 4.29 |  | 3566 | 3210 | 9.8 |  |
| Parabolic distribution | a=1.39 b=2.31 | 2.22 | 120 | 8923 | 7437 | 16.8 |  |
|  |  | 3.40 |  | 6815 | 5563 | 18.4 |  |
|  |  | 4.29 |  | 3566 | 3083 | 13.6 |  |

Table 8

Test results for open-hole specimens under CTBF loading at ST=87%, fB=30Hz.

| MF | Parameters | (%) |  |  |  | (%) |
| --- | --- | --- | --- | --- | --- | --- |
| Trapezoidal distribution | a=1.39 b=2.31 | 1.71 | 120 | 7904 | 6968 | 13.4 |
|  |  | 3.11 |  | 5714 | 4887 | 16.8 |
|  |  | 5.24 |  | 1775 | 1495 | 15.9 |
| Normal distribution | a=1.39 c=0.20 | 1.71 | 120 | 7904 | 9619 | -21.6 |
|  |  | 3.11 |  | 5714 | 4829 | 18.3 |
|  |  | 5.24 |  | 1775 | 1433 | 23.8 |
| Γ-type distribution | a=1.39 k=6.50 | 1.71 | 120 | 7904 | 8831 | -11.7 |
|  |  | 3.11 |  | 5714 | 5010 | 12.3 |
|  |  | 5.24 |  | 1775 | 1560 | 12.1 |
| Parabolic distribution | a=1.39 b=2.31 | 1.71 | 120 | 7904 | 6305 | 20.2 |
|  |  | 3.11 |  | 5714 | 4646 | 18.7 |
|  |  | 5.24 |  | 1775 | 1481 | 16.5 |

Table 9

Comparison of CTBF life predictions for standard specimens.

| (MPa) | (mm) | (%) |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  | Palmgrem-Miner model | Modified Miner model | Zhu’s interaction model | Proposed model |
| 570 | 0.3 | 1.48 | 12301 | 18369 | 14658 | 10087 | 11268 |
|  | 0.5 | 2.19 | 9634 | 17250 | 12023 | 6930 | 10568 |
|  | 0.8 | 3.86 | 5771 | 9890 | 6875 | 3890 | 6520 |
| 593 | 0.3 | 2.22 | 8923 | 10325 | 9968 | 6635 | 8369 |
|  | 0.5 | 3.40 | 6815 | 9501 | 7830 | 4680 | 6601 |
|  | 0.8 | 4.29 | 3566 | 7201 | 4980 | 2021 | 3210 |
| 630 | 0.3 | 3.04 | 5360 | 8895 | 6758 | 3603 | 4930 |
|  | 0.5 | 4.40 | 3077 | 6681 | 4680 | 1360 | 3512 |
|  | 0.8 | 5.46 | 1275 | 3683 | 1735 | 668 | 1620 |

Table 10

Comparison of CTBF fatigue life predictions for open-hole specimens.

| (MPa) | (mm) | (%) |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  | Palmgrem-Miner model | Modified miner model | Zhu’s interaction model | Proposed model |
| 370 | 0.3 | 1.09 | 28278 | 46253 | 40231 | 15123 | 37201 |
|  | 0.5 | 1.49 | 14944 | 32124 | 28653 | 8259 | 19230 |
|  | 0.8 | 2.75 | 5086 | 7598 | 6632 | 4230 | 5600 |
| 393 | 0.3 | 1.71 | 7904 | 9610 | 10112 | 4871 | 8831 |
|  | 0.5 | 3.11 | 5714 | 6574 | 7536 | 2687 | 5010 |
|  | 0.8 | 5.24 | 1775 | 3623 | 3120 | 3251 | 1560 |
| 406 | 0.3 | 2.58 | 3046 | 4635 | 5300 | 1231 | 3210 |
|  | 0.5 | 4.87 | 1205 | 3600 | 3101 | 823 | 1608 |
|  | 0.8 | 6.53 | 612 | 890 | 1023 | 489 | 750 |