Supporting Information

High energy storage capabilities of CaCu3Ti4O12 for paper based zinc air battery

Upasana Bhardwaja, Aditi Sharmaa, Vinay Guptab H.S Kushwahaa*

a Materials Research Centre, Malaviya National Institute of Technology Jaipur, Rajasthan, India-302017

b Department of Physics, Khalifa University of Science and Technology, Abu Dhabi 127788, United Arab Emirates

a*Corresponding author, e-mail: himmatsingh.mrc@mnit.ac.in;

Address: Materials Research Centre, MNITJ, India.

Figure.S1: XPS spectra of the prepared CaCu3Ti4O12 Perovskite material.

Figure.S2: EDS mapping and distribution of the as-prepared CaCu3Ti4O12 (CCTO) slurry on the electrode

Table.S1: EDS weight ratio of the perovskite catalyst-

| S.No. | El AN | Series | unn. C [wt.%] | norm. C [wt.%] | Atom. C [at.%] |
| --- | --- | --- | --- | --- | --- |
| 1. | C 6 | K-series | 49.18 | 40.95 | 75.45 |
| 2. | Cu 29 | K-series | 35.17 | 29.28 | 10.20 |
| 3. | Ti 22 | K-series | 20.45 | 17.02 | 7.87 |
| 4. | Ni 28 | K-series | 10.88 | 9.06 | 3.42 |
| 5. | Ca 20 | K-series | 2.94 | 2.45 | 1.35 |
| 6. | O 8 | K-series | 1.49 | 1.24 | 1.71 |

Figure S3: (a) N2 desorption and adsorption isotherms; (b) CCTO BET multi-point plot.