Supporting Information

Interpretable Machine Learning Reveals Atom-Resolved VOCs Adsorption and Reactivity on Metal Oxides

Biluan Zhang1,2, Pan Yan3, Lu Yan1,2, Dongbo Zhou4*, Jinlong Wang1,2,3*, Yanbing Guo1,2,3*

1Institute of Environmental and Applied Chemistry, College of Chemistry, Central China Normal University, Wuhan 430079, P. R. China

2Engineering Research Center of Photoenergy Utilization for Pollution Control and Carbon Reduction, Ministry of Education, Central China Normal University, Wuhan 430079, P. R. China

3Wuhan Institute of Photochemistry and Technology, Wuhan 430083, P. R. China

4Laboratory for Artificial Intelligence and New Forms of Education, Central China Normal University, Wuhan 430079, China

*Correspondence: zhoudongbo@mail.ccnu.edu.cn; wjl2022@ccnu.edu.cn; guoyanbing@mail.ccnu.edu.cn

Supplementary Notes

N1 Dataset description.

N2 Theoretical derivation of dual-tower network.

N3 Hyperparameters for AdsDT models.

N4 Sensitivity of the AdsDT model to surface geometric fluctuations.

N5 Calibration curve and miscalibration area.

N6 Error curve at various uncertainty cutoffs.

N7 Dimensionality reduction of datasets.

N8 Computational methods.

N9 Similarity between OC20-Dense and metal oxides-VOCs datasets.

N10 Computational cost comparison.

N11 Identify different types of adsorption sites from cross-attention scores.

N12 Correlation between atomic contribution and chemical structural units.

N13 GCN-Ads (Graph Convolutional Network) model for VOCs adsorption energy prediction.

N14 SHAP based atomic weight analysis for VOCs adsorption.

N15 The Construction of Bond Activation Score Sbond,ij

N16 Experimental methods.

Supplementary Figures

S1 The architecture of AdsDT encoder.

S2 Independent aggregator and late interaction aggregator.

S3 (a) Loss function (b) Mean absolute error (c) Root mean squard error (d) R-square of the test set and train set versus training size for the AdsDT approach trained on OC20 dataset.

S4 Robustness evaluation under different types and intensities of noise for the AdsDT approach trained on OC20 dataset.

S5 Prediction performance of transfer learning models with unfrozen backbone under three different dataset combinations.

S6 Ablation performance of transfer learning fine-tuning path.

S7 The periodic table outlining elements included in the the Open Catalyst 2020 datasets.

S8 The periodic table outlining elements included in the Alloys-VOCs datasets.

S9 The periodic table outlining elements included in the metal oxides-VOCs datasets.

S10 The uniform manifold approximation and projection (UMAP) plot of surface/adsorbate combinations in three datasets.

S11 Comparison of the process of building a database using traditional DFT and deep learning model methods.

S12 Error distribution of predicted adsorption energies against DFT-calculated adsorption energies.

S13 Distribution range of adsorption energy and boxplot statistical significance on TiO2 (Anatase, 101) surface.

S14 Comparison of SHAP analysis performance for analyzing the influence of functional groups on adsorption energy using on TiO2 (Anatase, 101) surface.

S15 Cross-attention-based reasoning for adsorption site prediction. Multi-head attention scores between the adsorbate and surface atoms are averaged and visualized as an attention-colored surface, highlighting the most favorable adsorption sites.

S16 Visualization of singly bonded carbon (C1) atomic attention weights.

S17 Visualization of double bonded carbon (C2) atomic attention weights.

S18 Visualization of singly bonded nitrogen (N1) atomic attention weights.

S19 Visualization of double bonded nitrogen (N2) atomic attention weights.

S20 Visualization of singly bonded oxygen (O1) atomic attention weights.

S21 Visualization of double bonded oxygen (O2) atomic attention weights

S22 Visualization of halogen atom (F, Cl, Br) attention weights.

S23 Visualization of attention weights for multifunctional VOCs molecules.

S24 Correlation of oxygen attention values with (a) adsorption energy and (b) oxygen charge loss across different functional groups on TiO2 (Anatase, 101) surface.

S25 Atomic attention weights for ethyl acetate molecules adsorbed on TiO2(Anatase, 101) surface.

S26 The projected density of states (PDOS) analysis of ethyl acetate adsorption on TiO2 (Anatase, 101) surface.

S27 Theoretical reaction pathways for ethyl acetate activation on TiO2 (Anatase, 101) surface.

S28 The XRD patterns of TiO2_Anatase catalyst.

S29 TEM images of TiO2_Anatase catalyst.

S30 In situ DRIFTS of ethyl acetate adsorption over TiO2_Anatase catalyst.

S31 Side and top views of the surface structures of eight metal oxides.

S32 GCN model performance for adsorption energy prediction on eight metal oxides

Supplementary Tables

S1 The hyperparameter specification table for AdsDT model.

S2 Comparison of input requirements for adsorption energy prediction models.

S3 Overall Test MAE results (eV) of AdsDT framework with different graph encoders on OC20-Dense datasets without transfer learning.

S4 Statistics of the DFT-constructed Alloys-VOCs dataset.

S5 Statistics of the DFT-constructed metal oxides-VOCs dataset.

S6 Performance table of progressive transfer learning fine-tuning path ablation.

S7 Dataset size and adsorption energy distribution of three datasets.

S8 Adsorbate information for OC20-Dense dataset.

S9 Adsorbate information for Alloys-VOCs and metal oxides-VOCs datasets.

S10 Chemical family distribution of adsorbates in the OC20-Dense dataset.

S11 Chemical family distribution of adsorbates in the Alloys-VOCs and metal oxides-VOCs datasets.

S12 Verify the selected data information, predictions, and DFT adsorption energy.

S13 Adsorption energy predictions for 816 VOC molecules on TiO2(anatase, 101) surface by the transferable AdsDT model.

S14 Atom-level attention weights extracted from the transferable AdsDT model for 816 VOC molecules adsorbed on the TiO2_Anatase (101) surface.

S15 In situ DRIFTS peak assignments for ethyl acetate on TiO2.

S16 Structural details of eight metal oxide surfaces.

S17 Complete performance metrics of the GCN model on training and test sets for eight metal oxide surfaces.

S18 Average atomic attention weights of different atomic environments for VOCs molecules on eight metal oxides surfaces.

S19 Calculated bond activation scores for all chemical bonds in ethanol on TiO2(anatase, 101) surface.

Supplementary Data

Data1 Atomic attention weights of all atoms across 816 VOCs molecules adsorbed on the eight metal oxide surfaces.

Data2 Bond activation scores of individual chemical bonds for 36 representative VOCs molecules adsorbed on the eight metal oxides surface.

Supplementary Notes

N1 Dataset description

The Open Catalyst 2020 (OC20) dataset is the most extensive and diverse dataset for heterogeneous catalysis. It contains over 1.2 million DFT relaxations computed using the revised Perdew-Burke-Ernzerhof (RPBE) functional. This dataset covers multiple tasks, including Initial Structure to Energy (IS2RE), Initial Structure to Relaxed Structure (IS2RS), and Structure to Energy and Force (S2EF). In our study, we focus on data from the IS2RE/IS2RS tasks, which consist of 460328 DFT relaxation trajectories. The core goal of the IS2RE task is to predict the relaxed adsorption energy from the unrelaxed initial atomic structure of each adsorbate-catalyst configuration. Accordingly, we extracted the final frame of these relaxation trajectories as our target energy labels. To systematically probe the global minimum adsorption energy of adsorbate-catalyst pairs, the OC20-Dense dataset was developed. While the original OC20 dataset covers broad types of adsorbates and catalytic surfaces, it lacks sufficient diversity in adsorption geometries. OC20-Dense addresses this gap by densely enumerating distinct adsorption configurations. Initial adsorbate-surface configurations were generated via both heuristic and random strategies, followed by structural relaxations using machine-learning and DFT methods. The OC20-Dense dataset contains 995 distinct adsorbate-catalyst pairs, evenly selected from the in-domain and three out-of-domain splits within the OC20 validation set. Therefore, the raw OC20-Dense dataset shares no overlap with the original OC20 training set. The official OC20-Dense provides an optional training subset containing 15450 data entries. Its validation set was randomly sampled with 9 001 entries from the three out-of-domain splits of the OC20 validation set. For its test set, ML-relaxed structures sourced from the same three out-of-domain splits of the OC20 validation set are provided by the Open Catalyst Challenge 2023. All noise-perturbation robustness tests reported in the main text were performed on this curated OC20-Dense dataset.

N2 Theoretical derivation of dual-tower network

The dual-tower network is a canonical two-branch encoding architecture with independently parameterized branches. Its core concept is to project heterogeneous input features originating from two distinct domains into a shared low-dimensional embedding space, enabling high-level semantic matching and similarity quantification. Owing to this decoupled encoding design, two-tower architectures deliver stable feature representations and strong noise robustness for matching-oriented tasks.

From a robustness perspective, this decoupled two-branch structure endows the model with intrinsic anti-interference properties. Input-level noise or perturbations only distort the embedding within one single branch, and cross-branch similarity computation mitigates biases introduced by local noise. Unlike single-branch architectures, the two-tower design prevents gradient aliasing of heterogeneous features during back-propagation. Since each branch updates its own parameters independently, stable training and consistent feature distributions can be maintained even under noisy conditions.

N3 Hyperparameters for AdsDT models

We optimized key hyperparameters of the AdsDT model via small-scale grid-search on a held-out subset of the OC20 dataset. The hyperparameters under tuning cover hidden-channel dimension, number of message-passing layers for graph encoders, layer count of vector encoders, batch size, initial learning rate, learning-rate decay factor (gamma), and maximum training epoch. Major hyperparameter settings for AdsDT are summarized in Table S1. Full hyperparameter configurations for all AdsDT variants are available at our GitHub repository: https://github.com/iojsea/metal-oxide-vocs-adsorption.

N4 Sensitivity of the AdsDT model to surface geometric fluctuations

To investigate the sensitivity of the AdsDT model to the surface’s geometry (e.g., atom distances and lattice constants), we introduced noise to input surface structures while preserving atomic connectivity via two strategies:

(1) Random perturbation of atomic coordinates along the x, y, and z directions (displacements < 0.2 Å);

(2) Random perturbation of the in-plane lattice vectors a and b (deviations < 2%). The c vector, which corresponds to the vacuum layer direction, was unchanged.

We assessed prediction fluctuations and mean energy offsets arising from geometric variations by comparing AdsDT predictions computed on pristine and noise-perturbed surface geometries. As shown in Figure S14, AdsDT models with different graph encoders exhibit low energy prediction fluctuation after adding geometric noise to the input surfaces. These observations demonstrate that our model exhibits low sensitivity to surface geometric distortions, provided that atomic connectivity is maintained. Such robustness is beneficial when processing surface structures retrieved from diverse crystallographic databases for interfacial interaction analysis.

N5 Calibration curve and miscalibration area

Calibration serves as a critical and rigorous metric for evaluating uncertainty estimation. It quantifies whether predicted uncertainty magnitudes yield statistically meaningful confidence intervals that match empirical observation. Although ensemble-based uncertainty quantification is widely adopted for deep neural networks, such predicted uncertainties can suffer from poor calibration, leading to either over-confident or under-confident model outputs. For instance, treating each model prediction and its associated uncertainty as the mean µ and standard deviation σ of a Gaussian distribution N(µ, σ2): at a nominal 95% confidence level, an over-confident model will enclose fewer than 95% of ground-truth data points within its predicted interval. By contrast, a well-calibrated model will capture approximately 95% of true observations inside this interval, whereas an under-confident model will enclose more than 95% of ground-truth points.

We followed standard protocols from prior literature to assess the calibration quality of our model-predicted uncertainties. For each sample xi, we treated the predicted adsorption-energy value µ(xi) and its uncertainty σ(xi) as the mean and standard deviation of a Gaussian distribution N. For a given nominal confidence level α, we computed the α-level confidence-interval bounds Li(α) and Ri(α) via the inverse cumulative-distribution function (inverse-CDF) of the corresponding Gaussian distribution. For an ideally calibrated model, the empirical fraction of ground-truth points falling within this interval should equal the nominal confidence level α. We calculated the observed empirical coverage fraction as:

f(α)=yiLi(α)≤yi≤Ri(α)ND             (S1)

where ND denotes the total number of data points. Plotting the empirical coverage fraction f(α) against the nominal confidence level α over the range 0≤α≤1 yields the calibration curve. A perfectly calibrated model produces a diagonal identity line. To numerically quantify miscalibration, we computed the integrated absolute area between the obtained calibration curve and this ideal diagonal reference line, known as the miscalibration area. All calibration-curve computation and miscalibration-area evaluation were performed using the Uncertainty Toolbox v0.1.1 software package

N6 Error curve at various uncertainty cutoffs

One common strategy for validating uncertainty estimates is to examine their correlation with actual prediction errors. A well-behaved uncertainty estimator is expected to deliver lower prediction error among its high-confidence predictions. We adopted a standard evaluation workflow to verify whether our predicted uncertainties correlate with real-world prediction errors. Test-set predictions are sorted in descending order of predicted uncertainty, indexed by ri. Under this ordering, ŷr1 corresponds to the prediction with the largest estimated uncertainty, whereas ŷrn represents the most confident prediction, with n being the total number of test samples. For each index i, we compute the cumulative mean absolute error (MAEi) over the subset of samples satisfying j ≥ i:

MAEi=1n−i+1∑j ≥ inŷrj−yri              (S2)

where yrj denotes the ground-truth reference value for the prediction ŷrj. This metric quantifies model prediction performance under different confidence cutoffs. For instance, setting i=0.5n yields the MAE evaluated at the 50 % confidence cutoff. We construct the error curve by plotting cumulative MAEi against varying confidence-cutoff thresholds.

N7 Dimensionality reduction of datasets

The imensionality reduction was carried out via the uniform manifold approximation and projection (UMAP) algorithm as implemented in umap-learn v0.5.5. UMAP constructs a weighted graph of three datasets in the high-dimensional space and then projects this graph to a two-dimensional space. Each node of the graph represents a surface/adsorbate combination, and each combination is depicted by the smooth overlap of atomic positions (SOAP) descriptors of surfaces concatenated with RDKit descriptors of adsorbates. The number of neighbors was set to 50, and the minimum distance between points was set to 0.4 Å. All other parameters were set to the default values (for reproducibility, a random seed of 16 was used). SOAP is a descriptor that encodes regions of atomic geometries by using a local expansion of a Gaussian smeared atomic density with orthonormal functions based on spherical harmonics and radial basis functions. In this work, average SOAP descriptors of catalyst surface were generated by DScribe v2.1.0 package. One way of turning a local SOAP descriptor matrix into a global descriptor vector is simply by taking the average over all sites. The inner averaging mode in DScribe was used, which is taken over the sites before summing up the magnetic quantum number based on:

Pnn'lZ1,Z2~∑m1nicnlmi,Z11nicn'lmi,Z2         (S3)

cnlmZR3ndVgn(r)Ylm(θ,ϕ)ρZ(r)               (S4)

where n and n’ are indices for the different radial basis functions up to nm is the angular degree of the spherical harmonics up to Ylm are atomic species, and ρZ(r) is the Gaussian smoothed atomic density for atoms. In general, the inner averaging will preserve the configurational information better. Additionally, the cutoff for the local region is set to 4.0 Å, the number of radial basis functions is set to 8, the maximum degree of spherical harmonics is set to 6, and the feature compression method is set to 2.

N8 Computational methods

Calculations performed in this work were carried out by using density functional theory (DFT) as performed by Vienna ab initio simulation package (VASP). Exchange-correlation functions are taken as the generalized gradient approximation (GGA) in the form of Perdew-Burke-Ernzerhof (PBE). The projector augmented wave (PAW) method was used to replace the pseudopotential of inner core electrons and nucleus with the valence electrons. The long-range van der Waals interaction was incorporated by adopting the zero damping DFT-D3 method of Grimme The Kohn-Sham electron wave functions were expanded using the plane-wave functions with an energy cutoff of 450 eV. The 2×2×1 k-point meshes in Brillouin zone was sampled for structure optimization and electronic property according to the Monk Horst-Pack scheme. The optimization was considered convergence and each atom would be fully relaxed until the spring force between adjacent images was less than 0.02 eV Å-1, the total energy change upon two steps for the electronic self-consistent field iteration was less than 1E-5 eV. The vacuum layer was set to 15 Å in the z-direction to avoide the interaction among mirror images. As for the adsorption case, the adsorption energy (Eads) was defined as:

Eads = Esubstrate+adsorbate - Esubstrate - Eadsorbate         (S5)

where Esubstrate+adsorbate, Esubstrate, and Eadsorbate are the energies of the optimized adsorbate/substrate model, the clean substrate slab, and the adsorbate, respectively. Crystal structure diagrams were drawn with Visualization for Electronical and Structural Analysis (VESTA).

N9 Similarity between OC20-Dense and Metal oxides-VOCs datasets

Domain similarity between source and target domains constitutes a critical prerequisite for effective transfer-learning performance. The OC20-Dense dataset is derived from the Open Catalyst Project, where surfaces and adsorbates follow the unified DFT calculation protocols of the original OC20 dataset. All surface structures are built from crystal entries retrieved from the Materials Project database, covering 54 chemical elements, diverse crystal systems and space groups, with surface facets limited to a maximum Miller index below 2.

Our target metal oxides-VOCs dataset also adopts crystal-structure inputs originating from the Materials Project database and follows consistent DFT calculation conventions for adsorption systems. Both datasets contain diverse solid surfaces and molecular adsorbates, and share common physical descriptors for characterizing surface-adsorbate interfacial interactions. Benefiting from these shared foundations, the source-domain OC20-Dense and target metal-oxides-VOCs datasets exhibit reasonable domain similarity, which supports effective knowledge transfer in our progressive transfer-learning workflow.

N10 Computational cost comparison

For the AdsDT model, predicting adsorption energies for 1000 surface-adsorbate pairs takes approximately 12 s on an RTX 3090 GPU, corresponding to a prediction latency of 0.012 s per pair. We benchmark AdsDT against the AdsorbML workflow, which combines machine-learning interatomic potentials (MLIPs) with heuristic structure searching for adsorption-energy evaluation. For one individual surface-adsorbate pair, AdsorbML generates 100 candidate initial adsorption geometries via heuristic and random sampling (numsite = 100). Each initial geometry is subsequently relaxed using an MLIP. With the GemNet-OC model (39 M parameters, pretrained on the OC20 dataset), each 80-step structural relaxation costs ~4 s on an RTX 3090 GPU. Consequently, AdsorbML requires roughly 400 s to evaluate the adsorption energy for a single surface-adsorbate pair. Under this benchmark, AdsDT achieves a speedup of ~3.3×104 relative to the AdsorbML pipeline.

Consider a target reaction with two key intermediate adsorbates and a catalyst library containing 200000 unique catalysts. Assuming 20 surface terminations are generated per catalyst, this yields a total of 4000000 candidate surfaces. Using AdsDT, computing adsorption energies for these two adsorbates across all candidate surfaces requires approximately 1 GPU day. In contrast, the AdsorbML pipeline based on the pretrained GemNet-OC (39 M) MLIP would demand ~37037 GPU days. Even with parallel computation across 100 GPUs, the full calculation would still take 370 days. Therefore, AdsDT exhibits superior computational efficiency and shows great promise for large-scale catalyst pre-screening, particularly for catalyst databases containing ≧1 M entries.

N11 Identify different types of adsorption sites from cross-attention scores

Furthermore, we explored extending our method to identify different types of adsorption sites rather than simply assessing the importance of individual surface atoms. Given a set of surface atoms A and their attention scores S, higher attention scores indicate that the atom is more important for strong adsorption. The maximum attention score is defined as smax, and the set of atoms with scores above 0.8smax is defined as the potential site atoms P. For the atom i in P, if no atom j in P satisfies Equation S6, then atom i is considered to constitute a top site. For the atom i in P, if there is only one atom j in P that satisfies Equation S6, then atoms i and j are considered to constitute a bridge site. If there are three atoms i, j and k in P, where dij, dik and djk all satisfy Equation S6 and form a triangle, then atoms i, j and k are considered to constitute a hollow site.

dij < ri+rj+δi≠j           (S6)

In Equation S6, dij represents the distance between atoms i and j, ri and rj are the covalent radii of atoms i and j, respectively, and δ can either be a fixed value or the geometric diameter of the adsorbate. We evaluated this extended method using our AdsDT models, without considering more complex site types. Based on the improved method described above, it is possible to identify adsorption site types (top, bridge, hollow) using attention scores and the distances between high-scoring atoms. Isolated high-scoring atoms without surrounding high-scoring atoms tend to form top sites, while high-scoring atoms close to each other are more likely to form bridge or hollow sites. The results show that the cross-attention scores have the potential to identify the adsorption site type through the improved method, which will be further studied in future work.

N12 Correlation between atomic contribution and chemical structural units

To further connect model-level interpretability with chemically meaningful structural units, we systematically analyzed the correlation between atom-wise attention contributions and the local chemical environments of adsorbate molecules. For each adsorbate-surface configuration, we extracted the cross-attention score assigned to every atom in the adsorbate molecule. These atom-level contributions were then grouped and aggregated according to predefined chemical structural units, including functional groups (e.g., -OH, -COOH, -NH₂, -NO₂, -SH, -Cl), heteroatom types (O, N, S, halogen), and bond types (C-C, C-H, C-O, C-N, C-S, C-halogen).

For a given structural unit u, we define its aggregated contribution Cu as the sum of attention scores of all atoms belonging to that unit:

Cu=a∈usa           (S7)

where sa denotes the cross-attention score of atom a. By comparing Cu across different structural units within the same molecule and across the entire dataset, we identified which chemical moieties dominate the adsorption interaction and which remain relatively inert.

The heteroatom-containing functional groups consistently exhibit higher aggregated contributions than hydrocarbon backbones. In particular, oxygen-containing groups (-OH, -COOH, -C=O) and nitrogen-containing groups (-NH2, -NO2) serve as the dominant adsorption anchors on most metal-oxide surfaces, owing to their strong lone-pair-metal coordination interactions. Sulfur- and halogen-containing groups show material-dependent behavior. They dominate adsorption on reducible metal oxides but contribute less on inert oxide surfaces.

Notably, the structural unit with the highest aggregated contribution does not always correspond to the bond that undergoes preferential cleavage during subsequent surface reactions. Instead, high-contribution anchoring groups induce significant interfacial electronic redistribution, which remotely activates neighboring C-H or C-C bonds within the hydrocarbon backbone. This observation is consistent with our earlier finding that the primary adsorption anchor is not necessarily the direct bond-cleavage site.

We further quantified the correlation between aggregated structural-unit contributions and experimentally/DFT-derived adsorption strengths using Pearson correlation coefficients. Across eight metal oxides and diverse heteroatom-containing VOCs, the aggregated contribution of the top-ranked structural unit shows a strong positive correlation with adsorption energy (R2>0.8), confirming that AdsDT-derived atom-wise contributions capture chemically meaningful structure-adsorption relationships. These results demonstrate that atom-level interpretability can be systematically mapped onto chemically intuitive structural units, providing a quantitative bridge between model attention weights and molecular-level adsorption chemistry.

N13 GCN-Ads (Graph Convolutional Network) Model for VOCs Adsorption Energy Prediction

Molecular Graph Representation and Node Feature Engineering. Each VOC molecule was represented as an undirected graph (G=V, E), the graph convolutional network (GCN)‑based model, where atoms correspond to node set V and covalent bonds form edge set E. Molecular graphs were constructed from SMILES strings via RDKit with explicit hydrogen atoms added. Bond‑type information was not adopted as input feature; edges only stored atom‑pair indices to define molecular topology. Each atomic node was encoded into a 29‑dimensional feature vector including element‑type one‑hot encoding, atomic degree, hybridization state, implicit valence, aromaticity flag, 3‑8‑membered ring membership, hydrogen‑bond donor‑acceptor tags, formal charge, shortest‑path distance to candidate adsorption‑relevant atoms, and binary marker for adsorption‑active sites. Candidate adsorption‑reactive atoms of VOCs were detected by RDKit‑based SMARTS sub‑structure matching for hydroxyl, carbonyl, amine, aromatic rings and halogen‑containing groups, and duplicate matches were removed by post‑processing.

The GCN‑Ads architecture contains five graph‑convolution layers followed by three fully‑connected layers. The hourglass‑shaped graph convolution block expands 29‑dim input features to 1024, compresses to 256, then expands back to 1024; batch normalization and ReLU activation follow each convolution layer. A global attention layer aggregates node embeddings into molecule‑level representation, and fully‑connected layers (1024 → 128 →16) output scalar adsorption‑energy prediction. The model was trained with batch size 128, Adam optimizer, initial learning rate 0.0001, decay factor 0.7 (triggered if validation‑set MSE plateaus for 10 epochs, learning‑rate decay factor = 0.00001), MSE loss function, maximum 1000 epochs. The checkpoint with optimal validation MSE was saved for prediction and interpretability. The curated dataset of VOCs adsorption‑energy samples was filtered by removing missing labels, physically unreasonable values, molecules >500 Da and non‑common elements, then split into training/validation/test sets.

N14 SHAP Based Atomic Weight Analysis for VOCs Adsorption

GraphSHAP was applied to quantify atomic‑level marginal contributions toward VOCs adsorption energy prediction. The Shapley value for atom i:

ϕi=S∈NS!(N−S−1)!N!fx(S∪i)−fx(S)         (S8)

where N is full atom set, S denotes atom subsets excluding atom i, and fx is trained GCN‑Ads prediction function. Monte‑Carlo sampling approximated exact Shapley values under chemical connectivity constraints for valid subgraphs; atomic masking was performed by zeroing node‑feature vectors. Two‑step standardization (Z‑score transformation followed by sigmoid mapping onto [-1,1] enabled cross‑molecule comparison. Positive SHAP values mean the atom increases predicted adsorption‑energy (promote adsorption); negative values mean the atom decreases adsorption‑energy (suppress adsorption). Standardized SHAP values were projected onto molecular diagrams for heatmap visualization. Structured SHAP further aggregated atomic contributions into functional‑group‑level scores, incorporating pairwise atomic interaction SHAP terms. The global attention weights from model internal layers were also extracted via forward‑pass hooks, min‑max normalized to [0,1] and mapped onto molecular structures as auxiliary heatmaps, which reveal which atomic regions the GCN model focuses on during adsorption energy regression task.

N15 The Construction of Bond Activation Score Sbond,ij

For each chemical bond (i-j) in VOCs molecules, three physically meaningful normalized sub-terms are defined to quantify atomic interaction, bond energetics and bond polarization, namely Aij (normalized attention contribution), Eij (normalized energetic contribution), and Pij (normalized polarization contribution).

Aij originates from atom-level weight parameters wi and wj of the two bonded atoms i and j. This term reflects synergistic or counteracting interactions between bonded atomic sites. Positive values occur when wi and wj share the same sign for cooperative sites, whereas negative values appear under opposite sign weights indicating mutual offset of atomic effects. Hydrogen atoms are assigned with fixed weight wH=0. Consequently, the weight-interaction component of Aij automatically equals zero for any bond involving hydrogen. An adsorption reward term Rij is embedded within Aij. Rij is calculated from the minimum weight of the two bonded atoms, based on the hypothesis that the atom with the lowest weight in bond (i-j) serves as the dominant adsorption active site and brings positive reward for bond activation. A tunable and interpretable hyperparameter λads ∈ [0,1] controls the relative magnitude of this adsorption reward effect.

Eij denotes the energetic contribution derived from the bond energy (homolytic bond dissociation energy) BDEij of bond (i-j), calculated as the ratio of the average bond dissociation energy within the same VOC molecule to the bond energy of the target bond It describes the intrinsic difficulty for homolytic cleavage of the target bond. Larger Eij corresponds to weaker intrinsic bond strength.

Pij is the polarization contribution calculated from absolute Pauling electronegativity difference χi−χj between atom i and j: Pij=1+χi−χjΔχ, where Δχ is the average electronegativity difference of all bonds within the same VOC molecule. It quantifies charge separation and polar character of covalent bonds. The constant baseline value of unity represents the inherent activation contribution of nonpolar bonds, and increasingly polarized bonds receive an enhanced contribution from the electronegativity difference term.

The final bond activation score Sbond,ij is obtained by multiplying the three sub-terms to capture their coupled effects: Sbond,ij=Aij · Eij· Pij. Sbond,ij provides an integrated measure of the susceptibility of bond (i-j) to activation. It jointly incorporates atomic weight adsorption effect, intrinsic bond energy and covalent bond polarizability. Higher Sbond,ij indicates that the corresponding covalent bond is more vulnerable to perturbation, polarization or activation under adsorption and catalytic conditions during VOCs oxidation. It should be noted that the physically driven Sbond,ij obeys physical monotonicity: bonds with lower bond energy and stronger polarity tend to acquire higher scores. Minor discrepancies are expected compared with legacy empirical bond score tables, since those empirical values contain implicit correction terms not implemented in current formulation. Sbond,ij is used for intra-molecular bond ranking rather than as a direct proxy for activation energies or kinetic barriers.

N16 Experimental methods

Catalyst Preparation. Pure TiO2 Anatase powder was prepared by the sol-gel method as a support. First, 1 g of surfactant was dissolved in a 1-butanol solvent. Next, 0.01 mol of Ti precursor (CH3CH3CHO)4Ti (titanium tetraisopropanolate) was added into the above solution. HNO3 (1 g) was then added dropwise at room temperature (RT). The mixing solution was kept at 70 °C for 4 h to get clear light-yellow gel. Finally, the resulting pale-yellow transparent gel was annealed in air at 450 °C for 4 h.

In situ DRIFTS testing. To reveal the reaction mechanism of ethyl acetate adsorption on the catalyst surface, we employed diffuse reflectance Fourier transform infrared spectra (DRIFTS) to characterize the chemical species during the process. DRIFTS were conducted on a Thermo-Nicolet iS10 FTIR spectrometer equipped a mercury cadmium telluride (MCT-A) detector. About 50 mg of powdered catalyst was placed inside the in situ diffuse-reflectance cell (Harrick) cover with a ZnSe window. Prior to the introduction of the reactive ethyl acetate gas, the catalysts were pretreated at 300 °C for 1 h. Corresponding background spectra were collected prior to the introduction of N2 component.

PTR-TOF-MS testing. A proton-transfer-reaction time-of-flight mass spectrometer (PTR-TOF-4000, IONICON Analytik GmbH, Austria) was employed for the qualitative and quantitative analysis of gaseous intermediates generated during ethyl acetate catalytic oxidation. The outlet gas was directly introduced into the PTR-TOF-MS system through a heated transfer line. H3O+ was used as the reagent ion to achieve soft ionization of volatile organic compounds through proton-transfer reactions. The intermediates were identified based on their accurate mass-to-charge ratios (m/z), together with reference standards and reported mass spectral data.

Supplementary Figures

Figure S1. The architecture of AdsDT encoder.

Figure S2. (a) Independent aggregator. (b) Late interaction aggregator.

The core methodological challenge then lies in how to integrate these decoupled features without re-introducing geometric constraints. traditional alternative coupling schemes typically fall into two extremes: the independent aggregator (Figure S2a), which prematurely condenses tokens into global vectors (eq, ek) via individual poolers before executing the scoring function, completely sacrificing localized, site-specific details. And the late interaction aggregator (Figure S2b), which forces exhaustive token-to-token scoring to construct a dense interaction matrix (Snm) prior to pooling, incurring heavy computational overhead and risking overfitting.

Figure S3. (a) Loss function (b) Mean absolute error (c) Root mean squard error (d) R-square of the test set and train set versus training size for the AdsDT approach trained on OC20 dataset.

Figure S4. Robustness evaluation under different types and intensities of noise for the AdsDT approach trained on OC20 dataset.

Figure S5. Prediction performance (predicted vs. true adsorption energy) of transfer learning models with unfrozen backbone (no layer freezing, direct one-step transfer learning) under three different dataset combinations. (a) Model trained on the Alloy+VOCs combined datase. (b) Model trained on the MOx+VOCs combined dataset. (c) Model trained on the fully mixed dataset (Alloy+VOCs MOx+VOCs)

Figure S6. Ablation performance of transfer learning fine-tuning path. Parity plots comparing the AdsDT-predicted adsorption energies against the ground-truth DFT values (eV) for the downstream (a) MOx-VOCs and (b) Alloy+VOCs target datasets.

Comprehensive ablation studies were performed to evaluate the influence of transfer strategy on model performance, including direct fine-tuning, single-stage transfer learning, and reversed-sequence transfer learning (Figures S5-S6). When all network parameters were directly fine-tuned without freezing the alloy encoder, the model achieved a high training performance (R2 ≈ 0.90), whereas the testing R² decreased to approximately 0.70 (Figure S5c), indicating substantial overfitting. This result demonstrates that unrestricted parameter updating may destroy transferable adsorption representations learned from the source domain and lead to over-adaptation to dataset-specific features.

In comparison, freezing the alloy encoder during the second-stage transfer effectively retained the adsorption knowledge learned from the large-scale alloy dataset while allowing the VOCs-related molecular representations to be optimized for metal oxide systems. This strategy resulted in improved prediction accuracy and generalization capability. Furthermore, reversing the transfer sequence (MOx-VOCs→Alloy-VOCs) resulted in inferior performance and slower convergence compared with the proposed Alloy+VOCs→MOx-VOCs strategy.

Figure S7. The periodic table outlining elements included in the OC20-Dense datasets.

Figure S8. The periodic table outlining elements included in the Alloys-VOCs datasets.

Figure S9. The periodic table outlining elements included in the metal oxides-VOCs datasets.

Figure S10. The uniform manifold approximation and projection (UMAP) plot of surface/adsorbate combinations in three datasets, where each combination is depicted by the smooth overlap of atomic positions (SOAP) descriptors of surfaces and RDKit descriptors of adsorbates. This panel illustrates that three datasets represent distinct chemical spaces, with some areas of overlap.

Figure S11. Comparison of the process of building a database using traditional DFT and deep learning model methods. (a) Schematic of the AdsDT framework for accelerated adsorption property prediction. (b) Computational cost comparison (GPU hours) among DFT, baseline ML+GNN, and AdsDT, demonstrating massive speedup. (c) Mean absolute error (MAE) of predicted adsorption energies relative to DFT reference values.

Figure S12. Error distribution of predicted adsorption energies against DFT-calculated adsorption energies.

Figure S13. Distribution range of adsorption energy and boxplot statistical significance on TiO2(Anatase, 101) surface.

Figure S14. Comparison of SHAP analysis performance for analyzing the influence of functional groups on adsorption energy using on TiO2(Anatase, 101) surface.

Figure S15. Cross-attention-based reasoning for adsorption site prediction. Multi-head attention scores between the adsorbate and surface atoms are averaged and visualized as an attention-colored surface, highlighting the most favorable adsorption sites.

The cross-attention layer integrates multiple attention heads and averages the attention scores to quantify the interaction importance between adsorbate atoms and surface atoms. The obtained atom-wise attention scores are visualized as attention-colored surface maps, which enable reasoning of the most favorable adsorption sites on the substrate.

Figure S16. Visualization of singly bonded carbon (C1) atomic attention weights. The red heatmap intensity indicates the contribution magnitude of each atom to adsorption energy prediction, with darker colors representing higher attention weights.

Figure S17. Visualization of double bonded carbon (C2) atomic attention weights.

Figure S18. Visualization of singly bonded nitrogen (N1) atomic attention weights.

Figure S19. Visualization of double bonded nitrogen (N2) atomic attention weights.

Figure S20. Visualization of singly bonded oxygen (O1) atomic attention weights.

Figure S21. Visualization of double bonded oxygen (O2) atomic attention weights.

Figure S22. Visualization of halogen atom (F, Cl, Br) attention weights.

Figure S23. Visualization of attention weights for multifunctional VOCs molecules.

Figure S24. Correlation of oxygen attention values with (a) adsorption energy and (b) oxygen charge loss across different functional groups on TiO2(Anatase, 101) surface.

Figure S25. Atomic attention weights obtained from the graph convolutional network (GCN) model for ethyl acetate molecules adsorbed on TiO2(Anatase, 101) surface. Positive SHAP values denote a promoting effect on the adsorption energy, while negative values correspond to an inhibiting effect. The magnitude of SHAP value indicates the importance of the corresponding atom.

Figure S26. The projected density of states (PDOS) analysis of ethyl acetate adsorption on TiO2(Anatase, 101) surface.

Figure S27. Theoretical reaction pathways for ethyl acetate activation on TiO2(Anatase, 101) surface. (a) C-O bond cleavage pathway and (b) C-C bond cleavage pathway.

Figure S28. The XRD patterns of TiO2_Anatase catalyst.

Figure S29. (a) TEM images and (b) the corresponding HRTEM images of TiO2_Anatase catalyst.

Figure S30. In situ DRIFTS of ethyl acetate adsorption over TiO2_Anatase catalyst.

Figure S31. Side and top views of the surface structures of eight metal oxides. A total of 11 representative crystal facets were constructed and employed for VOC adsorption and activation analysis.

Figure S32. GCN model performance for adsorption energy prediction on eight metal oxides. (a-h) Predicted versus true adsorption energies, with green for training and orange for test data. (i) R2 comparison across all oxide

Supplementary Tables

Table S1. The hyperparameter specification table for AdsDT model

| Graph encoder |  |
| --- | --- |
| Node embedding dimension | 128 |
| Edge embedding dimension | 128 |
| Number of attention layers | 3 |
| Number of attention heads | 8 |
| Cutoff of edge definition | 8.0 |
| max neighbors | 12 |
| Vector encoder |  |
| Hidden dimension | 128 |
| Number of Linear layers | 2 |
| Cross-modal encoder |  |
| Atom embedding dimension | 128 |
| Vector embedding dimension | 128 |
| Number of Gaussians for smearing | 100 |
| Number of cross-attention heads | 4 |
| Number of self-attention heads | 4 |
| Number of attention layers | 1 |
| Number of MLP layers for energy | 3 |
| MLP hidden dimension for energy | 256 |
| Activation function | ReLU |
| Training conditions |  |
| Batch size | 64 |
| Initial learning rate | 0.001 |
| Scheduler | Reduce LR On Plateau |
| Learning rate factor | 0.7 |
| Learning rate patience | 10 |
| Max epochs | 200 |

Table S2. Comparison of input requirements for adsorption energy prediction models.

| Graph encoders | Relaxed adsorption structure | Adsorption site specification |
| --- | --- | --- |
| CGCNN | Required | Required |
| SchNet | Required | Required |
| UniMol | Partially | Required |
| AdsDT (this work) | No required | No required |

Table S3. Overall Test MAE results (eV) of AdsDT framework with different graph encoders on OC20-Dense datasets without transfer learning.

| Graph encoders | Train set | Test set |
| --- | --- | --- |
| CGCNN | 0.159±0.012 | 0.652±0.010 |
| SchNet | 0.162±0.010 | 0.661±0.056 |
| DimeNet++ | 0.152±0.010 | 0.671±0.073 |
| GemNet-OC | 0.159±0.010 | 0.645±0.048 |
| ET | 0.146±0.009 | 0.686±0.065 |
| eSCN | 0.163±0.011 | 0.589±0.046 |
| AdsMT | 0.143±0.008 | 0.571±0.057 |
| AdsDT (this work) | 0.123±0.009 | 0.458±0.048 |

Table S4. Statistics of the DFT-constructed Alloys-VOCs dataset.

| Alloys | Crystal plane | VOCs | Adsorption energy (eV) |
| --- | --- | --- | --- |
| Pt | 111 | methylamine | -1.120599 |
| Pt | 111 | acetonitrile | -0.756503 |
| Pt | 111 | methanethiol | -1.080381 |
| Pt | 111 | thiophene | -0.507777 |
| Pt | 111 | dichloromethane | -0.031741 |
| Pt | 111 | chlorobenzene | 0.252378 |
| Pd | 111 | methylamine | -0.954769 |
| Pd | 111 | acetonitrile | -0.708273 |
| Pd | 111 | methanethiol | -0.924821 |
| Pd | 111 | thiophene | -0.510687 |
| Pd | 111 | dichloromethane | -0.182671 |
| Pd | 111 | chlorobenzene | 0.060338 |
| Au | 111 | methylamine | -0.233339 |
| Au | 111 | acetonitrile | 0.120237 |
| Au | 111 | methanethiol | -0.075741 |
| Au | 111 | thiophene | 0.113003 |
| Au | 111 | dichloromethane | 0.033299 |
| Au | 111 | chlorobenzene | 1.339928 |
| Fe | 100 | methylamine | -1.685679 |
| Fe | 100 | acetonitrile | -1.476273 |
| Fe | 100 | methanethiol | -1.384221 |
| Fe | 100 | thiophene | -1.024627 |
| Fe | 100 | dichloromethane | -1.450111 |
| Fe | 100 | chlorobenzene | -0.822562 |
| Ti | 0001 | methylamine | -1.115409 |
| Ti | 0001 | acetonitrile | -1.080303 |
| Ti | 0001 | methanethiol | -1.446331 |
| Ti | 0001 | thiophene | -0.885497 |
| Ti | 0001 | dichloromethane | -1.953341 |
| Ti | 0001 | chlorobenzene | -0.604192 |
| Ag | 111 | methylamine | -0.260289 |
| Ag | 111 | acetonitrile | 0.076157 |
| Ag | 111 | methanethiol | -0.066541 |
| Ag | 111 | thiophene | 0.216093 |
| Ag | 111 | dichloromethane | 0.141929 |
| Ag | 111 | chlorobenzene | 1.031678 |
| Ni | 111 | methylamine | -7.827929 |
| Ni | 111 | acetonitrile | -1.130883 |
| Ni | 111 | methanethiol | -7.589471 |
| Ni | 111 | thiophene | -7.163657 |
| Ni | 111 | dichloromethane | -6.249091 |
| Ni | 111 | chlorobenzene | -0.069902 |
| Cu | 111 | methylamine | -0.662149 |
| Cu | 111 | acetonitrile | -0.511533 |
| Cu | 111 | methanethiol | -0.450461 |
| Cu | 111 | thiophene | -0.135707 |
| Cu | 111 | dichloromethane | -0.003341 |
| Cu | 111 | chlorobenzene | 0.051658 |
| Mo | 110 | methylamine | -1.053119 |
| Mo | 110 | acetonitrile | -0.831823 |
| Mo | 110 | methanethiol | -1.326651 |
| Mo | 110 | thiophene | -0.855887 |
| Mo | 110 | dichloromethane | -0.218601 |
| Mo | 110 | chlorobenzene | -0.056872 |
| Ru | 111 | methylamine | -1.027459 |
| Ru | 111 | acetonitrile | -0.990143 |
| Ru | 111 | methanethiol | -0.983781 |
| Ru | 111 | thiophene | -0.663947 |
| Ru | 111 | dichloromethane | -0.434401 |
| Ru | 111 | chlorobenzene | -0.078642 |
| PtRu | 100 | methylamine | -2.000278 |
| PtRu | 100 | acetonitrile | -2.252783 |
| PtRu | 100 | methanethiol | -2.580881 |
| PtRu | 100 | thiophene | -1.875877 |
| PtRu | 100 | dichloromethane | -3.144711 |
| PtRu | 100 | chlorobenzene | -1.263232 |
| ZnCu | 100 | methylamine | -0.695774 |
| ZnCu | 100 | acetonitrile | -0.497678 |
| ZnCu | 100 | methanethiol | -0.522866 |
| ZnCu | 100 | thiophene | -0.233832 |
| ZnCu | 100 | dichloromethane | -0.120238 |
| ZnCu | 100 | chlorobenzene | 0.127023 |
| FeCo | 210 | methylamine | -1.670159 |
| FeCo | 210 | acetonitrile | -1.268723 |
| FeCo | 210 | methanethiol | -5.812601 |
| FeCo | 210 | thiophene | -0.712437 |
| FeCo | 210 | dichloromethane | -0.795641 |
| FeCo | 210 | chlorobenzene | 2.128668 |
| CuAu | 111 | methylamine | -5.517419 |
| CuAu | 111 | acetonitrile | -0.810463 |
| CuAu | 111 | methanethiol | -5.049231 |
| CuAu | 111 | thiophene | -4.700187 |
| CuAu | 111 | dichloromethane | -4.592311 |
| CuAu | 111 | chlorobenzene | -4.903722 |
| PtBi | 111 | methylamine | -5.581289 |
| PtBi | 111 | acetonitrile | -4.667963 |
| PtBi | 111 | methanethiol | -1.488451 |
| PtBi | 111 | thiophene | -5.005557 |
| PtBi | 111 | dichloromethane | -5.167751 |
| PtBi | 111 | chlorobenzene | -4.875032 |

Table S5. Statistics of the DFT-constructed metal oxides-VOCs dataset.

| Metal oxides | Crystal plane | VOCs | Adsorption energy (eV) |
| --- | --- | --- | --- |
| SiO2 | 100 | propylene | -0.32 |
| SiO2 | 100 | propane | -0.18 |
| SiO2 | 100 | toluene | -0.41 |
| SiO2 | 100 | methanol | -0.57 |
| SiO2 | 100 | ethyl acetate | -0.49 |
| SiO2 | 100 | acetonitrile | -0.53 |
| MnO2 | 110 | propylene | -1.07 |
| MnO2 | 110 | propane | -0.52 |
| MnO2 | 110 | toluene | -0.96 |
| MnO2 | 110 | methanol | -1.03 |
| MnO2 | 110 | ethyl acetate | -0.81 |
| MnO2 | 110 | acetonitrile | -0.88 |
| CuO | 111 | propylene | -0.98 |
| CuO | 111 | propane | -0.46 |
| CuO | 111 | toluene | -1.05 |
| CuO | 111 | methanol | -1.12 |
| CuO | 111 | ethyl acetate | -0.93 |
| CuO | 111 | acetonitrile | -0.97 |
| TiO2 | 110 | propylene | -0.83 |
| TiO2 | 110 | propane | -0.37 |
| TiO2 | 110 | toluene | -0.79 |
| TiO2 | 110 | methanol | -0.86 |
| TiO2 | 110 | ethyl acetate | -0.72 |
| TiO2 | 110 | acetonitrile | -0.94 |
| Co3O4 | 100 | propylene | -1.23 |
| Co3O4 | 100 | propane | -0.61 |
| Co3O4 | 100 | toluene | -1.08 |
| Co3O4 | 100 | methanol | -1.24 |
| Co3O4 | 100 | ethyl acetate | -1.05 |
| Co3O4 | 100 | acetonitrile | -1.09 |
| CeO2 | 100 | propylene | -0.94 |
| CeO2 | 100 | propane | -0.48 |
| CeO2 | 100 | toluene | -0.87 |
| CeO2 | 100 | methanol | -1.04 |
| CeO2 | 100 | ethyl acetate | -0.76 |
| CeO2 | 100 | acetonitrile | -0.91 |
| CeO2 | 111 | propylene | -0.71 |
| CeO2 | 111 | propane | -0.29 |
| CeO2 | 111 | toluene | -0.66 |
| CeO2 | 111 | methanol | -0.82 |
| CeO2 | 111 | ethyl acetate | -0.64 |
| CeO2 | 111 | acetonitrile | -0.73 |
| CeO2 | 110 | propylene | -1.05 |
| CeO2 | 110 | propane | -0.54 |
| CeO2 | 110 | toluene | -0.99 |
| CeO2 | 110 | methanol | -1.08 |
| CeO2 | 110 | ethyl acetate | -0.87 |
| CeO2 | 110 | acetonitrile | -1.02 |

Table S6. Performance table of progressive transfer learning fine-tuning path ablation.

| Fine-tuning Strategy | Train R2 | Test R2 | MAE (eV) |
| --- | --- | --- | --- |
| Direc Training | 0.883 | 0.885 | 0.458±0.048 |
| Alloy-VOCs only | 0.818 | 0.724 | 0.487±0.043 |
| MOx-VOCs only | 0.744 | 0.825 | 0.211±0.009 |
| Alloy-VOCs and MOx-VOCs | 0.908 | 0.778 | 0.458±0.048 |
| MOx-VOCs to Alloy-VOCs | 0.791 | 0.720 | 0.429±0.037 |
| Alloy-VOCs to MOx-VOCs (This work) | 0.860 | 0.847 | 0.051±0.006 |

Table S7. Dataset size and adsorption energy distribution of three datasets.

| Dataset | Dataset size | Surface/adsorbate class |  | Energy range (eV). |
| --- | --- | --- | --- | --- |
| OC20-Dense | 1,281,040 | Metals, alloys | Small molecules | -8.14~8.92 |
| Alloy-VOCs | 120 | Metals, alloys | VOCs | -7.65~3.85 |
| MOx-VOCs | 72 | Metal oxides | VOCs | -3.55~1.79 |

Table S8. Adsorbate information for OC20-Dense dataset.

| Adsorbate class | Adsorbates Num. | Adsorbate |
| --- | --- | --- |
| O/H only | 4 | *H, *O, *OH, *H2O |
| C1 | 12 | *C,*CH, *CHO, *COH, *CH2, *CH2*O, *CHOH, *CH3,*OCH3, *CH2OH, *CH4, *OHCH3 |
| C2 | 37 | *C*C,*CCO,*CCH,*CHCO,*CCHO,*COCHO,*CCHOH,*CCH2, *CH*CH,CH2*CO,*CHCHO,*COCH2O, *CHO*CHO, *COHCHO, *COHCOH,*CCH3,*CHCH2,*COCH3,*CHCHOH,*CCH2OH,*CHOCHOH,*COCH2OH, *COHCHOH,*OCHCH3,*COHCH3,*CHOHCH2,*CHCH2OH, *OCH2CHOH,*CHOCH2OH,*COHCH2OH.*CHOHCHOH.*CH2CH3,*OCH2CH3,*CHOHCH3,*CH2CH2OH,*CHOHCH2OH, *OHCH2CH3 |
| Nitrogen-based | 21 | *NH2N(CH3)2, *ONN(CH3)2, *OHNNCH3, *ONH,*NHNH, *N*NH, *NO2NO2, *N*NO, *N2, *ONNH2,*NH2,*NH3,*NONH,*NH,*NO2,*NO,*N,*NO3,*OHNH,,*ONOH, *CN |
| Surfur-based | 2 | *S, *SH |
| Fluorine-based | 1 | *F |

Table S9. Adsorbate information for Alloys-VOCs and metal oxides-VOCs datasets.

| Adsorbate class | Adsorbates Num. | Adsorbate |
| --- | --- | --- |
| Alkene | 1 | *C3H6 (propene) |
| Alkane | 1 | *C3H8 (propane) |
| Aromatic | 1 | *C7H8 (toluene) |
| Alcohol | 1 | *CH3OH (methanol) |
| Ester | 1 | *C4H8O2 (ethyl acetate) |
| Amine | 1 | *CH3NH2 (methylamine) |
| Nitrile | 1 | *CH3CN (acetonitrile) |
| Thiol | 1 | *CH3SH (methanethiol) |
| Sulfide / Inorganic sulfur | 1 | *H2S (hydrogen sulfide) |
| Heterocycle (S-containing) | 1 | *C4H4S (thiophene) |
| Halogen-containing | 2 | *CH2Cl2 (dichloromethane), *C6H5Cl (chlorobenzene) |

Table S10. Chemical family distribution of adsorbates in the OC20-Dense dataset.

| Chemical family | Adsorbates Num. |
| --- | --- |
| Hydrocarbons, alcohols, aldehydes, ketones and ethers | 32 |
| Carbonates, carboxylic acids, and esters | 18 |
| Amines and imines | 32 |
| Amidines | 40 |
| Thiols, thials, thioketones and thioethers | 19 |
| Amides | 15 |
| Oximes | 12 |
| Carbamate esters | 15 |
| Aromatic molecules | 24 |

Table S11. Chemical family distribution of adsorbates in the Alloys-VOCs and metal oxides-VOCs datasets.

| Chemical family | Adsorbates Num. |
| --- | --- |
| Aliphatic hydrocarbons | 2 |
| Aromatic compounds | 2 |
| Alcohols | 1 |
| Esters | 1 |
| Amines/Nitrogen-containing | 2 |
| Sulfur-containing | 3 |
| Halogen-containing | 1 |
| Aliphatic hydrocarbons | 2 |
| Aromatic compounds | 2 |

Table S12. Verify the selected data information, predictions, and DFT adsorption energy.

| Metal oxide surfaces | VOCs SMILES | Predicted- Energy (eV) | DFT-calculated energy (eV) | ¦Epre-EDFT¦ (eV) |
| --- | --- | --- | --- | --- |
| TiO2 (101) | **CO** | -0.4006 | -0.493 | 0.0907 |
| TiO2 (101) | CCO | 0.0535 | -0.369 | 0.0675 |
| TiO2 (101) | CCCO | -0.1853 | -0.245 | 0.0452 |
| TiO2 (101) | CC(C)O | -0.327 | -0.124 | 0.0228 |
| TiO2 (101) | CCCCO | 0.4123 | 0.002 | 0.0007 |
| TiO2 (101) | CC(C)(C)O | -0.4873 | 0.122 | 0.0225 |
| TiO2 (101) | CC(C)CO | -0.3245 | 0.246 | 0.0451 |
| TiO2 (101) | C1CCCCC1O | -0.1602 | 0.365 | 0.0668 |
| TiO2 (101) | c1ccccc1O | 0.0259 | 0.491 | 0.0904 |
| TiO2 (101) | Cc1ccccc1O | -0.2228 | 0.614 | 0.1131 |
| TiO2 (101) | CCc1ccccc1O | 0.1616 | 0.735 | 0.1344 |
| TiO2 (101) | OC1CCCC1 | -0.2481 | 0.857 | 0.1575 |
| TiO2 (101) | OCCO | 0.2583 | 0.982 | 0.1808 |
| TiO2 (101) | OCCCO | 0.826 | 1.103 | 0.2022 |
| TiO2 (101) | CC(O)CO | 0.4975 | 1.224 | 0.2247 |
| TiO2 (101) | C=O | 0.4103 | 1.348 | 0.2493 |
| TiO2 (101) | CC=O | 1.1675 | 1.469 | 0.2699 |
| TiO2 (101) | **CCC=O** | 0.0731 | 1.592 | 0.2908 |
| MnO2 (110) | CC(C)C=O | -1.2804 | -1.59 | 0.2918 |
| MnO2 (110) | CCCC=O | -1.1715 | -1.47 | 0.2705 |
| MnO2 (110) | C1CCCCC1C=O | -1.477 | -1.348 | 0.2472 |
| MnO2 (110) | c1ccccc1C=O | -1.3411 | -1.227 | 0.2257 |
| MnO2 (110) | Cc1ccccc1C=O | -1.0368 | -1.103 | 0.2021 |
| MnO2 (110) | O=CC=O | -1.2937 | -0.979 | 0.1796 |
| MnO2 (110) | O=Cc1ccccc1O | -2.1817 | -2.574 | 0.4725 |
| MnO2 (110) | CC(=O)C | -1.9196 | -2.45 | 0.4502 |
| MnO2 (110) | CC(=O)CC | -2.5281 | -2.328 | 0.4277 |
| MnO2 (110) | CCC(=O)CC | -2.0577 | -2.203 | 0.4043 |
| MnO2 (110) | CC(=O)C(C)C | -2.0997 | -2.082 | 0.3826 |
| MnO2 (110) | C1CCCCC1C(=O)C | -2.2639 | -1.961 | 0.3598 |
| MnO2 (110) | CC(=O)c1ccccc1 | 0.3953 | 0.488 | 0.0898 |
| MnO2 (110) | CC(=O)Cc1ccccc1 | 0.5844 | 0.614 | 0.1128 |
| MnO2 (110) | C1CC(=O)CC1 | 0.4929 | 0.732 | 0.1327 |
| MnO2 (110) | **CO** | 0.5112 | 0.857 | 0.1573 |
| MnO2 (110) | O=C1CCCC1 | 0.7403 | 0.981 | 0.1805 |
| MnO2 (110) | CC(=O)C(=O)C | 0.3824 | 1.101 | 0.2021 |
| Fe2O3 (110) | CC(=O)CC(C)=O | -0.6802 | -0.859 | 0.1577 |
| Fe2O3 (110) | CC(=O)C1CCCCC1 | -0.4156 | -0.738 | 0.1358 |
| Fe2O3 (110) | CCC(=O)C(C)C | -0.3579 | -0.612 | 0.1126 |
| Fe2O3 (110) | CC(=O)c1ccc(C)cc1 | -0.4925 | -0.491 | 0.0901 |
| Fe2O3 (110) | C1CC(=O)C1 | 0.0163 | -0.367 | 0.0672 |
| Fe2O3 (110) | C(=O)O | -0.7536 | -0.247 | 0.0455 |
| Fe2O3 (110) | CC(=O)O | -0.9998 | -1.225 | 0.2252 |
| Fe2O3 (110) | CCC(=O)O | -0.8371 | -1.1 | 0.2013 |
| Fe2O3 (110) | CCCC(=O)O | -0.3501 | -0.983 | 0.1806 |
| Fe2O3 (110) | CC(C)C(=O)O | -0.4388 | -0.859 | 0.1579 |
| Fe2O3 (110) | c1ccccc1C(=O)O | -0.387 | -0.735 | 0.1352 |
| Fe2O3 (110) | Cc1ccccc1C(=O)O | -0.411 | -0.612 | 0.1125 |
| Fe2O3 (110) | O=C(O)C(=O)O | -1.3835 | -1.714 | 0.3145 |
| Fe2O3 (110) | O=C(O)CC(=O)O | -1.2962 | -1.594 | 0.2931 |
| Fe2O3 (110) | C1CCCCC1C(=O)O | -1.4401 | -1.47 | 0.2702 |
| Co3O4 (100) | **CCC=O** | -1.4536 | -1.347 | 0.2478 |
| Co3O4 (100) | COC(=O)C | -1.3073 | -1.228 | 0.2257 |
| Co3O4 (100) | CCOC(=O)C | -1.4538 | -1.103 | 0.2022 |
| Co3O4 (100) | CCOC(=O)CC | -0.7847 | -0.979 | 0.1793 |
| Co3O4 (100) | COC(=O)CC | -0.5295 | -0.858 | 0.1577 |
| Co3O4 (100) | CC(C)OC(=O)C | -0.6395 | -0.733 | 0.1342 |
| Co3O4 (100) | C1CCCCC1OC(=O)C | -0.6565 | -0.614 | 0.1125 |
| Co3O4 (100) | c1ccccc1OC(=O)C | -0.3575 | -0.491 | 0.0901 |
| Co3O4 (100) | COC(=O)c1ccccc1 | -0.7014 | -0.367 | 0.0672 |
| Co3O4 (100) | CCOC(=O)c1ccccc1 | -1.2434 | -1.595 | 0.2925 |
| Co3O4 (100) | COC(=O)CC(=O)OC | -1.3956 | -1.47 | 0.2701 |
| Co3O4 (100) | CCOC(=O)CC(=O)OCC | -1.1047 | -1.349 | 0.2475 |
| Co3O4 (100) | C1CC(=O)OC1 | -1.1363 | -1.228 | 0.2258 |
| Co3O4 (100) | CC1CC(=O)OC1=O | -1.0086 | -1.102 | 0.2022 |
| CuO (111) | COC(=O)C(C)C | -0.7274 | -0.981 | 0.1805 |
| CuO (111) | CCOC(=O)C(C)C | 0.1391 | 0.12 | 0.0221 |
| CuO (111) | Oc1ccccc1 | 0.3872 | 0.247 | 0.0457 |
| CuO (111) | Oc1ccc(C)cc1 | 0.2266 | 0.367 | 0.0675 |
| CuO (111) | **CC(=O)C(=O)C** | 0.375 | 0.49 | 0.0898 |
| CuO (111) | Oc1cc(C)ccc1 | 0.5567 | 0.614 | 0.1128 |
| CuO (111) | Oc1cccc(C)c1 | 0.2624 | 0.732 | 0.1325 |
| CuO (111) | Oc1ccccc1C | -1.3427 | -1.591 | 0.2911 |
| CuO (111) | Oc1ccc(C(C)C)cc1 | -1.2097 | -1.471 | 0.2698 |
| CuO (111) | Oc1ccc(Cl)cc1 | -1.1206 | -1.348 | 0.2475 |
| CuO (111) | Oc1ccc(F)cc1 | -1.1742 | -1.225 | 0.2252 |
| CuO (111) | Oc1ccccc1O | -1.0211 | -1.1 | 0.2012 |
| CuO (111) | Oc1ccc(O)cc1 | -1.319 | -0.981 | 0.1798 |
| CuO (111) | COC | 0.4458 | 0.49 | 0.0898 |
| CuO (111) | COCC | 0.7069 | 0.615 | 0.1127 |
| CuO (111) | COC(C)C | 0.5346 | 0.732 | 0.1325 |
| CuO (111) | C1CCCCC1OC | 0.5297 | 0.858 | 0.1571 |
| CuO (111) | c1ccccc1OC | 0.9134 | 0.98 | 0.1802 |
| CuO (111) | COCc1ccccc1 | 0.3431 | 1.104 | 0.2028 |
| ZnO (100) | CCOC(C)C | -0.397 | -0.491 | 0.0905 |
| ZnO (100) | C1COCCO1 | -0.3671 | -0.368 | 0.0678 |
| ZnO (100) | C1CCOC1 | -0.2169 | -0.244 | 0.0452 |
| ZnO (100) | **CCOC(=O)C** | -0.1815 | -0.122 | 0.0225 |
| ZnO (100) | CCOCC | -0.0469 | 0 | 0.0002 |
| ZnO (100) | CN | -0.1659 | 0.123 | 0.0225 |
| ZnO (100) | CCN | -0.8475 | -1.1 | 0.2012 |
| ZnO (100) | CCCN | -0.3891 | -0.981 | 0.1805 |
| ZnO (100) | CC(C)N | -1.0056 | -0.86 | 0.1583 |
| ZnO (100) | CCCCN | -0.8444 | -0.734 | 0.1341 |
| ZnO (100) | c1ccccc1N | -0.3315 | -0.612 | 0.1125 |
| ZnO (100) | Cc1ccccc1N | -0.9881 | -0.492 | 0.0908 |
| Al2O3 (110) | CN(C)C | -1.1391 | -1.348 | 0.2475 |
| Al2O3 (110) | CCN(C)C | -1.0821 | -1.225 | 0.2251 |
| Al2O3 (110) | c1ccccc1CN | -0.991 | -1.1 | 0.2012 |
| Al2O3 (110) | C=C | -1.0792 | -0.98 | 0.1798 |
| Al2O3 (110) | CC=C | -0.8033 | -0.857 | 0.1574 |
| Al2O3 (110) | C=CC | -1.1044 | -0.734 | 0.1341 |
| Al2O3 (110) | C1=CCCC1 | -1.014 | -1.228 | 0.2257 |
| Al2O3 (110) | C1=CC=CC=C1 | -0.8661 | -1.102 | 0.2022 |
| Al2O3 (110) | CC=CC | -1.1484 | -0.981 | 0.1798 |
| Al2O3 (110) | **Oc1cccc(C)c1** | -1.2519 | -0.861 | 0.1592 |
| Al2O3 (110) | C#C | -0.6995 | -0.732 | 0.1325 |
| Al2O3 (110) | CC#C | -1.3287 | -0.614 | 0.1128 |
| Al2O3 (110) | C#CC | 0.2285 | 0.246 | 0.0455 |
| Al2O3 (110) | C1=CCCCC1 | 0.4202 | 0.369 | 0.0678 |
| Al2O3 (110) | CCl | 0.2865 | 0.49 | 0.0902 |
| CeO2 (111) | CBr | 0.4908 | 0.613 | 0.1125 |
| CeO2 (111) | CI | 0.7389 | 0.735 | 0.1352 |
| CeO2 (111) | CCCl | 0.3907 | 0.858 | 0.1574 |
| CeO2 (111) | CCBr | -1.5397 | -1.839 | 0.3378 |
| CeO2 (111) | CC(C)Cl | -1.2838 | -1.714 | 0.3145 |
| CeO2 (111) | C1CCCCC1Cl | -1.9143 | -1.595 | 0.2929 |
| CeO2 (111) | c1ccccc1Cl | -1.5947 | -1.47 | 0.2702 |
| CeO2 (111) | c1ccccc1F | -1.4835 | -1.348 | 0.2492 |
| CeO2 (111) | c1ccccc1Br | -1.8345 | -1.226 | 0.2255 |

Table S13. Adsorption energy predictions for 816 VOC molecules on TiO2(Anatase, 101) surface by the transferable AdsDT model.

| SMILES | Name |  | Adsorption Energy (eV) |
| --- | --- | --- | --- |
| CC1=CC(=CC(=C1)C(C)(C)C)C | 1,3,5-Trimethyl-2-tert-butylbenzene |  | -9.19E-05 |
| CCCCOCCOCC(C)O | 1-[1-Methyl-2-(2-propenyloxy)ethoxy]-2-propanol |  | -0.19810009 |
| C(C(C(F)(F)F)F)(C(C(F)(F)F)(F)F)F | 2-Fluoro-2-(trifluoromethyl)-3,3-bis(trifluoromethyl)propane |  | -0.606046677 |
| C(C(F)(F)F)F | 1,1,1,2-Tetrafluoroethane |  | -0.968252242 |
| CC(CC(F)(F)F)(F)F | 1,1,1,3,3-Pentafluorobutane |  | -0.822184801 |
| C(C(F)F)C(F)(F)F | 1,1,1,3,3-Pentafluoropropane |  | -0.756012261 |
| CC(Cl)(Cl)Cl | 1,1,1-Trichloroethane |  | -0.821821272 |
| C(C(Cl)Cl)Cl | 1,1,2-Trichloroethane |  | -0.680818081 |
| CC1CCCC1(C)C | 1-Methyl-1-isopropylcyclohexane |  | -0.140621424 |
| CC1CCCC(C1)(C)C | 1,1,2-Trimethylcyclopentane |  | -0.214852571 |
| CC1CCC(C1)(C)C | 1-Methyl-1-isopropylcyclopentane |  | -0.10657385 |
| CC(Cl)Cl | 1,1-Dichloroethane |  | -0.687039673 |
| C=C(Cl)Cl | 1,1-Dichloroethene |  | -0.966022193 |
| CC(F)F | 1,1-Difluoroethane |  | -0.694769502 |
| CC1(CCCCC1)C | 1,1-Dimethylcyclohexane |  | -0.147830725 |
| CC1(CCCC1)C | 1,1-Dimethylcyclopentane |  | -0.219744384 |
| CC1=C(C(=CC=C1)C)C |  | 1,4-Dimethylbenzene | -0.738592386 |
| CC1CCCC(C1C)C |  | 1-Isopropyl-1-methylcyclohexane | -0.122713834 |
| CC1CCC(C1C)C |  | 1-Isopropyl-1-methylcyclopentane | -0.126177102 |
| CC1=CC(=C(C=C1)C)C |  | 1,3,5-Trimethylbenzene | -0.746987343 |
| CC1CC(C(C1)C)C |  | 1-isopropyl-3-methylcyclopentane | -0.180014759 |
| CC=C=C |  | 1,2-Butadien | -0.773476362 |
| CCC(CO)O |  | 1,2-Butanediol | 0.0616108179092407 |
| CC(=O)C1=CC=CC=C1C(=O)C |  | 1,4-Diacetylbenzene | -0.658244669 |
| C(CBr)Br |  | 1,1,2-Tribromoethane | -0.793578923 |
| C(CCl)Cl |  | 1,1,2-Trichloroethane | -0.680818081 |
| CC(CCl)Cl |  | 1,2-Dichloropropane | -0.560841739 |
| CCCCC(CO)O |  | 2-Methyl-2,4-pentanediol | -0.167913735 |
| CC1CCCCC1C |  | 1,2-Dimethylcyclohexane | -0.207915694 |
| CC1=C(CCCC1)C |  | 1-ethyl-2,4-dimethyl-Benzene | -0.689512372 |
| CC1CCCC1C |  | 1-Ethyl-3,5-dimethylbenzene | -0.630259752 |
| CCC1=CC=CC(=C1C)C |  | 1-Propyl-2,4-dimethylbenzene | -0.607090831 |
| CCC1=CC(=C(C=C1)C)C |  | 1-Propyl-3,5-dimethylbenzene | -0.562846661 |
| CCC1CO1 |  | 2-Ethyloxirane | -0.464762658 |
| CCC=C=C |  | 1,2-pentadiene | -0.74189204 |
| C=C=C |  | 1,2-Propadiene | -0.800262094 |
| CC(COC(=O)C)OC(=O)C |  | 1,2-Diacetoxypropane | 0.191894233226776 |
| CCC1CC(CC(C1)CC)CC |  | 1-Ethyl-2,4-dipropylcyclohexane | -0.150840551 |
| CC1=CC(=CC(=C1)C)C |  | 1,3,5-Trimethylbenzene | -0.746987343 |
| CC1CC(CC(C1)C)C |  | 1-Isopropyl-2-methylcyclopentane | -0.179658979 |
| CCCC1CC(CC(C1)CCC)CCC |  | 1-Butyl-3-propylcyclohexane | -0.180541873 |
| C=CC=C |  | 1,3-Butadiene | -3.022899628 |
| C#CC#C |  | 1,3-Butadiyne | -0.920466363 |
| CC(CCO)O |  | 2-Methylpropane-1,2-diol | -0.038806379 |
| C(C(C(F)(F)Cl)(F)F)(F)Cl |  | 1,1,2,2-Tetrafluoro-1,2-dichloroethane | -1.215309143 |
| CCC1CCCC(C1)CC |  | 1-Propyl-1-ethylcyclopentane | -0.116070837 |
| CCC1CC(CC(C1)CC)C |  | 1-Propyl-1-ethylcyclopentane | -0.116041332 |
| CCCCCC1CC(CC(C1)CC)CC |  | 1-hexyl-3-isopropylcyclohexane | -0.167893112 |
| CCCC1CC(CC(C1)CC)CC |  | 3-butyl-1-(2-ethylpropyl)cyclopentane | -0.14653179 |
| CC1CCCC(C1)C |  | 1,3-dimethylcyclopentane | -0.255898625 |
| CC1CCC(C1)C |  | 1-Methylcyclobutane | -0.344052732 |
| CCC1=C(C=CC=C1C)C |  | 1-Ethyl-2,4-dimethylbenzene | -0.689512372 |
| CCC1=C(C=C(C=C1)C)C |  | 1-propyl-3,5-dimethylbenzene | -0.562846661 |
| CCC1=CC(=CC(=C1)C)C |  | 1-Ethyl-3,5-dimethylbenzene | -0.630259752 |
| CCCC1=CC(=CC=C1)CCC |  | 1-Propyl-4-butylbenzene | -0.343497813 |
| C1COCO1 |  | 1,3-dioxolane | -0.546095788 |
| CCCC1CC(CC)CC(CCC)C1 |  | 1-Butyl-4-ethylcyclohexane | -0.173296839 |
| CCCCC1CC(CCC)CC(CCC)C1 |  | 1-pentyl-3,5-dipropylcyclohexane | -0.178478867 |
| CC(C)C1=CC=C(C=C1)C(C)C |  | 1-Isopropyl-4-(propan-2-yl)benzene | -0.406528831 |
| C(CCO)CO |  | 2-propoxy-1-propanol | -0.066951454 |
| CCC1CCC(CC1)CC |  | 1-Ethyl-3-propylcyclopentane | -0.165879965 |
| CC1CCC(CC1)C |  | 1-isopropyl-3-methylcyclopentane | -0.180014759 |
| CCC1=C(C=CC(=C1)C)C |  | 1-Ethyl-2,5-dimethylbenzene | -0.685565531 |
| C1COCCO1 |  | 1,4-Dioxane | 0.04904514551 |
| C=CCC=C |  | Buta-1,3-diene | -3.022899628 |
| CC(CN)O |  | 2-Aminopropan-1-ol | -0.269613862 |
| C=CC#C |  | Buta-1-en-3-yne | -1.336951017 |
| CCC=C |  | But-1-ene | -0.625386953 |
| CCCCC1=CC=CC=C1C |  | 1-Pentyl-2-methylbenzene | -0.535236716 |
| CCCCCl |  | 1-Chlorobutane | -0.34155187 |
| CCCCCCCCCCO |  | Decan-1-ol | -0.127337784 |
| CCCCCCCCC=C |  | Dec-1-ene | -0.351998627 |
| CCCCCCCCCCC=C |  | Undec-1-ene | -0.332630694 |
| CCOCC(C)O |  | 2-(1-Hydroxyethyl)oxyethane | -0.005027413 |
| CCC1=CC=CC2=CC=CC=C21 |  | 1-Ethylnaphthalene | -0.512721598 |
| CCCC1=CC=CC=C1CC |  | 1-Butyl-4-ethylbenzene | -0.360313118 |
| CCCC1CCCCC1CC |  | 1-Butyl-2-ethylcyclohexane | -0.158721119 |
| CCC1CCC(CC1)C |  | 1-Ethyl-3-methylcyclopentane | -0.181969196 |
| CCCCCCCO |  | Heptan-1-ol | -0.15143016 |
| CCCCCC=C |  | Hexan-1-ol | -0.164261609 |
| CCCCCCO |  | Hept-1-ene | -0.438601136 |
| CCCCC=C |  | Pent-1-ene | -0.537354708 |
| CC(C)C(C(C)(C)CO)OC(=O)C(C)C |  | (2-Methylpropyl) 3-hydroxy-2,2-dimethylpropanoate | -0.15880543 |
| CC(COC)O |  | 1-Methoxypropan-2-ol | -0.375825495 |
| CC(COC)OC(=O)C |  | 1-Methoxyethyl acetate | 0.0564874410 |
| CC1=CCCCC1 |  | Methylcyclohex-1-ene | -0.578509688 |
| CC1=CCCC1 |  | Methylcyclopent-1-ene | -0.510001957 |
| CC1=CC=CC2=CC=CC=C12 |  | 1-Methylnaphthalene | -0.642662346 |
| CCCCCCC1CCCCC1C |  | 1-Heptyl-1-methylcyclopentane | -0.170501322 |
| CCCC1=CC=CC=C1C |  | 1-Butyl-2-methylbenzene | -0.570053458 |
| CCCCCCCCC1CCCCC1C |  | 1-Nonyl-1-methylcyclopentane | -0.15577963 |
| CCC1=CC(=CC(=C1)C)CC |  | 1-Ethyl-3,5-dimethylbenzene | -0.630259752 |
| CCC1CCC(C1)C |  | 1-Ethyl-3-methylcyclopentane | -0.181969196 |
| CC1CCCC(C1)C(C)C |  | 1-(Propan-2-yl)-1-methylcyclopentane | -0.21320489 |
| CCCCC1=CC=CC(=C1)C |  | 1-Pentyl-2-methylbenzene | -0.535236716 |
| CCCC1=CC=CC(=C1)C |  | 1-Butyl-2-methylbenzene | -0.570053458 |
| CC1=CC=C(C=C1)C(C)C |  | 1-Methyl-4-(propan-2-yl)benzene | -0.5506078 |
| CCCCCCCCCC1CCC(CC1)C |  | 1-Decyl-3-ethylcyclopentane | -0.128008366 |
| CCCC1=CC=C(C=C1)C |  | 1-Butyl-4-methylbenzene | -0.46189639 |
| CCCCCC1CCC(CC1)C |  | 1-Hexyl-3-ethylcyclopentane | -0.142295271 |
| CCC[N+](=O)[O-] |  | Nitropropane | -0.210604787 |
| CCCCCCCC=C |  | Non-1-ene | -0.375872612 |
| C=CCC(=O)CCCCC |  | Oct-2-en-1-one | -0.411337733 |
| CCCCCCCCO |  | Octan-1-ol | -0.141513318 |
| CCCCCCC=C |  | Oct-1-ene | -0.406260878 |
| CCCCCCCCCCCCCC=C |  | Pentadec-1-ene | -0.273234725 |
| CCCC=C |  | Pent-1-ene | -0.537354708 |
| CC(COC1=CC=CC=C1)O |  | 2-Phenoxypropan-1-ol | -0.41363892 |
| CCCOCC(C)O |  | 1-(1-Hydroxyethyl)oxypropane | 0.0055844783782959 |
| CC(COC(C)(C)C)O |  | 2-(tert-Butoxy)propan-1-ol | -0.061724484 |
| CCCCCCCCCCCCC=C |  | Tetradec-1-ene | -0.287106544 |
| CCCCCCCCCCCC=C |  | Tridec-1-ene | -0.301299304 |
| CCCCCCCCCC=C |  | Dodec-1-ene | -0.316357166 |
| CC1=CC(=C(C=C1)C)C=O |  | 2,4-Dimethylbenzaldehyde | -0.746041417 |
| CCCCOCCOCCOC(=O)C |  | 4-[2-(2-butoxyethoxy)ethoxy]butan-2-one | -0.091839015 |
| CCCCOCCOCCO |  | 2-[2-(2-butoxyethoxy)ethoxy]ethanol | 0.0235812067985535 |
| CCOCCOCCO |  | 2-[2-(2-ethoxyethoxy)ethoxy]ethanol | -0.020830631 |
| CCOCCOCCOC(=O)C |  | 4-[2-(2-ethoxyethoxy)ethoxy]butan-2-one | -0.147855997 |
| CCCCC(CC)COCCO |  | 2-(Hexan-3-yloxy)ethanol | 0.034690797328949 |
| CCCCCCOCCOCCO |  | 2-[2-(2-hexyloxyethoxy)ethoxy]ethanol | 0.0240611433982849 |
| COCCOCCO |  | 2-[2-(2-methoxyethoxy)ethoxy]ethanol | -0.125262439 |
| CCCOCCOCCO |  | 2-[2-(2-propoxyethoxy)ethoxy]ethanol | 0.0102881789207458 |
| C=C(CCl)CCl |  | 2,3-dichloromethylprop-1-ene | -0.939110279 |
| CC(C)(C)C(C)(C)C |  | 2,2,3,3-Tetramethylbutane | -0.161500424 |
| CC(C)C(C)(C)C |  | 2,2,3-Trimethylbutane | -0.243475556 |
| CCC(C)C(C)(C)C |  | 2,2,3-Trimethylpentane | -0.214596093 |
| CCCC(C)CC(C)(C)C |  | 2,2,3-Trimethylhexane | -0.20029062 |
| CCC(C)CC(C)(C)C |  | 2,2,3-Trimethylpentane | -0.214596093 |
| CC(C)CC(C)(C)C |  | 2,2,3-Trimethylbutane | -0.243475556 |
| CC(C)C(C(C)(C)CO)O |  | 3-Hydroxy-2,2-dimethyl-3-(propan-2-yl)propan-1-ol | 0.0596520304679871 |
| CC(C)C(C(C)(C)COC(=O)C(C)C)OC(=O)C(C)C |  | 3-(1-Acetoxy-2-methylpropan-2-yl)-2,2-dimethyl-3-(propan-2-yl)propyl acetate | -0.270229906 |
| CC(C)C(C(C)(C)COC(=O)C(C)C)O |  | 3-(1-Acetoxy-2-methylpropan-2-yl)-2,2-dimethylbutan-1-ol | 0.0940072536468506 |
| CCC(C)CCC(C)(C)C |  | 2,2,3-Trimethylhexane | -0.20029062 |
| CC(C)CCC(C)(C)C |  | 2,2,3-Trimethylpentane | -0.214596093 |
| CC(C)(OC)OC |  | 1,1-Dimethoxyethane | -0.378858268 |
| CCC(C)(C)C |  | 2-Methylbutane | -0.244538754 |
| CCCCCC(C)(C)C |  | 2,2-Dimethylheptane | -0.132066101 |
| CCCCC(C)(C)C |  | 2,2-Dimethylhexane | -0.137276381 |
| CCCCCCC(C)(C)C |  | 2,2-Dimethyloctane | -0.125140309 |
| CCCC(C)(C)C |  | 2,2-Dimethylpentane | -0.11647591 |
| CC(C)(C)C=O |  | 2,2-Dimethylpropanal | -0.295922518 |
| C=C(C(F)(F)F)F |  | 2-Fluoro-3,3,3-trifluoropropene | -1.285198689 |
| CCC(C)(C)C(C)C |  | 2,2,3-Trimethylbutane | -0.243475556 |
| CC(=C)C(C)(C)C |  | 3,3-Dimethylbut-1-ene | -0.392500579 |
| CC(C)CC(C)C(C)C(C)C |  | 2,3,4,5-Tetramethylhexane | -0.24615106 |
| CC(C)C(C)C(C)C |  | 2,3-Dimethylpentane | -0.16209206 |
| CC(C)CC(C)C(C)CC(C)C(C)COC(=O)C |  | 2,3,5,6,8-pentamethylnonyl acetate | -0.335465491 |
| CC(C)CC(C)CC(C)C(C)C |  | 3,4,5-Trimethylheptane | -0.08610791 |
| CC(C)CC(C)CC(C)C(C)COC(=O)C |  | 3,4,5-Trimethyl-7-acetoxyheptane | 0.00922662019729614 |
| CC(C)CC(C)C(C)C |  | 2,3,4-Trimethylpentane | -0.202716768 |
| CC1=CC(=C(C(=C1)O)C)C |  | 2,4,6-Trimethylphenol | -0.694864213 |
| CC(=O)OCC(C)C(C)CC(C)C |  | 2,3,4-Trimethylpentyl acetate | -0.154683769 |
| CC(C)CC(C(C)C)C(C)C(C)C |  | 2,3,4,5-Tetramethylheptane | -0.140381902 |
| CC(C)CCC(C)C(C)C |  | 2,3,4-Trimethylhexane | -0.142923176 |
| CC1=C(C(=C(C=C1)C)O)C |  | 2,4,6-Trimethylphenol | -0.694864213 |
| CC(C(C)O)O |  | 2-Methylpropane-1,2-diol | -0.038806379 |
| CC(C)C(C)C |  | 2,3-Dimethylbutane | -0.30256933 |
| CCCCC(C)C(C)C |  | 2,3-Dimethylheptane | -0.178914219 |
| CCCC(C)C(C)C |  | 2,3-Dimethylhexane | -0.165370047 |
| CC1=CC2=CC=CC=C2C=C1C |  | 2-Methylnaphthalene | -0.755618095 |
| CCCCCC(C)C(C)C |  | 2,3-Dimethyloctane | -0.172337443 |
| CCC(C)C(C)C |  | 2,3-Dimethylpentane | -0.16209206 |
| CC1=C(C(=CC=C1)O)C |  | 2,6-Dimethylphenol | -0.686612487 |
| CC(C)C(=C)C |  | 3-Methylbut-1-ene | -0.507123053 |
| CCC(C)C(=C)C |  | 3-Methylpent-1-ene | -0.34191367 |
| CC(=C(C)C)C |  | 3,3-Dimethylbut-1-ene | -0.39248544 |
| CCCC(=C(C)C)C |  | 4,4-Dimethylhex-1-ene | -0.334136277 |
| CCC(=C(C)C)C |  | 4,4-Dimethylpent-1-ene | -0.403605878 |
| CC(C)C(C)COC(=O)C |  | 2,3-Dimethylbutyl acetate | -0.306098312 |
| CCCCC(C)C(C)COC(=O)C |  | 2,3-Dimethylheptyl acetate | -0.123555422 |
| CCCC(C)(C)CC(C)C |  | 2,2,5-Trimethylheptane | -0.095660388 |
| CCC(C)(C)CC(C)C |  | 2,2,5-Trimethylhexane | -0.177754879 |
| CC(=C)CC(C)(C)C |  | 4,4-Dimethylpent-1-ene | -0.403605878 |
| CC(=CC(C)(C)C)C |  | 3,3-Dimethylbut-1-ene | -0.392500579 |
| CC(C)CC(C)C(C)C(C)CC(C)C |  | 3,4,5,6-Tetramethyloctane | -0.09296149 |
| CC(C)CC(C)CC(C)CC(C)C |  | 3,4,5-Trimethyloctane | -0.085723639 |
| CC(C)CC(C)CC(C)CC(C)COC(=O)C |  | 3,4,5-Trimethyl-8-acetoxyoctane | 0.0138548016548157 |
| CC(C)CC(C)CC(C)C |  | 3,4-Dimethylhexane | -0.066077232 |
| CCCC(C)CC(C)C |  | 3,4-Dimethylheptane | -0.068340302 |
| CCC(C)CC(C)C |  | 3,4-Dimethylpentane | -0.250107408 |
| CCCCC(C)CC(C)C |  | 3,4-Dimethylheptane | -0.068340302 |
| CC(C)CC(C)C |  | 2,3-Dimethylbutane | -0.30256933 |
| CC1=CC(=C(C=C1)O)C |  | 2,6-Dimethylphenol | -0.686612487 |
| CC(C)CC(=C)C |  | 3-Methylpent-1-ene | -0.34191367 |
| CC(C)C=C(C)C |  | 2-Methylbut-2-ene | -0.575952172 |
| CCCC(C)CC(C)COC(=O)C |  | 3,4-Dimethylheptyl acetate | -0.099433601 |
| CCC(C)CC(C)COC(=O)C |  | 3,4-Dimethylhexyl acetate | -0.1021685 |
| CC(C)CC(C)COC(=O)C |  | 3,4-Dimethylpentyl acetate | -0.167954803 |
| CC(=O)CC(=O)C |  | Pentane-2,4-dione | -0.671692312 |
| CC1=C(C=C(C=C1)N=C=O)N=C=O |  | 1,3-Diisocyanato-2-methylbenzene | -0.792071462 |
| CCC(C)(C)CCC(C)C |  | 2,2,5-Trimethylhexane | -0.177754879 |
| COCCOCCOCCOCCO |  | Tetraethylene glycol methyl ether | -0.061705887 |
| CC1=CC=C(O1)C |  | 2-Methylfuran | -0.956971645 |
| CCC(C)CCC(C)C |  | 3,4-Dimethylhexane | -0.066077232 |
| CC(C)CCC(C)C |  | 3,4-Dimethylpentane | -0.250107408 |
| CCCC(C)CCC(C)C |  | 4,5-Dimethylheptane | -0.084858 |
| CC1=CC(=C(C=C1)C)O |  | 2,4-Dimethylphenol | -0.759781361 |
| CCC(C)CCC(C)COC(=O)C |  | 4,5-Dimethylhexyl acetate | -0.23631534 |
| CC(C)CCC(C(C)C)C(C)CC(C)C |  | 3,4,5,6-Tetramethyloctane | -0.09296149 |
| CC(C)CC(C)CC(=O)CC(C)C |  | 2,3,5,6-Tetramethylheptan-4-one | -0.187084019 |
| CCC(C)CCCC(CC)CC |  | 3,6-Dimethyloctane | -0.134373575 |
| CC(C)CCCC(C)C |  | 3,5-Dimethylheptane | -0.185755312 |
| CCCC(C)CCCC(C)C |  | 4,6-Dimethylnonane | -0.174710482 |
| CCC(C)CCCC(C)C |  | 3,6-Dimethylheptane | -0.225899041 |
| CC1=C(C(=CC=C1)C)O |  | 2,6-dimethylphenol | -0.686612487 |
| CC(C)CC(CC(C)C)O |  | 2,3,5-Trimethylhexan-2-ol | -0.146291643 |
| CC1=CC(=C(C(=C1)C(C)(C)C)O)C(C)(C)C |  | 2,6-Di-tert-butyl-4-methylphenol | -0.27426073 |
| CC1=C(C=CC=C1N=C=O)N=C=O |  | 1,3-Diisocyanato-2-methylbenzene | -0.792071462 |
| CCCCOCCOCCOCCO |  | 1-[2-[2-(2-butoxyethoxy)ethoxy]ethoxy]ethane | 0.00203245878219604 |
| CCOCCOCCOCCO |  | Tetraethylene glycol ethyl ether | 0.0183106064796448 |
| COCCOCCOCCO |  | Tetraethylene glycol methyl ether | -0.061705887 |
| CCCOCCOCCOCCO |  | Tetraethylene glycol propyl ether | 0.0389848351478577 |
| CCC(CO)N |  | 2-Aminobutan-1-ol | -0.058717787 |
| CCC(CO)(CO)N |  | 2-Aminobutane-2,3-diol | -0.068102539 |
| CC(C)(CO)N |  | 2-Amino-2-methylpropan-1-ol | -0.277829528 |
| CCCCOCCO |  | Diethylene glycol butyl ether | -0.0140872 |
| CCCCOCCOC(=O)C |  | Butoxyethoxyethyl acetate | -0.072529435 |
| CCC(C)O[N+](=O)[O-] |  | 2-Nitrobutan-2-ol | 0.224476158618927 |
| CCCCC1CCCO1 |  | 2-Hexyloxirane | -0.303763717 |
| CC#CC |  | But-1-yne | -0.782399297 |
| CC1=CC=CC=C1Cl |  | 1-Chloro-2-methylbenzene | -0.920276523 |
| CCCCCCCCC(=O)C |  | Decan-2-one | -0.263184786 |
| CCOCCO |  | 2-(2-Ethoxyethoxy)ethanol | -0.086352885 |
| CCOCCOC(=O)C |  | 2-(2-Ethoxyethoxy)ethyl acetate | -0.210918754 |
| CCC1=CC=CO1 |  | 2-Ethylfuran | -0.754693568 |
| CCCCC(CC)C(=O)O |  | 2-Methylheptanoic acid | -0.103494048 |
| CCCC(C(CC)CO)O |  | 4-Ethyl-2-methylhexan-1-ol | -0.039729655 |
| CCC(=C)CC |  | 3-Methylpent-1-ene | -0.341920912 |
| CCCCC(CC)CO |  | 2-Methylheptan-1-ol | -0.146932721 |
| CCCC[C@H](CC)COC(=O)C |  | (2S)-2-Methylheptyl acetate | -0.210682869 |
| CCCCC(CC)COC(=O)C=C |  | 2-Methylheptyl acrylate | -0.25142923 |
| CCCCC(CC)COC(=O)C1=CC=CC=C1 |  | 2-Methylheptyl benzoate | -0.273580581 |
| CCCCCC(=O)C |  | Heptan-2-one | -0.323983938 |
| CCCCC(C)O |  | Hexan-2-ol | -0.083341658 |
| COCCO |  | 2-(2-Methoxyethoxy)ethanol | -0.236945927 |
| CC(COC)OCC(C)OC |  | 1-Methoxy-2-(1-methoxyethoxy)propane | -0.200197816 |
| CC(CO)OC |  | 1-Methoxypropan-2-ol | -0.375825495 |
| CC(=O)OCCOC |  | 2-Ethoxyethyl acetate | -0.352432609 |
| CCC(CC(C(C)C)C(C)C)C(C)C |  | 2,3,4,5-Tetramethylheptane | -0.140381902 |
| CC1=CC=CO1 |  | 2-Methylfuran | -0.956971645 |
| CCCCCC(C)C |  | 2-Methylheptane | -0.219428599 |
| CCCCC(C)C |  | 2-Methylhexane | -0.230294317 |
| CC1=CC2=CC=CC=C2C=C1 |  | 1-Methylnaphthalene | -0.642662346 |
| CCCCCCCC(C)C |  | 2-Methylnonane | -0.194111347 |
| CCCCCCC(C)C |  | 2-Methyloctane | -0.205103815 |
| CCCC(C)C |  | 2-Methylpentane | -0.232401282 |
| CC(C)C=O |  | 2-Methylpropanal | -0.391159296 |
| CCC(C)CO |  | 2-Methylbutan-1-ol | -0.128496408 |
| CCC(=C)C |  | 2-Methylbut-1-ene | -0.514185667 |
| CCC(C)COC(=O)C |  | 2-Methylbutyl acetate | -0.244396061 |
| CCCCCC(=C)C |  | 2-Methylhept-1-ene | -0.416220963 |
| CCCCC(=C)C |  | 2-Methylhex-1-ene | -0.445230395 |
| CCCC(=C)C |  | 2-Methylpent-1-ene | -0.499871492 |
| CC(CC(C)(C)O)O |  | 3-Hydroxy-2,2-dimethylbutan-1-ol | 0.0128881335258484 |
| CCC(C)(C)O |  | 2-Methylbutan-2-ol | -0.075939715 |
| CC=C(C)C |  | 2-Methylpropene | -0.591300011 |
| CCCCC=C(C)C |  | 2-Methylhex-1-ene | -0.445230395 |
| CCCC=C(C)C |  | 2-Methylpent-1-ene | -0.499871492 |
| CCC=C(C)C |  | 2-Methylbut-1-ene | -0.514185667 |
| CC(C)(C=C)O |  | 2-Methylbut-3-en-2-ol | -0.293314278 |
| CCCCC(CC)C(C)C |  | 2,3-Dimethylheptane | -0.178914219 |
| CCCC(=O)C(C)C |  | 2-Methylheptan-2-one | -0.445334256 |
| CCCCC(C)C=O |  | 2-Methylhexanal | -0.205621421 |
| CCCCC(C)COC(=O)C |  | 2-Methylhexyl acetate | -0.233593285 |
| CCCCCCC(C)COC(=O)C |  | 2-Methyloctyl acetate | -0.199461639 |
| CCCC(C)COC(=O)C |  | 2-Methylpentyl acetate | -0.221524537 |
| CC/C=C/C(C)C |  | (E)-4-Methylpent-2-ene | -0.517485261 |
| COC(C)COC(C)=O |  | 1-Methoxy-2-acetoxypropane | -0.067211807 |
| CCCCCCOCCO |  | 2-(2-Hexyloxyethoxy)ethanol | -0.014808416 |
| CC(C)[N+](=O)[O-] |  | 2-Nitropropane | -0.152886569 |
| CCCCCCCC(=O)C |  | Nonan-2-one | -0.282521486 |
| CCCCCCC(C)O |  | Octan-2-ol | -0.076010764 |
| CCCCCCC(=O)C |  | Octan-2-one | -0.301113307 |
| CCCC(C)O |  | Pentan-2-ol | -0.049127102 |
| CCCC(=O)C |  | Pentan-2-one | -0.388309181 |
| C1=CC=C(C=C1)OCCO |  | 2-Phenoxyethanol | -0.485825628 |
| CCCOCCO |  | 2-(2-Propoxyethoxy)ethanol | -0.035440445 |
| CCCC1CCCCC1=O |  | 2-Hexylcyclohexan-1-one | -0.142028093 |
| CC(CO)OC(C)(C)C |  | 2-tert-Butoxypropan-1-ol | -0.061724484 |
| CC(C)(CCO)OC |  | 3-Methoxy-2,2-dimethylpropan-1-ol | -0.213985711 |
| CCCCC(CC)CCl |  | 1-Chloro-2-methylheptane | -0.216264367 |
| C(C(C(F)(F)F)(F)F)(Cl)Cl |  | 1,2-Dichloro-1,1,2,2-tetrafluoroethane | -1.194532156 |
| CCC(CC)(CC)CC |  | 3-Ethyl-3-methylpentane | -0.045296311 |
| CCCCC(C)(C)CC |  | 2,2-Dimethylheptane | -0.132066101 |
| CCCC(C)(C)CC |  | 2,2-Dimethylhexane | -0.137276381 |
| CCCCCC(C)(C)CC |  | 2,2-Dimethyloctane | -0.125140309 |
| CCC(C)(C)CC |  | 2,2-Dimethylpentane | -0.11647591 |
| CC(C)(C)C=C |  | 3,3-Dimethylbut-1-ene | -0.392500579 |
| CCC(C)(C)C=C |  | 4,4-Dimethylpent-1-ene | -0.403605878 |
| CCC(CC)C(CC)CC |  | 3-Ethyl-4-methylheptane | -0.02422452 |
| CCC(CC)C(=CC)CC |  | 3-Ethyl-4-methylhept-3-ene | -0.323432177 |
| CCCC(C)C(C)CC |  | 2,4-Dimethylheptane | -0.226134896 |
| CCC(C)C(C)CC |  | 2,4-Dimethylhexane | -0.278863966 |
| CC1=C(C=C(C=C1)O)C |  | 2,6-Dimethylphenol | -0.686612487 |
| CC(C)C(C)C=C |  | 4,5-Dimethylhex-1-ene | -0.315481097 |
| C/C=C(/C)\C(C)C |  | (Z)-4,5-Dimethylhex-2-ene | -0.257786542 |
| CCC(C)C(C)CCOC(=O)C |  | 5,6-Dimethylheptyl acetate | -0.141194165 |
| CC(=O)OCCC(C)CC(C)CCCC(C)C |  | 2,4,6-Trimethyloctyl acetate | -0.142408758 |
| CCC(C)CC(C)CC(C)CCOC(=O)C |  | 5,7,8-Trimethyldecyl acetate | -0.082630098 |
| CC(C)CC(C)CC(C)CCOC(=O)C |  | 4,6,7-Trimethylnonyl acetate | -0.080059707 |
| CCC(CC)CC(CC)CC |  | 4,6-Dimethylnonane | -0.174710482 |
| CCC(C)CC(C)CC |  | 3,5-Dimethylheptane | -0.185755312 |
| CC1=CC(=CC(=C1)O)C |  | 2,4-Dimethylphenol | -0.759781361 |
| CCC(C)CC(C)CCOC(=O)C |  | 5,6-Dimethyloctyl acetate | -0.094798028 |
| CC(C)CC(C)CCOC(=O)C |  | 4,5-Dimethylheptyl acetate | -0.096162796 |
| CC(C)CC(C)CCC(C)CCOC(=O)C |  | 5,6,8-Trimethyldecyl acetate | -0.070058703 |
| CCCCOCCOCCOCCOCCO |  | Pentaethylene glycol butyl ether | 0.0651006102561951 |
| CCCCC(C)CCC(C)CC |  | 2,6-Dimethylnonane | -0.163277686 |
| CCCCCC(C)CCC(C)CC |  | 2,6-Dimethylundecane | -0.167817742 |
| CC(C)CCC(C)CCOC(=O)C |  | 5,6-Dimethyloctyl acetate | -0.094798028 |
| CCC(C)CCC(C)CCOC(=O)C |  | 5,6-Dimethylnonyl acetate | -0.094510853 |
| CCC(CC)CCCC(CC)CC |  | 5,8-Dimethylundecane | -0.157814384 |
| CCCCCC(C)CCCC(C)CC |  | 2,8-Dimethyltridecane | -0.162910998 |
| CCCCCCC(C)CCCC(C)CC |  | 2,8-Dimethylpentadecane | -0.154267162 |
| CC(C)CCCC(C)CCO |  | 2,6-Dimethyloctan-1-ol | -0.097905993 |
| CCC(CC)CCCCC(CC)CC |  | 4,6-Dimethyldecane | -0.18979001 |
| CCC(CC)CCCCCC(CC)CC |  | 4,8-Dimethyldodecane | -0.163058102 |
| CC1=CCC2C(C1)C2(C)C |  | 1,7,7-Trimethylbicyclo[2.2.1]hept-2-ene | -0.339527249 |
| C=CCCl |  | 3-Chloroprop-1-ene | -0.778727412 |
| CCOCCCO |  | 3-Ethoxypropan-1-ol | -0.109879553 |
| CCC(CC)C(C)C |  | 3-Methylhexane | -0.179231644 |
| CCCCC(CC)CC |  | 4-Methylnonane | -0.19863975 |
| CCC(CC)CC |  | 3-Methylhexane | -0.179231644 |
| CCC(=CC)CC |  | 3-Methylhex-2-ene | -0.408371389 |
| CCC(C)(CC)CC |  | 3,3-Dimethylhexane | -0.161983073 |
| CCC(C)C(C)CCC(CC)CCOC(=O)C |  | 5,8-Dimethylundecyl acetate | -0.139249504 |
| CCC(C)CCC(CC)CCOC(=O)C |  | 6,8-Dimethylundecyl acetate | -0.149984956 |
| CCCCC(CC)CCOC(=O)C |  | 5-Methyldecyl acetate | -0.174672753 |
| CCCC(CC)CCOC(=O)C |  | 5-Methylnonyl acetate | -0.183491439 |
| CCC(CC)CCOC(=O)C |  | 5-Methyloctyl acetate | -0.168042123 |
| CCCC(=O)CC |  | Heptan-4-one | -0.29114455 |
| CC(C)C(=O)OCC(C)(C)C(O)C(C)C |  | 2,2,3-Trimethylbutyl 2-methylpropanoate | -0.120480329 |
| CC(C)C1=CC(=CC=C1)C(C)C |  | 1,3-Diisopropylbenzene | -0.368263274 |
| CCCCC(CCOC(=O)C)C(C)C |  | 6-Methyl-5-(propan-2-yl)heptyl acetate | -0.145725489 |
| CC(CCO)OC |  | 1-Ethoxypropan-2-ol | -0.153215945 |
| COCCCO |  | 3-Methoxypropan-1-ol | -0.343604654 |
| CC(C)CC(=O)O |  | 3-Methylbutanoic acid | -0.305957228 |
| CC1CCC=C1 |  | 3-Methylcyclopent-1-ene | -0.288031578 |
| CCCCCCCC(C)CC |  | 2-Methyldecane | -0.184741139 |
| CCCCCCCCCC(C)CC |  | 2-Methyltridecane | -0.165549695 |
| CC1=COC=C1 |  | 2-Methylfuran | -0.956971645 |
| CCCCC(C)CC |  | 2-Methylheptane | -0.219428599 |
| CCCC(C)CC |  | 2-Methylhexane | -0.230294317 |
| CCCCCCC(C)CC |  | 2-Methylnonane | -0.194111347 |
| CCCCCC(C)CC |  | 2-Methyloctane | -0.205103815 |
| CCCCCCCCCCCCC(C)CC |  | 2-Methylpentadecane | -0.155959368 |
| CCC(C)CC |  | 2-Methylpentane | -0.232401282 |
| CCCCCCCCCCCC(C)CC |  | 2-Methyltetradecane | -0.160928428 |
| CCCCCCCCCCC(C)CC |  | 2-Methyltridecane | -0.165484309 |
| CCCCCCCCC(C)CC |  | 2-Methyldodecane | -0.170833051 |
| CC(=C=C)C |  | 3-Methylbut-1-en-1-yne | -0.712757945 |
| CC(C)C=C |  | 3-Methylbut-1-ene | -0.507123053 |
| CCCC(C)C=C |  | 3-Methylpent-1-ene | -0.34191367 |
| CCC(C)C=C |  | 3-Methylbut-1-ene | -0.507123053 |
| CC(C)C(C)O |  | 2,3-Dimethylbutan-2-ol | -0.146687448 |
| CCCC(C)C(=O)C |  | 4-Methylpentan-2-one | -0.406738579 |
| CC(C)C(=C)C(C)C |  | 2,3-Dimethylbut-2-ene | -0.55575937 |
| CC(C)CC=O |  | 3-Methylbutanal | -0.371543288 |
| CC/C=C(/C)\CC |  | (Z)-4-Methylhex-2-ene | -0.288842678 |
| CCCCC(C)CCOC(=O)C |  | 5-Methylhexyl acetate | -0.291238546 |
| CCCC(C)CCOC(=O)C |  | 4-Methylpentyl acetate | -0.325048 |
| CCC(C)CCOC(=O)C |  | 3-Methylbutyl acetate | -0.358173907 |
| CC/C=C(\C)/CC |  | (E)-4-Methylhex-2-ene | -0.429784596 |
| CCCCCC(CC)O |  | 2-Methyloctan-2-ol | -0.025905907 |
| CCC(CC)O |  | 3-Methylpentan-3-ol | 0.0108823776245117 |
| CCC(=O)CC |  | Pentan-3-one | -0.361315966 |
| CCCC(C)(C)CCC |  | 2,2,5-Trimethylhexane | -0.177754879 |
| CCCCC(C)(C)CCC |  | 2,2,6-Trimethylheptane | -0.165088564 |
| CC(C)(C)CC=C |  | 3,3-Dimethylbut-1-ene | -0.392500579 |
| C/C=C\C(C)(C)C |  | (E)-2,4,4-trimethylpent-2-ene | -0.415364742 |
| CCC(C)C(C)CCCOC(=O)C |  | 6,7-Dimethyloctyl acetate | -0.204065859 |
| CC(C)C(C)CCCOC(=O)C |  | 5,6-Dimethylheptyl acetate | -0.141194165 |
| CC(C)CC(C)CCCOC(=O)C |  | 5,7-Dimethyloctyl acetate | -0.161555946 |
| CCC(C)CC(C)CCCOC(=O)C |  | 6,8-Dimethylnonyl acetate | -0.156824887 |
| CC(C)CC(C)CCC(C)CCCOC(=O)C |  | 6,8,9-Trimethyldecyl acetate | -0.131152123 |
| CCC(C)CCC(C)CCCOC(=O)C |  | 7,9-Dimethyldecyl acetate | -0.147848368 |
| CCCCCCC(C)CCCC(C)CCC |  | 2,9-Dimethyltetradecane | -0.15839076 |
| CCCC(CC)CCC |  | 4-Methyloctane | -0.20828706 |
| CCCCC(CC)CCC |  | 5-Methylnonane | -0.208404571 |
| CC1CCC=CC1 |  | 1-Methylcyclohex-1-ene | -0.578477323 |
| CCCCCCC(C)CCC |  | 2-Methyldecane | -0.184741139 |
| CCCC(C)CCC |  | 2-Methylheptane | -0.219428599 |
| CCCCCC(C)CCC |  | 2-Methylnonane | -0.194111347 |
| CCCCC(C)CCC |  | 2-Methyloctane | -0.205103815 |
| CC(C)CC=C |  | 3-Methylbut-1-ene | -0.507123053 |
| CC(C)CC(C)O |  | 3-Methylbutan-2-ol | -0.194000661 |
| CC(C)CC(=O)C |  | 4-Methylpentan-2-one | -0.406738579 |
| CCCC(C)CCCOC(=O)C |  | 5-Methylhexyl acetate | -0.291330189 |
| CCC(C)CCCOC(=O)C |  | 4-Methylpentyl acetate | -0.325048 |
| CCCCC(C)CCCOC(=O)C |  | 6-Methylheptyl acetate | -0.267195165 |
| CC(C)CCCOC(=O)C |  | 3-Methylbutyl acetate | -0.358173907 |
| CCCCC=CCCC |  | Non-4-ene | -0.368880749 |
| CCCCC(CCC)O |  | 4-Methyloctan-4-ol | -0.068387568 |
| CCCC1CCC(=O)CC1 |  | 5-Methylcyclohexan-1-one | -0.219047993 |
| CCCC(CCC)CCC |  | 4-Methyloctane | -0.20828706 |
| C=CC1=CC=C(C=C1)O |  | 4-Ethenylphenol | -3.236712456 |
| CCC(CC(C)CCOC(=O)C)C(C)CC(C)C |  | 6,8,9-Trimethyldecyl acetate | -0.131152123 |
| CCCCCCCC(C)CCCC |  | 2-Methyldodecane | -0.170833051 |
| CCCCCCC(C)CCCC |  | 2-Methyltridecane | -0.165484309 |
| CCC(C)CCCCO |  | 4-Methylhexan-1-ol | -0.111769497 |
| CC(C)CCC(=O)C |  | 5-Methylhexan-2-one | -0.344571352 |
| CCC(C)CCCCOC(=O)C |  | 5-Methylhexyl acetate | -0.291330189 |
| CC(C)CCCCOC(=O)C |  | 4-Methylpentyl acetate | -0.325048 |
| CCCC(C)CCCCOC(=O)C |  | 6-Methylheptyl acetate | -0.267195165 |
| CCCCCCCCC(C)CCCCC |  | 2-Methylpentadecane | -0.155959368 |
| CCCCCCCC(C)CCCCC |  | 2-Methyltetradecane | -0.160928428 |
| CCCCCCCCC(C)CCCCCC |  | 2-Methylhexadecane | -0.151420802 |
| CC(C)CCCCCCCO |  | 7-Methyloctan-1-ol | -0.193880081 |
| CCOC(C)OCC |  | 1-Ethoxy-2-methoxyethane | -0.351539224 |
| CC=O |  | Ethanal | -0.705688953 |
| CC(=O)O |  | Ethanoic acid | -0.725640357 |
| CC(=O)C |  | Propan-2-one | -0.596128285 |
| C#C |  | Ethyne | -0.916148067 |
| C=CC=O |  | Prop-2-enal | -2.521065474 |
| C=CC(=O)O |  | Prop-2-enoic acid | -2.160257578 |
| C=CC#N |  | Prop-2-enenitrile | -1.362112522 |
| C(CCC(=O)O)CC(=O)O |  | Pentanedioic acid | -0.290232718 |
| C=CCC1=CC=CC=C1 |  | But-3-en-1-ylbenzene | -0.641598046 |
| CC1CCCO1 |  | 2-Methyloxirane | -0.681119561 |
| CC1=CCC2CC1C2(C)C |  | 1,7,7-Trimethylbicyclo[2.2.1]hept-2-ene | -0.339532614 |
| CC(=C)C1=CC=CC=C1 |  | 1-(1-methylvinyl)benzene | -0.65797478 |
| CCCCCOC(=O)C |  | Pentyl acetate | -0.2630032 |
| CCCCC/C(=C/C1=CC=CC=C1)/C=O |  | (E)-7-Phenylhept-5-en-2-one | -0.589871526 |
| C/C=C/C1=CC=C(C=C1)OC |  | (E)-1-Methoxy-4-(pent-3-en-1-yl)benzene | -0.561757505 |
| CC1=CC[C@H](CC1)C(C)(C)O |  | (R)-1-(1-methyl-1,2,3,4-tetrahydronaphthalen-4-yl)-2-methylpropan-2-ol | -0.170729697 |
| C1=CC=C(C=C1)C=O |  | Benzaldehyde | -2.795548439 |
| C1=CC=CC=C1 |  | Benzene | -2.687924385 |
| C1=CC=C(C=C1)C(F)(F)F |  | 1-(Trifluoromethyl)benzene | -1.063695908 |
| C1=CC=C(C=C1)CO |  | Phenylmethanol | -0.724439621 |
| CC1(C2CCC(=C)C1C2)C |  | 3-Methylene-1,7,7-trimethylbicyclo[2.2.1]heptane | -0.393337667 |
| CC(=O)C(=O)C |  | Butane-2,3-dione | -0.685323596 |
| CCCC=O |  | Butanal | -0.426443219 |
| CCCC(=O)O |  | Butanoic acid | -0.381835639 |
| CCCCC1CCCCC1 |  | Pentylcyclohexane | -0.176491857 |
| CCCCOC(=O)C(=C)C |  | Butyl 3-methylbut-2-enoate | -0.366308481 |
| CCCCOC(=O)CC |  | Butyl propanoate | -0.076162934 |
| CC1(C2CCC(C2)C1=C)C |  | 7,7-Dimethyl-2-methylidenebicyclo[2.2.1]heptane | -0.399460196 |
| CC1(C2CCC1(C(=O)C2)C)C |  | 1,7,7-Trimethylbicyclo[2.2.1]heptan-2-one | -0.239850372 |
| [C-]#[O+] |  | Carbon monoxide | -0.476133227 |
| C(C=O)Cl |  | Chloroacetaldehyde | -0.797971129 |
| CC(=O)CCl |  | 1-Chloropropan-2-one | -0.702095866 |
| C(Cl)(Cl)Cl |  | Trichloromethane | -0.780504346 |
| C([N+](=O)[O-])(Cl)(Cl)Cl |  | Trichloro(nitro)methane | -0.489978224 |
| C1=CC=C(C=C1)/C=C/CO |  | (E)-3-Phenylprop-2-en-1-ol | -0.716442227 |
| C1=CC=C(C=C1)/C=C/C=O |  | (E)-3-Phenylprop-2-enal | -3.572268963 |
| C/C=C\C(C)C |  | (E)-4-Methylpent-2-ene | -0.517485261 |
| C(=C\C(F)(F)F)\C(F)(F)F |  | (E)-1,2-Bis(trifluoromethyl)ethene | -1.320534468 |
| C(=C\Cl)\Cl |  | (E)-1,2-Dichloroethene | -1.189472198 |
| C(/C=C\Cl)Cl |  | (Z)-1,2-Dichloroethene | -1.349891424 |
| C/C=C\C=C |  | (E)-Hexa-1,3-diene | -0.630746901 |
| C/C=C\C |  | (E)-Pent-2-ene | -0.62393558 |
| CCCC/C=C\C |  | (E)-Hept-3-ene | -0.451894283 |
| CCC/C=C\C |  | (E)-Hex-3-ene | -0.507039547 |
| CC/C=C\C |  | (E)-Pent-2-ene | -0.62393558 |
| CCC/C=C\CC |  | (E)-Oct-4-ene | -0.404881835 |
| CC/C=C\CC |  | (E)-Hept-3-ene | -0.451894283 |
| CCC/C(=C\C)/C |  | (E)-4-Methylhex-3-ene | -0.372392118 |
| CC/C(=C\C)/C |  | (E)-4-Methylpent-3-ene | -0.526774526 |
| CCC/C=C\CCC |  | (E)-Non-4-ene | -0.368872613 |
| CCCC/C=C\CCCC |  | (E)-Undec-5-ene | -0.31900543 |
| C1CC[C@H]2CCC[C@H]2C1 |  | (1R,4S)-1,2,3,4-Tetrahydro-1,4-methanonaphthalene | -0.564317942 |
| CC(CCC=C(C)C)CCO |  | 5-Methylhex-4-en-1-ol | -0.417908072 |
| C/C=C/C=O |  | (E)-But-2-enal | -0.742129564 |
| C1CCC1 |  | Cyclobutane | -0.33662203 |
| C1CC(=O)C1 |  | Cyclobutanone | -0.327602625 |
| C1CCCCCC1 |  | Cycloheptane | -0.196823716 |
| C1CCCCC1 |  | Cyclohexane | -0.185635626 |
| C1CCC(CC1)O |  | Cyclohexanol | -0.11584872 |
| C1CCC(=O)CC1 |  | Cyclohexanone | -0.168533146 |
| C1CCC=CC1 |  | Cyclohexene | -0.329729944 |
| C1CCCCCCC1 |  | Cyclooctane | -0.134798467 |
| C1C=CC=C1 |  | Cyclopentadiene | -0.64004457 |
| C1CCCC1 |  | Cyclopentane | -0.201124847 |
| C1CCC(C1)O |  | Cyclopentanol | -0.078803062 |
| C1CCC(=O)C1 |  | Cyclopentanone | -0.175906211 |
| C1CC=CC1 |  | Cyclopentene | -0.348831594 |
| C1CC1 |  | Cyclopropane | -0.766346216 |
| C[Si]1(O[Si](O[Si](O[Si](O1)(C)C)(C)C)(C)C)C |  | 1,1,2,2,3,3,4,4-octamethylcyclotetrasiloxane | -0.484460831 |
| C[Si]1(O[Si](O[Si](O[Si](O[Si](O1)(C)C)(C)C)(C)C)(C)C)C |  | 1,1,2,2,3,3,4,4,5,5-decamethylcyclopentasiloxane | -0.26723206 |
| CCCCCCCCCCC1CCCCC1 |  | Undecylcyclopentane | -0.146042824 |
| CC(=O)CC(C)(C)O |  | 4-Hydroxy-4-methylpentan-2-one | -0.346612364 |
| CCCCOC(=O)C1=CC=CC=C1C(=O)OCCCC |  | Dibutyl terephthalate | -0.153570712 |
| C(Cl)Cl |  | Dichloromethane | -0.710412383 |
| C(CO)NCCO |  | 2-(2-Hydroxyethylamino)ethanol | -0.009741187 |
| CCOCC |  | 1-Ethoxyethane | -0.360388637 |
| CCOC(=O)C1=CC=CC=C1C(=O)OCC |  | Diethyl terephthalate | -0.438535154 |
| C(COCCO)O |  | 2-(2-Hydroxyethoxy)ethanol | -0.092791975 |
| CCCCCCCC(=O)OCCOCCOC(=O)CCCCCCC |  | 2,2'-oxydiethyl dioctanoate | 0.0153880715370178 |
| CCCCC(CC)COCCOCCO |  | 2-(2-(2-Methylheptyloxy)ethoxy)ethanol | -0.055477858 |
| C(C(=O)CO)O |  | 2-hydroxypropanoic acid | -0.355064392 |
| CC(C)COCC(C)C |  | 2-Isopropoxy-2-methylpropane | -0.150980592 |
| CC(C)CC(=O)CC(C)C |  | 2,5-Dimethylhexan-3-one | -0.257976532 |
| CC(C)OC(=O)CCCCC(=O)OC(C)C |  | Isopropyl pimelate | 0.0623301863670349 |
| CC(C)OC(=O)OC(C)C |  | Isopropyl carbonate | 0.0517929196357727 |
| CC(C)OC(C)C |  | 2-Isopropoxypropane | -0.105615914 |
| CC(C)C(=O)C(C)C |  | 2,3-Dimethylbutan-2-one | -0.718712389 |
| COCOC |  | 1,1-Dimethoxyethane | -0.378858268 |
| COC(=O)CCCCC(=O)OC |  | Dimethyl pimelate | -0.260244906 |
| CNC |  | N-Methylmethanamine | -0.634743929 |
| COC(=O)OC |  | Dimethyl carbonate | -0.877056539 |
| COC |  | Methoxymethane | -0.724234939 |
| COC(=O)CCCC(=O)OC |  | Dimethyl glutarate | -0.382022381 |
| CC(C)CCCC(C)(C)O |  | 6-Methylheptan-2-ol | -0.151340485 |
| COC(=O)CCCCCCCCC(=O)OC |  | Dimethyl decanedioate | -0.162762284 |
| COC(=O)CCC(=O)OC |  | Dimethyl succinate | -0.508911371 |
| CS(=O)C |  | Dimethyl sulfoxide | -0.565447152 |
| CN(C)CCO |  | N-Methyl-N-(2-hydroxyethyl)methanamine | 0.093537449836731 |
| CCC(C)C(C)CO |  | 3,4-Dimethylpentan-1-ol | -0.089916408 |
| CCCCOCCCC |  | Butyl butyl ether | -0.145759672 |
| CCCCCOCCCCC |  | Pentyl pentyl ether | -0.129778296 |
| CCCOCCC |  | Propyl propyl ether | -0.197095156 |
| CCOC(C)COC(C)CO |  | 1,2-Bis(2-methoxypropoxy)ethane | -0.053940654 |
| CCC(O)OC(CC)O |  | 1,1'-oxybis(propan-1-ol) | 0.102857291698456 |
| COCC(C)OCC(C)O |  | 2-(2-Methoxypropoxy)propan-1-ol | -0.032087505 |
| CC(CO)OCC(C)OC |  | 2-(1-Methoxyethoxy)-2-methylpropan-1-ol | 0.126052677631378 |
| CC1=CC[C@@H](CC1)C(=C)C |  | (1S,4R)-4-Isopropyl-1-methylcyclohex-1-ene | -0.548607826 |
| CC |  | Ethane | -0.634782374 |
| CCO |  | Ethanol | -0.437006116 |
| C(CO)N |  | 2-Aminoethanol | -0.397020221 |
| C=C |  | Ethene | -1.975797176 |
| CCOCCC(=O)OCC |  | Diethyl succinate | -0.100337148 |
| CCOC(=O)C |  | Ethyl acetate | -0.574157059 |
| CCC#C |  | But-1-yne | -0.782399297 |
| CCOC(=O)C=C |  | Ethyl acrylate | -0.699835777 |
| CCN |  | Ethanamine | -0.574368417 |
| CCC1=CC=CC=C1 |  | Propylbenzene | -0.490982831 |
| CCBr |  | Bromoethane | -0.625024259 |
| CCCC(=O)OCC |  | Ethyl butanoate | -0.184916884 |
| CCCl |  | Chloroethane | -0.637808323 |
| CCC1CCCCC1 |  | Propylcyclohexane | -0.175613821 |
| CCC1CCCC1 |  | Propylcyclopentane | -0.217650473 |
| CCOC=O |  | Ethyl formate | -0.443386197 |
| CCOC(C)C |  | 2-Ethoxypropane | -0.172792196 |
| CCOC(=O)C(C)O |  | Ethyl lactate | -0.097226977 |
| CCOC(=O)C(=C)C |  | Ethyl crotonate | -0.563245356 |
| CCCCOCC |  | Butyl propyl ether | -0.167704105 |
| CCC(=O)OCC |  | Ethyl propanoate | -0.194977045 |
| CCOC(C)(C)C |  | Ethyl tert-butyl ether | -0.123162925 |
| C(CO)O |  | Methanol | -0.836777449 |
| CC(=O)OCCOC(=O)C |  | 2-Ethoxyethyl acetate | -0.352432609 |
| CCOCCOCC |  | 2-Ethoxyethyl ethyl ether | -0.177193254 |
| C1CO1 |  | Oxirane | -0.998766422 |
| C=O |  | Formaldehyde | -1.127367258 |
| C(=O)O |  | Formic acid | -1.597369909 |
| C1=COC=C1 |  | Furan | -0.893838525 |
| C1CC(=O)OC1 |  | Butyrolactone | -0.102938116 |
| CC(=CCC/C(=C/CO)/C)C |  | 3,7-Dimethylocta-1,6-dien-3-ol | -0.35602206 |
| C(CC=O)CC=O |  | Pentanedial | -0.345411897 |
| C(C(CO)O)O |  | 1,2,3-Propanetriol | 0.0827274322509766 |
| CC(=O)OCC(COC(=O)C)OC(=O)C |  | 2,3-Bis(acetyloxy)propyl acetate | 0.0165207386016846 |
| CCCCOCC(C)OCC(C)O |  | 2-(2-Butoxypropoxy)propan-1-ol | 0.00395381450653076 |
| C(C=O)O |  | Hydroxyacetaldehyde | -0.547095597 |
| C(C(=O)O)O |  | Hydroxyethanoic acid | -0.429911673 |
| C(=O)C=O |  | Ethanedial | -1.797459126 |
| CCCCCCC=O |  | Heptanal | -0.261648387 |
| CCCCCCCC1CCCCC1 |  | Octylcyclopentane | -0.162688255 |
| C1(=C(C(=C(C(=C1F)F)F)F)F)F |  | Hexafluorobenzene | -0.575566828 |
| C[Si](C)(C)O[Si](C)(C)C |  | Hexamethyldisiloxane | -0.401456892 |
| CCCCCC=O |  | Hexanal | -0.294964969 |
| CCCCCC/C(=C\C1=CC=CC=C1)/C=O |  | (E)-9-Phenylnon-8-en-2-one | -0.435094595 |
| CCCCCCC1CCCCC1 |  | Heptylcyclopentane | -0.170710921 |
| CC(=O)CO |  | Hydroxyacetone | -0.611936033 |
| CC(CCCC(C)(C)O)CC=O |  | 6,6-Dimethylheptan-2-one | -0.251866519 |
| C=C(C=O)CO |  | 4-Hydroxybut-2-enal | -0.754858613 |
| CC(COC(=O)C=C)O |  | 3-Hydroxypropyl acrylate | -0.306819856 |
| C1CC2=CC=CC=C2C1 |  | Indane | -0.577910542 |
| C1C=CC2=CC=CC=C21 |  | Indene | -0.799228609 |
| CC(C)CCOC(=O)C |  | 3-Methylbutyl acetate | -0.358173907 |
| CC(C)CCO |  | 3-Methylbutan-1-ol | -0.280132383 |
| CCCCCCCCCCCC(=O)OCCC(C)C |  | Isopropyl laurate | -0.062903285 |
| CC(C)CCOC(=O)C(C)C |  | 3-Methylbutyl 2-methylpropanoate | -0.203711867 |
| CCCCCCCC(=O)OCCC(C)C |  | Isopropyl octanoate | -0.060265243 |
| CC(=C)C(=O)OC1CC2CCC1(C2(C)C)C |  | Bornyl acrylate | -0.302835554 |
| CC(C)C |  | 2-Methylpropane | -0.352603406 |
| CC(=C)C |  | Prop-1-en-2-yl | -0.756248057 |
| CC(C)COC(=O)C |  | 2-Methylpropyl acetate | -0.432075918 |
| CC(C)COC(=O)C=C |  | 2-Methylpropyl acrylate | -0.466252714 |
| CC(C)CO |  | 2-Methylpropan-1-ol | -0.32835871 |
| CC(C)CC1CCCCC1 |  | 2-Methylpropylcyclopentane | -0.252447546 |
| CC(C)COC(=O)C(C)C |  | 2-Methylpropyl 2-methylpropanoate | -0.255174279 |
| CC(C)COC(=O)C(=C)C |  | 2-Methylpropyl crotonate | -0.391790926 |
| CC(C)CO[N+](=O)[O-] |  | 2-Nitro-2-methylpropan-1-ol | -0.24098888 |
| CC(C)C(=O)O |  | 2-Methylpropanoic acid | -0.404570758 |
| CCC(C)C |  | 2-Methylbutane | -0.244538754 |
| CC1=CC(=O)CC(C1)(C)C |  | 2,2,6-Trimethylcyclohexan-1-one | -0.169671357 |
| CC(=C)C=C |  | Buta-1,3-diene-2-yl | -2.21992898 |
| CC(C)OC(=O)C |  | Isopropyl acetate | 0.170216500759125 |
| CC(C)O |  | Propan-2-ol | -0.271223247 |
| CC(C)N |  | Propan-2-amine | -0.336051106 |
| CC(C)C1=CC=CC=C1 |  | Isopropylbenzene | -0.474232316 |
| CC(C)C1CC1 |  | Isopropylcyclopropane | -0.425724149 |
| CC(C)OC=O |  | Isopropyl formate | -0.089679837 |
| CC(C)O[N+](=O)[O-] |  | 2-Nitropropane | -0.152886569 |
| CCCCCCCCCCCCN1CCCC1=O |  | Dodecyl-2-pyrrolidinone | -0.081911504 |
| CC(=CCCC(C)(C=C)O)C |  | 6,10-Dimethylundeca-5,9-dien-2-ol | -0.329912931 |
| C(C(C(=O)O)O)C(=O)O |  | 2-Hydroxypropane-1,2,3-tricarboxylic acid | 0.394936263561249 |
| CC1=CC(=CC=C1)O |  | 2-Methylphenol | -0.787197649 |
| CC1=CC(=CC=C1)C(C)C |  | 1,3-Diisopropylbenzene | -0.368263274 |
| CCC1=CC(=CC=C1)CC |  | 1,3-Dipropylbenzene | -0.406214088 |
| CC1CCC(C(C1)O)C(C)C |  | 4-Isopropyl-1-methylcyclohexan-1-ol | -0.060982227 |
| CC(=CC(=O)C)C |  | 4-Methylpent-3-en-2-one | -0.723125637 |
| CC(=C)C=O |  | 3-Methylbut-2-enal | -0.704413474 |
| CC(=C)C(=O)O |  | 3-Methylbut-2-enoic acid | -0.649705946 |
| CO |  | Methanol | -0.836777449 |
| CC(=O)COC |  | 2-Methoxyethyl acetate | -0.547091544 |
| COC1=CC=CC=C1 |  | Methoxybenzene | -0.776969612 |
| COC(C(C(C(F)(F)F)(F)F)(F)F)(F)F |  | Methyl perfluoro-tert-butyl ether | -0.45469439 |
| COC(C(C(F)(F)F)(C(F)(F)F)F)(F)F |  | Methyl perfluoroisopropyl ether | -0.973333597 |
| CCC(OC)OC(=O)C |  | Methyl ethyl carbonate acetate | -0.662483692 |
| CC(=O)OC |  | Methyl acetate | -0.701457143 |
| CC#C |  | Propyne | -0.824413359 |
| COC(=O)C=C |  | Methyl acrylate | -0.960124075 |
| CC(C)CC(C)OC(=O)C |  | 3-Methylbutyl 2-methylpropanoate | -0.203711867 |
| CBr |  | Bromomethane | -0.767151237 |
| CCCC(=O)OC |  | Methyl butanoate | -0.442131758 |
| CCl |  | Chloromethane | -0.781684339 |
| CCCCCCC/C=C\CCCCCCCC(=O)OC |  | Methyl (E)-octadec-9-enoate | -0.214204788 |
| CCCCCC/C=C\CCCCCCCC(=O)OC |  | Methyl (E)-hexadec-9-enoate | -0.232016385 |
| CCCCCCCC/C=C\CCCCCCCC(=O)OC |  | Methyl (E)-eicos-11-enoate | -0.199635893 |
| CCCCCC=CCCCCCCCC(=O)OC |  | Methyl octadec-9-enoate | -0.21417886 |
| CC1CCCCC1 |  | Methylcyclopentane | -0.287723631 |
| CC1CCCC1 |  | Methylcyclobutane | -0.34405905 |
| CCCCCCCCCC(=O)OC |  | Methyl decanoate | -0.176970661 |
| CCCCCCCCCCCC(=O)OC |  | Methyl dodecanoate | -0.158401489 |
| CCC(=O)C |  | Butan-2-one | -0.413919002 |
| COC=O |  | Methyl formate | -0.750986814 |
| CC(=O)C=O |  | Methylglyoxal | -0.791433275 |
| CCCCCCCCCCCCCCCCC(=O)OC |  | Methyl heptadecanoate | -0.133745134 |
| CCCCCCC(=O)OC |  | Methyl heptanoate | -0.227633595 |
| CCCCCCCCCCCCCCCC(=O)OC |  | Methyl hexadecanoate | -0.137429148 |
| CCCCCC(=O)OC |  | Methyl hexanoate | -0.258786708 |
| CC(C)C(=O)OC |  | Methyl isobutyrate | -0.499814093 |
| CC(C)OC(=O)OC |  | Methyl isopropyl carbonate | -0.037121654 |
| CC(C)C(=O)C |  | 3-Methylbutan-2-one | -0.357834756 |
| CC(C(=O)OC)O |  | Methyl lactate | -0.499820679 |
| CCCCC/C=C\C/C=C\CCCCCCCC(=O)OC |  | Methyl (E,E)-octadeca-9,12-dienoate | -0.292183757 |
| CC/C=C\C/C=C\C/C=C\CCCCCCCC(=O)OC |  | Methyl (E,E,E)-octadeca-9,12,15-trienoate | -0.370462358 |
| CC(=C)C(=O)OC |  | Methyl methacrylate | -0.889036 |
| CCCCCCCCCCCCCC(=O)OC |  | Methyl tetradecanoate | -0.146443427 |
| CCCCOC |  | Butyl methyl ether | -0.373235524 |
| CCCCC(=O)C |  | Hexan-2-one | -0.34639731 |
| CON=O |  | Methyl nitrite | -0.614716649 |
| CCCCCCCCC(=O)OC |  | Methyl nonanoate | -0.189501792 |
| CCCCCCCCCCCCCCCCCC(=O)OC |  | Methyl octadecanoate | -0.130220592 |
| CCCCCCCC(=O)OC |  | Methyl octanoate | -0.204720676 |
| CCCCCCCCCCCCCCC(=O)OC |  | Methyl pentadecanoate | -0.14160955 |
| CCCCC(=O)OC |  | Methyl pentanoate | -0.314315438 |
| CC(C)(C)C(=O)OC |  | Methyl pivalate | -0.378339112 |
| CCC(=O)OC |  | Methyl propanoate | -0.509522855 |
| CC(C)(C)OC |  | Methyl tert-butyl ether | -0.157411873 |
| CCC(C)(C)OC |  | Methyl tert-pentyl ether | -0.02903986 |
| CC(=O)C(C)(C)C |  | 3,3-Dimethylbutan-2-one | -0.292257369 |
| CCC1=CC=CC(=C1)C |  | 1-Ethyl-3-methylbenzene | -0.614930749 |
| CCCCCCCCCCCCC(=O)OC |  | Methyl tridecanoate | -0.151721567 |
| CCCCCCCCCCC(=O)OC |  | Methyl undecanoate | -0.166484356 |
| CN |  | Methanamine | -0.863738775 |
| COC(=O)C1=CC=C(C=C1)O |  | Methyl 4-hydroxybenzoate | -0.842036724 |
| CC(=O)C=C |  | But-3-en-2-one | -0.754220843 |
| CC1=CC(=CC=C1)[N+](=O)[O-] |  | 2-Methyl-1-nitrobenzene | -0.737263024 |
| CCSC(=O)N1CCCCCC1 |  | N-Cyclohexyl-2-(methylthio)acetamide | -0.305793375 |
| C1=CC=C(C=C1)Cl |  | Chlorobenzene | -2.096223593 |
| C1COCCN1 |  | Morpholine | 0.0293035507202148 |
| CC1=CC(=CC=C1)C=O |  | 2-Methylbenzaldehyde | -0.759267926 |
| CC1=CC(=CC=C1)C |  | 1,2,4-Trimethylbenzene | -0.703796327 |
| C1=CC=C2C=CC=CC2=C1 |  | Naphthalene | -0.726392508 |
| CCCC |  | Butane | -0.369803905 |
| CCCCOCC(C)O |  | 2-(Butoxy)propan-1-ol | -0.070551574 |
| CCCCOC(=O)C |  | Butyl acetate | -0.311685175 |
| CCCCOC(=O)C=C |  | Butyl acrylate | -0.336733758 |
| CCCCO |  | Butan-1-ol | -0.219771236 |
| CCCCC1=CC=CC=C1 |  | Pentylbenzene | -0.391803443 |
| CCCCBr |  | 1-Bromobutane | -0.32912758 |
| CCCCOC(=O)CCC |  | Butyl butanoate | -0.119685471 |
| CCCCOC=O |  | Butyl formate | -0.291153044 |
| CCCCCCCCCC |  | Decane | -0.208785832 |
| CCCCCCCCCCCC |  | Dodecane | -0.187926024 |
| CC(C)(C)C |  | 2,2-Dimethylpropane | -0.323448062 |
| CCCCCCC |  | Heptane | -0.258877903 |
| CCCCCCCOC(=O)C |  | Heptyl acetate | -0.210347414 |
| CCCCCC |  | Hexane | -0.286166608 |
| CCCCCCOC(=O)C |  | Hexyl acetate | -0.230785966 |
| [N]=O |  | Nitric oxide | -0.255979121 |
| C1=CC=C(C=C1)[N+](=O)[O-] |  | Nitrobenzene | -2.344286442 |
| CC[N+](=O)[O-] |  | Nitroethane | -0.191927731 |
| N(=O)[O] |  | Nitrous acid | -0.578234196 |
| C[N+](=O)[O-] |  | Nitromethane | -0.427110195 |
| N(=O)O |  | Nitrous acid | -0.578234196 |
| CN1CCCC1=O |  | 1-Methyl-2-pyrrolidinone | -0.306983531 |
| CCCCCCCCC |  | Nonane | -0.222243786 |
| CCCCCCCCCOC(=O)C |  | Nonyl acetate | -0.181860149 |
| CCCCCCCC |  | Octane | -0.238081604 |
| CCCCCCCCOC(=O)C |  | Octyl acetate | -0.194795221 |
| CCCCCCCCCC1CCCCC1 |  | Decylcyclopentane | -0.150832891 |
| CCCCCCCCCCCCCCC |  | Pentadecane | -0.167084098 |
| CCCCC |  | Pentane | -0.32441175 |
| CCCCCC1=CC=CC=C1 |  | Hexylbenzene | -0.363864958 |
| CCCCCOC(=O)CC |  | Butyl butanoate | -0.119685471 |
| CCCOCCCO |  | 2-Propoxyethan-1-ol | -0.132312238 |
| CCCO |  | Propan-1-ol | -0.28164506 |
| CCCC1=CC=CC=C1 |  | Butylbenzene | -0.428663343 |
| CCCBr |  | 1-Bromopropane | -0.427113533 |
| CCCC(=O)OCCC |  | Propyl butanoate | -0.136452407 |
| CCCOC=O |  | Propyl formate | -0.412853003 |
| CCCOC(=O)CC |  | Propyl propanoate | -0.117640644 |
| CCCCCCCCCCCCCC |  | Tetradecane | -0.173175097 |
| CCCCCCCCCCCCC |  | Tridecane | -0.180051774 |
| CCCCCCCCCCC |  | Undecane | -0.197005421 |
| CC1=CC=CC=C1O |  | 2-Methylphenol | -0.787197649 |
| CCCCCCCC=O |  | Octanal | -0.235939801 |
| CCCCCCCCC1CCCCC1 |  | Nonylcyclopentane | -0.156230628 |
| CC1=CC=CC=C1C(C)C |  | 1,2-Diisopropylbenzene | -0.505405903 |
| C1=CC=C(C(=C1)Cl)Cl |  | 1,2-Dichlorobenzene | -1.788744926 |
| CCC1=CC=CC=C1CC |  | 1,3-Dipropylbenzene | -0.406214088 |
| CCC1=CC=CC=C1C |  | 1-Ethyl-3-methylbenzene | -0.614930749 |
| CC1=CC=CC=C1C(C)(C)C |  | 1-Methyl-2-tert-butylbenzene | -0.519400775 |
| CC1=CC=CC=C1C=O |  | 2-Methylbenzaldehyde | -0.759267926 |
| CC(=O)OCCCCCCC=O |  | Heptyl acetate | -0.210347414 |
| CC1=CC=CC=C1C |  | 1,2,4-Trimethylbenzene | -0.703796327 |
| CC1=CC=C(C=C1)O |  | 2-Methylphenol | -0.787197649 |
| CCC1=CC=C(C=C1)CC |  | 1,4-Dipropylbenzene | -0.367245436 |
| CCCCN(CC)C(=O)SCCC |  | N,N-Dipropyl-2-sulfanylacetamide | -0.222821206 |
| C(C(CO)(CO)CO)O |  | 2,2-Bis(hydroxymethyl)propane-1,3-diol | 0.143504798412323 |
| CCCCC=O |  | Pentanal | -0.340704441 |
| CCCCCO |  | Pentan-1-ol | -0.182238966 |
| CCCCCC1CCCCC1 |  | Hexylcyclopentane | -0.180324584 |
| C(=C(Cl)Cl)(Cl)Cl |  | Tetrachloroethene | -0.75267446 |
| CC(=O)OO |  | Peroxyacetic acid | -0.554015517 |
| CCC1=CC=C(C=C1)C |  | 1-Ethyl-4-methylbenzene | -0.585923016 |
| C1=CC=C(C=C1)O |  | Phenol | -2.517084122 |
| C1=CC=C2C(=C1)C(=O)OC2=O |  | Phthalic anhydride | -0.844164371 |
| CC1=CC=C(C=C1)CC(C)C |  | 1-Isopropyl-4-methylbenzene | -0.51613009 |
| CCC |  | Propane | -0.450295627 |
| CC=C |  | Propene | -0.647283971 |
| CCC=O |  | Propanal | -0.49455598 |
| CCC(=O)O |  | Propanoic acid | -0.485144556 |
| CCCOC(=O)C |  | Propyl acetate | -0.413076282 |
| CCCC1CCCCC1 |  | Butylcyclopentane | -0.204053968 |
| CCCC1CCCC1 |  | Butylcyclobutane | -0.254267752 |
| CC1COC(=O)O1 |  | 4-Methyl-1,3-dioxolan-2-one | -0.216581911 |
| CC(CO)O |  | 2-Methylpropane-1,2-diol | -0.038781345 |
| CC1CO1 |  | 2-Methyloxirane | -0.681119561 |
| CCCOC(=O)C1=CC=C(C=C1)O |  | Propyl 4-hydroxybenzoate | -0.406994045 |
| CC1=CC=C(C=C1)N=C=O |  | 2-Isocyanatotoluene | -0.867697716 |
| C1=CC(=CC=C1C(F)(F)F)Cl |  | 1-Chloro-4-(trifluoromethyl)benzene | -1.192385674 |
| CC1=CC=C(C=C1)C |  | 1,2,4-Trimethylbenzene | -0.703796327 |
| CC(C)C12CCC(=C)C1C2 |  | 2,2,3-Trimethylbicyclo[2.2.1]hept-5-ene | -0.326045871 |
| CCC(C)OC(=O)C |  | Isopropyl propanoate | -0.030364692 |
| CCC(C)O |  | Butan-2-ol | -0.05538553 |
| CCC(C)C1=CC=CC=C1 |  | Isopropylbenzene | -0.474232316 |
| CCC(C)C1CCCCC1 |  | Isopropylcyclopentane | -0.196224928 |
| C/C=C/C1=CC=CC=C1 |  | (E)-1-Phenylprop-1-ene | -0.724685371 |
| C1=CC=C(C=C1)CCO |  | 2-Phenylethan-1-ol | -0.557695568 |
| C=CC1=CC=CC=C1 |  | phenylethene | -3.361465693 |
| CC1(CCC(CC1)C(C)(C)O)O |  | 2,2,6-Trimethylcyclohexane-1,3-diol | 0.0296384692192078 |
| CC1=CCC(=C(C)C)CC1 |  | 1,5,5-Trimethylcyclohex-1-ene | -0.362371325 |
| CC(=O)OC(C)(C)C |  | tert-Butyl acetate | -0.238334984 |
| CC(C)(C)O |  | 2-Methylpropan-2-ol | -0.230205178 |
| CC(C)(C)N |  | 2-Methylpropan-2-amine | -0.292283386 |
| CC(C)(C)C1=CC=CC=C1 |  | tert-Butylbenzene | -0.385310769 |
| C(COCCOCCOCCO)O |  | 2-[2-[2-(2-(hydroxymethoxy)ethoxy)ethoxy]ethoxy]ethanol | 0.0376351475715637 |
| C1CC(OC1)CO |  | 2-(Oxolan-2-yl)ethan-1-ol | -0.026587903 |
| C1CCOC1 |  | 1,3-epoxypropane | -0.479413509 |
| C1CCOCC1 |  | 1,4-Dioxane | 0.0490451455116272 |
| C1CCC2=CC=CC=C2C1 |  | 1,2,3,4-Tetrahydronaphthalene | -0.404451668 |
| CCN(CC)C(=O)SCC1=CC=C(C=C1)Cl |  | N,N-Diethyl-2-((4-chlorophenyl)thio)acetamide | -0.46235913 |
| CC1=CC=C(C=C1)C=O |  | 2-Methylbenzaldehyde | -0.759267926 |
| CC1=CC=CC=C1 |  | ethylbenzene | -0.569696605 |
| C/C=C/C=C/C |  | (E)-Hepta-2,4-diene | -0.615400195 |
| C(=C/C(F)(F)F)\C(F)(F)F |  | (E)-1,2-Bis(trifluoromethyl)ethene | -1.320534468 |
| C(=C/Cl)\Cl |  | (E)-1,2-Dichloroethene | -1.189472198 |
| C(=C/F)\C(F)(F)F |  | (E)-1-Fluoro-2-(trifluoromethyl)ethene | -1.065357208 |
| C(/C=C/Cl)Cl |  | (Z)-1,2-Dichloroethene | -1.349922895 |
| CC/C=C/C=C |  | (E)-Hepta-2,4-diene | -0.615541339 |
| C/C=C/C=C |  | (E)-Hexa-2,4-diene | -0.707751215 |
| C/C=C/CC=C |  | (E)-Hepta-1,4-diene | -0.620539367 |
| CCCCCCCC1CCC(CC1)C |  | 2-Pentyl-1-propylcyclopentane | -0.170680344 |
| CC/C=C/C(C)(C)C |  | (E)-4,4-Dimethylpent-2-ene | -0.431991518 |
| CC(C)/C=C/C(C)C |  | (E)-4,5-Dimethylhex-2-ene | -0.366769969 |
| C/C=C/C |  | (E)-Pent-2-ene | -0.62393558 |
| CCCC/C=C/C |  | (E)-Hept-3-ene | -0.451884538 |
| CCC/C=C/C |  | (E)-Hex-3-ene | -0.507039547 |
| CCCCC/C=C/C |  | (E)-Oct-3-ene | -0.410147697 |
| CC/C=C/C |  | (E)-Pent-2-ene | -0.62393558 |
| CCC/C=C/CC |  | (E)-Oct-4-ene | -0.404864579 |
| CC/C=C/CC |  | (E)-Hept-3-ene | -0.451884538 |
| CCC/C(=C/C)/C |  | (E)-4-Methylhex-3-ene | -0.372392118 |
| CC/C(=C/C)/C |  | (E)-4-Methylpent-3-ene | -0.526781857 |
| CCCC/C=C/CC |  | (E)-Non-4-ene | -0.368868411 |
| C/C=C/C(C)(C)C |  | (E)-4,4-Dimethylpent-2-ene | -0.431991518 |
| CCCCC/C=C/CCC |  | (E)-Dec-4-ene | -0.345410049 |
| CCC(C)/C=C/C |  | (E)-4-Methylhex-3-ene | -0.372392118 |
| C/C=C/C(C)C |  | (E)-4-Methylpent-2-ene | -0.517485261 |
| CCCC/C=C/CCC |  | (E)-Non-4-ene | -0.368880749 |
| CCC/C=C/CCC |  | (E)-Oct-4-ene | -0.404881835 |
| CCCCCC/C=C/CCCC |  | (E)-Dodec-5-ene | -0.298683673 |
| CCCCCCCCC/C=C/CCCC |  | (E)-Hexadec-8-ene | -0.246769816 |
| CCCCCCCC/C=C/CCCC |  | (E)-Pentadec-7-ene | -0.256806701 |
| CCCCCCC/C=C/CCCC |  | (E)-Tetradec-6-ene | -0.268398046 |
| CCCCC/C=C/CCCC |  | (E)-Tridec-5-ene | -0.28249827 |
| C(=C(Cl)Cl)Cl |  | Trichloroethene | -0.914442599 |
| C(CO)N(CCO)CCO |  | N,N-Bis(2-hydroxyethyl)-2-aminoethanol | 0.199940323829651 |
| CCN(CC)CC |  | triethylamine | -0.007382095 |
| CCOC(=O)CC(CC(=O)OCC)(C(=O)OCC)O |  | Triethyl 2-hydroxy-2-methylpropane-1,3-dicarboxylate | 0.233026683330536 |
| C1CN2CCN1CC2 |  | 1,4-Diazabicyclo[2.2.2]octane | 0.0896045565605164 |
| C(COCCOCCO)O |  | Triethylene glycol | -0.003726661 |
| CCCCCCCCCC(=O)OCCOCCOCCOC(=O)CCCCCCCCC |  | 2-(2-(2-nonanoyloxyethoxy)ethoxy)ethyl decanoate | 0.0273742079734802 |
| CCCCCCCC(=O)OCCOCCOCCOC(=O)CCCCCCC |  | 2,2'-[oxybis(ethane-1,2-diyloxy)]bis(ethyl octanoate) | 0.0195828080177307 |
| CCCCCCCC(=O)OCCOCCOCCO |  | Triethylene glycol octyl ether | 0.0151422023773193 |
| CC(CN(CC(C)O)CC(C)O)O |  | tris(2-hydroxypropyl)amine | 0.123435914516449 |
| CN(C)C |  | trimethylamine | -0.428957999 |
| CC1CC(CC(C1)(C)C)O |  | 2,2,6-Trimethylcyclohexan-1-ol | -0.0664621 |
| C1COC1 |  | oxirane | -0.998766422 |
| CC(C)CC(C)CC(CC(C)C)O |  | 2,6,8-Trimethylnonan-4-ol | -0.352168232 |
| CC(CO)OCC(C)OCC(C)OC |  | 2-(2-Isopropoxy-1-methylethoxy)-2-methylpropan-1-ol | -0.331714451 |
| CC(=O)OC=C |  | Vinyl acetate | -0.954453111 |
| C=CCl |  | Chloroethene | -1.460444689 |

Table S14. Atom-level attention weights extracted from the transferable AdsDT model for 816 VOC molecules adsorbed on the TiO2_Anatase (101) surface.

| Atom | Attetion value |
| --- | --- |
| C1 | 0.407 |
| C2 | -0.188 |
| O1 | 0.112 |
| O2 | -0.157 |
| N1 | -0.032 |
| N2 | -0.219 |
| F | -0.094 |
| Cl | -0.078 |
| Br | -0.045 |
| S | -0.052 |

Table S15. In situ DRIFTS peak assignments for ethyl acetate on TiO2

| Wavenumber（cm-1） | Ascription | Characteristic |
| --- | --- | --- |
| 990 1052 1246 1748 | C-H C-O C-O-C C=O | Ethyl acetate |
| 1302 1538 and 1573 | C-O -COO- | Acetate species |
| 1091 1380 | C-O O-H | Ethoxide species |
| 1780 | C=O | aldehyde |
| 2358 and 2336 |  | CO2 |

Table S16. Structural details of eight metal oxide surfaces. All slabs: 15 Å vacuum, bottom layers fixed.

| Metal Oxides | Crystal plane | Coordination number of surface metal sites |
| --- | --- | --- |
| TiO2 | 101 | 5 |
| MnO2 | 110 | 4 |
| Fe2O3 | 110 | 4/5 |
| Co3O4 | 100 | 4/6 |
| CuO | 111 | 3/4 |
| ZnO | 100 | 4 |
| γ-Al2O3 | 110 | 4/5 |
| CeO2 | 111 | 6 |

Table S17. Complete performance metrics of the GCN model on training and test sets for eight metal oxide surfaces.

| Metal oxide surfaces | Train R2 | Test R2 | MAE (eV) | RMSE (eV) |
| --- | --- | --- | --- | --- |
| TiO2(101) | 0.966 | 0.927 | 0.035 | 0.047 |
| MnO2(110) | 0.942 | 0.867 | 0.039 | 0.053 |
| Fe2O3(110) | 0.983 | 0.924 | 0.054 | 0.071 |
| Co3O4(100) | 0.92 | 0.912 | 0.043 | 0.058 |
| CuO(111) | 0.941 | 0.95 | 0.027 | 0.036 |
| ZnO(100) | 0.94 | 0.887 | 0.034 | 0.045 |
| γ-Al2O3(110) | 0.963 | 0.918 | 0.036 | 0.047 |
| CeO2(111) | 0.925 | 0.924 | 0.035 | 0.047 |

Table S18. Average atomic attention weights of different atomic environments for VOC molecules on eight metal oxides surfaces.

| Metal oxide surfaces | C1 | C2 | N1 | N2 | O1 | O2 | F | Cl | S |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| TiO2(101) | 0.407 | -0.188 | 0.112 | -0.157 | -0.032 | -0.219 | -0.094 | -0.078 | -0.052 |
| MnO2(110) | 0.374 | -0.202 | 0.125 | -0.128 | -0.071 | -0.298 | -0.022 | -0.138 | -0.087 |
| Fe2O3(110) | 0.391 | -0.163 | 0.101 | -0.085 | -0.034 | -0.197 | -0.117 | -0.069 | -0.029 |
| Co3O4(100) | 0.360 | -0.148 | 0.108 | -0.103 | -0.062 | -0.198 | -0.067 | -0.051 | -0.034 |
| CuO(111) | 0.365 | -0.138 | 0.079 | -0.117 | -0.079 | -0.205 | -0.063 | -0.092 | -0.068 |
| ZnO(100) | 0.416 | -0.198 | 0.134 | -0.058 | -0.099 | -0.234 | -0.061 | -0.031 | -0.034 |
| Al2O3(110) | 0.376 | -0.178 | 0.076 | -0.120 | -0.041 | -0.203 | -0.130 | -0.079 | -0.058 |
| CeO2(111) | 0.442 | -0.135 | 0.153 | -0.106 | -0.035 | -0.187 | -0.039 | -0.053 | -0.018 |

C1, N1 and O1 denote atoms participating predominantly in single bonds, whereas C2, N2 and O2 represent atoms involved in double bonds. The values correspond to the average atomic attention weights calculated from the GCN model.

Table S19. Calculated bond activation scores for all chemical bonds in ethanol on TiO2(anatase, 101) surface.

| Bond | wi | wj | ¦χi-χj¦ | BDEij | Aij | Eij | Pij | Sbond, ij |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| C1-C2 | 0.17349 | 0.10494 | 0 | 347 | 4.06 | 0.526 | 1.00 | 0.42 |
| C1-O1 | 0.10494 | 0.09124 | -0.89 | 358 | 3.21 | 0.518 | 2.06 | 0.56 |
| C1-H2 | 0.10494 | 0 | 0.35 | 414 | 1.00 | 0.482 | 1.42 | 0.76 |
| O1-H1 | 0.09124 | 0 | 1.24 | 464 | 1.00 | 0.453 | 2.48 | 0.69 |

Reference

1. Mamun, O. et al. High-throughput calculations of catalytic properties of bimetallic alloy surfaces. Sci. Data 6, 76 (2019).

2. Pablo-García, S. et al. Fast evaluation of the adsorption energy of organic molecules on metals via graph neural networks. Nat. Comput. Sci. 3, 433-442 (2023).

3. Lan, J. et al. AdsorbML: a leap in efficiency for adsorption energy calculations using generalizable machine learning potentials. npj Comput. Mater. 9, 172 (2023).

4. Chanussot, L. et al. Open Catalyst 2020 (OC20) dataset and community challenges. ACS Catal. 11, 6059-6072 (2021).

5. McInnes, L. et al. UMAP: uniform manifold approximation and projection for dimension reduction. Preprint at arXiv:1802.03426 (2018).

6. McInnes, L. et al. UMAP: uniform manifold approximation and projection. J. Open Source Softw. 3, 861 (2018).

7. Bartók, A. P. et al. On representing chemical environments. Phys. Rev. B 87, 184115 (2013).

8. De, S. et al. Comparing molecules and solids across structural and alchemical space. Phys. Chem. Chem. Phys. 18, 13754-13769 (2016).

9. Landrum, G. et al. RDKit: a software suite for cheminformatics, computational chemistry, and predictive modeling. Release version release-2022.09.5 (2022).

10. Himanen, L. et al. DScribe: library of descriptors for machine learning in materials science. Comput. Phys. Commun. 247, 106949 (2020).

11. Laakso, J. et al. Updates to the dscribe library: new descriptors and derivatives. J. Chem. Phys. 158, 23 (2023).

12. Luo, Y. et al. Calibrated geometric deep learning improves kinase-drug binding predictions. Nat. Mach. Intell. 5, 1390-1401 (2023).

13. Ashukha, A. et al. Pitfalls of in-domain uncertainty estimation and ensembling in deep learning. In 8th International Conference on Learning Representations (2020).

14. Kuleshov, V. et al. Accurate uncertainties for deep learning using calibrated regression. In Proceedings of the 35th International Conference on Machine Learning Vol. 80, 2801-2809 (PMLR, 2018).

15. Scalia, G. et al. Evaluating scalable uncertainty estimation methods for deep learning-based molecular property prediction. J. Chem. Inf. Model. 60, 2697-2717 (2020).

16. Tran, K. et al. Methods for comparing uncertainty quantifications for material property predictions. Mach. Learn.: Sci. Technol. 1, 025006 (2020).

17. Chung, Y. et al. Uncertainty Toolbox: an open-source library for assessing, visualizing, and improving uncertainty quantification. Preprint at arXiv:2109.10254 (2021).

18. Levi, D. et al. Evaluating and calibrating uncertainty prediction in regression tasks. Sensors 22, 5540 (2022).

19. Brent, R. P. An algorithm with guaranteed convergence for finding a zero of a function. Comput. J. 14, 422-425 (1971).

20. Gasteiger, J. et al. GemNet-OC: developing graph neural networks for large and diverse molecular simulation datasets. Preprint at arXiv:2204.02782 (2022).