Supporting Information

Tannic acid/poly(vinyl alcohol)-modified chitosan/bacterial cellulose composite membranes with enhanced surface hydrophilicity and wet-state stability for anti-adhesion applications

Ying Liu1 · Yuhan Liu2 · Kaidi Ding3 · Jing Zeng2 · Jingbo Chen1 · Jiang Liu4 · Xuejia Ding2

1 School of Materials Science & Engineering, Zhengzhou University, Zhengzhou, China.

2 Beijing Laboratory of Biomedical Materials, Beijing University of Chemical Technology, Beijing, China.

3 National Institutes for Drug Control, Beijing, China.

4 Department of Neurosurgery, China-Japan Friendship Hospital, Beijing, China.

Correspondence:

Jiang Liu: liujiang889@126.com

Xuejia Ding: dingxj@mail.buct.edu.cn

Content:

- Supplementary methods

- Fig. S1

- Fig. S2

- Fig. S3

Supplementary methods

X-ray diffraction measurement

The crystalline structures of CS and CS/BC composite membranes were characterized by X-ray diffraction (XRD). Membrane specimens were cut into 15 mm × 15 mm pieces. XRD patterns were recorded using an X-ray diffractometer (D8 ADVANCE, Bruker AXS GmbH, Germany) with Cu Kα radiation over a 2θ range of 5–50° at a scanning rate of 4° min⁻¹.

Water absorption measurement

Membrane specimens were cut into 20 mm × 20 mm pieces and dried before weighing to obtain the initial dry mass (M0). The specimens were immersed in deionized water at room temperature for 24 h. After immersion, excess surface water was gently removed using filter paper and the swollen samples were immediately weighed (M1). At least three independent specimens were tested for each group. The water absorption was calculated as:

Water absorption (%)=M1-M0M0×100%

Fig. S1 Structural characterization of CS, BC, and CS/BC composite membranes with different BC contents: (a) FTIR spectra and (b) XRD patterns

Fig. S2 Surface and cross-sectional SEM images of CS and CS/BC composite membranes with different BC contents. (a–h) Surface morphologies (Scale bar = 5 μm) and (i–p) corresponding cross-sectional morphologies (Scale bar = 25 μm) of CS, CB3, CB5, CB7, CB10, CB15, CB20, and CB25, respectively

Fig. S3 Wet-state mechanical and water-uptake properties of CS and CS/BC composite membranes with different BC contents: (a) tensile strength; (b) elongation at break; (c) swelling ratio; and (d) water absorption