Supporting information for

Termination controlled Phase-Pure Ti3C2Tx MXenes Towards Efficient Electrocatalysis Gyanprakash Mishra,1,2,3 Saswati Mishra,1,2 Brijesh K. Patel,4 Satyabrata Sahoo,1,3 Ashutosh Rath,*2,3 Simantini Nayak*1,2

1Department of Materials Chemistry and Interfacial Engineering, CSIR-Institute of Minerals and Materials Technology, Bhubaneswar 751013, India

2Department of Mineralogy and Materials Characterisation, CSIR-Institute of Minerals and Materials Technology, Bhubaneswar 751013, India

3Academy of Scientific and Innovative Research (AcSIR), Gaziabad 201002, India

4Tata Institute of Fundamental Research, 36/P, Gopanpally Village, Hyderabad 500046, India

*Corresponding authors

Email: ashutosh.immt@csir.res.in

Email: simantini.immt@csir.res.in

Contents:

| Experimental Section |  |
| --- | --- |
| Supplementary Figures |  |
| XRD patterns of Ti3AlC2 MAX phase |  |
| - Supplementary Fig. 1. | Sintered at different temperatures (1200, 1250, 1300 and 1350 °C) for 4 h |
| - Supplementary Fig. 2. | Sintered using different precursor ratios at 1300 °C for 4 h |
| - Supplementary Fig. 3. | Sintered at 1300 °C for different times: 2 h and 4 h |
| XRD patterns of Ti3C2-F and Ti3C2-O MXenes |  |
| - Supplementary Fig. 4. | Ti3C2-F MXene formed via in situ HF etching at RT and with heating (55 °C) for 24 h |
| - Supplementary Fig. 5. | Ti3C2-F MXene formed via in situ HF etching at 55 °C for different durations (12, 18, 24 and 30 h) |
| - Supplementary Fig. 6. | Ti3C2-O MXene formed at different molten salt etching durations (6, 12 and 24 h) at 700 °C |
| Surface area, pore size distribution and thermal analysis |  |
| - Supplementary Fig. 7. | N2 adsorption–desorption isotherm with pore size distribution |
| - Supplementary Fig. 8. | Thermogravimetric Differential Scanning Calorimetry (TG-DSC) analysis of Ti3AlC2 MAX phase, Ti3C2-F and Ti3C2-O MXenes |
| XPS analysis |  |
| - Supplementary Fig. 9. | XPS characterisations of Ti3AlC2 MAX phase |
| - Supplementary Fig. 10. | XPS characterisations of Ti3C2-F MXene |
| - Supplementary Fig. 11. | XPS characterisations of Ti3C2-O MXene |
| - Supplementary Fig. 12. | Comparison of XPS survey spectra of Ti3AlC2 MAX phase, Ti3C2-F and Ti3C2-O MXenes |
| Electrochemical analysis |  |
| - Supplementary Fig. 13. | Electrochemically active surface area (ECSA) characterisation of MXenes for universal pH hydrogen evolution reaction (HER) |
| - Supplementary Fig. 14. | ECSA characterisation of MXenes for oxygen evolution reaction (OER) |
| - Supplementary Fig. 15. | Cdl measurements of Ti3C2-F and Ti3C2-O MXenes for HER and OER |
| - Supplementary Fig. 16. | Electrochemical impedance spectroscopy (EIS; Nyquist plots) of Ti3C2-F and Ti3C2-O MXenes in 0.5 M H2SO4 and 1 M KOH |
| - Supplementary Fig. 17. | Faradaic efficiencies of Ti3C2-F MXene in 0.5 M H2SO4 |
| - Supplementary Fig. 18. | Post-electrochemical (FESEM and XPS) analysis of Ti3C2-F MXene after HER stability test |
| - Supplementary Fig. 19. | Post-electrochemical (FESEM and XPS) analysis of Ti3C2-O MXene after HER stability test |
| - Supplementary Fig. 20. | Post-electrochemical (FESEM and XPS) analysis of Ti3C2-O MXene after OER stability test |
| Supplementary Tables |  |
| - Supplementary Table 1. | Assignment of XPS peaks observed for Ti 2p, C 1s, O 1s and Al 2p spectra of Ti3AlC2 MAX phase |
| - Supplementary Table 2. | Assignment of XPS peaks observed for Ti 2p, C 1s, O 1s, Al 2p and F 1s spectra of Ti3C2-F MXene |
| - Supplementary Table 3. | Assignment of XPS peaks observed for Ti 2p, C 1s, O 1s, Al 2p, Cl 2p and S 2p spectra of Ti3C2-O MXene |
| - Supplementary Table 4. | Atomic percentage of elements of Ti3AlC2, Ti3C2-F and Ti3C2-O MXenes derived from XPS spectra |
| - Supplementary Table 5. | Comparison of the synthesis parameters and phase purities of the synthesised Ti3AlC2 MAX phase |
| - Supplementary Table 6. | Comparison of the synthesis parameters and phase purities of the Ti3C2-F and Ti3C2-O MXenes |
| - Supplementary Table 7. | Double-layer capacitance (Cdl) and ECSA values of Ti3C2-F and Ti3C2-O MXenes in 0.5 M H2SO4 and 1 M KOH |
| - Supplementary Table 8. | Comparison of the HER performance of the Ti3C2-F and Ti3C2-O MXenes in universal pH with reported MXene-based electrocatalysts |
| - Supplementary Table 9. | Comparison of the overall water-splitting performance of the Ti3C2-F and Ti3C2-O MXenes in 1 M KOH with reported MXene-based electrocatalysts |
| References |  |

XRD patterns of Ti3AlC2 MAX phase:

- Effect of sintering temperatures:

Supplementary Fig. 1. XRD pattern of Ti3AlC2 MAX phase sintered at 1200 °C, 1250 °C, 1300 °C and 1350 °C for 4 h.

We investigated the effect of sintering temperature on the phase purity of the Ti3AlC2 MAX phase, produced at 1200 °C (MAX1), 1250 °C (MAX2’), 1250 °C (MAX2), 1300 °C (MAX3), and 1350 °C (MAX4) for 1-4 h in air. XRD patterns of Ti3AlC2 MAX phase synthesised at 1200 and 1250 °C show a peak at 2θ ~13° corresponding to Ti2AlC impurities, whereas this peak is absent in the sample formed at 1300 °C.

- Effect of precursor ratios:

Supplementary Fig. 2. XRD pattern of Ti3AlC2 MAX phase sintered using different precursor ratios at 1300 °C for 4 h.

We studied how precursor molar ratios affect Ti3AlC2 MAX phase formation at 1300 °C over 4 h. Using Ti, TiC, and Al at molar ratios of 1.1:2:1.4, 1.2:2:1.8, and 1.25:2:2.2, XRD showed that the 1.1 ratio yielded an 89.22% phase-pure Ti3AlC2 MAX phase, with minimal Ti2AlC and TiC phases. Increasing the Ti and Al ratios increased MAX phase purity to 99.48% with lower Ti2AlC and TiC phases, indicating that higher Al promotes conversion to the Ti3AlC2 MAX phase.

Supplementary Fig. 3. XRD pattern of Ti3AlC2 MAX phase sintered at 1300 °C for 2 h and 4 h.

Effect of sintering time:

We investigated the effect of sintering time on the phase purity of the Ti3AlC2 MAX phase. We sintered the Ti3AlC2 MAX phase at 1300 °C for 4 h and 2 h. Different sintering times for the formation of the Ti3AlC2 MAX phase show that the peak at 2θ=13° for the (002) plane of the Ti2AlC phase was present at 2 hours but absent at 4 hours. Hence, this result indicates that a minimum sintering duration of 4 hours at 1300 °C is required to form a highly phase-pure Ti3AlC2 MAX phase.

XRD patterns of Ti3C2-F and Ti3C2-O MXenes

- Effect of temperature on the formation of Ti3C2-F MXene via in situ HF etching

Supplementary Fig. 4.  XRD pattern of Ti3C2-F MXene formation at different in situ HF etching temperature for 24 h.

To evaluate the effect of temperature during in situ HF etching of the Ti3AlC2 MAX phase to obtain Ti3C2-F MXene, we performed etching at room temperature (RT) and at 55 °C for 24 h.  XRD pattern of the Ti3C2-F MXene formed by RT etching shows a peak at ~9.6° for the (002) plane of Ti3AlC2, whereas this peak was absent in the 55 °C etching, indicating the complete conversion of the MAX phase to the Ti3C2-F MXene.

- Effect of etching duration on the formation of Ti3C2-F MXene via in situ HF etching:

Supplementary Fig. 5. XRD pattern of Ti3C2-F MXene formation at different in situ HF etching times at 55 °C.

We have performed in situ HF etching of the Ti3AlC2 MAX phase at 55 °C for 12, 18, 24, and 30 h. XRD pattern shows that, by varying the etching time to 12, 18, 24, and 30 h at 55 °C, the peak at ~9.6° of the (002) plane for the Ti3AlC2 MAX phase was still present after 12 h and 18 h of etching, while it was absent after 24 h and 30 h of etching. Hence, it shows that for effective and complete etching of the Ti3AlC2 MAX phase, a minimum etching time of 24 hours is required.

Supplementary Fig. 6. XRD pattern of Ti3C2-O MXene formation at different molten salt etching times: 6, 12, and 24 h at 700 °C.

Effect of etching duration on the formation of Ti3C2-O MXene via molten salt etching:

We have investigated the molten salt etching time for the formation of Ti3C2-O MXene at 700 °C for 6 h, 12 h and 24 h. XRD patterns of the Ti3C2-O MXene formed at 700 ⁰C with different etching durations show that the peak at 2θ ~ 39⁰ for the (104) plane of the MAX phase completely vanishes for 6, 12 and 24 h of etching. However, for 6 h and 12 h etching times, the peak at ~9.5° for the (002) plane of MXene was found to be present, while it completely vanished with 24 h etching time and instead a peak at ~25.5° was visible for the (102) plane due to the formation of oxides. Hence, for effective and complete etching of the Ti3AlC2 MAX phase, a molten salt etching time of at least 6 h is required at 700 °C.

a

Surface area, pore size distribution:

Supplementary Fig. 7. N2 adsorption–desorption isotherm with the associated BJH pore size distribution (inset). a, Ti3C2-F MXene. b, Ti3C2-O MXene.

b

We have investigated the surface area and pore size of the Ti3C2-F and Ti3C2-O MXenes. The specific surface area of Ti3C2-F MXene was found to be ~8.18 ± 0.11 m²/g, and the associated Barrett-Joyner-Halenda (BJH) pore size distribution spanned 3-180 nm, with most pore diameters between ~5 and 30 nm and a total pore volume of 0.019 cm3g-1. The specific surface area of Ti3C2-O MXene was found to be ~98.96 ± 0.40 m²/g, and the associated BJH pore size distribution spanned 1.5-221 nm, with most pore diameters between ~2 and 50 nm and a total pore volume of 0.1445 cm3g-1.

Thermal Analysis:

c

b

a

Supplementary Fig. 8. TG-DSC curves of synthesised MAX phase and MXenes. a, Ti3AlC2 MAX phase. b, Ti3C2-F MXene. c, Ti3C2-O MXene.

XPS analysis of Ti3AlC2 MAX phase and Ti3C2Tx MXene:

XPS analysis of the Ti3AlC2 MAX phase and Ti3C2Tx MXene are presented in Supplementary Figs. 9-12. The XPS survey spectra (Supplementary Fig. 12) show that the Ti3AlC2 MAX phase contains Ti 2p, Al 2p, and C 1s signals along with a strong O 1s signal, indicating partial surface oxidation of the MAX phase. The XPS survey spectra of both Ti3C2-F and Ti3C2-O MXenes formed after the etching process show that the Ti 2p peak intensity is enhanced, whereas the Al 2p peak intensity is weaker than in the Ti3AlC2 MAX phase, confirming the removal of Al. Moreover, no significant amounts of Cu were detected in Ti3C2-O MXene. The high-resolution Al 2p survey spectrum of the Ti3AlC2 MAX phase shows Al–Ti (71.49 eV) and Al-C (73.85 eV) bonds, confirming Al is bonded in a Ti-Al-C framework, and the presence of Al2O3(74.7 eV) confirms the formation of the Ti3AlC2 MAX phase with minor impurities (Supplementary Fig. 9e).1 Ti3C2-F MXene contains trace amounts of Al2O3 and AlF3 impurities, indicating efficient Al extraction from the Ti3AlC2 MAX phase (Supplementary Fig. 10e).2 In contrast, the Ti3C2-O MXene has a higher Al2O3 content than Ti3C2-F, suggesting more residual or newly formed oxide species, likely due to differences in etching conditions: molten salt etching promotes oxidation relative to in situ HF etching. The high-resolution C 1s spectrum of the Ti3AlC2 MAX phase shows a dominant C-C+CHx (284.8 eV) along with a Ti-C (281.22 eV) bond, confirming the carbide nature of the MAX phase. Additionally, C-OH (286.86 eV) and COO (288.75 eV) components indicate slight surface oxidation and the presence of surface carbonaceous environments (Supplementary Fig. 9d).1,3,4 After etching, both Ti3C2-F and Ti3C2-O (Supplementary Fig. 10d and 11d) MXenes show a dominant C-C+CHx contribution, indicating that the carbon framework remains structurally stable during MXene formation. The retained Ti–C contribution, together with the presence of C=O components in Ti3C2-F, suggests partial surface oxidation and a stable carbide framework after HF etching. In contrast, the absence of Ti–C bonding, along with pronounced C-O and COO functionalities in Ti3C2-O MXene, indicates extensive oxygen-rich surface functionalization induced by the molten salt etching route, as illustrated in Supplementary Fig. 11b. Supplementary Fig. 10f shows F 1s peaks of Ti3C2-F MXene at 684.56 and 686.37 eV corresponding to C-Ti-F and Al-(OF)ₓ, arising from in situ HF etching using LIF in HCl solution. For Ti3C2-O MXene, the Cl 2p peaks at 198.44 and 200.06 eV (Supplementary Fig. 11f) indicate Ti-Cl bonding from molten-salt etching with a mixture of NaCl and KCl. Additionally, S 2p peaks at 169 eV and 170.28 eV (Supplementary Fig. 11g) correspond to S–O species introduced during ammonium persulfate treatment, while no Cu signal is observed (Supplementary Fig. 11h), confirming complete removal of Cu²⁺.5

XPS analysis of Ti3AlC2 MAX phase:

Supplementary Fig. 9. XPS characterizations of Ti3AlC2 MAX phase. a, survey spectrum b, Ti 2p c, O 1s d, C 1s e, Al 2p.

c

e

b

d

a

|  | B. E. (eV) | Assigned to |
| --- | --- | --- |
| Ti 2p3/2 (2p1/2) | 454.01 (460.05) | Ti-C |
|  | 458.43 (464.18) | TiO2 |
|  | 455.33 | TiO |
| C 1s | 281.22 | Ti-C |
|  | 284.8 | C-C + CHx |
|  | 286.86 | C-OH |
|  | 288.75 | COO |
| O 1s | 529.86 | TiO2 |
|  | 530.93 | OH-TiO2 |
|  | 532.04 | Al2O3 |
| Al 2p | 71.49 | Al-Ti |
|  | 73.85 | Al-C |
|  | 74.70 | Al2O3 |

Supplementary Table 1. Assignment of XPS peaks observed for Ti 2p, C 1s, O 1s and Al 2p spectra of the Ti3AlC2 MAX phase.

XPS analysis of Ti3C2-F MXene:

Supplementary Fig. 10. XPS characterizations of Ti3C2-F MXene. a, XPS survey spectrum. b, Ti 2p c, O 1s d, C 1s e, Al 2p f, F 1s.

f

e

d

a

c

b

|  | B. E. (eV) | Assigned to |
| --- | --- | --- |
| Ti 2p3/2 (2p1/2) | 454.53 (460.51) | Ti-C-TO |
|  | 459.01 (464.89) | TiO2 |
|  | 457.01 | Ti-Cl |
|  | 455.44 (461.81) | Ti-C-TF |
| C 1s | 281.44 | Ti-C |
|  | 284.8 | C-C + CHx |
|  | 287.95 | C=O |
| O 1s | 529.15 | TiO2 |
|  | 530.25 | C-Ti-Ox |
|  | 531.35 | C-Ti-(OH)x |
|  | 533.60 | H2Oads |
| Al 2p | 74.79 | Al2O3 |
|  | 76.08 | AlF3 |
| F 1s | 684.56 | C-Ti-F |
|  | 686.37 | Al-(OF)x |

Supplementary Table 2. Assignment of XPS peaks observed for Ti 2p, C 1s, O 1s, Al 2p and F 1s spectra of Ti3C2- F MXene.

g

h

Supplementary Fig. 11. XPS characterisations of Ti3C2-O MXene. a, survey spectrum. b, Ti 2p c, O 1s d, C 1s e, Al 2p f, Cl 2p g, S 2p h, Cu 2p.

XPS analysis of Ti3C2-O MXene:

f

e

d

c

b

a

|  | B. E. (eV) | Assigned to |
| --- | --- | --- |
| Ti 2p3/2 (2p1/2) | 457.61 (460.1) | Ti-S |
|  | 459.93 (465.53) | Ti-Cl |
|  | 460.01 (465.53) | Ti-O |
| C 1s | 284.8 | C-C+ CHx |
|  | 286.51 | C-O |
|  | 288.87 | COO |
| O 1s | 530.39 | C-Ti-Ox |
|  | 531.65 | Al2O3 |
|  | 532.93 | H2Oads |
| Al 2p | 74.70 | Al2O3 |
|  | 76.02 | AlCl3 |
| Cl 2p3/2 (2p1/2) | 198.44 (200.06) | Cl-Ti |
| S 2p3/2 (2p1/2) | 169 (170.28) | S-O |

Supplementary Table 3. Assignment of XPS peaks observed for Ti 2p, C 1s, O 1s, Al 2p, Cl 2p and S 2p spectra of Ti3C2-O MXene.

Supplementary Fig. 12. XPS Survey spectra of the Ti3AlC2 MAX phase, Ti3C2-F, and Ti3C2-O MXenes.

XPS Survey spectra:

| Sample | Name | Position | FWHM | Area | Atomic % |
| --- | --- | --- | --- | --- | --- |
| Ti3AlC2 | Ti 2p | 457.26 | 7.21 | 303.36 | 21.11 |
|  | C 1s | 283.78 | 2.98 | 224.57 | 15.63 |
|  | Al 2p | 73.28 | 2.74 | 87.95 | 6.12 |
|  | O 1s | 530.57 | 3.61 | 821.30 | 57.15 |
| Ti3C2-F | Ti 2p | 458.07 | 2.47 | 365.69 | 32.78 |
|  | C 1s | 284.00 | 3.14 | 165.89 | 14.87 |
|  | Al 2p | 74.08 | 1.30 | 6.27 | 0.56 |
|  | O 1s | 529.33 | 3.15 | 258.05 | 23.13 |
|  | F 1s | 684.99 | 2.55 | 286.11 | 25.65 |
|  | Cl 2p | 198.07 | 3.78 | 33.65 | 3.02 |
| Ti3C2-O | Ti 2p | 457.79 | 2.25 | 569.35 | 34.28 |
|  | C 1s | 283.82 | 3.16 | 164.11 | 9.88 |
|  | Al 2p | 73.59 | 2.33 | 27.50 | 1.66 |
|  | O 1s | 529.83 | 3.50 | 874.06 | 52.63 |
|  | S 2p | 168.09 | 2.11 | 15.07 | 0.91 |
|  | Cl 2p | 196.79 | 1.73 | 10.67 | 0.64 |

Supplementary Table 4. Atomic percentages of elements in Ti3AlC2, Ti3C2-F, and Ti3C2-O MXenes derived from XPS spectra.

|  | Ti3AlC2 MAX phase |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Sample | Precursor (molar ratio) |  |  | Synthesis parameters |  | Phase (wt %) |  |  |
|  | Ti | TiC | Al | Temp (°C) | Time (h) | Ti2AlC | TiC | Ti3AlC2 |
| MAX1 | 1.25 | 2 | 2.2 | 1200 | 4 | 1.45 | 2.6 | 95.94 |
| MAX2’ | 1.25 | 2 | 2.2 | 1250 | 1 | 3.79 | 1.50 | 94.71 |
| MAX2 | 1.25 | 2 | 2.2 | 1250 | 4 | 0.19 | 0.71 | 99.0 |
| MAX3a | 1.1 | 2 | 1.4 | 1300 | 4 | 1.12 | 9.66 | 89.22 |
| MAX3b | 1.2 | 2 | 1.8 | 1300 | 4 | 3.48 | 6.88 | 89.64 |
| MAX3ć | 1.25 | 2 | 2.2 | 1300 | 2 | 4.77 | 3.41 | 91.82 |
| MAX3 /MAX3c | 1.25 | 2 | 2.2 | 1300 | 4 | 0.04 | 0.50 | 99.48 |
| MAX4 | 1.25 | 2 | 2.2 | 1350 | 4 | 0.34 | 2.68 | 96.98 |

Supplementary Table 5. Comparison of the synthesis parameters and phase purity of the synthesised Ti3AlC2 MAX phase.

Comparison of the synthesis parameters and phase purity of MAX phase and MXenes:

| Ti3C2Tx MXene | Etching parameters |  |  | Phase (wt %) |
| --- | --- | --- | --- | --- |
|  | Etchants | Temp (°C) | Time (h) |  |
| Ti3C2-F | LiF+ HCl | RT | 24 | 30.70 |
|  |  | 55 | 12 | 96.40 |
|  |  | 55 | 18 | 99.36 |
|  |  | 55 | 24 | 99.71 |
|  |  | 55 | 30 | 97.89 |
| Ti3C2-O | CuCl2 | 700 | 6 | 97.81 |
|  |  | 700 | 12 | 99.66 |
|  |  | 700 | 24 | -- |

Supplementary Table 6. Comparison of the synthesis parameters and phase purity of the Ti3C2-F and Ti3C2-O MXenes.

After sintering at 1200 °C for 4 h, the wt% of Ti3AlC2 was 95.94%, Ti2AlC was 1.45%, and TiC was 2.6%. Increasing temperature to 1250 °C for 1 h decreased Ti3AlC2 to 94.71%, increased Ti2AlC to 3.79%, and lowered TiC to 1.5%. Longer sintering at 1250 °C for 4 h improved Ti3AlC2 to 99.0%, with Ti2AlC at 0.19% and TiC at 0.71%. At 1300 °C, Ti3AlC2 increased to 99.48%, while Ti2AlC and TiC decreased. At 1350 °C, the Ti3AlC2 content dropped to 96.98%, while the Ti2AlC and TiC contents increased. For high-purity Ti3AlC2, 1300 °C for 4 h is optimal; temperatures above 1300 °C cause conversion to Ti2AlC and TiC. Varying precursor ratios, a molar ratio of 1.25:2:2.2 (MAX3c) yielded 99.48% Ti3AlC2, while lower ratios resulted in less pure phases. Reducing sintering time to 2 h lowered Ti3AlC2 to 91.82%, increasing Ti2AlC and TiC.

a

b

c

d

Supplementary Fig. 13. Electrochemically active surface area characterization for universal pH HER. CV curves of Ti3C2-F and Ti3C2-O MXenes during HER: a, b in 0.5 M H2SO4; c, d in 1 M KOH, from which double-layer capacitance (Cdl) values are derived from the linear slope, which is equivalent to twice of Cdl.

Electrochemical analysis:

f

a

b

Supplementary Fig. 14. Electrochemically active surface area characterization for OER. a, b, CV curves of Ti3C2-F and Ti3C2-O MXenes during OER in 1 M KOH, from which Cdl values are derived from the linear slope, which is equivalent to twice Cdl.

a

b

Supplementary Fig. 15. Cdl measurements of Ti3C2-F and Ti3C2-O MXenes. a, for HER in 0.5 M H2SO4 and 1 M KOH.  b, for OER in 1 M KOH.

| Media | Sample | HER |  |  | OER |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | Cdl (mF cm-2) | ECSA (cm2) | RF | Cdl (mF cm-2) | ECSA (cm2) | RF |
| 0.5 M H2SO4 | Ti3C2-F | 19.71 | 563.14 | 2252.56 |  |  |  |
|  | Ti3C2-O | 4.87 | 121.79 | 487.16 |  |  |  |
| 1 M KOH | Ti3C2-F | 2.68 | 67 | 268 | 2.29 | 57.25 | 114.5 |
|  | Ti3C2-O | 3.03 | 75.75 | 300 | 3.84 | 96 | 192 |

Supplementary Table 7.  Cdl and ECSA values of Ti3C2-F and Ti3C2-O MXenes in 0.5 M H2SO4 and 1 M KOH.

Supplementary Fig. 16.  Electrochemical impedance spectroscopy (EIS; Nyquist plots) with fitting data of Ti3C2-F and Ti3C2-O MXenes in 0.5 M H2SO4 and 1 M KOH electrolytes.

The impedance spectra were fitted to equivalent circuit models that included solution resistance (Rs), charge-transfer resistance (Rct), and a constant phase element (CPE) to describe the non-ideal interfacial capacitance. The Nyquist spectra of both catalysts show a semicircle in the high-frequency region and an inclined line at lower frequencies, indicating the coexistence of charge transfer and diffusion-controlled processes. In 0.5 M H2SO4, Ti3C2-F shows a lower Rs of 0.76 Ω and an Rct of 20.12 Ω compared to Ti3C2-O (Rs = 0.86 Ω, Rct = 39.5 Ω). In contrast, in 1 M KOH, Ti3C2-O exhibits lower Rs (2.06 Ω) and Rct (61.8 Ω) values than Ti3C2-F (Rs = 1.33 Ω, Rct = 308.5 Ω).

Supplementary Fig. 17. Faradaic efficiencies of Ti3C2-F MXene at acidic pH at different time intervals.

Supplementary Fig. 18. Post-electrochemical analysis of Ti3C2-F MXene during the HER stability test (39.05 h, E = -0.34 V vs RHE) in 0.5 M H2SO4: a) morphological analysis i) before and ii) after the HER stability test. b) XPS spectra of i) Ti 2p and ii) C 1s before and after the stability test.

a

b

i

ii

ii

i

Post-electrochemical stability analysis:

b

i

ii

a

i

ii

Supplementary Fig. 19. Post-electrochemical analysis of Ti3C2-O MXene during the HER stability test (19.2 h, E = -0.36 V vs RHE) in 1 M KOH: a) morphological analysis i) before and ii) after the HER stability test. b) XPS spectra of i) Ti 2p and ii) C 1s before and after the HER stability test.

Supplementary Fig. 20. Post-electrochemical analysis of Ti3C2-O MXene during the OER stability test (17.8 h, E = +1.87 V vs RHE) in 1 M KOH: a) morphological analysis i) before and ii) after the OER stability test. b) XPS spectra of i) Ti 2p and ii) C 1s before and after the OER stability test.

b

ii

a

i

i

ii

Post-electrochemical XPS analysis reveals that both Ti₃C₂-F and Ti₃C₂-O exhibit notable changes in their surface chemical states after electrolysis, consistent with morphological alterations observed in FESEM images. The preserved layered structure, combined with increased surface roughness and partial agglomeration, suggests surface modification of the MXene during electrochemical stability. For Ti₃C₂-F, the Ti 2p spectrum is primarily characterised by Ti–O/TiO₂ after HER, with the Ti–C signal in the C 1s spectrum disappearing. This points to substantial surface oxidation and modification during acidic HER. Similarly, after HER and OER, Ti₃C₂-O's Ti 2p spectra are dominated by broad Ti–O or TiO₂ peaks, with another Ti feature no longer clearly visible. In the C 1s spectra, the C=O peak intensity decreased, and the C–O peak vanished after electrolysis. These findings indicate that both cathodic and anodic alkaline operations induced significant surface oxidation.

| Materials | Catalyst mass loading (mg cm-2) | 0.5 M H2SO4 |  |  | 1 M KOH |  |  | Ref. |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | ⴄ10 (mV) | Tafel slope (mV dec-1) | Stability | ⴄ10 (mV) | Tafel slope (mV dec-1) | Stability |  |
| Ti3C2Tx MXene |  |  |  |  |  |  |  |  |
| Ti3C2Tx | 1 | 70 | 150 |  |  |  |  | 6 |
| Ti3C2Ox | 0.19 | 190 | 60.7 | 2000 cycles |  |  |  | 7 |
| TiVCTx | 0.025 | 151 | 116 | 12 h |  |  |  | 8 |
| Ti3C2 | 2 |  |  |  | 188 | 110 | 2000 cycles | 3 |
| Ti2CTx | 0.1 |  |  |  | 570 | 157 | 1000 cycles | 9 |
| Doped/ Heterostructured Ti3C2Tx MXene |  |  |  |  |  |  |  |  |
| Re@Ti3C2Tx | 0.708 | 298 | 110 | 30 h |  |  |  | 10 |
| Ti3C2Tx |  | 584 | 186.8 |  |  |  |  |  |
| Ru-NS-Ti3C2Tx |  | 76 | 90 | 16 h |  |  |  | 11 |
| Ti3C2Tx |  | 673 | 271 |  |  |  |  |  |
| RuSA@Ti3C2Tx | 1 |  |  |  | 40.3 | 90 | 24 h, 5000 cycles | 12 |
| Ti3C2Tx |  |  |  |  | 516 | 660 |  |  |
| Ti3C2-F | 0.625 | 87 | 55 | 39.05 h, 9000 cycles | 143 | 103 |  | This work |
| Ti3C2-O |  | 105 | 76 |  | 76 | 86 | 19.2 h, 2100 cycles |  |

Supplementary Table 8. Comparison of the HER performance of the Ti3C2-F and Ti3C2-O MXenes in universal pH with reported MXene-based electrocatalysts.

Supplementary Table 9. Comparison of the overall water-splitting performance of the Ti3C2-F and Ti3C2-O MXenes in 1 M KOH with reported MXene-based electrocatalysts.

| Materials | Catalyst mass loading (mg cm-2) | HER |  |  | OER |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | ⴄ10 (mV) | Tafel slope (mV dec-1) | Stability | ⴄ10 (mV) | Tafel slope (mV dec-1) | Stability | Ref. |
| Ti3C2Tx MXene |  |  |  |  |  |  |  |  |
| Ti3C2Tx | 0.7 | 245 | 107 | 24 h, 3000 cycles | 267 | 81 | 24 h, 3100 cycles | 13 |
| Ti3C2Tx MXene Heterostructures |  |  |  |  |  |  |  |  |
| Co/N-CNTs@Ti3C2Tx | 0.408 |  |  |  | 411 | 79.1 | 5.5 h, 2000 cycles | 14 |
| Ti3C2Tx |  |  |  |  | 484 | 227 |  |  |
| RuSA@Ti3C2Tx | 1 | 40.3 | 90 | 24 h, 5000 cycles |  |  |  | 12 |
| Ti3C2Tx |  | 516 | 660 |  |  |  |  |  |
| CoNi-Ti3C2Tx | 1 | 31 | 33 | 10 h | 241 | 79.8 | 10 h | 15 |
| Ti3C2Tx |  | 145 | 176 |  | 375 | 112.6 |  |  |
| d-Ti3C2/V2O5 | 2 | 90 | 49 | 24 h | 450 | 52 | 24 h | 16 |
| d-Ti3C2 |  | 192 | 68 |  | 240 | 63 |  |  |
| Ti3C2-F | 0.625 | 143 | 103 |  | 176 | 110 |  | This work |
| Ti3C2-O |  | 76 | 86 | 19.2 h, 2100 cycles | 165 | 102 | 17.8 h, 2100 cycles |  |

References

1. 	Naslund, L. Å., Persson, P. O. Å. & Rosen, J. X-ray photoelectron spectroscopy of Ti3AlC2, Ti3C2Tz, and TiC provides evidence for the electrostatic interaction between laminated layers in max-phase materials. Journal of Physical Chemistry C 124, 27732–27742 (2020).

2. 	Yang, H. et al. Catalytic Performance for the Conversion of Potent Fluorinated Greenhouse Gases by Aluminium Fluorides with Different Morphology. Catal. Letters 151, 2065–2074 (2021).

3. 	Sharma, P., Kainth, S., Pandey, O. P. & Mahajan, R. Customized Synthesis of 2D Ti3C2 MXene for Improved Overall Water Splitting. ACS Appl. Nano Mater. 6, 21788–21802 (2023).

4. 	Li, Y. et al. A general Lewis acidic etching route for preparing MXenes with enhanced electrochemical performance in non-aqueous electrolyte. Nat. Mater. 19, 894–899 (2020).

5. 	Yuan, K., Hao, P., Hu, X., Zhang, J. & Zhou, Y. Experimental and computational studies on S-decorated Ti3C2 MXene as anode material in Li-ion batteries. J. Mater. Sci. 57, 7001–7011 (2022).

6. 	Navjyoti, N. et al. Modulation of Surface Ti-O Species in 2D-Ti3C2Tx MXene for Developing a Highly Efficient Electrocatalyst for Hydrogen Evolution and Methanol Oxidation Reactions. Langmuir 39, 2995–3005 (2023).

7. 	Jiang, Y. et al. Oxygen-Functionalized Ultrathin Ti3C2Tx MXene for Enhanced Electrocatalytic Hydrogen Evolution. ChemSusChem 12, 1368–1373 (2019).

8. 	Wen, Y. et al. 2D TiVCTx layered nanosheets grown on nickel foam as highly efficient electrocatalysts for the hydrogen evolution reaction. RSC Adv. 12, 23584–23594 (2022).

9. 	Pang, S. Y. et al. Universal Strategy for HF-Free Facile and Rapid Synthesis of Two-dimensional MXenes as Multifunctional Energy Materials. J. Am. Chem. Soc. 141, 9610–9616 (2019).

10. 	Suragtkhuu, S. et al. Rhenium anchored Ti3C2Tx (MXene) nanosheets for electrocatalytic hydrogen production. Nanoscale Adv. 5, 349–355 (2022).

11. 	Ramalingam, V. et al. Heteroatom-Mediated Interactions between Ruthenium Single Atoms and an MXene Support for Efficient Hydrogen Evolution. Advanced Materials 31, (2019).

12. 	Zou, Y. et al. Ruthenium single-atom modulated Ti3C2Tx MXene for efficient alkaline electrocatalytic hydrogen production. EcoMat 5, (2023).

13. 	Lv, Z. et al. Induction of Co2P Growth on a MXene (Ti3C2Tx)-Modified Self-Supporting Electrode for Efficient Overall Water Splitting. Journal of Physical Chemistry Letters 12, 4841–4848 (2021).

14. 	Zhang, Y. et al. In Situ Growth of Cobalt Nanoparticles Encapsulated Nitrogen-Doped Carbon Nanotubes among Ti3C2Tx (MXene) Matrix for Oxygen Reduction and Evolution. Adv. Mater. Interfaces 5, (2018).

15. 	Zhao, X. et al. Dual-Atom Co/Ni Electrocatalyst Anchored at the Surface-Modified Ti3C2Tx MXene Enables Efficient Hydrogen and Oxygen Evolution Reactions. ACS Nano 18, 4256–4268 (2024).

16. 	Ashraf, I. et al. Hydrothermal synthesis and water splitting application of d-Ti3C2 MXene/V2O5 hybrid nanostructures as an efficient bifunctional catalyst. Int. J. Hydrogen Energy 47, 27383–27396 (2022).