Selective Resonance Energy Transfer and Fabry-Perot Oscillation: A New Paradigm for Electrically Driven Laser in Quasi-2D Ruddlesden-Popper Perovskite Microplates Film

Perovskite Structure

Figure S1. Schematic of different organic chains connecting the perovskite octahedron.

Contact Angle Measurement

Figure S2. Contact angle of 3D perovskite and our synthesized quasi-2D perovskite.

PL & Absorption Spectrum of Different Perovskite

Figure S3. Absorption spectra of 2D, quasi 2D and 3D perovskite films. (b) Deconvoluted PL spectra of quasi 2D perovskite, the fitted peaks are listed in the Table S1.

Table S1. List of reported PL positions of quasi 2D perovskite microplate together with our results

| Unit cell layer number in perovskite | PL wavelength (nm) |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
|  | Ref (1) | Ref (2) | Ref (3) | Ref (4) | Present work |
| 1 |  | 433 | 396 |  | 412 |
| 2 | 431 | 450 | 443 | 435 | 435 |
| 3 | 451 | 474 | 456 | 455 | 452 |
| 4 | 475 | 485 | 477 | 473 | 477 |
| 5 | 490 | 490 | 490 | 489 | 490 |
| 6 | 504 | 505 | -- | 505 | 501 |

X-Ray Diffraction Study

Figure S4. XRD pattern of 2D and quasi 2D perovskites.

XRD peak positions of (HA)2(MA)n-1PbnBr3n+1 RP perovskite are calculated from (00l) crystallographic planes. The estimated interlayer spacing is 21 Å +5.91 Å ×(n-1), where 5.91 Å is the thickness of each cubic phase lead bromide octahedron layer and 21 Å is the interlayer spacing of spacer cations based 2D perovskite (i.e., n=1) obtained from XRD data of 100% 2D spacer cation sample. The calculated result is consistent with published literature.5 In quasi 2D perovskite, 2-6 crystallographic planes are distinguished clearly, which are consistent with observed PL and absorption spectrum.

UV Absorption and Photoelectron Emission Spectra

Figure S5. (a)-(c) Tauc plots of 2D, quasi 2D and 3D perovskite films. (d) Ultraviolet photoelectron emission spectra of films containing 2D, quasi 2D and 3D perovskites.

Angle Dependent Random Laser

Figure S6. Angle-dependent random lasing spectra of quasi-2D RP perovskite.

Emission and Absorption Spectrum of Quasi-2D Perovskite

Figure S7. Spectral overlap between the emission and absorption spectrum of quasi-2D perovskite.

Life-Time Measurement from TRPL

Figure S8. Exciton lifetime of quasi-2D RP perovskite at different wavelengths from TRPL study.

Injection Current Dependent Emitted Light Power

Figure S9. Variation of Emitted Light Power with injection Current density.

FDTD Simulation for Light Extraction

Figure S10. FDTD simulation of Light extraction from perovskite/ZnO heterostructure considering the perovskite thickness of 1 and 2 μm.

External Quantum Efficiency & Device Stability

Figure S11. The external quantum efficiency of green light emission from the device at different intervals of time.

Device Fabrication

Figure S12. Different steps of light-emitting device fabrication.

References

1.	Tyagi, P., Arveson, S.M. & Tisdale, W.A. Colloidal Organohalide Perovskite Nanoplatelets Exhibiting Quantum Confinement. J. Phys. Chem. Let. 6, 1911-1916 (2015).

2.	Cho, J., Choi, Y.-H., O’Loughlin, T.E., De Jesus, L. & Banerjee, S. Ligand-Mediated Modulation of Layer Thicknesses of Perovskite Methylammonium Lead Bromide Nanoplatelets. Chem. Mater. 28, 6909-6916 (2016).

3.	Wang, Q. et al. Quantum confinement effect and exciton binding energy of layered perovskite nanoplatelets. AIP Adv. 8, 025108 (2018).

4.	Li, M. et al. Enhanced Exciton and Photon Confinement in Ruddlesden–Popper Perovskite Microplatelets for Highly Stable Low-Threshold Polarized Lasing. Adv. Mater. 30, 1707235 (2018).

5.	Tabuchi, Y., Asai, K., Rikukawa, M., Sanui, K. & Ishigure, K. Preparation and characterization of natural lower dimensional layered perovskite-type compounds. J. Phys. Chem. Solids 61, 837-845 (2000).