Geometric control and multi-case crashworthiness optimization of functionally graded cross-section thin-walled conical tubes

Zhichao Xu1, Xinrui Shao2, Yuxin Chen1, Jiangchen Li3,* and Zhichao Li4,**

1 Suzhou City University, Suzhou 215204, Jiangsu, PR China

2 Nanjing University of Science and Technology, Nanjing 210094, China

3 Nanjing University of Aeronautics and Astronautics, Nanjing 210016, Jiangsu, PR China

4 Suzhou University of Technology, Suzhou 215500, Jiangsu, PR China

* Corresponding author: Jiangchen Li (jiangchen@nuaa.edu.cn);

** Co-corresponding author: Zhichao Li (lizhichao7302@126.com).

Supplementary Table S1. Sampling points of the smaller-gradient partition (0 <= m <= 1): test number and design variables (gradient parameter m, wall thickness t, initial yield strength sigma_y).

| No. | m | t / mm | sigma_y / MPa |
| --- | --- | --- | --- |
| 1 | 0.263 | 1.579 | 133.16 |
| 2 | 1 | 2.053 | 128.95 |
| 3 | 0.053 | 2.684 | 86.84 |
| 4 | 0.684 | 1.737 | 145.79 |
| 5 | 0.579 | 1.816 | 78.42 |
| 6 | 0.737 | 2.447 | 150 |
| 7 | 0.368 | 2.368 | 107.89 |
| 8 | 0.316 | 2.289 | 141.58 |
| 9 | 0.789 | 2.605 | 116.32 |
| 10 | 0.947 | 2.211 | 91.05 |
| 11 | 0.158 | 1.974 | 70 |
| 12 | 0.842 | 2.842 | 82.63 |
| 13 | 0.474 | 2.526 | 74.21 |
| 14 | 0.0177 | 2.132 | 120.53 |
| 15 | 0.211 | 1.658 | 99.47 |
| 16 | 0.632 | 1.895 | 112.11 |
| 17 | 0.895 | 1.5 | 95.26 |
| 18 | 0.526 | 2.921 | 137.37 |
| 19 | 0.105 | 2.763 | 124.74 |
| 20 | 0.421 | 3 | 103.68 |

Supplementary Table S2. Sampling points of the larger-gradient partition (1 < m <= 10): test number and design variables (gradient parameter m, wall thickness t, initial yield strength sigma_y).

| No. | m | t / mm | sigma_y / MPa |
| --- | --- | --- | --- |
| 1 | 4.79 | 2.132 | 128.95 |
| 2 | 10 | 1.974 | 103.68 |
| 3 | 3.84 | 2.053 | 70 |
| 4 | 8.11 | 2.526 | 145.79 |
| 5 | 5.26 | 1.5 | 141.58 |
| 6 | 1.47 | 2.211 | 95.26 |
| 7 | 7.16 | 3 | 86.84 |
| 8 | 9.05 | 2.447 | 78.42 |
| 9 | 5.74 | 2.289 | 99.47 |
| 10 | 8.58 | 1.895 | 137.37 |
| 11 | 9.53 | 2.605 | 112.11 |
| 12 | 7.63 | 1.816 | 74.21 |
| 13 | 1 | 2.368 | 133.16 |
| 14 | 6.21 | 2.921 | 120.53 |
| 15 | 6.68 | 1.658 | 107.89 |
| 16 | 3.37 | 2.763 | 82.63 |
| 17 | 2.42 | 2.842 | 116.32 |
| 18 | 2.89 | 1.579 | 91.05 |
| 19 | 1.95 | 1.737 | 124.74 |
| 20 | 4.32 | 2.684 | 150 |

Supplementary Table S3. Model-accuracy evaluation sample points and simulation results (design variables, SEA under four loading angles, and initial and global peak crushing forces at 0° and 10° for 10 validation samples). F_max denotes the initial peak crushing force and G_max the global peak crushing force (Finit and Fglobal in the main text).

| No. | m | t / mm | sigma_y / MPa | SEA 0 deg / (J/g) | F_max / kN | G_max / kN | SEA 10 deg / (J/g) | F_max 10 deg / kN | G_max 10 deg / kN | SEA 20 deg / (J/g) | SEA 30 deg / (J/g) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | 0.11 | 1.83 | 123.33 | 17.519 | 49.816 | 56.286 | 15.842 | 46.805 | 46.805 | 12.167 | 11.037 |
| 2 | 0.33 | 2.33 | 132.22 | 24.189 | 76.502 | 76.502 | 22.377 | 59.585 | 67.042 | 17.260 | 13.204 |
| 3 | 0.56 | 2.00 | 114.44 | 19.419 | 50.851 | 50.851 | 18.973 | 38.813 | 43.809 | 15.752 | 11.775 |
| 4 | 0.67 | 2.50 | 78.89 | 19.038 | 56.318 | 56.408 | 18.256 | 41.963 | 51.866 | 15.431 | 11.092 |
| 5 | 0.89 | 2.17 | 87.78 | 19.551 | 46.233 | 52.590 | 17.823 | 33.844 | 41.012 | 15.418 | 10.812 |
| 6 | 7.62 | 1.575 | 97.25 | 18.996 | 28.566 | 28.566 | 14.388 | 18.503 | 20.899 | 12.301 | 5.867 |
| 7 | 3.38 | 2.975 | 130.75 | 31.859 | 75.110 | 83.236 | 28.633 | 55.896 | 80.859 | 22.603 | 15.407 |
| 8 | 1.25 | 1.92 | 110.00 | 23.532 | 35.001 | 46.422 | 20.557 | 27.235 | 39.748 | 16.286 | 11.928 |
| 9 | 5.50 | 2.62 | 72.50 | 21.538 | 50.056 | 51.918 | 17.557 | 34.102 | 41.425 | 13.347 | 8.226 |
| 10 | 9.75 | 2.28 | 147.50 | 28.939 | 54.442 | 54.442 | 19.245 | 40.098 | 46.658 | 8.420 | 7.863 |

Supplementary Table S4. Weighted SEA and oblique SEA retention rates of the 10 validation samples.

| No. | m | SEA 0 deg / (J/g) | SEA_w / (J/g) | eta_10 / % | eta_20 / % | eta_30 / % |
| --- | --- | --- | --- | --- | --- | --- |
| 1 | 0.11 | 17.519 | 15.297 | 90.4 | 69.5 | 63.0 |
| 2 | 0.33 | 24.189 | 21.161 | 92.5 | 71.4 | 54.6 |
| 3 | 0.56 | 19.419 | 17.787 | 97.7 | 81.1 | 60.6 |
| 4 | 0.67 | 19.038 | 17.287 | 95.9 | 81.1 | 58.3 |
| 5 | 0.89 | 19.551 | 17.332 | 91.2 | 78.9 | 55.3 |
| 6 | 7.62 | 18.996 | 14.962 | 75.7 | 64.8 | 30.9 |
| 7 | 3.38 | 31.859 | 27.395 | 89.9 | 70.9 | 48.4 |
| 8 | 1.25 | 23.532 | 20.030 | 87.4 | 69.2 | 50.7 |
| 9 | 5.50 | 21.538 | 17.374 | 81.5 | 62.0 | 38.2 |
| 10 | 9.75 | 28.939 | 19.819 | 66.5 | 29.1 | 27.2 |

Supplementary Tables S5-S20. Response-surface coefficient vectors (A1)-(A16), listed in the term order [1, x1, x2, x3, x12, x22, x32, x1x2, x1x3, x2x3, x13, x23, x33]. Tables S7-S9 correspond to (A1)-(A3) (axial loading, m in (0,1): SEA, Fmax, Gmax); S10-S12 to (A4)-(A6) (m in (1,10)); S13-S15 to (A7)-(A9) (10°, m in (0,1)); S16-S18 to (A10)-(A12) (10°, m in (1,10)); S19-S20 to (A13)-(A14) (20°, m in (0,1)); S21-S22 to (A15)-(A16) (30°, m in (1,10)). The numeric coefficient vectors are reproduced verbatim from the source document (see embedded objects below). When using them, the physical variables should be converted into the regression coordinates adopted by the original fitting; the existing record does not fully specify the input coding, so one cannot directly assume that the physical quantities carrying mm and MPa units are identical to the regression coordinates.

Supplementary Table S5.

Supplementary Table S6.

Supplementary Table S7.

Supplementary Table S8.

Supplementary Table S9.

Supplementary Table S10.

Supplementary Table S11.

Supplementary Table S12.

Supplementary Table S13.

Supplementary Table S14.

Supplementary Table S15.

Supplementary Table S16.

Supplementary Table S17.

Supplementary Table S18.

Supplementary Table S19.

Supplementary Table S20.

Supplementary Notes

Supplementary Note 1 - Benchmark-comparison scope (related to Table 1). The response quantities examined in this section are the crush distance and the total energy absorption. Because the existing comparison table does not provide experimental data for the initial and global peak crushing forces, the conclusions concerning the peak response and the FGCS configurations are still limited to the numerical-analysis scope of this paper. The reference-case comparison provides a basis for the subsequent analysis, but it is not extended into a complete verification of all configurations and all loading cases.

Supplementary Note 2 - Mechanism-discussion boundary (related to the 'Crushing deformation morphology' subsection of the Results section of the main text). For finite m, equation (1) varies continuously within the tube wall and introduces no cross-sectional jump from the power-law expression itself. Therefore, this paper describes the rear-stage feature using 'an increasing cross-sectional expansion rate' or 'concentrated geometric transition', rather than unquantifiedly calling it a stiffness jump. Correspondingly, the mechanism discussion in this paper is an interpretive link between the geometric analysis and the existing numerical phenomena, and does not replace a critical instability condition or a plastic-energy-dissipation decomposition.

Supplementary Note 3 - Accuracy indicators, MAPE definition and Table 1 note (related to Table 1). Table 1 retains all the accuracy values from the original calculation report, in which the error columns for each angle keep the original notation MAPE so as to correspond to the original record. The existing record does not fully specify the normalization relation between the error columns and the dimensional responses; therefore, this paper does not directly interpret these values as percentages, nor does it replace the original calculation by supplementing some scaling rule. The mean absolute percentage error is conventionally defined as MAPE = (1/n) sum_{i=1}^{n} |(y_i - y hat_i)/y_i| x 100%; in the present work the MAPE values are retained in the original notation of Table 1 and no percentage conversion is asserted for the tabulated values. Note: Table 1 retains the RMSE and MAPE values and notations according to the original calculation record; the correspondence among their names, formulas and normalization scales remains to be checked, and no unconfirmed percentage conversion is performed.

Supplementary Note 4 - Sample-7 discussion (related to Table S4). Sample 7 has a comprehensive SEA of 27.395 J/g, which is relatively high among the 10 validation samples, but its 30 deg retention rate is 48.4% and it is not the sample with the highest retention rate. It can be seen that the absolute energy-absorption level and the relative retention ability after the angle change should not be confused either. The comprehensive objective of this paper still adopts the weighted SEA and peak-load control, and the retention rate is used to explain the angle sensitivity without changing the definition of the original multi-objective problem.

Supplementary Note 5 - Complete-combination caveat (related to Table S4). The above comparison targets complete design combinations. Since the m, t and sigma_y of the samples are different, the ranking change can illustrate the necessity of the multi-angle evaluation, but it cannot be used to quantitatively identify the independent causal contribution of m, nor can it replace a dedicated comparison of the two partitions under equivalent conditions.