Supplementary Data

Green Rosemary Extract-Mediated Synthesis of Ag/Co/La2O3/Chitosan Nanocomposite for Multifunctional Antibacterial Activity and Simultaneous Removal of Binary Dyes from Water

Section S1. Materials and Methods

1. Reagents and Chemicals

Silver nitrate (AgNO3, ≥99.9%), cobalt nitrate hexahydrate [Co(NO3)2·6H2O, ≥98%], lanthanum oxide (La2O3, ≥99.9%), chitosan (medium molecular weight, degree of deacetylation ≥75%), glacial acetic acid (≥99.7%), hydrochloric acid (HCl, 37%), sodium hydroxide (NaOH, ≥98%), and ethanol (≥99.8%) were of analytical grade and used without further purification. Methylene blue (MB, ≥95%) and crystal violet (CV, ≥90%) were used as model dyes. 2’,7’-Dichlorodihydrofluorescein diacetate (DCFH-DA, ≥97%) was used for ROS detection. Mueller-Hinton agar, nutrient broth, and the selected antibiotic standard were used for the antibacterial assay. All aqueous solutions were prepared using distilled water. Certified Ag and Co standard solutions (1000 mg L-1) were used for atomic absorption spectrometric calibration.

2. Instruments

UV-Vis spectra and dye-removal measurements were recorded using a Spekol 11 spectrophotometer (Analytik Jena AG, Jena, Germany). Fourier-transform infrared (FTIR) spectra were obtained using a Nicolet iS10 spectrometer (Thermo Fisher Scientific, USA) to identify the characteristic functional groups. The morphology and particle structure were examined by high-resolution transmission electron microscopy (HR-TEM; Thermo Scientific Talos F200i) and scanning electron microscopy (SEM; FEI, Czech Republic) operated at an accelerating voltage of 30.0 kV and magnifications of 1000-5000×. Elemental composition and spatial distribution were determined by energy-dispersive X-ray spectroscopy (EDX) and elemental mapping using the FEI SEM system under the same operating conditions. X-ray diffraction (XRD) patterns were recorded using a PANalytical Philips diffractometer to determine the crystalline phases of the synthesized materials. Specific surface area and porosity were evaluated using a BELSORP-mini X surface-area analyzer (MicrotracBEL Corp., Japan); samples were degassed under vacuum at 120 °C for 6 h prior to analysis. An Elma Schmidbauer GmbH sonicator (Singen, Germany) was used for ultrasonic dispersion during nanocomposite preparation, while centrifugation was performed using an Allegra X-15R centrifuge (Beckman Coulter, California, USA).

Section S2: Results

Table S1. Linear fitting equations obtained from the Tauc plots αhν2 versus photon energy hνand the corresponding calculated direct optical band-gap energies (Eg) of rosemary extract, Ag/Co/La2O3 nanocomposite (NC), and Ag/Co/La2O3/chitosan (CS) nanocomposite.

| Sample | Material | Linear fitting equation a | x-intercept (Eg=-c/m)) (eV) | Calculated direct band gap, (Eg) (eV) |
| --- | --- | --- | --- | --- |
| A | Rosemary extract | (y = 3.2812x - 5.7786) | 1.761 | 1.76 |
| B | Ag/Co/La2O3 NC | (y = -7.2986x + 28.379) | 3.888 | 3.89 |
| C | Ag/Co/La2O3/CS NC | (y = -3.0481x + 15.304) | 2.943 | 2.94 |

[a] The optical band-gap energy (Eg) was estimated from the intercept of the linear region of the Tauc plots according to:

αhν2=Ahν-Eg

where αis the absorption coefficient, hνis the photon energy, Ais a proportionality constant, and Egwas calculated from the x-intercept of the fitted line using Eg=-c/m, where mand care the slope and intercept of the linear fitting equation, respectively.

Table S2. FTIR absorption bands (cm-1) and functional group assignments of rosemary extract, Ag/Co/La2O3 nanocomposite (NC), and Ag/Co/La2O3/chitosan (CS) nanocomposite, demonstrating the involvement of phytochemicals in nanoparticle synthesis and the successful incorporation of chitosan into the hybrid nanocomposite.

| Functional group / Vibrational assignment | Rosemary extract (cm-1) | Ag/Co/La2O3 NC (cm-1) | Ag/Co/La2O3/CS NC (cm-1) |
| --- | --- | --- | --- |
| O-H/N-H stretching | 3383 | 3549 | 3231 |
| Aliphatic C-H stretching | 2936, 2881 | 2915 | - |
| C=O stretching / Amide I | 1673, 1613 | - | 1559 |
| Aromatic C=C / N-H bending (Amide II) | 1570, 1539 | 1534 | 1533 |
| CH2 deformation / C-N stretching | 1465, 1397, 1349 | 1448, 1407, 1349, 1305 | 1452, 1423, 1396, 1332 |
| C-O-C / C-O stretching | 1259, 1194, 1146, 1079, 1048, 1027 | 1014 | 1052, 1015 |
| Aromatic C-H out-of-plane bending | 987, 928, 875, 825, 780 | 940, 872, 830, 732 | 943, 833, 734 |
| Metal-oxygen (La-O, Co-O, Ag-O) lattice vibrations | 659, 600, 554, 522, 428 | 666, 630, 614, 530, 467, 408, 367 | 664, 610, 507, 465 |

Table S3. Electrophoretic and zeta potential parameters of the green-synthesized Ag/Co/La2O3 nanocomposite (NC) determined by laser Doppler electrophoresis at 23 °C. The measured zeta potential and electrophoretic mobility reflect the surface charge characteristics and colloidal stability of the synthesized nanocomposite.

| Parameter | Ag/Co/La2O3 NC | Unit / Description |
| --- | --- | --- |
| Average zeta potential | +8.19 | mV |
| Average electrophoretic mobility | +0.57 | ×10-4 cm2 V-1 s-1 |
| Frequency shift | 1.11 | Hz |
| Sample peak frequency | 261.23 | Hz |
| Reference peak frequency | 260.12 | Hz |
| Cell current | 0.88 | mA |
| Conductivity factor | 4.04 | Dimensionless |
| Electric field strength | 3.75 | V cm-1 |
| Sample temperature | 23.0 | °C |
| Liquid viscosity | 0.995 | cP |
| Dielectric constant | 78.50 | Dimensionless |
| Refractive index | 1.333 | Dimensionless |
| Laser wavelength | 632.8 | nm (He–Ne laser) |
| Scattering angle | 90 | ° |
| Channel width | 500 | μs |
| Measurement time | 2 min 13 s | Total acquisition time |

Table S4. Electrophoretic and zeta potential parameters of the Ag/Co/La2O3/CS NC determined by laser Doppler electrophoresis at 23 °C. Chitosan functionalization increased the positive surface charge and electrophoretic mobility, indicating enhanced colloidal stability through protonated amino groups on the polymer-coated nanocomposite.

| Parameter | Ag/Co/La2O3/CS NC | Unit / Description |
| --- | --- | --- |
| Average zeta potential | +13.78 | mV |
| Average electrophoretic mobility | +0.96 | ×10-4 cm2 V-1 s-1 |
| Frequency shift | 1.54 | Hz |
| Sample peak frequency | 261.40 | Hz |
| Reference peak frequency | 259.86 | Hz |
| Cell current | 0.74 | mA |
| Conductivity factor | 4.89 | Dimensionless |
| Electric field strength | 3.75 | V cm-1 |
| Sample temperature | 23.0 | °C |
| Liquid viscosity | 0.995 | cP |
| Dielectric constant | 78.50 | Dimensionless |
| Refractive index | 1.333 | Dimensionless |
| Laser wavelength | 632.8 | nm (He-Ne laser) |
| Scattering angle | 90 | ° |
| Channel width | 500 | μs |
| Measurement time | 2 min 17 s | Total acquisition time |

Table S5. EDX elemental composition of the synthesized nanocomposites.

| Nanocomposite | Element | Line | Weight (%) | Atomic (%) | Error (%) |
| --- | --- | --- | --- | --- | --- |
| Ag/Co/La2O3 NC | O | K | 31.52 | 76.86 | 11.12 |
|  | Ag | L | 37.29 | 13.49 | 1.89 |
|  | La | L | 28.87 | 8.11 | 4.78 |
|  | Co | K | 2.33 | 1.54 | 15.36 |
| Ag/Co/La2O3/CS NC | C | K | 1.10 | 2.54 | 24.88 |
|  | N | K | 8.32 | 16.50 | 11.24 |
|  | O | K | 39.13 | 67.94 | 9.47 |
|  | Ag | L | 5.72 | 1.47 | 6.03 |
|  | La | L | 36.89 | 7.38 | 3.87 |
|  | Co | K | 8.85 | 4.17 | 5.72 |

Table S6. Elemental mapping composition and contribution of the synthesized nanocomposites.

| Nanocomposite | Element | Line | Weight (%) | Atomic (%) | Error (%) | Mapping contribution (%) |
| --- | --- | --- | --- | --- | --- | --- |
| Ag/Co/La2O3 NC | O | K | 25.17 | 71.29 | 10.28 | 12 |
|  | Ag | L | 35.30 | 14.83 | 1.76 | 53 |
|  | La | L | 37.31 | 12.17 | 2.68 | 30 |
|  | Co | K | 2.22 | 1.71 | 9.72 | 6 |
| Ag/Co/La2O3/CS NC | C | K | 1.15 | 2.82 | 21.10 | 2 |
|  | N | K | 7.50 | 15.70 | 11.05 | 5 |
|  | O | K | 36.49 | 66.83 | 9.30 | 27 |
|  | Ag | L | 5.78 | 1.57 | 5.73 | 13 |
|  | La | L | 39.51 | 8.33 | 3.41 | 38 |
|  | Co | K | 9.56 | 4.75 | 5.30 | 16 |

Table S7. X-ray diffraction peak indexing, phase identification, and crystallographic parameters of the green-synthesized Ag/La2O3 nanocomposite (NC). Experimental diffraction peaks were matched with the ICDD/PDF database to identify the crystalline phases, crystal systems, space groups, and corresponding Miller indices (hkl). Rietveld phase analysis revealed the coexistence of AgCl, metallic Ag, La(OH)3, and La2O3 phases, confirming the successful formation of a multiphase crystalline nanocomposite.

| 2θ (°) | d-spacing (Å) | Relative intensity (%) | Identified phase | Chemical formula | ICDD/PDF No. | Crystal system (Space group) | (hkl) |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 15.786 | 5.6096 | 6.8 | Lanthanum hydroxide | La(OH)3 | PDF 01-077-3933 | Hexagonal (P6₃/m) | (100) |
| 27.397 | 3.2527 | 13.1 | Lanthanum hydroxide | La(OH)3 | PDF 01-077-3933 | Hexagonal (P6₃/m) | (110) |
| 27.940 | 3.1908 | 40.5 | Silver chloride | AgCl | PDF 00-001-1013 | Cubic (Fm-3m) | (111) |
| 29.493 | 3.0262 | 9.2 | Lanthanum oxide | La2O3 | PDF 01-088-3887 | Hexagonal (P-3m1) | (011) |
| 31.741 | 2.8169 | 5.4 | Lanthanum hydroxide | La(OH)3 | PDF 01-077-3933 | Hexagonal (P6₃/m) | (200) |
| 32.346 | 2.7655 | 100.0 | Silver chloride | AgCl | PDF 00-001-1013 | Cubic (Fm-3m) | (200) |
| 38.220 | 2.3529 | 63.3 | Metallic silver | Ag | PDF 01-087-0720 | Cubic (Fm-3m) | (111) |
| 39.604 | 2.2738 | 19.2 | Lanthanum hydroxide | La(OH)3 | PDF 01-077-3933 | Hexagonal (P6₃/m) | (201) |
| 44.387 | 2.0392 | 23.5 | Metallic silver | Ag | PDF 01-087-0720 | Cubic (Fm-3m) | (200) |
| 46.332 | 1.9581 | 70.5 | Silver chloride | AgCl | PDF 00-001-1013 | Cubic (Fm-3m) | (220) |
| 48.782 | 1.8653 | 19.6 | Lanthanum hydroxide | La(OH)3 | PDF 01-077-3933 | Hexagonal (P6₃/m) | (202) |
| 54.911 | 1.6707 | 24.1 | Silver chloride | AgCl | PDF 00-001-1013 | Cubic (Fm-3m) | (311) |
| 57.552 | 1.6002 | 21.4 | Silver chloride | AgCl | PDF 00-001-1013 | Cubic (Fm-3m) | (222) |
| 64.541 | 1.4427 | 26.4 | Metallic silver | Ag | PDF 01-087-0720 | Cubic (Fm-3m) | (220) |
| 76.798 | 1.2402 | 23.7 | Silver chloride | AgCl | PDF 00-001-1013 | Cubic (Fm-3m) | (420) |
| 77.485 | 1.2309 | 31.6 | Metallic silver | Ag | PDF 01-087-0720 | Cubic (Fm-3m) | (311) |

Table S8. X-ray diffraction peak indexing, crystallographic phase identification, and quantitative phase composition of the Ag/Co/La2O3/chitosan (CS) nanocomposite. Diffraction peaks were indexed using the ICDD/PDF database, confirming the formation of a multifunctional hybrid nanocomposite consisting of crystalline AgCl, metallic Ag, La2O3, La(OH)3, Co(OH)2, and chitosan L-ascorbate phases after polymer functionalization.

| 2θ (°) | d-spacing (Å) | Relative intensity (%) | Identified phase | Chemical formula | ICDD/PDF No. | Crystal system (Space group) | (hkl) |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 7.804 | 11.3200 | 3.0 | Chitosan L-ascorbate | (C12H21NO11)n | PDF 00-054-1952 | Monoclinic (P21) | (100) |
| 9.045 | 9.7690 | 100.0 | Chitosan L-ascorbate | (C12H21NO11)n | PDF 00-054-1952 | Monoclinic (P21) | (001) |
| 15.694 | 5.6422 | 40.7 | Lanthanum hydroxide | La(OH)3 | PDF 01-077-3933 | Hexagonal (P63/m) | (100) |
| 18.626 | 4.7600 | 67.0 | Chitosan L-ascorbate | (C12H21NO11)n | PDF 00-054-1952 | Monoclinic (P21) | (012) |
| 20.165 | 4.4000 | 64.0 | Cobalt hydroxide | Co(OH)2 | PDF 00-001-0357 | Hexagonal | - |
| 21.136 | 4.2000 | 11.0 | Lanthanum oxide | La2O3 | PDF 00-022-0641 | Monoclinic (P21/m) | (-202) |
| 24.780 | 3.5900 | 21.0 | Lanthanum oxide | La2O3 | PDF 00-022-0641 | Monoclinic (P21/m) | (202) |
| 27.357 | 3.2575 | 57.2 | Lanthanum hydroxide | La(OH)3 | PDF 01-077-3933 | Hexagonal (P63/m) | (110) |
| 27.839 | 3.2022 | 42.9 | Silver chloride | AgCl | PDF 01-071-5209 | Cubic (Fm-3m) | (111) |
| 28.015 | 3.1824 | 99.9 | Lanthanum hydroxide | La(OH)3 | PDF 01-077-3933 | Hexagonal (P63/m) | (011) |
| 30.753 | 2.9050 | 100.0 | Lanthanum oxide | La2O3 | PDF 00-022-0641 | Monoclinic (P21/m) | (-501) |
| 31.692 | 2.8211 | 23.6 | Lanthanum hydroxide | La(OH)3 | PDF 01-077-3933 | Hexagonal (P63/m) | (200) |
| 32.254 | 2.7732 | 99.9 | Silver chloride | AgCl | PDF 01-071-5209 | Cubic (Fm-3m) | (200) |
| 35.452 | 2.5300 | 100.0 | Chitosan L-ascorbate | (C12H21NO11)n | PDF 00-054-1952 | Monoclinic (P21) | (014) |
| 36.073 | 2.4879 | 7.3 | Lanthanum hydroxide | La(OH)3 | PDF 01-077-3933 | Hexagonal (P6₃/m) | (111) |
| 36.806 | 2.4400 | 27.0 | Cobalt hydroxide | Co(OH)2 | PDF 00-001-0357 | Hexagonal | (101) |
| 38.121 | 2.3588 | 99.9 | Metallic silver | Ag | PDF 01-071-3762 | Cubic (Fm-3m) | (111) |
| 38.958 | 2.3100 | 100.0 | Cobalt hydroxide | Co(OH)2 | PDF 00-001-0357 | Hexagonal | (002) |
| 39.557 | 2.2764 | 89.2 | Lanthanum hydroxide | La(OH)3 | PDF 01-077-3933 | Hexagonal (P63/m) | (201) |
| 42.350 | 2.1325 | 18.1 | Lanthanum hydroxide | La(OH)3 | PDF 01-077-3933 | Hexagonal (P63/m) | (210) |
| 44.307 | 2.0428 | 52.5 | Metallic silver | Ag | PDF 01-071-3762 | Cubic (Fm-3m) | (200) |
| 46.261 | 1.9609 | 68.0 | Silver chloride | AgCl | PDF 01-071-5209 | Cubic (Fm-3m) | (220) |
| 48.357 | 1.8807 | 36.1 | Lanthanum hydroxide | La(OH)3 | PDF 01-077-3933 | Hexagonal (P63/m) | (102) |
| 48.765 | 1.8659 | 72.6 | Lanthanum hydroxide | La(OH)3 | PDF 01-077-3933 | Hexagonal (P63/m) | (211) |
| 50.674 | 1.8000 | 62.0 | Cobalt hydroxide | Co(OH)2 | PDF 00-001-0357 | Hexagonal | (102) |
| 54.856 | 1.6723 | 15.0 | Silver chloride | AgCl | PDF 01-071-5209 | Cubic (Fm-3m) | (311) |
| 55.349 | 1.6585 | 27.1 | Lanthanum hydroxide | La(OH)3 | PDF 01-077-3933 | Hexagonal (P63/m) | (112) |
| 57.516 | 1.6011 | 19.3 | Silver chloride | AgCl | PDF 01-071-5209 | Cubic (Fm-3m) | (222) |
| 61.799 | 1.5000 | 15.0 | Cobalt hydroxide | Co(OH)2 | PDF 00-001-0357 | Hexagonal | (111) |
| 64.456 | 1.4444 | 37.2 | Metallic silver | Ag | PDF 01-071-3762 | Cubic (Fm-3m) | (220) |
| 67.496 | 1.3866 | 7.0 | Silver chloride | AgCl | PDF 01-071-5209 | Cubic (Fm-3m) | (400) |
| 68.425 | 1.3700 | 55.0 | Cobalt hydroxide | Co(OH)2 | PDF 00-001-0357 | Hexagonal | (200) |
| 76.795 | 1.2402 | 14.8 | Silver chloride | AgCl | PDF 01-071-5209 | Cubic (Fm-3m) | (420) |
| 77.414 | 1.2318 | 43.5 | Metallic silver | Ag | PDF 01-071-3762 | Cubic (Fm-3m) | (311) |

Table S9. Antibacterial efficacy of rosemary extract, Ag/Co/La2O3 NC, Ag/Co/La2O3/CS NC, and azithromycin (1 mg mL-1) against representative pathogenic bacteria as determined by the agar diffusion method. Data are expressed as mean ± standard deviation (SD) of three independent experiments (n = 3). NA indicates no detectable inhibition zone.

| Microorganism | Rosemary extract (mm) | Ag/Co/La2O3 NC (mm) | Ag/Co/La2O3/CS NC (mm) | Azithromycin (1 mg mL-1) (mm) |
| --- | --- | --- | --- | --- |
| Gram-negative bacteria |  |  |  |  |
| Escherichia coli (ATCC 10536) | NA | NA | 12.0 ± 0.58 | NA |
| Salmonella typhimurium (ATCC 25566) | NA | 13.0 ± 0.58 | NA | 13.0 ± 0.58 |
| Klebsiella pneumoniae (ATCC 10031) | NA | 12.0 ± 1.00 | 14.0 ± 0.58 | 12.0 ± 0.58 |
| Enterobacter cloacae (DMS 30054) | NA | 12.0 ± 0.58 | 16.0 ± 1.00 | 11.0 ± 0.58 |
| Gram-positive bacteria |  |  |  |  |
| Bacillus subtilis (DMS 1088) | NA | 18.0 ± 1.00 | 19.0 ± 0.58 | 14.0 ± 0.58 |
| Bacillus cereus (EMCC 1080) | NA | 21.0 ± 0.58 | 19.0 ± 1.00 | 21.0 ± 0.58 |
| Staphylococcus aureus (ATCC 6538) | NA | 14.0 ± 0.58 | 16.0 ± 0.58 | 18.0 ± 1.00 |
| Staphylococcus epidermidis (EMCC 1353T) | NA | 18.0 ± 0.58 | 22.0 ± 1.00 | 19.0 ± 0.58 |

Values are presented as the mean inhibition zone diameter ± SD (n = 3). The diameter of the paper disc (6 mm) is included in the measured inhibition zone. NA indicates that no measurable inhibition zone was observed under the experimental conditions.

Table S10. Dark adsorption of MB and CV onto Ag/Co/La2O3/CS NC as a function of contact time. Experiments were performed using an equimolar binary MB/CV solution ([MB]₀ = [CV]₀ = 10 mg L-1), catalyst dosage of 0.50 g L-1, initial pH 9.0, and temperature of 25 °C. Adsorption approached equilibrium after approximately 40 min. Values are presented as mean ± SD (n = 3).

| Dark-contact time (min) | MB adsorption (%) | CV adsorption (%) |
| --- | --- | --- |
| 0 | 0.0 ± 0.0 | 0.0 ± 0.0 |
| 5 | 12.5 ± 1.0 | 15.0 ± 1.1 |
| 10 | 20.5 ± 1.1 | 24.0 ± 1.2 |
| 20 | 27.5 ± 1.3 | 32.0 ± 1.4 |
| 30 | 32.0 ± 1.4 | 37.0 ± 1.5 |
| 40 | 33.5 ± 1.4 | 38.5 ± 1.5 |
| 50 | 34.0 ± 1.5 | 39.0 ± 1.6 |
| 60 | 34.2 ± 1.5 | 39.2 ± 1.6 |

Table S11. Control experiments for MB and CV removal.

| Experimental condition | Catalyst | Light | MB removal (%) | CV removal (%) |
| --- | --- | --- | --- | --- |
| Dark stability | Absent | Absent | 0.5 ± 0.2 | 0.6 ± 0.2 |
| Photolysis | Absent | Present | 4.5 ± 0.6 | 4.0 ± 0.7 |
| Dark adsorption | 0.50 g L-1 | Absent | 33.5 ± 1.4 | 38.5 ± 1.5 |
| Photocatalysis | 0.50 g L-1 | Present | 97.5 ± 0.7 | 94.0 ± 0.9 |

Table S12. Effect of different experimental parameters on the photocatalytic removal of methylene blue (MB) and crystal violet (CV) by Ag/Co/La2O3/CS NC. Unless otherwise indicated, the experiments were performed using an equimolar binary MB/CV solution ([MB]₀ = [CV]₀ = 10 mg L-1), catalyst dosage of 0.50 g L-1, initial pH 9.0, temperature of 25 °C, and irradiation time of 180 min. For the irradiation-time and catalyst-dosage experiments, the initial pH was maintained at 7.0 and the temperature at 25 °C. For the pH experiment, the catalyst dosage was 0.50 g L-1, and the temperature was 25 °C. For the initial dye-concentration experiment, the MB: CV concentration ratio was maintained at 1:1. For the temperature experiment, the initial pH was 9.0, the catalyst dosage was 0.50 g L-1, and irradiation time was 180 min. Values are presented as mean ± SD (n = 3).

| Parameters | Variables | MB removal (%) | CV removal (%) |
| --- | --- | --- | --- |
| Irradiation time (min) | 0 | 0.0 ± 0.0 | 0.0 ± 0.0 |
|  | 10 | 42.0 ± 1.5 | 37.5 ± 1.7 |
|  | 20 | 58.5 ± 1.6 | 51.0 ± 1.8 |
|  | 30 | 70.5 ± 1.7 | 62.5 ± 1.9 |
|  | 60 | 85.5 ± 1.3 | 78.0 ± 1.5 |
|  | 90 | 91.5 ± 1.1 | 84.0 ± 1.3 |
|  | 120 | 95.0 ± 0.9 | 88.0 ± 1.1 |
|  | 150 | 96.8 ± 0.8 | 92.0 ± 1.0 |
|  | 180 | 97.5 ± 0.7 | 94.0 ± 0.9 |
| Catalyst dosage (g L-1) | 0.10 | 68.0 ± 2.0 | 63.5 ± 2.2 |
|  | 0.25 | 82.5 ± 1.6 | 74.5 ± 1.8 |
|  | 0.50 | 97.5 ± 0.7 | 93.5 ± 1.1 |
|  | 0.75 | 98.0 ± 0.6 | 94.8 ± 0.9 |
|  | 1.00 | 98.1 ± 0.6 | 95.5 ± 0.8 |
|  | 1.50 | 97.8 ± 0.7 | 95.7 ± 0.9 |
| Initial pH | 3 | 72.5 ± 1.8 | 68.0 ± 2.0 |
|  | 5 | 86.0 ± 1.4 | 82.5 ± 1.6 |
|  | 7 | 95.5 ± 0.9 | 93.5 ± 1.1 |
|  | 9 | 97.5 ± 0.7 | 94.0 ± 0.9 |
|  | 11 | 92.5 ± 1.1 | 90.5 ± 1.3 |
| Initial dye concentration (mg L-1) | MB 5 / CV 5 | 98.0 ± 0.6 | 97.0 ± 0.8 |
|  | MB 10 / CV 10 | 97.5 ± 0.7 | 94.0 ± 0.9 |
|  | MB 20 / CV 20 | 91.5 ± 1.2 | 89.5 ± 1.4 |
|  | MB 30 / CV 30 | 84.0 ± 1.5 | 81.5 ± 1.7 |
|  | MB 50 / CV 50 | 71.5 ± 2.0 | 68.5 ± 2.2 |
| Temperature (°C) | 20 | 91.5 ± 1.2 | 93.0 ± 1.3 |
|  | 25 | 97.5 ± 0.7 | 94.0 ± 0.9 |
|  | 30 | 94.0 ± 1.0 | 94.5 ± 1.1 |
|  | 40 | 96.0 ± 0.8 | 95.0 ± 1.0 |
|  | 50 | 97.0 ± 0.7 | 95.5 ± 0.9 |
|  | 60 | 97.5 ± 0.7 | 94.0 ± 0.9 |

Table S13. Time-dependent photocatalytic removal and adsorption capacity of MB and CV

| Irradiation time (min) | MB removal (%) | MB, qt (mg g-1) | CV removal (%) | CV, qt (mg g-1) |
| --- | --- | --- | --- | --- |
| 0 | 0.0 ± 0.0 | 0.00 | 0.0 ± 0.0 | 0.00 |
| 10 | 42.0 ± 1.5 | 8.40 | 37.5 ± 1.7 | 7.50 |
| 20 | 58.5 ± 1.6 | 11.70 | 51.0 ± 1.8 | 10.20 |
| 30 | 70.5 ± 1.7 | 14.10 | 62.5 ± 1.9 | 12.50 |
| 60 | 85.5 ± 1.3 | 17.10 | 78.0 ± 1.5 | 15.60 |
| 90 | 91.5 ± 1.1 | 18.30 | 84.0 ± 1.3 | 16.80 |
| 120 | 95.0 ± 0.9 | 19.00 | 88.0 ± 1.1 | 17.60 |
| 150 | 96.8 ± 0.8 | 19.36 | 92.0 ± 1.0 | 18.40 |
| 180 | 97.5 ± 0.7 | 19.50 | 94.0 ± 0.9 | 18.80 |

Note: qt was calculated from the percentage removal using qt = (C0-Ct) V/m, where C0 = 10 mg L-1, V = 0.100 L, and m = 0.050 g.

Table S14. Kinetic parameters for photocatalytic removal of MB and CV by Ag/Co/La2O3/chitosan nanocomposite.

| Kinetic model | Parameter | MB | CV |
| --- | --- | --- | --- |
| Experimental | qe,exp (mg g-1) | 19.50 | 18.80 |
| Pseudo-first-order | k1 (min-1) | 0.0296 | 0.0221 |
|  | qe,cal (mg g-1) | 14.54 | 13.38 |
|  | R2 | 0.9923 | 0.9852 |
| Pseudo-second-order | k2 (g mg-1 min-1) | 0.00308 | 0.00244 |
|  | qe,cal (mg g-1) | 21.28 | 20.75 |
|  | h (mg g-1 min-1) | 1.393 | 1.051 |
|  | R2 | 0.9998 | 0.9996 |
| Elovich | 1/β slope | 3.910 | 3.983 |
|  | intercept | 0.154 | -1.398 |
|  | R2 | 0.9723 | 0.9907 |
| Intraparticle diffusion | kid (mg g-1 min-1/2) | 1.027 | 1.063 |
|  | C (mg g-1) | 7.338 | 5.782 |
|  | R2 | 0.8825 | 0.9279 |

Table S15. Experimental equilibrium data used for adsorption isotherm analysis

| C0 (mg L-1) | MB removal (%) | MB Ce (mg L-1) | MB qe (mg g-1) | CV removal (%) | CV Ce (mg L-1) | CV qe (mg g-1) |
| --- | --- | --- | --- | --- | --- | --- |
| 5 | 98.0 | 0.10 | 9.80 | 97.0 | 0.15 | 9.70 |
| 10 | 97.5 | 0.25 | 19.50 | 94.0 | 0.60 | 18.80 |
| 20 | 91.5 | 1.70 | 36.60 | 89.5 | 2.10 | 35.80 |
| 30 | 84.0 | 4.80 | 50.40 | 81.5 | 5.55 | 48.90 |
| 50 | 71.5 | 14.25 | 71.50 | 68.5 | 15.75 | 68.50 |

Note: The qe values were calculated using qe = (C0-Ce) =V/m, where V = 0.100 L and m = 0.050 g. The values represent the adsorption capacity corresponding to the residual concentration after the 180-min treatment.

Table S16. Adsorption isotherm parameters and coefficients of determination (R2) for MB and CV adsorption by the Ag/Co/La2O3/chitosan nanocomposite.

| Isotherm model | Parameter | MB | CV |
| --- | --- | --- | --- |
| Langmuir | qmax(mg g-1) | 75.925 | 75.062 |
|  | KL(L mg-1) | 0.765 | 0.522 |
|  | R2 | 0.9828 | 0.9867 |
| Freundlich | KF[(mg g-1)(L mg-1)1/n] | 27.863 | 23.143 |
|  | n | 2.628 | 2.353 |
|  | R2 | 0.9731 | 0.9891 |
| Temkin | B(J mol-1) | 11.833 | 12.657 |
|  | AT(L mg-1) | 19.311 | 10.076 |
|  | R2 | 0.9741 | 0.9697 |
| Dubinin-Radushkevich | qs(mg g-1) | 50.727 | 44.697 |
|  | KDR(mol2 kJ-2) | 0.0490 | 0.0645 |
|  | E(kJ mol-1) | 3.193 | 2.784 |
|  | R2 | 0.9096 | 0.8082 |

Note: For the Langmuir model, qmax=1/slopeand KL=1/qmax×intercept. For the Freundlich model, n=1/slopeand KF=10intercept. For the Temkin model, B=slopeand AT=exp⁡intercept/B. For the D-R model, KDR=-slope, qs=exp⁡intercept, and E=2KDR-1/2. Linear regression was performed using the corresponding linearized forms of each isotherm.

Table S17. Temperature-dependent equilibrium parameters used for thermodynamic analysis of MB and CV removal by Ag/Co/La2O3/chitosan nanocomposite.

| Temperature (°C) | Temperature (K) | MB removal (%) | MB Ce (mg L-1) | MB qe (mg g-1) | MB Kc (L g-1) | CV removal (%) | CV Ce (mg L-1) | CV qe (mg g-1) | CV Kc (L g-1) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 20 | 293.15 | 91.5 | 0.85 | 18.30 | 21.529 | 93.0 | 0.70 | 18.60 | 26.571 |
| 25 | 298.15 | 97.5 | 0.25 | 19.50 | 78.000 | 94.0 | 0.60 | 18.80 | 31.333 |
| 30 | 303.15 | 94.0 | 0.60 | 18.80 | 31.333 | 94.5 | 0.55 | 18.90 | 34.364 |
| 40 | 313.15 | 96.0 | 0.40 | 19.20 | 48.000 | 95.0 | 0.50 | 19.00 | 38.000 |
| 50 | 323.15 | 97.0 | 0.30 | 19.40 | 64.667 | 95.5 | 0.45 | 19.10 | 42.444 |
| 60 | 333.15 | 97.5 | 0.25 | 19.50 | 78.000 | 94.0 | 0.60 | 18.80 | 31.333 |

Note: Ce=C01-R/100, qe=C0-CeV/m, and Kc=qe/Ce, where C0=10mg L⁻¹, V=0.100L, and m=0.050g. Kcis reported according to the commonly used adsorption equilibrium expression qe/Ce. For rigorous thermodynamic comparison, the convention used to define the equilibrium constant should be stated explicitly.

Table S18. Van’t Hoff parameters for thermodynamic analysis of MB and CV removal by Ag/Co/La2O3/chitosan nanocomposite.

| Temperature (°C) | Temperature (K) | 1/T (K-1) | ln Kc (MB) | ln Kc (CV) |
| --- | --- | --- | --- | --- |
| 20 | 293.15 | 0.0034112 | 3.0694 | 3.2798 |
| 25 | 298.15 | 0.0033540 | 4.3567 | 3.4447 |
| 30 | 303.15 | 0.0032987 | 3.4447 | 3.5370 |
| 40 | 313.15 | 0.0031934 | 3.8712 | 3.6376 |
| 50 | 323.15 | 0.0030945 | 4.1692 | 3.7482 |
| 60 | 333.15 | 0.0030017 | 4.3567 | 3.4447 |

lnKc versus 1T
using the linear Van’t Hoff equation:

lnKc=-ΔH∘R1T+ΔS∘R
where Kcis the adsorption equilibrium constant, Tis the absolute temperature (K), Ris the gas constant (8.314 J mol-1 K-1), ΔH∘is the standard enthalpy change, and ΔS∘is the standard entropy change.

Table S19. Thermodynamic parameters for MB and CV removal.

| Dye | Van’t Hoff slope | Intercept | R2 | ΔH° (kJ mol-1) | ΔS° (J mol-1 K-1) |
| --- | --- | --- | --- | --- | --- |
| MB | -2129.392 | 10.7465 | 0.4082 | +17.704 | +89.347 |
| CV | -560.257 | 5.3225 | 0.2897 | +4.658 | +44.251 |

The values were obtained from:

ΔH∘=-slope×R
ΔS°= intercept × R

Table S20. Gibbs free-energy changes for MB and CV removal.

| Temperature (°C) | Temperature (K) | ΔG° MB (kJ mol-1) | ΔG° CV (kJ mol-1) |
| --- | --- | --- | --- |
| 20 | 293.15 | -7.481 | -7.994 |
| 25 | 298.15 | -10.799 | -8.538 |
| 30 | 303.15 | -8.682 | -8.915 |
| 40 | 313.15 | -10.079 | -9.471 |
| 50 | 323.15 | -11.201 | -10.070 |
| 60 | 333.15 | -12.067 | -9.541 |

where:

ΔG∘=ΔH∘-TΔS∘
ΔG∘=-RTlnKc

Table S21. Reusability of Ag/Co/La2O3/chitosan nanocomposite.

| Cycle | MB removal (%) | CV removal (%) | MB retained activity (%) | CV retained activity (%) |
| --- | --- | --- | --- | --- |
| 1 | 97.5 ± 0.7 | 94.0 ± 0.9 | 100.00 | 100.00 |
| 2 | 96.8 ± 0.8 | 93.2 ± 1.0 | 99.28 | 99.15 |
| 3 | 95.9 ± 0.9 | 91.3 ± 1.1 | 98.36 | 97.13 |
| 4 | 94.8 ± 1.0 | 88.2 ± 1.2 | 97.23 | 93.83 |
| 5 | 93.7 ± 1.1 | 86.1 ± 1.3 | 96.10 | 91.60 |
| 6 | 92.6 ± 1.2 | 84.0 ± 1.4 | 94.97 | 89.36 |
| 7 | 91.5 ± 1.3 | 82.8 ± 1.5 | 93.85 | 88.09 |

Conditions: [MB]₀ = [CV]₀ = 10 mg L-1, catalyst dosage = 0.50 g L-1, pH = 9, 25 °C, irradiation = 180 min.

Table S22. Comparison of the photocatalytic performance of Ag/Co/La2O3/chitosan nanocomposite with recently reported photocatalytic materials.

| Photocatalyst | Target dye(s) | Irradiation | pH | Time (min) | Removal (%) | Reusability | Ref. |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Ag/Co/La2O3/CS NC | MB + CV | Light irradiation | 9.0 | 180 | MB: 97.5; CV: 94.0 | MB: 93.85%; CV: 88.09% after 7 cycles | This work |
| MgFe2O4-TiO2/chitosan | MB | Light irradiation | - | 60 | 99.53 | Not stated | [1] |
| TiO2/ZnO-chitosan | MB | Visible light | - | 90 | ≈99 | 89% after 4 cycles | [2] |
| TiO2 nanostructure | MB + CV | Direct sunlight | - | 30 | ≈100 | Up to 10 cycles | [3] |
| Zr-modified ETS-4 | MB | Visible light | - | Not stated | 86.6 | Not stated | [4] |
| Zr-modified ETS-4 | CV | Visible light | - | Not stated | 76.6 | Not stated | [4] |
| Co2GeO4/m-g-C3N4 | MB + CV | Visible light | - | 30 | MB: 95.5; CV: 95.0 | 4 cycles | [5] |
| CaMoO4/g-C3N4 | MB + CV | Photocatalysis | - | Not stated | High removal | 3 cycles | [6] |

Table S23. Silver and cobalt release from Ag/Co/La2O3/chitosan nanocomposite at different nanocomposite concentrations after incubation in deionized water at 37 ± 1 °C and 150 rpm for 24 h. Metal concentrations were determined by atomic absorption spectrophotometry using acid-digested nanocomposite controls as the reference for total extractable metal content. Values are presented as mean ± SD (n = 3).

| Ag/Co/La2O3/chitosan NC concentration (g/L) | Ag release (mg/L) | Co release (mg/L) | Ag release (%) | Co release (%) |
| --- | --- | --- | --- | --- |
| 0.10 | 0.18 ± 0.02 | 0.09 ± 0.01 | 3.6 | 2.7 |
| 0.25 | 0.42 ± 0.04 | 0.21 ± 0.02 | 3.4 | 2.5 |
| 0.50 | 0.81 ± 0.06 | 0.40 ± 0.03 | 3.2 | 2.4 |
| 0.75 | 1.17 ± 0.08 | 0.57 ± 0.04 | 3.1 | 2.3 |
| 1.00 | 1.52 ± 0.10 | 0.73 ± 0.05 | 3.0 | 2.2 |

Table S24. Concentration-dependent generation of reactive oxygen species (ROS) by the Ag/Co/La2O3/chitosan NC. ROS generation was determined using the 2’,7’-dichlorodihydrofluorescein diacetate (DCFH-DA) fluorescent probe at increasing concentrations of the nanocomposite. The fluorescence intensity of the oxidized DCFH-DA product was measured under identical incubation conditions. Relative ROS generation was calculated relative to the untreated control. Values are presented as mean ± SD (n = 3).

| Ag/Co/La2O3/chitosan NC concentration (µg mL-1) | DCFH-DA fluorescence intensity (a.u.) | Relative ROS generation (%) |
| --- | --- | --- |
| 25 | 118.4 ± 4.2 | 18.4 ± 1.5 |
| 50 | 143.7 ± 5.1 | 29.7 ± 1.8 |
| 100 | 186.5 ± 6.3 | 45.8 ± 2.2 |
| 200 | 254.8 ± 8.1 | 65.9 ± 2.7 |
| 400 | 341.6 ± 10.4 | 91.3 ± 3.1 |
| 800 | 458.2 ± 13.7 | 132.6 ± 4.0 |
| 1000 | 501.5 ± 14.8 | 144.2 ± 4.3 |

Table S25. FTIR spectral characteristics of Crystal Violet (CV), Methylene Blue (MB), CV and MB after treatment with the Ag/Co/La2O3/chitosan nanocomposite, and the treated CV/MB binary dye mixture. Wavenumbers are reported as whole-number values. The observed spectral shifts, attenuation, and disappearance of characteristic dye bands were used to assess changes in the molecular environment and chemical structure of the dyes following nanocomposite treatment.

| Sample | Wavenumbers (cm-1) | Major functional-group/vibrational assignments | Interpretation |
| --- | --- | --- | --- |
| Crystal Violet (CV) | 3382, 3213, 1662, 1583, 1518, 1478, 1440, 1362, 1328, 1290, 1221, 1185, 1163, 1110, 1058, 938, 907, 833, 795, 755, 721, 663, 618, 561, 508, 415 | O-H/N-H stretching; aromatic C=C/C=N vibrations; aromatic C-C skeletal vibrations; C-N stretching; C-H in-plane/out-of-plane bending; fingerprint-region aromatic/ring vibrations | The numerous characteristic bands confirm the aromatic and amine-rich structure of CV. The broad high-wavenumber bands indicate O-H/N-H-type stretching, whereas the bands around 1583-1478 cm-1 are mainly associated with aromatic skeletal vibrations. |
| Methylene Blue (MB) | 2987, 2902, 1640, 1587, 1526, 1483, 1439, 1382, 1317, 1276, 1238, 1208, 1165, 1127, 1073, 1032, 942, 921, 876, 819, 701, 660, 616, 529, 489, 445, 391 | Aliphatic C-H stretching; aromatic C=C/C=N vibrations; C-N stretching; aromatic C-H bending; heterocyclic/ring vibrations; fingerprint-region skeletal vibrations | The MB spectrum displays the expected aromatic heterocyclic and amine-associated vibrations. The bands at approximately 1587, 1526, 1483, and 1439 cm-1 are characteristic of aromatic/heterocyclic skeletal vibrations, while the lower-wavenumber bands represent ring and fingerprint-region modes. |
| CV after treatment with Ag/Co/La2O3/chitosan NC | 3300, 3261, 2921, 1665, 1532, 1446, 1409, 1301, 1152, 1078, 1014, 983, 891, 821, 665, 609 | O-H/N-H stretching; aliphatic C–H stretching; aromatic C=C/C=N vibrations; C-N/C-O-related vibrations; aromatic C-H bending; fingerprint-region ring vibrations | Treatment produced substantial attenuation/disappearance of several CV bands and shifts of the remaining bands. The disappearance of many fingerprint-region signals and changes around 3300, 1665, 1532, and 1446 cm-1 indicate alteration of the dye molecular environment following nanocomposite treatment. |
| MB after treatment with Ag/Co/La2O3/chitosan NC | 3297, 1552, 1531, 1449, 1407, 1332, 1302, 1150, 1078, 1014, 983, 941, 821, 665, 609, 466 | O-H/N-H stretching; aromatic/heterocyclic C=C/C=N vibrations; C-N/C-O-related vibrations; aromatic C-H bending; ring/fingerprint vibrations | Compared with untreated MB, several characteristic bands disappeared or decreased, while the remaining bands exhibited positional changes. These spectral modifications demonstrate changes in the chemical environment of MB after nanocomposite treatment and support interaction/degradation of the dye. |
| CV/MB binary mixture after treatment with Ag/Co/La2O3/chitosan NC | 3346, 2917, 1586, 1252, 1024, 990, 790, 612, 532, 464, 415 | O-H/N-H stretching; aliphatic C-H stretching; aromatic/heterocyclic skeletal vibrations; C-N/C-O-related vibrations; aromatic C-H out-of-plane bending; fingerprint-region vibrations | The binary treated sample exhibited a markedly simplified FTIR profile compared with the individual untreated dyes. The disappearance of numerous CV- and MB-associated bands and the persistence of only selected vibrational features indicate substantial modification/removal of dye-related molecular structures during nanocomposite treatment. |

References

[1]	Hieu, N.H., Hai, N.D., Dat, N.M., Nam, N.T.H., Giang, N.T.H., Cong, C.Q. and Huong, L.M., 2024. Chitosan-mediated coupling of MgFe2O4–TiO2 nanocomposites for efficient methylene blue photodegradation. ACS Applied Nano Materials, 7(6), pp.6583-6595.

[2]	Adnan, M.A.M., Majnis, M.F., Norman, M.A.M., Rahman, M.D.A., Johan, M.R. and Julkapli, N.M., 2025. Visible-light-activated TiO2/ZnO-chitosan catalyst for photodegradation of methylene blue dye: An experimental and predictive modelling using artificial neural networks. Journal of Water Process Engineering, 77, p.108423.

[3]	Sanadi, P.D., Chougale, R.K., Malavekar, D.B., Kim, J.H., Masimukku, S., Chang-Chien, G.P., Lee, Y.Y., Ghaware, R.C., Kolekar, S.S. and Kamble, G.S., 2025. Controllable synthesis of semiconducting anatase TiO2 nanostructures for visible light driven photocatalytic degradation of crystal violet and methylene blue dye. Spectrochimica Acta Part A: Molecular and Biomolecular Spectroscopy, 341, p.126404.

[4]	Lazarova, H.I., Rusew, R.I., Tsvetanova, L.V., Barbov, B.Z., Tacheva, E.S. and Shivachev, B.L., 2025. Elaboration and Characterization of Different Zirconium Modified ETS Photocatalysts for the Degradation of Crystal Violet and Methylene Blue. ChemistryOpen, 14(3), p.e202400348.

[5]	Amritha, V.K., Mukundan, G. and Badhulika, S., 2025. Rapid photocatalytic degradation of organic dyes using Co2GeO4/mesoporous graphitic carbon nitride (g-C3N4) heterojunction. Materials Science and Engineering: B, 320, p.118426.

[6]	Castro, M.A.M., Tranquilin, R.L., Paiva, A.E.M., Teodoro, M.D., Correa, M.A., Motta, F.V. and Bomio, M.R.D., 2024. Improvement of dye degradation by photocatalysis and synergistic effect of sonophotocatalysis processes using CaMoO4/g-C3N4 heterojunction. Optik, 300, p.171682.