Supplementary Section 1:

Optical Properties of ML-TMDCs

*Calculation of the Absorption Coefficient of ML-TMDCs

Analytical investigation of the optical properties of ML-TMDCs, including the absorption coefficient and oscillator strengths between different energy states, based on a Hamiltonian formalism, is one of the main objectives of this study. In the following, employing a semiclassical approach in conjunction with perturbation theory, we derive fully analytical expressions for the interaction Hamiltonian and the absorption coefficient of the considered structure. We begin with the massive Dirac-like Hamiltonian governing ML-TMDCs and define the Fermi velocity of the monolayer as vf=atℏ​. The Hamiltonian for the structure under consideration can then be written as follows [1–3]:

Η=ℏvf τkxσx+kyσy+∆2σz+λsτ2I2-σz            (A1)

σx,y,z denotes the Pauli matrices, a is the lattice constant of each ML-TMDC with a hexagonal crystal structure, t is the effective hopping energy, Δ is the monolayer band gap, and 2λ represents the spin–orbit coupling (SOC) splitting. The indices s and τ denote the spin and valley indices, respectively, with τ=±1 corresponding to the K and K' valleys. The parameters of the ML-TMDC Hamiltonian for the different materials considered in this study are summarized in Table A1.

Table A1. Structural parameters of various ML-TMDC semiconductors

| 2λ (eV) | t (eV) | ∆ (eV) | z=a (A°) | Material |
| --- | --- | --- | --- | --- |
| 0.15 | 1.10 | 1.66 | 3.193 | ML-MoS₂ |
| 0.18 | 0.94 | 1.47 | 3.313 | ML-MoSe₂ |
| 0.43 | 1.37 | 1.79 | 3.197 | ML-WS₂ |
| 0.46 | 1.19 | 1.60 | 3.310 | ML-WSe₂ |

In the presence of an electromagnetic field, the momentum is modified according to p→p+ecA, where p denotes the electron momentum operator and A is the vector potential. Accordingly, the Hamiltonian of the monolayer in the presence of the electromagnetic field can be written as follows:

Η=-iℏvFτσx∂x-eiℏcAx+σy∂y-eiℏcAy+Δ2σz-λτs2(σz-1)       (A2)

Thus, the total Hamiltonian of the system in the presence of the electromagnetic field can be expressed as Ht=ΗTMDC+Hem. This Hamiltonian can be conveniently decomposed into a non-interacting Hamiltonian (H0) and an interaction Hamiltonian (Hint), such that it can be rewritten as Ht=H0+Hint. Finally, by defining σ for the K valley as σ=σxi+σyj, the interaction Hamiltonian for this valley can be simplified to Hint=evFcσ.A. Likewise, by defining σ' for the K' valley as σ'=-σxi+σyj, the corresponding interaction Hamiltonian for this valley is obtained as Hint=evFcσ'.A.

The effect of the electromagnetic field on the solid-state system is treated as a perturbation, driving the system from its initial state ψi to a final state ψf after a time t. Within first-order perturbation theory, only the term linear in the electromagnetic field is retained, given by HA=Hint. We then examine the transition between the initial and final states induced by the incident light. By considering the time-dependent Schrödinger equation and carrying out the necessary calculations, the final form of Fermi’s golden rule is obtained as follows:

aftf=-iℏtitfHint,fie-iE0i-E0ftℏdt               (A3)

Consequently, Pfi=af(tf)2 represents the transition probability of a carrier from the initial state ψi to the final state ψf. We assume that a classical optical field E is incident on the system and is described by:

E=-E0cos(k'⋅r-ωt)e'           (A4)

where e' denotes the polarization vector of the incident electromagnetic field and ω is the corresponding angular frequency. If the electromagnetic wave is incident on the x-y plane at an θ angle (Fig. 1), the coordinates of the incident wave are denoted by primed coordinates, whereas the coordinates of the structure are represented by unprimed coordinates. Accordingly, based on the considerations presented above, if the propagation direction of the electromagnetic wave is x' along (k'=kx'), the circular polarization vectors in the primed coordinate system for right- and left-handed circularly polarized light are given by e'RHS=(y'+iz')2 and e'LHS=(y'-iz')2, respectively.

Using the three relations given above, together with the interaction Hamiltonian of the structure and the defined classical electromagnetic field, we proceed to solve the problem. We define the vector potential associated with the incident field as Aopt=icEω. For the K valley, substituting this vector potential and the classical optical field into Hint yields the following interaction Hamiltonian:

Hint=E0evF2iω[eik'⋅r-ωt+e-ik'⋅r-ωt]σ∙e'              (A5)

When light is incident on the system, it can induce electric dipole, electric quadrupole, and magnetic dipole transitions in the material.

We assume that the incident radiation lies in the visible and infrared spectral ranges, with a wavelength of approximately λ=400-600 nm, which is much larger than the unit-cell size of the ML-TMDCs, Λ=0.3-0.4 nm, i.e., λ≫Λ. Therefore, we can infer the relation k⋅r≪1, and the interaction Hamiltonian takes the form Hint≅p+ik⋅rp≅p. Under these physical conditions, the electric-dipole contribution is the dominant transition mechanism. Accordingly, we employ the electric-dipole approximation. Finally, Hint is obtained in the form Hint=E0evF2iω[eiωt+e-iωt]σ∙e'.

We now return to the calculation of the transition probability. To evaluate this quantity, we first need to calculate Hint,fi in the form Hint,fix=E0evF2iωeiωt+e-iωt<ψ0fqσ∙e'ψ0iq>. Furthermore, according to the definition of E0f-E0i=ℏωfi, the above integral can be rewritten as:

titfHint,fie-iE0i-E0ftℏdt=titf(E0evF2iωeiωt+e-iωt<ψ0fqσ∙e'ψ0iq>)eiωfitdt        (A6)

By defining Fx as Fx=<ψ0fqσ∙e'ψ0iq>, and noting that the wavefunctions have no explicit time dependence, the above expression can be written as titfHint,fie-iE0i-E0ftℏdt=E0evF2iωFxtitfei(ωfi+ω)t+ei(ωfi-ω)tdt. Taking t as the transition time and employing the rotating-wave approximation, or equivalently considering the resonant transitions, together with the properties of the Dirac delta function, we obtain the transition probability in the following form:

Pfi=E0evFFxℏω2πt2δωfi-ω                  (A7)

The total transition probability Pt is obtained by integrating over all the states involved in the transition and is defined as Pt=E0evFℏω2t8π-∞+∞Fx2δωfi-ωdK.

Interband absorption is the dominant absorption mechanism and is particularly important in crystals with a direct band gap. The dependence of the absorption coefficient on the frequency of the incident electromagnetic radiation can be determined from the definition of the absorption coefficient. Considering the transition in the vicinity of K=0, introducing the reduced mass as 1mr=1mc+1mv, and applying the divergence theorem to convert the volume integral into a surface integral, while accounting for the two-dimensional nature of the structure, the transition probability is obtained as

Pt=122E0evFFx2(mr)32ℏ2(ℏω-Eg(ℏω)2)t           (A8)

We next establish the relationship between the transition probability and the absorption coefficient. The absorption coefficient is defined as the transition rate per unit photon flux, given by α=1∅dPtotdt. The photon flux is, in turn, defined as the number of incident photons per unit area per unit time, i.e., ∅=<S>ℏω. It can also be determined from the time-averaged magnitude of the Poynting vector (S), normalized by the incident photon energy, according to <S>=12c0ε0n|E0|2. Therefore, based on these definitions, the absorption coefficient can be directly expressed in terms of the transition probability. Substituting the transition probability obtained for the present structure from Eq. (A8) yields the following fully analytical expression for the absorption coefficient:

αTMDC=e2vF2mr322c0ε0nℏ2Fx2[ℏω-Egℏω]Θℏω-Eg          (A9)

A key feature of ML-TMDCs is their unique optical response. Owing to their electronic structure and the associated optical selection rules, light with e'RHS​ polarization couples selectively to the K valley, whereas light with e'LHS​ polarization couples selectively to the K' valley. As discussed above, for the K valley, the matrix σ, which was defined for an individual monolayer, takes the form σ=σxx+σyy. Similarly, when the K' valley is considered, σ' is defined as σ'=-σxx+σyy. Furthermore, as derived above, F(x) is given by Fx=<ψ0fqσ∙e'ψ0iq>. We can therefore obtain F(x) in the unprimed coordinate system by transforming the primed coordinates using the corresponding coordinate-transformation matrix. After carrying out the necessary algebra, F(x) is obtained in the following form:

Fx=<ψ0fqσ∙e'ψ0iq>=                      FRHSx=12i±sinθF1x+F2x   for K(K') valleyFLHSx=12i∓sinθF1x+F2x   for K(K') valley          (A10)

If the functions g1(2)​ are defined as g1(2)=ψ0f,A*qψ0i,Bq±ψ0f,B*qψ0i,Aq, and the relation F1(2)x=-∞+∞dxg1(2) is satisfied, then FRHSx can be simplified and expressed as FRHSx=12i(sinθF1x+F2x). We can next consider the K' valley for light with the same right-handed circular polarization. Following the same procedure and using the definitions introduced above, we ultimately obtain the relation FRHSx=12i(-sinθF1x+F2x) for this particular case. The same analysis can then be repeated for left-handed circularly polarized light.

In the subsequent calculations, we need to derive analytical expressions for the coefficients F1(2)​ consistent with the specific structure under consideration. Owing to their crystal structure, ML-TMDCs consist of two sublattices, denoted by A and B. Accordingly, the wavefunction of these materials is represented by a two-component spinor, ψk=ψk,Aψk,B, and the corresponding eigenfunctions and eigenvalues have been extensively reported in the literature [4,5]. By employing these material-specific properties together with Fourier transformations, we evaluate the integral in two-dimensional polar coordinates and ultimately obtain the following analytical expression:

F1=π33(ΔsτℏvF)2[1-1+(2ℏvFΔsτ)2kcutoff232]        (A11)

Here, the effective band gap is defined as Δsτ=Δ-λsτ, and the relation kcutoff=πalattice has also been used. This model therefore describes the carriers in the vicinity of the K and K' points in momentum space, with the corresponding wave functions represented in spinor form. The same procedure can subsequently be applied to F2, which ultimately leads to the same expression given above. Consequently, we obtain F1​=F2.

Oscillator Strength (ffi):

An important optical parameter of the structure is the quantum-mechanical oscillator strength. In quantum mechanics, the dimensionless quantity ffi​ is referred to as the oscillator strength associated with the transition frequency ωfi and is defined as ffi=2mωfie2ℏ|dfi|2, where dfi​ denotes the electric-dipole matrix element between the initial and final states. The central task in this section is therefore to calculate the dipole moment for the system under consideration, namely, to evaluate dfi=<ψferψi>. To calculate this quantity, we first evaluate the commutator of the position operator r with the Hamiltonian H, i.e., r,Htx. Considering the K valley and rewriting the Hamiltonian of the structure, the Hamiltonian takes the form Ηt=vFσ∙p+Δ2σz-λs2(σz-1). Since the position operator r commutes with the spin components, r,σz=0, we obtain r,Htx=r,vFσ∙p=iℏvFσ.

Sandwiching this relation between the initial and final states of the system yields <ψ0fr,Htxψ0i>=iℏ<ψ0fvFσψ0i>. On the other hand, expanding the first term on the right-hand side of this relation gives <ψ0fr,Htxψ0i>=(Ei-Ef)<ψ0frψ0i>. Comparing this result with the second part of the relation ultimately leads to the following expressions for the dipole-moment matrix elements in the K and K' valleys:

dfi=<ψ0ferψ0i>=eℏvFiℏωfi<ψ0fσψ0i>            for K valleydfi'=<ψ0ferψ0i>=eℏvFiℏωfi<ψ0fσ'ψ0i>        for K' valley         (A12)

Consequently, the oscillator strength ffi​, which plays a crucial role in determining the optical absorption, is obtained as

ffi=2mvF2ℏωfi|<ψ0fσψ0i>|2               for K valleyffi'=2mvF2ℏωfi|<ψ0fσ'ψ0i>|2           for K 'valley            (A13)

Finally, using the definitions of σ and σ' for the K and K ' valleys, respectively, together with the expressions for F1(2)​, the modified expression for the oscillator strength is obtained as

ffi=ffi'=2mvF2ℏωfiF1x2+F2x2       (A14)

In conclusion, a fully analytical framework has been developed here for investigating the optical properties of ML-TMDCs.

References (A):

[1] Xiao, D., Liu, G. B., Feng, W., Xu, X., & Yao, W. (2012). Coupled spin and valley physics in monolayers of MoS 2 and other group-VI dichalcogenides. Physical review letters, 108(19), 196802.

[2] Liu, G. B., Xiao, D., Yao, Y., Xu, X., & Yao, W. (2015). Electronic structures and theoretical modelling of two-dimensional group-VIB transition metal dichalcogenides. Chemical Society Reviews, 44(9), 2643-2663.

[3] Kormányos, A., Burkard, G., Gmitra, M., Fabian, J., Zólyomi, V., Drummond, N. D., & Fal’ko, V. (2015). k· p theory for two-dimensional transition metal dichalcogenide semiconductors. 2D Materials, 2(2), 022001.

[4] Kormányos, A., Burkard, G., Gmitra, M., Fabian, J., Zólyomi, V., Drummond, N. D., & Fal’ko, V. (2015). k· p theory for two-dimensional transition metal dichalcogenide semiconductors. 2D Materials, 2(2), 022001.

[5] Xiao, D., Liu, G. B., Feng, W., Xu, X., & Yao, W. (2012). Coupled spin and valley physics in monolayers of MoS 2 and other group-VI dichalcogenides. Physical review letters, 108(19), 196802.