Online resource 1: Detailed methodologies and supplementary figures

How pore size distribution affects fracture-enhanced permeability in lava domes

Colombier, M.1, Kendrick, J.E.1, Birnbaum, J.1, Vasseur, J.1, Lamur, A.1, Lavallée, Y.1, Dobson K.J.2, Miwa, T.3, Scheu, B.1, Kueppers, U.1

1Department of Earth and Environmental Sciences, Ludwig-Maximilians-Universität München, Munich, Germany

2Department of Civil & Environmental Engineering, University of Strathclyde, Glasgow, United Kingdom

3National Research Institute for Earth Science and Disaster Resilience (NIED), Japan

Corresponding author: m.colombier@lmu.de

Figure SM1. The different segmentation and virtual cracking steps in our study.

Figure SM2. A 2D schematic illustration of the different segmentation methods used in our study prior to virtual cracking. a) Segmentation S1 was achieved by simple binarization of the porous network.  Macro-pores are largely connected to the exterior. Micro-pores are also strongly interconnected to one another, to macro-pores and to the exterior. b) Segmentation S2 was obtained by an erosion step of 2 pixels to remove micro-pores (either as individual clusters or as rims surrounding macro-pores). As a consequence of the micro-porosity removal, some macro-pores were no longer connected to one another and the whole pore network transitioned from permeable in S1 to impermeable in S2. c) Segmentation S3 was based on a separation of all pores present in S1, causing individualization and isolation of micro-pores and a reduction in size of macro-pores. Connectivity was significantly reduced in this step mostly as a result of the separation of micro-pores from the large interconnected cluster, as well as the separation of some macro-pores not connected anymore to the exterior.

Figure SM3. The clustered distribution of micro-pores in the Unzen dacite. The separation with macro-pores was obtained by an erosion of 2 pixels on S1 to exclude macro-pores. Note the presence of a large interconnected micro-pore cluster in blue, which may be caused by partial volume effect during segmentation (Ketcham and Carlson, 2001).