Supporting Information: Mechanism and Inhibition of Preferential Corrosion of Cold-Sprayed Copper in Dilute Nitric Acid

Sebastian A. Skaanvik1*, Sherry Cao1, Jessica E. M. Winslade1, Xuejie Li1, Diego A. Membreno1, Mehran Behazin2, Peter G. Keech3, David W. Shoesmith1,4, and James J. Noël1,4*

1Department of Chemistry, Western University, London, ON, N6A 5B7, Canada

2Nuclear Waste Management Organization, Toronto, ON, M4T 2S3, Canada

3Department of Chemical Engineering and Applied Chemistry, University of Toronto, Toronto, ON, M5S 3E5, Canada

4Surface Science Western, Western University, London, ON, N6G 0J3, Canada

Correspondence: sskaanvi@uwo.ca/jjnoel@uwo.ca

- Potentiodynamic Polarization Sequence

Figure S1: Sequence for potentiodynamic polarization experiments: i) initial period at the Ecorr to let the system reach a steady state (2 hours); ii) Cathodic sweep, starting from Ecorr; iii) 30-minute period at the Ecorr to let the system reach a steady state again; iv) Anodic sweep, starting from Ecorr; v) 60-minute period at the Ecorr; subsequently, the potentiodynamic polarization sequence was further carried out repetitively from step ii-v.

- Evaluation of Corrosion Damage at Particle-Particle Boundaries

Figure S2: Atomic force microscopy topographic imaging for determining the depth of corrosion damage at the particle-particle boundaries of cold-sprayed copper after immersion in 0.1 M HNO3 for 72 h under constant Ar-sparging.

- Evaluation of Particle-Particle Boundaries Dissolution Under Inert Conditions

Figure S3: Scanning electron micrograph of cold-sprayed copper after immersion in 0.05 M H2SO4 for 72 h under constant Ar-sparging.

- Atomic Force Microscopy Images of Cold-Sprayed Cu After Immersion in 0.1 M HNO3 + 4 mM HCl

Figure S4: Atomic force microscopy topography images of cold-sprayed copper after 72 h immersion in deaerated 0.1 M HNO3 + 4 mM HCl. A/B) Regions with no pores. C) Region with pores.

- Cu Particles Collected from Immersion Solution

Figure S5: Scanning electron micrograph of particles collected after 24 h immersion of cold-sprayed copper in aerated 0.1 M HNO3.

- Potentiodynamic Polarization Curves of Wrought Copper in 0.1 M HNO3

Figure S6: Potentiodynamic polarization curves of oxygen-free, phosphorus-doped, wrought copper in deaerated 0.1 M HNO3. The scan rate was 2 mV/s, and scans started at Ecorr.

- Effect of Chloride on Oxygen Evolution on Copper in 0.05 M H2SO4

Figure S7: Potentiodynamic polarization curves of oxygen-free, phosphorus-doped, wrought copper in aerated, 0.1 M HNO3 without (A) and with (B) 4 mM HCl . The scan rate was 2 mV/s, and scans started at Ecorr.