Table 1: Descriptive statistical data on experimental results.

| Literature | SiO₂ (%) | OPC Compressive Strength (MPa) | WSA (%) | WAS Compressive Strength (MPa) | OPC Split Tensile Strength (MPa) |  | WSA Split Tensile Strength, (MPa) |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Babar et al. (2022) | 73.95 | 32.56 | 5 | 33.83 | - |  | - |
|  |  |  | 10 | 35.10 | - |  | - |
|  |  |  | 15 | 31.63 | - |  | - |
|  |  |  | 20 | 29.72 | - |  | - |
| Qudoos et al. (2019) | 65.70 | 62.00 | 20 | 65.00 | 5.50 |  | 5.80 |
| Ahmad et al. (2021) | 39.63 | 28.10 | 10 | 33.20 | 3.40 |  | 3.80 |
| Katman et al. (2022) | 67.34 | 27.00 | 5 | 29.00 | 2.90 |  | 3.10 |
|  |  |  | 10 | 30.00 | - |  | 3.20 |
|  |  |  | 15 | 30.50 | - |  | 3.25 |
|  |  |  | 20 | 32.50 | - |  | 3.40 |
| Amin et al. (2019) | 53.69 | 19.50 | 15 | 19.00 | - |  | - |
|  |  |  | 20 | 18.60 | - |  | - |
|  |  |  | 25 | 15.30 | - |  | - |
|  |  |  | 30 | 10.70 | - |  | - |
| Khushnood et al. (2014) | 73.95 | 65.00 | 10 | 68.00 | 18.50 |  | 19.00 |
| Memon et al. (2021) | 71.98 | 22.00 | 5 | 27.00 | - |  | - |
|  |  |  | 10 | 26.00 | - |  | - |
|  |  |  | 15 | 27.00 | - |  | - |
|  |  |  | 20 | 22.00 | - |  | - |
| Bheel et al. (2021) | 67.34 | 29.80 | 10 | 31.50 | 3.10 |  | 3.28 |
|  |  |  | 20 | 32.70 | - |  | 3.40 |
|  |  |  | 30 | 33.20 | - |  | 3.44 |
|  |  |  | 40 | 30.50 | - |  | 3.12 |
| Sayed et al. (2019) | 50.00 | - | 5 | 42.00 | 4.23 |  | 3.57 |
|  |  |  | 10 | 44.00 | - |  | 3.74 |
|  |  |  | 15 | 51.00 | - |  | 4.34 |
|  |  |  | 20 | 45.00 | - |  | 3.83 |
| Siffat et al. (2021) | 61.07 | 41.10 | 10 | 40.50 | 2.74 |  | 2.69 |
|  |  |  | 20 | 43.36 | - |  | 2.77 |
| Dogruyol & Catin (2025) | 85.19 | 41.00 | 2.5 | 45.00 | - |  | - |
|  |  |  | 5 | 47.00 | - |  | - |
|  |  |  | 7.5 | 48.00 | - |  | - |
|  |  |  | 10 | 43.00 | - |  | - |
| Hossain et al. (2025) | - | 27.50 | 5% | 28.5 |  | 2.6 | 2.75 2.85 2.45 2.20 |
|  |  |  | 10% | 31.0 |  |  |  |
|  |  |  | 15% | 26.0 |  |  |  |
|  |  |  | 20% | 22.8 |  |  |  |
| Jankovsky et al. (2017) | 47.5 | 64.5 | 10% | 67.7 |  | - | - |
|  |  |  | 15% | 65.2 |  |  |  |
|  |  |  | 20% | 59.8 |  |  |  |
| Darweesh & MR (2020) | 57.0 | - | 4% | 60.0 |  | - | - |
|  |  |  | 8% | 64.0 |  |  |  |
|  |  |  | 12% | 68.0 |  |  |  |
|  |  |  | 16% | 70.0 |  |  |  |
|  |  |  | 20% | 53.5 |  |  |  |
| Hussein et al. (2024) | 48.7 | 30.0 | 2% | 46.0 |  | - | - |
|  |  |  | 4% | 47.2 |  |  |  |
|  |  |  | 6% | 49.4 |  |  |  |
|  |  |  | 8% | 51.2 |  |  |  |
| Khan et al. (2019) | 73.4 | 21.0 | 10% | 20.5 |  | - | - |
|  |  |  | 20% | 15.0 |  |  |  |
|  |  |  | 30% | 13.5 |  |  |  |

Table 2. Specification of high-strength cement type CEM I 42.5r according to the manufacturer.

Physical properties

Specific surface area:		 3.400cm2/g

Specific Gravity:	 	 3.10 g/cm3

Chemical Composition

____________________________________________________________________________________

Oxides % wt. of cement	 	SiO2 	Al2O3	 Fe2O3	 CaO	 MgO	  SO3	 LOI*		 	 	 	 	 	20.9	  5.1	  2.7     	  63.4	  2.1	  3.7	 3.5

LOI*: loss on ignition (residual carbon content).

Table 3. Physical properties of the Wheat Straw Ash (WSA).

WSA Types					WSA-1			WSA-2

Specific surface area (m2/Kg)		 	322 m2/kg			357 m2/kg

Mean particle size (μm)				28.53μm 			24.18μm

Table 4. Wheat Straw Ash (WSA) Chemical composition (% wt. of ash).

WSA Types	SiO2	Al2O3	Fe2O3 	CaO	K2O	P2O5	SO3 	 MgO	 LOI

WSA-1	 	83.16	2.96	2.51	1.37	2.57	1.13	1.09	1.65	3.53

WSA-2		90.8	1.61	1.8	1.09	1.25	0.45	0.52	1.06	1.35

Table 5. Mix proportion of WSA -concrete admixture

| WSA% | Cement (Kg/m3) | WSA (Kg/m3) | Water (Kg/m3) | Fine aggregate (Kg/m3) | Coarse Aggregate (Kg/m3) | SP (%wt. of binder) |
| --- | --- | --- | --- | --- | --- | --- |
| 0% | 460 | 0 | 230 | 785 | 800 | 0.25 |
| 5% | 437 | 23 | 230 | 785 | 800 | 0.25 |
| 10% | 414 | 46 | 230 | 785 | 800 | 0.25 |
| 15% | 391 | 69 | 230 | 785 | 800 | 0.25 |
| 20% | 368 | 92 | 230 | 785 | 800 | 0.25 |
| 25% | 345 | 115 | 230 | 785 | 800 | 0.50 |
| 30% | 322 | 138 | 230 | 785 | 800 | 0.50 |
| 35% | 299 | 161 | 230 | 785 | 800 | 1.00 |
| 40% | 276 | 184 | 230 | 785 | 800 | 1.00 |
| 45% | 253 | 207 | 230 | 785 | 800 | 1.50 |
| 50% | 230 | 230 | 230 | 785 | 800 | 2.00 |