Table 1 – Characterizations used on the modified electrode and the final solution.

| Analytical technique | Equipment | Operating conditions | Analysis objective |
| --- | --- | --- | --- |
| TGA | Netzsch brand, model STA 449 F3 Júpiter | Inert atphosphere with flow of 100 mL·min-1, heating rate of 20°C·min-1 over range of 25 to 800°C | To evaluate termal stability across a given temperature range |
| FT-IR | Bruker brand, model Vertex 7.0 | Attenuated total reflectance (ATR), spectral scan in the 4000 to 400 cm-1 region, resolution of 4 cm-1 over 64 scans | Identify the functional groups and chemical bonds present in the material |
| SEM/EDS | Tescan brand, model MIRA 3 | Operated at 8 kV, in temperature of 21 ± 3°C | Conduct an analysis of the material's surface |
| FAAS | Varian brand, model AA 240MS | Operating at a wavelength of 327 nm, compressed air/acetylene was used as the gas, and a hollow-cathode lamp was used | Iron concentration in the catalyst and in the final solution |

Source: Santana (2025)

Table 2 – Description of exposure times for each treatment system used for drug degradation

| Trials | Time of exposure to the system (min) |  | Time total of treatment (min) |
| --- | --- | --- | --- |
|  | Electro-Fenton | Photo-Fenton |  |
| 1 | 30 | 30 | 60 |
| 2 | 30 | 45 | 75 |
| 3 | 30 | 60 | 90 |
| 4 | 45 | 30 | 75 |
| 5 | 45 | 45 | 90 |
| 6 | 45 | 60 | 105 |
| 7 | 60 | 30 | 90 |
| 8 | 60 | 45 | 105 |
| 9 | 60 | 60 | 120 |

Source: the authors (2026)

Table 3 – Degradation and exposure times of the drug solution after being subjected to each treatment system

| Trials | Electro-Fenton |  | Photo-Fenton |  | Total time (min) | Total degradation (%) |
| --- | --- | --- | --- | --- | --- | --- |
|  | Time (min) | Degradation (%) | Time (min) | Degradation (%) |  |  |
| 1 | 30 | 66.42 | 30 | 11.21 | 60 | 77.63 |
| 2 | 30 | 65.19 | 45 | 22.11 | 75 | 87.30 |
| 3 | 30 | 64.66 | 60 | 26.04 | 90 | 90.70 |
| 4 | 45 | 77.13 | 30 | 18.09 | 75 | 95.22 |
| 5 | 45 | 75.83 | 45 | 17.17 | 90 | 93.00 |
| 6 | 45 | 76.71 | 60 | 17.40 | 105 | 94.11 |
| 7 | 60 | 86.72 | 30 | 8.31 | 90 | 95.03 |
| 8 | 60 | 84.38 | 45 | 8.77 | 105 | 93.15 |
| 9 | 60 | 85.26 | 60 | 10.78 | 120 | 96.34 |

Source: the authors (2026)

Table 4 – Kinetic parameters of the tested models

| Model | Parameter |  |
| --- | --- | --- |
| Chan; Chu (2003) | R2 | 0,97 |
|  | Sr2 | 2,01x10-3 |
|  | 1/σ | 1,053 ± 0,0292 |
|  | 1/ρ (min-1) | 0,080 ± 0,020 |
| He et al. (2016) | R2 | 0,91 |
|  | Sr2 | 7,49x10-3 |
|  | K (min-1) | 0,04 ± 0,005 |

Source: the authors (2026)

Table 5 – Germination index (GI) and root growth index (RGI) for broccoli-cabbage and yellow onion seeds exposed to the treated samples

| Samples | Broccoli-cabbage |  | Yellow onion |  |
| --- | --- | --- | --- | --- |
|  | GI (%) | RGI | GI (%) | RGI |
| Negative control | 100.0 | 1.00 | 100.00 | 1.00 |
| Inicial solution | 79.86 | 0.79 | 48.97 | 0.55 |
| 30 min | 56.90 | 0.56 | 28.86 | 0.51 |
| 60 min | 63.92 | 0.61 | 53.36 | 0.70 |
| 70 min | 48.07 | 0.52 | 63.31 | 0.78 |
| 90 min | 31.49 | 0.29 | 76.84 | 0.82 |
| 120 min | 57.06 | 0.55 | 93.76 | 0.88 |

Source: the authors (2026)

Table 6 – Bacterial growth results

| Samples | Escherichia coli |  | Salmonella enteritidis |  |
| --- | --- | --- | --- | --- |
|  | OD600 | Growth (%) | OD600 | Growth (%) |
| Negative control | 0.207±0.017 | 100.00 | 0.593±0.016 | 100.00 |
| Inicial solution | 0.135±0.054 | 65.14 | 0.485±0.010 | 81.87 |
| Final solution (EF) | 0.094±0.009 | 45.19 | 0.694±0.053 | 117.11 |
| Final solution (EF+PF) | 0.061±0.002 | 29.56 | 0.604±0.041 | 101.93 |

OD600 – Optical density measured turbidimetrically at 600 nm; EF = electro-Fenton and PF = photo-Fenton.

Source: the author (2026)