Cerium–Selenium Co-Substituted Hydroxyapatite Nanoparticles with Enhanced Bio-functional Performance for Bone Substitute Applications

Asfia Saeed1, Aalia Khanem2, Farwa Naqvi3, Maria Khalid4, Farhan Younas2, Almas Jabeen3, Muhammad Nawaz 5 Talha Nisar6, Veit Wagner6, Muhammad Raza Shah4, Ali Haider7, Abdul Samad Khan8

¹ Department of Dental Materials, Shifa College of Dentistry, Shifa Tameer-e-Millat University, Pakistan

² Center for Interdisciplinary Research in Basic Sciences (CIRBS), International Islamic University, Islamabad, Pakistan

³ Dr. Panjwani Center for Molecular Medicine and Drug Research, International Centre for Chemical and Biological Sciences, University of Karachi, Karachi, 75270, Pakistan

4 HEJ Research Institute of Chemistry, International Center for Chemical and Biological Sciences, University of Karachi, Karachi 75270, Pakistan

5 Department of Nano-Medicine Research, Institute for Research and Medical Consultations (IRMC), Imam Abdulrahman Bin Faisal University, Dammam, Saudi Arabia

6 School of Science, Constructor University, Campus ring 1, 28759, Bremen, Germany.

7 Department of Chemistry, Quaid-i-Azam University, Islamabad, Pakistan.

8 Department of Restorative Dental Sciences, College of Dentistry, Imam Abdulrahman Bin Faisal University, Dammam, Saudi Arabia

S1. Experimental Details

XRD

X-ray diffraction (XRD) was used to analyze the phase composition, crystallite size, lattice parameters, unit cell volume, lattice strain, and crystallinity of the synthesized nanoparticles. The lattice parameter a was determined from the (300) reflection, while the c parameter was calculated using the (002) and (004) reflections according to the following relation:

1d2=43h2+hk+k2a2+l2c2

Where d is the interplanar spacing and (hkl) are the Miller indices.

The unit cell volume (V) was calculated using the expression:

V=0.866 a2c

To determine the crystallite size, the Debye-Scherrer’s formula was used:

Xs=0.94λ​/βcos θ

Where Xs is the crystallite size (nm), λ is the wavelength of the X-ray beam, FWHM is the full width at half maximum for the diffraction peak under consideration (rad), and θ is the Bragg angle. Diffraction peaks (002), (211), and (300) were used for calculation, and the average crystallite size was reported.

The Williamson–Hall method was applied to determine lattice strain. Crystallinity was reported based on the sharpness of diffraction peaks and FWHM values. Crystallinity was classified as high for FWHM ≤ 0.1°, moderate for 0.1° < FWHM ≤ 0.2°, and low for FWHM > 0.2°.

Figure S1

Figure S1. FTIR spectra of as-prepared and calcined Hap, demonstrating increased crystallinity and reduction of adsorbed water upon calcination

Figure S2

Figure S2. XRD spectrum of synthesized pure HA index against JCPDS 09-0432