NAND and NOR logic-in-memory comprising silicon nanowire feedback field-effect transistors

Yejin Yang1, Juhee Jeon2, Jaemin Son2, Kyoungah Cho 2 and Sangsig Kim1,2*

1Department of Semiconductor Systems Engineering, Korea University, Republic of Korea

2Department of Electrical Engineering, Korea University, 145 Anam-ro, Seongbuk-gu, 
Seoul 02841, Republic of Korea

Table of contents

Supplementary Section 1 | Cross-sectional view of a single-gated SiNW FBFETs

Supplementary Section 2 | Logic performance of the NAND and NOR LIMs

Supplementary Section 3 | Dynamic voltage-transfer characteristics of NAND LIM sweeping VIN1 analyzed using timing diagrams and truth tables.

Supplementary Section 4 | Dynamic voltage-transfer characteristics of NAND LIM sweeping VIN2 with different pulse values of VIN1.

Supplementary Section 5 | Dynamic voltage-transfer characteristics of NAND LIM sweeping VIN2 analyzed using timing diagrams and truth tables.

Supplementary Section 6 | Dynamic voltage-transfer characteristics of NOR LIM in a sweep of VIN1 analyzed using timing diagrams and truth tables.

Supplementary Section 7 | Dynamic voltage-transfer characteristics of NOR LIM sweeping VIN2 with different pulse values of VIN1.

Supplementary Section 8 | Dynamic voltage-transfer characteristics of NOR LIM in a sweep of VIN2 analyzed using timing diagrams and truth tables.

Supplementary Section 1. Cross-sectional view of single-gated SiNW FBFETs

Figure S1 shows a cross-sectional view of the p- and n-FBFETs utilized in the NAND and NOR LIMs. The dimensional parameters of the p-FFBET, shown in Fig. S1(a), are a channel length (LCH) of 150 nm, a gate oxide thickness (TOX) of 6 nm, p+ drain and n+ source region lengths of 50 nm, and a silicon channel thickness (TSi) of 25 nm. The non-gated channel length (LNG) and gated channel length (LG) are 1/2LCH. All the doping concentrations of the p+ drain, n+ source, LNG, and LG regions were 1 × 1020 cm-3. The dimensional parameters of the n-FFBET shown in Fig. S1(b) are an LCH of 200 nm, a TOX of 3.4 nm, p+ drain and n+ source region lengths of 50 nm, and a TSi of 15 nm. The LNG and LG were 1/2LCH. The doping concentrations were 1 × 1020 cm-3 for the p+ drain and n+ source regions, 5 × 1019 cm-3 for the LNG region, and 9 × 1019 cm-3 for the LG region. The work functions of the gate metals are 4.1 eV for the p-FBFET and 5.0 eV for the n-FBFET.

Figure S1. Cross-sectional view of single-gated SiNW (a) p- and (b) n-FBFETs.

Supplementary Section 2. Logic performance of the NAND and NOR LIM

Figures S2(a) and (b) show the output voltage corresponding to the logic operation of the NAND and NOR LIM connected to the supply voltages (VDD and VSS). The plots shown in Figs. S2(a) and (b) illustrate VOUT versus time, which corresponds to the output logic when two-input voltage pulses are applied according to time with a certain sequence (‘00’, ‘01’, ‘10’, and ‘11’), that is, the dynamic logic circuit illustrates the logic operation of the LIM, which depends on the characteristics of the FBFETs that maintain the charge carriers in the channel region based on a positive feedback mechanism during the applied logic input pulses [1-4]. In the NAND LIM configuration, as shown in Fig. S2(a), when either one or both input pulses are low (input logic ‘0’) at VDD = 1.6 V and VSS = −2.5 V, the pull-up network (PUN) consisting of two p-FBFETs connected in parallel pulls VDD up to VOUT, while the pull-down network (PDN) consisting of two n-FBFETs connected in series is cut off. On the other hand, when both input pulses are high (input logic ‘1’), the PUN is cut off because the two p-FBFETs are turned off while the PDN pulls VOUT down to VSS because the two n-FBFETs are turned on. In the NOR LIM configuration, as shown in Fig. S2(b), when both input pulses are low at VDD = 2.5 V and VSS = −1.6 V, the PUN consisting of two p-FBFETs connected in series pulls VDD up to VOUT, while the PDN consisting of two n-FBFETs connected in parallel is cut off. On the other hand, when either one or both input pulses are high, the PUN is cut off because one or both of the p-FBFETs are turned off, while the PDN pulls VOUT down to VSS because one or both of the n-FBFETs are turned on. Although the output voltage levels exhibit a slight difference due to temporary variation in the number of charge carriers in the channel region when input pulses are applied, the output logic states of the NAND and NOR LIM are well-operated for the combination of input logic gates. Accordingly, the NAND and NOR LIM comprising the FBFETs can be compatible with CMOS gates comprising MOSFETs for logic operation. These results allow for an extension of the NAND and NOR LIM operations under dynamic conditions.

Figure S2. Timing diagrams of output voltage of (a) NAND and (b) NOR LIM with supply voltages of VDD and VSS. Insets show truth tables for four logic combinations.

Supplementary Section 3. Dynamic voltage-transfer characteristics of the NAND LIM sweeping VIN1 analyzed using timing diagram and truth table

Figure S3 shows the electrical characteristics of the NAND LIM, reflecting dynamic LIM operation conditions by changing the input node 1 (VIN1) logic state with a sequence of ‘1’, ‘0’, and ‘1’ while maintaining the input node 2 (VIN2) logic stage at ‘0’ and ‘1’, respectively. Figures S3(a) and (d) show the dynamic voltage-transfer characteristics (VTC) curves for operating VIN1 clockwise with pulses of (a) VIN2 = 1.0 V and (d) VIN2 = −1.0 V, corresponding to the blue and black lines, respectively (see Fig. 4(a) in the main text). Notation ① indicates the starting point, and notations ②–⑨ indicate a sequence of operating VIN1 clockwise, as shown in Figs. S3(a) and (d). To explain the consecutive operations in detail, these symbols are also used in Figs. S3(b), (c), (e), and (f). Figures S3(b) and (e) show timing diagrams reflecting the dynamic operation of a pulse width of 5 ns for input logic and a hold time of 10 ns for memory operation under all zero-bias conditions. Notation ①, the starting point of the graph, indicates the input logic ‘11’ (or ‘10’) in the truth table of the NAND LIM, and its corresponding results, output logic ‘0’ (or ‘1’), are also shown in Fig. S3(c) (and Fig. S3(f)). Notation ② indicates a ramping (rising/falling) time of 1 ns for the logic operation, which is the time to reach the next operation, notation ③. Notation ③ shows the hold ‘0’ (or ‘1’) operation that retains the previous output logic ‘0’ (or ‘1’) under VDD, VSS, VIN1, and VIN2 of 0.0 V. Notation ④ indicates a ramping time of 1 ns to proceed to the next notation ⑤. Notation ⑤ indicates the input logic ‘01’ (or ‘00’), and both output logics are set to ‘1’. To move to the next operation of holding output logic ‘1’, notation ⑥ indicates a ramping time of 1 ns. The hold ‘1’ values are maintained, which achieves approximately zero static power consumption shown in notation ⑦. After notation ⑧ operates, which represents a ramping time of 1 ns, the input logic ‘11’ (or ‘10’) corresponding to notation ⑨ operates. Finally, the closed memory windows of the dynamic VTCs are completed as the VIN1 sweeps clockwise to 1.0 V. Figures S3(a) shows a large memory window that indicates not only the input logic combinations ‘11’, ‘01’, and ‘11’ of the NAND LIM, but also the memory operation of the output logic under all zero bias conditions. Figure S3(d) shows a small memory window because the input logic combinations ‘10’, ‘00’, and ‘10’ result in similar output logic values of ‘1’. The notations ①, ⑤, and ⑨ operations, corresponding to the logic operation of the NAND LIM, are summarized in Figs. S3(c) and (f), respectively.

Figure S3. Dynamic VTCs of the NAND LIM sweeping VIN1 with pulse values of (a) VIN2 = 1.0 V and (d) VIN2 = −1.0 V. (b) and (e) indicate timing diagrams corresponding to the sequential dynamic VTCs, respectively. Tables (c) and (f) summarize the performed logic operations, respectively.

Supplementary Section 4. Dynamic voltage-transfer characteristics of the NAND LIM sweeping VIN2 with different pulse values of VIN1.

Figure S4. Dynamic VTCs of the NAND LIM sweeping VIN2 with different pulse values of VIN1.

Supplementary Section 5. Dynamic voltage-transfer characteristics of the NAND LIM sweeping VIN2 analyzed using timing diagrams and truth tables.

To confirm that the same LIM operation is performed regardless of the sweeping input nodes (VIN1 and VIN2), the VTCs shown in Fig. S5 are performed by changing the VIN2 state while maintaining the VIN1 logic state, as opposed to Fig. S3 in the NAND LIM operation. Figures. S5(a) and (d) show the dynamic VTC curves of operating VIN2 anticlockwise from 1.0 V while maintaining VIN1 of (a) 1.0 V and (d) −1.0 V, corresponding to the blue and black lines, respectively (see Fig. S4 in Supplementary Section 4). Notations ①–⑨ indicate a sequence of operating VIN2 anticlockwise, as shown in Figs. S5(a) and (d). Notation ① indicates the input logic ‘11’ (or ‘01’) in the truth table of the NAND LIM. Notation ② indicates a ramping time of 1 ns, which is the time to reach the next operation, notation ③. Notation ③ indicates hold ‘0’ (or ‘1’) that maintains the previous output logic ‘0’ (or ‘1’) operation under hold bias conditions. Notation ④ represents a ramping time of 1 ns to proceed to notation ⑤. Notation ⑤ shows that both output logic values are set to ‘1’ by applying input logic values of ‘10’ (or ‘00’). Notation ⑥ represents a ramping time of 1 ns to perform the next operation. The hold ‘1’s are maintained under all zero bias conditions shown in notation ⑦. After notation ⑧, a ramping time of 1 ns, notation ⑨ indicates the operation of the input logic ‘11’ (or ‘01’), and thereby the memory windows of the dynamic VTC are completed. Figures S5(c) and (f) are summaries of the logic operations performed in Figs. S5(a) and (d), respectively. Consequently, the memory windows, as shown in Figs. S5(a) and (d), show all the states of the NAND LIM operations under dynamic conditions, as shown in Fig. 2(a) of the main text. Moreover, the operations shown in Figs. S3 and S5 indicate that the same output logic is performed when the NAND LIM operation is performed regardless of the VIN1 and VIN2 that sweep.

Figure S5. Dynamic VTCs of the NAND LIM sweeping VIN2 with pulse values of (a) VIN1 = 1.0 V and (d) VIN1 = −1.0 V. (b) and (e) indicate timing diagrams corresponding to the sequential dynamic VTCs, respectively. Tables (c) and (f) summarize the performed logic operations, respectively.

Supplementary Section 6. Dynamic voltage-transfer characteristics of the NOR LIM in a sweep of VIN1 analyzed using timing diagrams and truth tables.

Figure S6 shows the dynamic VTCs reflecting the NOR LIM operation. Figures S6(a) and (d) show the dynamic VTC curves of operating VIN1 clockwise from 1.0 V while maintaining (a) VIN2 of 1.0 V and (d) −1.0 V, corresponding to the blue and black lines, respectively (see Fig. 4(b) in the main text). Notations ①–⑨ indicate a sequence of operating VIN1 clockwise, as shown in Figs. S6(a) and (d). Notation ① indicates input logic ‘11’ (or ‘10’) in the truth table of the NOR LIM. Notation ② represents a ramping time of 1 ns, which is the time required to reach notation ③. Notation ③ reflects the hold ‘0’ operation that stores the previous output logic ‘0’ under all zero bias conditions, respectively. Notation ④ indicates a ramping time of 1 ns to proceed to notation ⑤. Notation ⑤ indicates that the output logic is set to ‘0’ (or ‘1’) by applying input logic ‘01’ (or ‘00’). Notation ⑥ indicates a ramping time of 1 ns to perform the next operation. The hold ‘0’ (or ‘1’) is maintained under all zero-bias conditions shown in notation ⑦. After notation ⑧, indicating a ramping time of 1 ns, notation ⑨ shows the operation of input logic ‘11’ (or ‘10’), and thereby the memory windows of the dynamic VTC are completed. The memory windows, as shown in Figs. S6(a) and (d) reveal not only the logic operation of the NOR LIM but also the operation that stores the output logic, and the logic operation of the NOR LIM is summarized in Figs. S6(c) and (f), respectively.

Figure S6. Dynamic VTC of the NOR LIM in a sweep of VIN1 with pulse values of (a) VIN2 = 1.0 V and (d) VIN2 = −1.0 V. (b) and (e) indicate timing diagrams corresponding to the sequential dynamic VTCs, respectively. Tables (c) and (f) summarize the performed logic operations, respectively.

Supplementary Section 7. Dynamic voltage-transfer characteristics of NOR LIM in a sweep of VIN1

Figure S7. Dynamic VTCs of the NOR LIM sweeping VIN2 with different pulse values of VIN1.

Supplementary Section 8. Dynamic voltage-transfer characteristics of the NOR LIM in a sweep of VIN2 analyzed using timing diagrams and truth tables.

Figure S8 shows a similarity to the operation shown in Fig. S6, except for changing VIN2 and maintaining VIN1 in the NOR LIM operation. Figures S8(a) and (d) show the dynamic VTC curves of operating VIN2 anticlockwise from 1.0 V while maintaining VIN1 of (a) 1.0 V and (d) −1.0 V, corresponding to the blue and black lines, respectively (see Fig. S7 in Supplementary Section 7). Notations ①–⑨ indicate a sequence of operating VIN2 anticlockwise, as shown in Figs. S8(a) and (d). Notation ① indicates the input logic ‘11’ (or ‘01’) in the truth table of the NOR LIM. Notation ② represents a ramping time of 1 ns, which is the time required to reach notation ③. Notation ③ indicates the hold ‘0’ operation that holds the previous output logic ‘0’ under the hold bias conditions. Notation ④ indicates a ramping time of 1 ns to proceed to notation ⑤. Notation ⑤ shows that the output logic is set to ‘0’ (or ‘1’) by applying the input logic ‘10’ (or ‘00’). Notation ⑥ indicates a ramping time of 1 ns to perform the next operation. The hold ‘0’ (or ‘1’) is maintained under all zero-bias conditions shown in notation ⑦. After notation ⑧, indicating a ramping time of 1 ns, the input logic ‘11’ (or ‘01’) operates as shown in notation ⑨, and thereby the memory windows of the dynamic VTC are completed. Figures S8(c) and (f) are summaries of the logic operations conducted in Figs. S8(a) and (d), respectively. The NOR LIM operation is a well-defined logical output regardless of the VIN1 and VIN2 that sweep, as shown in Figs. S6 and S8. As a result, the proposed dynamic VTCs provide new evidence for the proposed LIM operation interpretation under dynamic conditions.

Figure S8. Dynamic VTC of the NOR LIM in a sweep of VIN2 with pulse values of (a) VIN1 = 1.0 V and (d) VIN1 = −1.0 V. (b) and (e) indicate timing diagrams corresponding to the sequential dynamic VTCs, respectively. Tables (c) and (f) summarize the performed logic operations, respectively.

References:

1. Kim, J.-S. et al. Dynamic Logic Circuits Using a-IGZO TFTs. IEEE Trans. Electron Devices 64, 4123-4130 (2017).

2. Kim, M. et al. Steep switching characteristics of single-gated feedback field-effect transistors. Nanotechnology 28, 055205 (2017).

3. Kim, Y. et al. Switchable‐Memory Operation of Silicon Nanowire Transistor. Adv. Electron. Mater. 4, 1800429 (2018).

4. Woo, S. et al. Device design of single-gated feedback field-effect transistors to achieve latch-up behaviors with high current gains. Curr. Appl. Phys. 20, 1156-1162 (2020).