Supplementary Materials for

Phase-locked Constructing Dynamic Supramolecular Ionic Conductive Elastomers with Superior Toughness, Autonomous Self-healing and Recyclability

Jing Chen1, Yiyang Gao1, Lei Shi2, Wei Yu1, Zongjie Sun1, Shuang Liu3, Heng Mao1, Dongyang Zhang1, Quan Chen3, Demei Yu1, Shujiang Ding1*

1School of Chemistry, Xi'an Jiaotong University, Xi'an Key Laboratory of Sustainable Energy Materials Chemistry, State Key Laboratory for Mechanical Behavior of Materials, Xi'an 710049, P. R. China

2School of Materials, Sun Yat-sen University, Shenzhen 518107, P. R. China

3StateKey Laboratory of Polymer Physics and Chemistry, Changchun Institute of Applied Chemistry, Chinese Academy of Sciences, Changchun 130022, P. R. China

* Corresponding author. Email: dingsj@xjtu.edu.cn

This PDF file includes:

Figs. S1 to S20

Tables S1 to S2

Movies S1 to S3

Fig. S1. Synthetic route of dynamic supramolecular elastomers (DSE) via condensation polymerization.

Fig. S2. 1H NMR spectra of DSE-0~3 in CDCl3 (400 MHz). In the 1H NMR spectra, the peaks of PTMEG protons appeared at 3.4 and 1.6 ppm, the peaks of HMDI unit appeared at 1.1~0.9 ppm, the peaks of HEDS unit appeared at 3.7 and 2.7 ppm, the three characteristic peaks of 12.99, 11.89 and 9.93 ppm in the downfield was observed in the DSE-1, DSE-2 and DSE-3, which demonstrated the existence of the UPy motifs.

Fig. S3. ATR-FTIR characterization of all DSE samples. (A) FTIR spectra from DSE-0~3 in the range of 500-4000 cm-1. The existence of N-H stretching vibration around 3315 cm-1 indicated the formation of self-complementary N-H hydrogen bonds. (B) The disappearance of the peaks at 2260 cm-1 (N=C=O stretching band) suggested the diisocyanate monomers conduct complete reaction. (C) The peak associated with H-bonded C=O in urea (~1660 cm-1) increases from DSE-0 to DSE-3. Similarly, the peak associated with H-bonded C=O in urethane (~1695 cm-1) increases as the amount of UPy in the DSE polymer increases. The increases in these peaks shows the clear increase in the amount of hydrogen bonding present in the polymers as the amount of UPy increases.

Fig. S4. Raman spectra investigation of all DSE samples. The peak appears at 510 cm-1 is responsible for ν(S-S), the peak appears at 640 cm-1 is responsible for ν(C-S).

Fig. S5. GPC elution curves of DSE-0~3 with THF as the eluent and PS as the standard

Fig. S6. 2D SAXS images of DSE samples.

Fig. S7. TGA traces of DSE samples at 10 °C min-1 under N2 atmosphere.

Fig. S8. (A) The calculated mechanism of toughness: integral area of stress-stain curve. (B) Toughness of DSE-0~3.

Fig. S9. Cyclic stress-strain curves of DSE-3 when stretched to 100%, 300%, 500%, respectively.

Fig. S10. DMA curves of DSE samples.

Fig. S11. Digital photos of the prepared DSICE samples: colorless transparent liquid and casting film.

Fig. S12. EIS spectra of DSICE 10-35 samples at different temperatures from 30 °C to 70 °C. (A) EIS spectra of DSICE-10. (B) EIS spectra of DSICE-20. (C)EIS spectra of DSICE-30. (D) EIS spectra of DSICE-35. (E) EIS spectra of DSICE-40.

Fig. S13. Plot of DSICE-35 ionic conductivity versus the elevated temperatures (30 °C-70 °C).

Fig. S14. EIS spectra of DSE-0~3 samples with the same 35 wt.% LiTFSI at 30 °C.

Fig. S15. TGA traces of DSICE samples at 10 °C min-1 under N2 atmosphere.

Fig. S16. Storage modulus G′ and loss modulus G″ as functions of angular frequency ω for the DSICE-30 at different sweeping temperatures.

Fig. S17. Optical microscopy image of the completely self-healed cut-off DSICE-30 sample.

Fig. S18. Typical stress-stain curves of DSICE-35 after three recycling.

Fig. S19. The impedance change of DSICE-30 when stretched to different tensile elongation.

Fig. S20. The impedance change of DSICE-30 at different touched stimuli when stretched.

Table S1. Molecular weight of the synthesized DSE samples

| Sample Code | Mn(g/mol) | Mw(g/mol) | Polymer Dispersity Index（PDI） |
| --- | --- | --- | --- |
| DSE-0 | 3.42×104 | 6.71×104 | 1.96 |
| DSE-1 | 2.78×104 | 5.37×104 | 1.93 |
| DSE-2 | 2.44×104 | 5.02×104 | 2.04 |
| DSE-3 | 1.62×104 | 3.60×104 | 2.22 |

Table S2. A rough comparison of the overall performance between this work and recently reported typical ionic conductor materials

| Ionic Conductors Materials |  | Ionic conductivity (S m-1) | Mechanical Properties |  |  | Self-healing (r. t.) | Recyclability |  | Transparency (%) | Refs. |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  | Stretchability (%) | Strength（MPa） | Toughness (MJ m-3) |  |  |  |  |  |
| PAA/x-Ch ionogel | 5.15×10-3 |  | 1200 | 0.235 | NA | None | None | Opaque |  | 5 |
| PBA ICE | 10-4~10-3 |  | 1100 | 0.25 | NA | None | None | 92.1 |  | 8 |
| P(SPMA-r-MMA) ionogel | 4.1×10-2 |  | 677 | 0.3 | 0.114 | 3 h 70.9% | None | >90 |  | 9 |
| LM-PDES elastomer | 1.3×10-2 |  | 2600 | 0.125 | 2.36 | 24 h, ~98% | None | 94 |  | 26 |
| P(AAm/ChCl-co-MA/ChCl) elastomer | 4.1×10-2 |  | 450 | 0.6 | NA | 24 h 88.9% | None | 95.1 |  | 27 |
| PLA ICE | 2.4×10-3 |  | 800 | 0.18 | 1.3 | 15 h 90.1% | Yes | 91.1 |  | 28 |
| P(MEA-co-IBA) elastomer | 4.20×10-4 |  | 1640 | 1.05 | 0.039 | 24 h, ~30% | None | 90 |  | 29 |
| PIL elastomer | 1.31×10-2 |  | 540 | 0.24 | NA | 2 h ~100% | None | Opaque |  | 46 |
| PAA/betaine elastomer | 2×10-5 |  | 1600 | ~5 | NA | 12 h, ~100% | None | 99.7 |  | 47 |
| DSICE | 3.77×10-3 |  | 2615.17 | 27.83 | 164.36 | 6 h, ~99% | Yes | 92.3 |  | This work |

Movie S1. This Movie showed excellent fast self-healing capability of DSICE-30 at ambient temperature. The dumbbell-shaped DSICE-30 film colored blue and red with standard 12 mm × 2 mm rectangular and a thickness of 0.5 mm was cut into two pieces, respectively. And then put any two colored pieces into contact for 5 min and stretched to a large strain >800%.

Movie S2. This Movie showed the impedance changes of DSICE-30 when stretched to different tensile elongation.

Movie S3. This Movie showed the impedance changes of DSICE-30 at different touched stimuli

when stretched.