Supporting information

Table S1 BET surface and pore structures of the obtained samples.

| Samples | BET surface area (m²/g) | Pore volume (cm³/g) | Pore size (nm) |
| --- | --- | --- | --- |
| initial CB | 185.97 | 0.073 | 21.04 |
| 500C-SCB | 249.01 | 0.165 | 15.61 |
| 2Au/500C-SCB | 237.49 | 0.102 | 15.22 |

Table S2 Comparison of XPS components relative rations for initial CB, 500C-SCB, and 2Au/500C-SCB

| Samples | sp2 carbon (graphitic C=C) | sp3 carbon (hydrocarbon C-C) | C-O | π-π transition |
| --- | --- | --- | --- | --- |
| BE (eV) | 284.6 | 285.8 | 286.9 | 289.5 |
| initial CB | 66.1% | 9.83% | 6.43% | 17.64% |
| 500C-SCB | 55.59% | 28.35% | 7.91% | 8.15% |
| 2Au/500C-SCB | 52.62% | 22.44% | 16.81% | 8.13% |

Fig. S1. Time-dependent UV-Vis absorption spectra of 4-NP adsorption by (a) 500C-SCB and (b) 2Au/500C-SCB. (c) UV-Vis absorption spectra of 4-NP and 4-NP + NaBH4.

Fig. S2 (a-c) Plots of Ct/C0, (d-f) -ln (Ct/C0) vs. reaction time of 4-NP reduction and (g-i) Time-dependent UV-Vis absorption spectra of 4-NP reduction over xAu/T-SCB catalysts (x = 0.5, 1, 1.5, 2 and 2.5; T = 300C, 400C and 500C). Reaction conditions: C(4-NP) = 0.2 mM, C(NaBH4) = 40 mM, m(catalysts) = 10 mg, initial pH = 5.62, and room temperature.

Fig. S3. Zeta potential of 2Au/500C-SCB at pH of 2-9.

Fig. S4. The Arrhenius plots of 2Au/500C-SCB.

Fig. S5 Time-dependent UV-Vis absorption spectra of (a) 2-NP, (b) 3-NP and (c) 2,4-DNP reduction catalyzed by 2Au/500C-SCB. (D) Plots of Ct/C0 vs. time. Reaction conditions: C(2-NP, 3-NP and 2,4-DNP) = 0.2 mM, C(NaBH4) = 40 mM, m(2Au/500C-SCB) = 10 mg, room temperature.

Fig. S6. Time-dependent UV-Vis absorption spectra of (a) MO, (b) CR and (c) EBT reduction catalyzed by 2Au/500C-SCB. (D) Plots of Ct/C0 vs. time.

Fig. S7. (a) Recycling test for the catalytic reduction of 4-NP over 2Au/500C-SCB catalysts. (b) Time-dependent UV-Vis absorption spectra of 4-NP reduction over 4-AP pretreated 2Au/500C-SCB catalysts.