Supplementary Information

Electrochemical activation of C–H by electron-deficient W2C nanocrystals for simultaneous alkoxylation and hydrogen evolution

Xiu Lin1, Shi-Nan Zhang1, Dong Xu1, Jun-Jun Zhang1, Yun-Xiao Lin1, Guang-Yao Zhai1, Hui Su1, Zhong-Hua Xue1, Xi Liu1, Markus Antonietti2, Jie-Sheng Chen1, Xin-Hao Li1*

1School of Chemistry and Chemical Engineering, Shanghai Jiao Tong University, Shanghai 200240, P. R. China.

2Department of Colloid Chemistry, Max-Planck Institute of Colloids and Interfaces, Wissenschaftspark Golm, Potsdam 14424, Germany.

*e-mail: xinhaoli@sjtu.edu.cn

Supplementary Figure 1. Detailed synthetic route for the preparation of W2C/NxC samples, where x represents the nitrogen contents (at.%). Temperatures (T): 1000, 1100 and 1200 °C for W2C/N3.0C, W2C/N2.3C and W2C/N1.4C, respectively; Colour codes: C, grey; N, blue; H, white; W, purple.

Supplementary Figure 2. High-resolution C 1s (a), N 1s (b) and W 4f (c) spectra of W2C/NxC samples. (d) Nitrogen contents estimated from the XPS analysis results. The N contents (at.%) are 3.0%, 2.3% and 1.4% for W2C/N3.0C, W2C/N2.3C and W2C/N1.4C, respectively.

Supplementary Figure 3. (a-c) SEM images of W2C/N3.0C, W2C/N2.3C and W2C/N1.4C samples, respectively. All samples exhibit similar morphology with rough surfaces.

Supplementary Figure 4. N2 adsorption-desorption isotherms and specific surface areas (SBET) of W2C/NxC samples.

Supplementary Figure 5. (a and b) TEM images of W2C/N3.0C. W2C particles disperse uniformly on few-layer carbon supports without obvious aggregation. (c) HAADF-STEM image of W2C/N3.0C. (d) Selected-area electron diffraction pattern illustrates the formation of W2C nanocrystals.

Supplementary Figure 6. (a and b) TEM images of W2C/N2.3C. (c) HAADF-STEM image of W2C/N2.3C. (d) Selected-area electron diffraction pattern illustrates the formation of W2C nanocrystals.

Supplementary Figure 7. (a and b) TEM images of W2C/N1.4C. (c) HAADF-STEM image of W2C/N1.4C. (d) Selected-area electron diffraction pattern illustrates the formation of W2C nanocrystals.

Supplementary Figure 8. The size distribution of W2C/N3.0C (a), W2C/N2.3C (b) and W2C/N1.4C (c). The gradually elevated synthetic temperatures did not change the size distribution of these samples.

Supplementary Figure 9. XRD patterns of W2C/NxC samples. The XRD peaks of W2C/NxC samples could be attributed to the characteristic(002), (300) and (302) facets of α-W2C (black bars, JCPDS no. 35-776).

Supplementary Figure 10. Computation models and density of states of N1.4C (a and d), N2.3C (b and e) and N3.0C (c and f). Colour code: C, grey; N, blue. (g) The band gaps of N1.4C, N2.3C and N3.0C were 0.071, 0.112 and 0.245 eV, respectively. Doping more nitrogen atoms into the carbon support opened the band gap.

Supplementary Figure 11. The calculation models and charge density distribution of W2C/NxC models. The top view and side view of W2C/N1.4C (a and d), W2C/N2.3C (b and e) and W2C/N3.0C (c and f). Charge density difference stereograms of W2C/N1.4C (g), W2C/N2.3C (h) and W2C/N3.0C (i) models (electron-deficient area, blue; electron-rich area, red); Colour code: C, grey; N, blue; W, purple.

Supplementary Figure 12. Quantitative of electrons transfer from W2C cluster to various nitrogen-doped carbon support based on DFT calculations for W2C/N1.4C (a), W2C/N2.3C (b) and W2C/N3.0C (c) models. Hirshfeld charge analysis shows that 0.338, 0.373 and 0.397 electrons were transferred from W2C to carbon support for W2C/N1.4C, W2C/N2.3C and W2C/N3.0C models, respectively, rather speaking for the enhanced electron transfer between W2C nanocrystals and nitrogen-doped carbons due to the formation of Schottky heterojunction at a higher nitrogen content.

Supplementary Figure 13. UPS patterns of typical W2C/NxC samples. Secondary electron cut-off (Ecut-off) (a) and onset (EF) energy (b). The work function (Φ), as calculated by the equation of Φ = 21.21 eV - (Ecutoff - EF)S1, are 5.69, 5.63 and 5.42 eV for W2C/N3.0C, W2C/N2.3C and W2C/N1.4C samples, respectively.

Supplementary Figure 14. EELS spectra of W2C/NxC samples. The W M4,5 peaks shift positively with the increase of nitrogen contents, which indicates that more electrons flowing from W2C nanocrystals to nitrogen-doped carbons.

Supplementary Figure 15. Photograph of the reactor for electrochemical alkoxylation. A home-made reactor, composed of W2C/NxC anodes, Ti cathode and saturated calomel electrode (SCE) reference electrode, was used in this reaction system at room temperature. The electrolyte consisted of methanol (15 mL), ethylbenzene (0.5 mmol) and lithium perchlorate (1 mmol).

Supplementary Figure 16. Optimation of reaction conditions of W2C/N3.0C catalyst. Conversions of (1-methoxyethyl)benzene with different catalyst loadings (a), substrate contents (b) and potentials (c) for the alkoxylation of ethylbenzene. According to the results, 0.66 mg/cm2 of catalysts, and 0.5 mmol of ethylbenzene were used as the optimal parameters for all subsequent reactions at 2.0 V within 3 h.

Supplementary Figure 17. Gas chromatography-mass spectrometry (GC-MS) spectrum of the electrolyte after electrochemical alkoxylation over the W2C/N3.0C for 3 h. (1-methoxyethyl)benzene as the only product demonstrates the excellent selectivity. Dodecane was used as the internal standard for quantification.

Supplementary Figure 18. Qualitative analysis of hydrogen. (a and b) The formation of hydrogen gas bubbles on the arbitrary cathode (exemplified with Pt mesh, please see Supplementary Video 1). (c) Gas chromatography (GC) spectrum of the collected gas during the alkoxylation reaction. Only hydrogen signal was detected in Ar carrier gas. GC analysis results are also used for following quantification of H2 production.

Supplementary Figure 19. Linear sweep voltammetry and chronoamperometric curves of W2C/NxC samples in the presence of ethylbenzene(a and b) and the absence of ethylbenzene (c and d) in the electrolyte.

Supplementary Figure 20. Quantitative analysis of formaldehyde. (a) UV-vis absorption curves of standard solutions with known formaldehyde concentrations. The standard solutions consisted of different concentrations of formaldehyde and fixed amounts of acetylacetone solutions containing ammonium acetate (0.25 g), acetic acid (0.03 mL), acetylacetone (0.004 mL) and deionized water (2 mL). And then the pH of the solution was tuned to 6 by sulphuric acid (0.5 M). (b) Calibration curve used for the determination of formaldehyde at 413 nm. Time course of formaldehyde concentration on bare carbon cloth (c) and W2C/N3.0C (d) anodes, respectively, generating a trace amount of formaldehyde (5 and 6 μmol, respectively) within 18 h, whilst 0.5 mmol of ethylbenzene was dehydrogenated and then transformed into (1-methoxyethyl)benzene. This observation excludes the obvious contribution of direct dehydrogenation reaction of methanol to formaldehyde to the total FE for hydrogen evolution reactions.

Supplementary Figure 21. Radicals quench experiments. (a) GC-MS spectrum of reaction solution with butylated hydroxytoluene (BHT). (b) Conversions of ethylbenzene over W2C/N3.0C anode under standard reaction conditions (1) and in the control reaction with the addition of BHT (0.1 mmol) (2). After the addition of BHT, 2,6-ditert-butyl-4-methoxy-4-methyl-2,5-cyclohexadien-1-one and 3,5-di-tert-butyl-4-methoxybenzaldehyde with retention time of 8.6 min and 10.3 min were observed. All these results indicate that BHT could successfully trap the methoxy radicals and quench the methoxylation reactionS2. Standard reaction conditions: ethylbenzene (0.5 mmol), lithium perchlorate (1 mmol), methanol (15 mL), W2C/N3.0C anode and Ti mesh cathode with a controlled potential of 2.0 V versus SCE for 3 h at room temperature.

Supplementary Figure 22. (a) Linear sweep voltammetry curves of W2C/N3.0C anode before adding ethylbenzene (grey) and after adding ethylbenzene (red) under standard reaction conditions with a scanning rate of 10 mV/s. The enhanced current density after the addition of ethylbenzene suggests the activation of ethylbenzene in our electrochemical system. (b) Linear sweep voltammetry curves of W2C/NxC and bare carbon cloth as anodes under standard reaction conditions in the presence of ethylbenzene. The decreased overpotentials by the W2C/NxC-based anodes further confirm the role of W2C/NxC materials as active components for the activation of ethylbenzene.

Supplementary Figure 23. The electron numbers from benzylic H atom of ethylbenzene molecule to the surface of W2C (a) and W2C-0.08e- (b) models. The significant difference in Hirshfeld charge of benzylic H atom on the electron-deficient W2C surface directly certifies the polarization role of benzylic C−H bonds of ethylbenzene.

Supplementary Figure 24. The relative adsorption volumes of ethylbenzene absorbed by W2C/NxC samples and bare NC support, which are 4.7, 3.5 and 2.4 times for W2C/N3.0C, W2C/N2.3C and W2C/N1.4C, respectively.

Supplementary Figure 25. The negligible effect of oxygen residues in W2C/N3.0C on the final activity. W 4f XPS spectra (a) and conversions (b) of W2C/N3.0C, the reduced W2C/N3.0C sample (W2C/N3.0C-H) and W2O3. The W2C/N3.0C material was reduced by a mixed gas of H2 (5 %) and Ar (95 %) at 500 °C for 2 h to remove all exposable oxygen active species. Oxygen contents and the activity of W2C/N3.0C electrode materials remain similar after such a reduction process, demonstrating that the oxygen species, mainly in the form of metal oxides as the minority of W components, is not exposable to reaction environment for possible reactions. Moreover, a poor conversion of ethylbenzene on the control W2O3 anode with the same loading of W2C/N3.0C under standard conditions further exclude the possible role of W2O3 as active sites in our electrochemical synthesis system.

Supplementary Figure 26. TEM (a) and HRTEM (b) images of W2C/N3.0C-used (recycle 4 times). (c) STEM image and EDX elemental mapping of W2C/N3.0C-used. The sizes of W2C nanocrystals and content of NC support in the W2C/N3.0C anode were maintained well after long-term use, demonstrating the excellent electrochemical stability of W2C/N3.0C electrode materials.

Supplementary Figure 27. Reusability of W2C/N3.0C anodes for four runs (R1-4).

Supplementary Figure 28. The electrochemical stability of W2C/N3.0C, titanium mesh (Ti) and nickel plate (Ni) anodes. (a) The photos of electrodes before and after uses under standard reaction conditions. The Ti and Ni electrodes became decomposed during the reaction. (b) Conversions of ethylbenzene on various anodes at 2.0 V for 3 h. No products were detected Ni and Ti anodes under standard reaction conditions for 3 h, further highlighting the excellent stability of W2C/N3.0C anode. (c) The photos of Ti, Ni and W2C/N3.0C anodes during the reaction with different times.

Supplementary Table 1.Elemental compositions content of W2C/NxC samples.

| Element Sample | Atomic ratio (%) |  | W (wt%) by XPS | W (wt%) by ICP |
| --- | --- | --- | --- | --- |
|  | C | N |  |  |
| W2C/N3.0C | 87.2 | 3.0 | 50.7 | 65.8 |
| W2C/N2.3C | 88.3 | 2.3 | 50.0 | 62.4 |
| W2C/N1.4C | 89.5 | 1.4 | 50.9 | 63.2 |

Supplementary Table 2.Scope of substrates catalyzed by W2C/N3.0C anode.

To be continued

| Substrate | Conversion (%) | Products (Selectivity %) |  |
| --- | --- | --- | --- |
| 1 | 88% | 69% | 31% |
| 2 | 98% | 99% | - |
| 3 | 93% | 99% | - |
| 4 | 20% | 99% | - |
| 5 | 31% | 99% | - |
| 6 | 20% | 99% | - |
| 7 | 76% | 99% | - |
| 8 | 32% | 99% | - |
| 9 | 15% | 99% | - |
| 10 | 90% | 99% | - |
| 11 | 99% | 99% | - |
| 12 | 57% | 99% | - |
| 13 | 38% | 99% | - |
| 14 | 34% | 99% | - |
| 15 | 35% | 99% | - |

Standard reaction conditions: 1-11, substrate (0.5 mmol), lithium perchlorate (1 mmol), methanol (15 mL), W2C/N3.0C anode and Ti mesh cathode with a controlled potential of 2.0 V versus SCE reference electrode at room temperature. 12-15, ethylbenzene (0.5 mmol), alcohols (15 mL), W2C/N3.0C anode and Ti mesh cathode with a controlled potential of 2.0 V versus SCE reference electrode at room temperature.

The scope of the electron-deficient W2C-based anode for electrochemical alkoxylation was examined with different benzylic C−H substrates with various functional groups under standard conditions. Toluene was methoxylated to (methoxymethyl)benzene and (dimethoxymethyl)benzene with a high conversion (1). Benzenes with alkyl chains, including propylbenzene, pentylbenzene, isobutylene and even halide-substituted substrates (2-6), were successfully transformed into target products with good conversions (20%-98%) and very high selectivity (> 99%). Alkoxylation of tertiary C–H in cumene (7) could also proceed smoothly with the alkoxylation product as the sole product. Alkylbenzenes with electron-withdrawing groups were also tolerated on the electron-deficient W2C-based anode for highly selective alkoxylation reactions even with high steric hindrance (8 and 9). It is also not surprising that benzhydryls (10 and 11) with activated C-H bonds could be rapidly transformed into alkoxylation products under standard conditions with very high selectivity (>99%). Electron-deficient W2C-based anode was also powerful for the alkoxylation of ethylbenzene with different types of aliphatic alcohols (12-15). All these results again reveal the efficiency of the electron-deficient W2C catalyst for the benzylic C–H bonds alkoxylation with excellent chemical tolerance to various functional groups.

Supplementary Table 3. Summary of TOF values of various catalysts for the methoxylation of benzylic C–H bonds.

| Catalyst | TOF (h-1) | Substrate | Notes | T (°C) | Reference |
| --- | --- | --- | --- | --- | --- |
| W2C/N3.0C | 18.8 | Ethylbenzene | - | rt | This work |
| CuCl + 2,2′-bioxazoline a | 0.5 | Ethylbenzene | NFSI, (MeO)2P(O)H | 40 | 38 |
| [Ir(dF(CF3)ppy)2(5,5’-dCF3bpy)] PF6b | 12.2 | 4-ethylanisole | Cu(TFA)2(MeCN), 427 nm blue LED | rt | 39 |

Reaction conditions: a substrate (0.2 mmol), MeOH (1 mmol), CuCl (10 mol%), 2,2′-bioxazoline (10 mol%), N-fluorobenzenesulfonimide (NFSI) (2.0 equiv.), (MeO)2P(O)H (0.5 equiv.), dichloromethane (DCM): hexafluoroisopropanol (HFIP) = 4:1 (1.0 ml) and 16 h under N2. b substrate (0.6 mmol, 1 equiv.), [Ir(dF(CF3)ppy)2(5,5’-dCF3bpy)]PF6 (1 mol%), K2HPO4 (3 equiv), Cu(TFA)2(MeCN) (1.2 equiv), methanol (2 equiv), MeCN (0.2 M), 6 h.

Supplementary Table 4. TOF values of W2C/N3.0C heterogeneous catalyst in the alkoxylation of C−H bonds.

| Heterogenous catalyst | TOF (h-1) | Substrate | Notes | T (°C) | Reference |
| --- | --- | --- | --- | --- | --- |
| W2C/N3.0C | 18.8 | Ethylbenzene | 2.0 V versus SCE | rt | This work |

Supplementary Table 5. Summary of TOF values of homogeneous catalyst in the functionalization of C−H bonds.

| Homogeneous catalyst | Current collector | TOF (h-1) | Substrate | Notes | T (°C) | Reference |
| --- | --- | --- | --- | --- | --- | --- |
| Ni(DME)Cl2 | RVC | 0.6 | Amides | NaO2CAd, 1-AdCO2H, 8 mA | 130 | S3 |
| Co(OAc)2· 4H2O | Carbon cloth | 1.2 | N-(quinolin-8-yl)thiophene-2-carbox amide | NaOPiv· H2O, 10 mA | 65 | S4 |
| Cp*Rh(OAc)2 | RVC | 2.2 | N-(2-pyridyl) aniline | 3 mA | 65 | S5 |
| (TAML)Fe | Graphite | 0.8 | Ethylbenzene | 1.25 V versus Ag/AgCl | rt | S6 |
| Pd(OAc)2 | Graphite | 1.2 | 8-methylquinoline | Benzoquinone, 8 mA | 35 | S7 |
| PdCl2 | Pt | 3.1 | 2-phenylpyridine | 20 mA | 90 | S8 |

Supplementary References

S1.	Liu, J. et al. Metal-free efficient photocatalyst for stable visible water splitting via a two-electron pathway. Science 347, 970–974 (2015).

S2.	Kovarova, J., Rotschova, J., Brede, O. & Burgers, M. The effect of transformation products of the antioxidant BHT on the initial stages of thermo- and photo-oxidation of LDPE. Can. J. Chem. 73, 1862–1868 (1995).

S3.	Zhang, S. K., Struwe, J., Hu, L. & Ackermann, L. Nickela‐electrocatalyzed C−H alkoxylation with secondary alcohols: Oxidation‐induced reductive elimination at Nickel (III). Angew. Chem. Int. Ed. 59, 3178–3183 (2020).

S4.	Gao, X., Wang, P., Zeng, L., Tang, S. & Lei, A. Cobalt (II)-catalyzed electrooxidative C–H amination of arenes with alkylamines. J. Am. Chem. Soc. 140, 4195–4199 (2018).

S5.	Wu, Z. J. et al. Scalable rhodium (III)‐catalyzed aryl C−H phosphorylation enabled by anodic oxidation induced reductive elimination. Angew. Chem. Int. Ed. 58, 16770–16774 (2019).

S6.	Yang, Q.-L. et al. Electrochemistry-enabled Ir-catalyzed vinylic C–H functionalization. J. Am. Chem. Soc. 141, 18970–18976 (2019).

S7.	Das, A., Nutting, J. E. & Stahl, S. S. Electrochemical C–H oxygenation and alcohol dehydrogenation involving Fe-oxo species using water as the oxygen source. Chem. Sci. 10, 7542–7548 (2019).

S8.	Kakiuchi, F. et al. Palladium-catalyzed aromatic C-H halogenation with hydrogen halides by means of electrochemical oxidation. J. Am. Chem. Soc. 131, 11310–11311 (2009).