Supplementary Information

Network-structured Ru/RuO2-FeNiCo-LDH as a high-performance bifunctional electrocatalyst for overall water splitting

Aoxing Zhao1, Sibei Li1, Shun Wang2, Zhe Jia2, Zhengxi Guo1, Miao Zhang3, Lei Yang4, Jianguo Lv,

1 School of Physics and Materials Engineering and Anhui Province Key Laboratory of Simulation Calculation and Design for Electronic Information System, Hefei Normal University, Hefei 230601, China

2 School of Materials Science and Engineering, Southeast University, Nanjing, China

3 School of Physics and Material Science, Anhui University, Hefei 230039, China

4 Department of Chemistry and Materials Engineering, Hefei University, Hefei 230601, China

1. Characterization

XRD patterns were tested using a SmartLab X-ray diffractometer. The morphology was determined by SEM (Thermo Scientific Apera2), TEM and HRTEM (JEOL- F200). The elemental distribution was characterized via EDS elemental mapping. X-ray photoelectron spectroscopy (XPS, Thermo Scientific K-Alpha) was utilized to investigate the surface elemental composition and valence states.

2. Electrochemical Measurements

Electrochemical measurements of the samples were performed in a 1 M KOH aqueous solution using a standard three-electrode system. Linear sweep voltammetry (LSV) curves for HER and OER were recorded at a scan rate of 5 mV s. The Tafel slopes were derived by fitting the linear segments of the Tafel plots according to the equation η= b logj+a. Electrochemical impedance spectroscopy (EIS) tests were conducted over a frequency range of 100 kHz to 0.01 Hz. CV measurements at various scan rates (40, 80, 120, 160, and 200 mV s) were implemented in the non-Faradaic region to determine the double-layer capacitance (Cdl). The electrochemical active surface area (ECSA) was calculated from the Cdl values using the formula:ECSA=Cdl/Cs, where a specific capacitance Cs of 0.040 mF cm-2 was adopted for calculation . All potentials calibrated versus the Ag/AgCl electrode were converted to the reversible hydrogen electrode (RHE) using the following equation: E (RHE)=E(Ag/AgCl)+0.059×pH+0.197V.

Fig. S1 XRD patterns of Co-0.05-LDH/NF, Co-0.1-LDH/NF, Co-0.25-LDH/NF and Fe-0.1-Co-0.1-LDH/NF

Fig. S2 CV curves in the non-Faraday region of Co-0.05-LDH/NF

Fig. S3 CV curves in the non-Faraday region of Co-0.1-LDH/NF

Fig. S4 CV curves in the non-Faraday region of Co-0.25-LDH/NF

Fig. S5 CV curves in the non-Faraday region of Fe-0.1-Co-0.1-LDH/NF

Fig. S6 CV curves in the non-Faraday region of Ru/RuO2-Fe-0.1-Co-0.1-LDH/NF

Table S1 Charge transfer resistance (Rct) of the electrocatalysts.

| Electrocatalysts | Co-0.05-LDH/NF | Co-0.1-LDH/NF | Co-0.25-LDH/NF | Fe-0.1-Co-0.1-LDH/NF | Ru/RuO2-Fe-0.1-Co-0.1-LDH/NF |
| --- | --- | --- | --- | --- | --- |
| Rct (Ω) | 30.1 | 18.3 | 28.4 | 15.8 | 13.7 |

Table S2 Cdl and ECSA of the electrocatalysts.

| Electrocatalysts | Co-0.05-LDH/NF | Co-0.1-LDH/NF | Co-0.25-LDH/NF | Fe-0.1-Co-0.1-LDH/NF | Ru/RuO2-Fe-0.1-Co-0.1-LDH/NF |
| --- | --- | --- | --- | --- | --- |
| Cdl (mF cm-2) | 4.93 | 5.08 | 4.46 | 8.86 | 28.18 |
| ECSA (cm2) | 123.3 | 127 | 111.5 | 221.5 | 704.5 |

Table S3 Comparison of OWS performances of Ru/RuO2-Fe-0.1-Co-0.1-LDH/NF with other recently reported bifunctional electrocatalysts.

| Catalysts | Cell voltage (V) at 10 mA cm-2 | References |
| --- | --- | --- |
| NiFe-NCs/NF | 1.67 | [1] |
| Pt-NiCo2O4 | 1.62 | [2] |
| Co-P-1 | 1.60 | [3] |
| Co-Ni3S2/NF | 1.57 | [4] |
| NiMoO4/BP | 1.55 | [5] |
| Mn3O4/MnO/RuO2@C | 1.55 | [6] |
| NiFeMo/NiFeMoCx | 1.52 | [7] |
| Ru/NF | 1.50 | [8] |
| Pt-NiFeOxHy@NiFe-LDH | 1.48 | [9] |
| Pt−NiFe-MOF/NF | 1.45 | [10] |
| FeCoNiP@NiFe-LDH@CuO/CF | 1.44 | [11] |
| Ru/RuO2-Fe-0.1-Co-0.1-LDH/NF | 1.40 | This Work |

References:

[1] A. Kumar, S. Bhattacharyy, Porous NiFe-Oxide Nanocubes as Bifunctional Electrocatalysts for Efficient Water-Splitting, ACS Applied Materials & Interfaces, (2017).

[2] W. Cheng, Z. Cui, S. Xu, S. Cheng, N. Gao, M. Yang, H. Li, Pt doped NiCo2O4 electrolysis for achieving highly efficient overall water splitting in alkaline condition, Journal of Power Sources, 641 (2025) 236891.

[3] X. He, J. Cai, J. Zhou, Q. Chen, Q. Zhong, J. Liu, Z. Sun, D. Qu, Y. Li, Facile Electrochemical Synthesis of Bifunctional Needle-like Co-P Nanoarray for Efficient Overall Water Splitting, Molecules, 28 (2023) 6101.

[4] J. Jian, L. Yuan, H. Li, H. Liu, X. Zhang, X. Sun, H. Yuan, S. Feng, Hydrothermal Synthesized Co-Ni3S2 Ultrathin Nanosheets for Efficient and Enhanced Overall Water Splitting, Chemical Research in Chinese Universities, (2019).

[5] C. Hua, Y. Zhu, H. Fan, P. Feng, The Bifunctional Electrocatalytic Performance of NiMoO4/BP Sheets for Overall Water Splitting and Its Promising High Stability, Journal of Electronic Materials, 53 (2024) 3258-3267.

[6] J. Zhang, S. Li, J. Cao, L. Hu, Y. Ren, J. Yao, X. Wang, J. Zhu, Synergistic interface engineering in carbon-coated Mn3O4/MnO/RuO2 heterostructure toward high-performance overall water splitting, International Journal of Hydrogen Energy, 158 (2025) 150504.

[7] J. Mo, N. Fu, S. Mu, J. Peng, Y. Liu, G. Zhang, Facile Synthesis of Metal/Carbide Hybrid toward Overall Water Splitting, Catalysts, 14 (2024) 730.

[8] Y. Hou, Z. Qin, X. Han, Thermal evaporation-driven fabrication of Ru/RuO2 nanoparticles onto nickel foam for efficient overall water splitting, Nanoscale, 16 (2024) 6662-6668.

[9] L. Liu, H. Liu, B. Jia, X. Qu, M. Qin, Durable Pt-Decorated NiFe-LDH for High-Current-Density Electrocatalytic Water Splitting Under Alkaline Conditions, Nanomaterials, 15 (2025) 1683.

[10] J. Yin, C. Wang, J. Li, S. Yu, Z. Wu, Y. Zhang, Y. Du, In Situ Electrodeposition of Ultralow Pt into NiFe-Metal-Organic Framework/Nickel Foam Nanosheet Arrays as a Bifunctional Catalyst for Overall Water Splitting, Inorganic Chemistry, 63 (2024) 5167-5174.

[11] Y.F. Zhang, X.W. Wang, Z.Y. Zheng, W.H. Zhang, X. Liu, J.Q. Niu, The interfacial synergy of hierarchical FeCoNiP@FeNi-LDH heterojunction for efficient alkaline water splitting, Journal of colloid and interface science, 673 797-806.

Corresponding author. E–mail address: zhejia@seu.edu.cn (Z. Jia)

Corresponding authors. E-mail addresses: jglv@hfnu.edu.cn (J. Lv)