Supplementary Information

2D LDH-MoS2 clay nanosheets: synthesis, catalase-mimic capacity, and imaging-guided tumor photo-therapy

Jiayan Zhao,a,b,1 Hang Wu,c,1 Jiulong Zhao,a Yichen Yin,b Zhilun Zhang,b Shige Wang,b and Kun Lina*

a Department of Gastroenterology, Changhai Hospital, Second Military Medical University, No. 168 Changhai Road, Shanghai, 200433, P. R. China

b College of Science, University of Shanghai for Science and Technology, No. 334 Jungong Road, Shanghai, 200093, P. R. China

c Department of General surgery ,Xinhua Hospital, Shanghai jiaotong University school of medicine , No. 1665 Kongjiang Road, Shanghai, 200433, P. R. China

1 These authors contributed equally to this work. *To whom correspondence should be addressed email: lin17321171461@163.com (Mr. Lin)

Figure S1 XPS spectra of LMM: (a) Mo 3d, (b) Al 2p, (c) Mg 1s and (d) S 2p.

Figure S2 Dynamic light scattering of LMM@BSA nanosheets dispersed in DMEM.

Figure S3 (a) Cell viability profiles; (b-f) appearance of calcein-AM/PI dyed L929 cells treated with different concentration of LMM@BSA clay nanosheets (incubation time: 24h): (b) control; (c) 50 μg/mL; (d) 100 μg/mL; (e) 250 μg/mL; (f) 500 μg/mL.

Figure S4 (a-b) The morphology of cell treated with (a) saline and (b) LMM@BSA clay nanosheets (500 μg/mL).

Figure S5 Hemolysis percentage of mRBCs co-incubated with LMM@BSA clay nanosheets (concentration: 0-500 μg/mL) for 2 h.

Figure S6 UV-vis-NIR spectra of prepared nanosheets.

Figure S7 (a) Cell viability profiles; (b-d) appearance of calcein-AM/PI dyed cells after PTT treatments (1 W/cm2) with different concentration of LMM@BSA clay nanosheets: (b) 100 μg/mL; (c) 250 μg/mL; (d) 500 μg/mL.

Figure S8 (a) Cell viability profiles after different treatments; (b-g) appearance of calcein-AM/PI stained cells treated with (b) DMEM + saline without laser; (c) DMEM + LMM@BSA without laser; (d-g) DMEM + LMM@BSA with laser of (d) 0.2 W/cm2; (e) 0.5 W/cm2; (f) 0.8 W/cm2; (g) 1.0 W/cm2. Control: 0 2 W/cm2.

Figure S9 (a) Cell viability profiles treated with LMM@BSA/Ce6 annd 660 nm laser (0.1 W/cm2) irradiation for different time points; (b-f) appearance of calcein-AM/PI stained cells after PDT treatments with varied irradiated duration: (b) 0 min; (c) 1 min; (d) 2 min; (e) 3 min; (f) 5 min.

Figure S10 The routine blood test of mice (a) white blood cell (WBC); (b) red blood cells (RBC); (c) hemoglobin (HGB); (d) hematocrit (HCT); (e) mean corpuscular volume (MCV); (f) mean corpuscular hemoglobin (MCH); (g) mean corpuscular hemoglobin concentration (MCHC); (h) platelet (PLT); and (i) red cell distribution width (RDW) with feeding for varied days.

Figure S11 H&E-stained tissue sections of major organs of KM mice that injected with saline or LMM@BSA/Ce6 nanosheets and fed for 1 and 7 days.

Figure S12 In vitro cumulative release profiles of DOX from LMM@BSA/DOX nanosheets under different pH and temperature.