Can local mineral reserves support the path towards energy independence? A resource assessment of recyclable perovskite photovoltaics.

Authors

Savannah Bennetta,b, Zhenni Wua,b, Markus Kohlstädtc,d, Ian Marius Petersa,b,*.

*Corresponding author: i.peters@fz-juelich.de

Author affiliations

a. Helmholtz Institute Erlangen-Nürnberg For Renewable Energy, Immerwahrstr 2, 91054 Erlangen, Germany. Email: i.peters@fz-juelich.de

b. Friedrich-Alexander University of Erlangen-Nuremberg, Martensstr. 5a, 91058 Erlangen, Germany.

c. Freiburg Materials Research Centre FMF, University of Freiburg, Stefan-Meier-Str 21, 79104 Freiburg im Breisgau, Germany.

d. Fraunhofer Institute for Solar Energy Systems ISE, Heidenhofstr 2, 79110 Freiburg im Breisgau, Germany.

Perovskite solar cell data

The Solaronix estimated material quantity for a 1m2 module is provided in Table 1. Similarly, the University of Freiburg estimated material quantity for 1m2 module is provided in Table 2. These values were originally reported in (Bennett et al., 2026).

Table 1: Metal/mineral requirements for producing a 1m2 Solaronix module.

| Layer | Material | Symbol | Quantity in 1m2 (kg) |
| --- | --- | --- | --- |
| Substrate | Fluorine | F | 0.0000695 |
|  | Tin | Sn | 0.00104 |
| Insulating layer | Zirconium dioxide | ZrO2 | 0.0142 |
| Electron transport layer | Titanium dioxide | TiO2 | 0.0079 |
| Blocking layer | Titanium dioxide | TiO2 | 0.00032 |
| Perovskite | Lead | Pb | 0.00220 |
| Cathode | Graphite | G | 0.0606 |
| Contacts | Silver | Ag | 0.00162 |

Table 2: Metal/mineral requirements for producing a 1m2 University of Freiburg module.

| Layer | Material | Symbol | Quantity in 1m2 (kg) |
| --- | --- | --- | --- |
| Substrate | Indium | In | 0.000797 |
|  | Tin | Sn | 8.44E-05 |
| Perovskite | Caesium | Cs | 9.62E-05 |
|  | Lead | Pb | 0.000881 |
| Hole transport layer | Phosphorus | P | 6.75E-07 |
| Contacts | Aluminium | Al | 0.000405 |

The cell data for the HIERN module was reported in (Wu et al., 2026). The 6.25cm2 cell was produced by spin-coating. The 1m2 module scale-up values were estimated conservatively, assuming that spin coating retains 10% (Yilbas et al., 2019) of the deposited solution and that there is a 1-to-1 scale-up from a 6.25cm2 cell to a 1m2 module. The value for the indium, tin and silver were assumed the same as the Solaronix module.

Table 3: Metal/mineral requirements for producing a 1m2 Helmholtz Institute of Erlangen-Nürnberg for Renewable Energy module.

| Layer | Material | Symbol | Quantity in 1m2 (kg) |
| --- | --- | --- | --- |
| Substrate | Indium | In | 0.000797 |
|  | Tin | Sn | 8.44E-05 |
| Perovskite | Caesium | Cs | 0.000119 |
|  | Lead | Pb | 0.00346 |
| Hole transport layer | Nickel | Ni | 5.029E-05 |
|  | Phosphorous | P | 5.98E-06 |
| Contacts | Silver | Ag | 0.00162 |

Figure one: unit conversions and fuel reserve data

The world proven oil, gas and uranium reserves are generally reported in million barrels, billion standard cubic metres, and tonnes. These values are then converted to terawatt-hours (TWh) using the conversion factors in Table 4. For oil and natural gas, these values are further converted from TWh embedded energy to TWh electricity, accounting for heat losses in the process of converting the fuel to electricity. This is not done for uranium, as the 0.044 conversion value already accounts for heat losses.

Table 4: Unit conversion of oil, natural gas and uranium to TWh energy and TWh electricity.

| Unit conversions of oil |  |  |
| --- | --- | --- |
| Million barrels | Energy (TWh) | Source |
| 1 | 1.63 | (EIA, 2026) |
| Energy (TWh) | Electricity (TWh) |  |
| 1 | 0.37 | (IEA, 2008) |
| Unit conversion of natural gas |  |  |
| m3 natural gas | Energy (TWh) |  |
| 1 | 11.11 | (GOV.UK, 2014) |
| Energy (TWh) | Electricity |  |
| 1 | 0.40 | (IEA, 2008) |
| Unit conversion of uranium |  |  |
| Tonne uranium | Energy (TWh) |  |
| 1 | 0.044 | (World Nuclear Association, 2023) |

The world proven oil reserves are reported by the Organization of the Petroleum Exporting Countries (OPEC, 2025). These values are taken from the Annual Statistical Bulletin, Table 3.1 page 22. Some of the countries in Table 5 below are grouped differently to the original report. The million barrels are converted to TWh using the conversions provided in Table 4.

Table 5: World proven crude oil reserves by country and region in million barrels, in TWh, and in TWh* after the conversion to electricity.

| Country/Region | 2024 (mb) | 2024 (TWh) | 2024 (TWh)* |
| --- | --- | --- | --- |
| North America | 54644 | 88727 | 32829 |
| Canada | 4344 | 7073 | 2617 |
| Mexico | 5136 | 8362 | 3094 |
| United States | 45014 | 73292 | 27118 |
| Europe | 10399 | 18420 | 6815 |
| Denmark | 365 | 594 | 220 |
| Norway | 6912 | 11254 | 4164 |
| United Kingdom | 1500 | 2442 | 904 |
| Others | 1622 | 2641 | 977 |
| Other Europe | 914 | 1488 | 551 |
| Asia Pacific | 1892 | 3081 | 1140 |
| Australia | 1803 | 2936 | 1086 |
| Others | 89 | 145 | 54 |
| China | 28182 | 45886 | 16978 |
| India | 4981 | 8110 | 3001 |
| Asia | 11519 | 18755 | 6939 |
| Brunei | 1100 | 1791 | 663 |
| Indonesia | 2410 | 3924 | 1452 |
| Malaysia | 2700 | 4396 | 1627 |
| Vietnam | 4400 | 7164 | 2651 |
| Others | 909 | 1480 | 548 |
| South America | 344883 | 561783 | 207860 |
| Argentina | 2999 | 4883 | 1807 |
| Brazil | 15894 | 25879 | 9575 |
| Chile | 150 | 244 | 90 |
| Colombia | 2019 | 3287 | 1216 |
| Ecuador | 8273 | 13470 | 4984 |
| Venezuela | 303221 | 493704 | 182671 |
| Others | 12477 | 20315 | 7517 |
| Middle East | 871218 | 1418517 | 524851 |
| Iran | 208600 | 339643 | 125668 |
| Iraq | 145019 | 236120 | 87364 |
| Kuwait | 101500 | 165262 | 61147 |
| Oman | 4971 | 8094 | 2995 |
| Qatar | 25244 | 41102 | 15208 |
| Saudi Arabia | 267200 | 435055 | 160970 |
| United Arab Emirates | 113000 | 183987 | 68075 |
| Others | 5684 | 9255 | 3424 |
| Africa | 119363 | 194347 | 71908 |
| Algeria | 12200 | 19864 | 7350 |
| Angola | 2550 | 4152 | 1536 |
| Congo | 1811 | 2949 | 1091 |
| Egypt | 3300 | 5373 | 1988 |
| Equatorial Guinea | 1100 | 1791 | 663 |
| Gabon | 2000 | 3256 | 1205 |
| Libya | 48363 | 78745 | 29136 |
| Nigeria | 37280 | 60699 | 22459 |
| Sudan | 5000 | 8141 | 3012 |
| Others | 5759 | 9377 | 3469 |
| Russia | 80000 | 130256 | 48195 |
| Eurasia | 38874 | 63295 | 23419 |
| Azerbaijan | 7000 | 11397 | 4217 |
| Belarus | 198 | 322 | 119 |
| Kazakhstan | 30000 | 48846 | 18073 |
| Turkmenistan | 600 | 977 | 361 |
| Ukraine | 395 | 643 | 238 |
| Uzbekistan | 594 | 967 | 358 |
| Others | 87 | 142 | 52 |
| Total world | 1566869 | 2551176 | 943935 |

The world proven natural gas reserves are reported by the Organization of the Petroleum Exporting Countries (OPEC, 2025). These values are taken from the Annual Statistical Bulletin, Table 9.1 page 76. Some of the countries in Table 6 below are grouped differently to the original report.

Table 6: World proven natural gas reserves by country and region in billion standard cubic meters, in TWh, and in TWh* after the conversion to electricity.

| Country/Region | 2024 (mb) | 2024 (TWh) | 2024 (TWh)* |
| --- | --- | --- | --- |
| North America | 20661 | 229444 | 91778 |
| Canada | 2462 | 27356 | 10942 |
| Mexico | 276 | 3067 | 1227 |
| United States | 17912 | 199022 | 79609 |
| Europe | 3132 | 35844 | 14338 |
| Denmark | 90 | 1000 | 400 |
| Germany | 17 | 189 | 76 |
| Italy | 47 | 522 | 209 |
| Netherlands | 74 | 822 | 329 |
| Norway | 1890 | 21000 | 8400 |
| Poland | 90 | 1000 | 400 |
| United Kingdom | 161 | 1789 | 716 |
| Others | 763 | 8478 | 3391 |
| Other Europe | 94 | 1044 | 418 |
| Bulgaria | 4 | 44 | 18 |
| Romania | 80 | 889 | 356 |
| Asia Pacific | 3516 | 38822 | 15529 |
| Australia | 2741 | 30456 | 12182 |
| New Zealand | 45 | 500 | 200 |
| Others | 708 | 7867 | 3147 |
| China | 2890 | 32111 | 12844 |
| India | 1145 | 12722 | 5089 |
| Asia | 4751 | 52789 | 21116 |
| Bangladesh | 186 | 2067 | 827 |
| Brunei | 217 | 2411 | 964 |
| Indonesia | 894 | 9933 | 3973 |
| Japan | 22 | 244 | 98 |
| Malaysia | 2112 | 23467 | 9387 |
| Myanmar | 217 | 2411 | 964 |
| Pakistan | 427 | 4744 | 1898 |
| Thailand | 162 | 1800 | 720 |
| Vietnam | 174 | 1933 | 773 |
| Others | 362 | 4022 | 1609 |
| South America | 7390 | 82111 | 32844 |
| Argentina | 470 | 5222 | 2089 |
| Bolivia | 175 | 1944 | 778 |
| Brazil | 628 | 6978 | 2791 |
| Chile | 10 | 111 | 44 |
| Colombia | 54 | 600 | 240 |
| Ecuador | 9 | 100 | 40 |
| Peru | 237 | 2633 | 1053 |
| Trinidad & Tobago | 299 | 3322 | 1329 |
| Venezuela | 5511 | 61233 | 24493 |
| Others | 8 | 89 | 36 |
| Middle East | 82522 | 916911 | 366764 |
| Iran | 33988 | 377644 | 151058 |
| Iraq | 3714 | 41267 | 16507 |
| Kuwait | 1784 | 19822 | 7929 |
| Oman | 644 | 7156 | 2862 |
| Qatar | 23831 | 264789 | 105916 |
| Saudi Arabia | 9727 | 108078 | 43231 |
| United Arab Emirates | 8210 | 91222 | 36489 |
| Others | 624 | 6933 | 2773 |
| Africa | 17221 | 191344 | 76538 |
| Algeria | 4504 | 50044 | 20018 |
| Angola | 129 | 1433 | 573 |
| Cameroon | 170 | 1889 | 756 |
| Congo | 284 | 3156 | 1262 |
| Egypt | 2209 | 24544 | 9818 |
| Equatorial Guinea | 40 | 444 | 178 |
| Gabon | 27 | 300 | 120 |
| Libya | 730 | 8111 | 3244 |
| Mozambique | 2840 | 31556 | 12622 |
| Nigeria | 5979 | 66433 | 26573 |
| Others | 309 | 3433 | 1373 |
| Russia | 46832 | 520356 | 208142 |
| Eurasia | 18739 | 208211 | 83284 |
| Azerbaijan | 1900 | 21111 | 8444 |
| Kazakhstan | 1830 | 20333 | 8133 |
| Turkmenistan | 13900 | 154444 | 61778 |
| Ukraine | 239 | 2656 | 1062 |
| Uzbekistan | 846 | 9400 | 3760 |
| Others | 24 | 267 | 107 |
| Others | 10 | 111 | 44 |
| Total world | 208892 | 2321022 | 928409 |

The world proven uranium reserves are reported by the Nuclear Energy Agency (Nuclear Energy Agency & International Atomic Energy Agency, 2024). These values are taken from the Uranium Resources, Production and Demand report, Table 1.2a page 22. The total tonnes are the sum of the uranium in the cost range of 40$/kgU to 260$/kgU.

Table 7: World proven uranium reserves by country and region, in tonnes and TWh* after the conversion to electricity.

| Country | Total (Tonnes) | 2024 (TWh*) |
| --- | --- | --- |
| Africa | 3528700 | 155263 |
| Algeria | 19500 | 858 |
| Botswana | 174400 | 7674 |
| Cameroon | 21000 | 924 |
| Central African Republic | 29200 | 1285 |
| Chad | 2400 | 106 |
| Congo, Dem. Rep. | 2700 | 119 |
| Egypt | 12500 | 550 |
| Gabon | 10600 | 466 |
| Jordan | 49000 | 2156 |
| Malawi | 34500 | 1518 |
| Mali | 17800 | 783 |
| Mauritania | 43700 | 1923 |
| Namibia | 1081900 | 47604 |
| Niger | 821700 | 36155 |
| Senegal | 4700 | 207 |
| Somalia | 7600 | 334 |
| South Africa | 985300 | 43353 |
| Tanzania | 162200 | 7137 |
| Zambia | 46000 | 2024 |
| Zimbabwe | 2000 | 88 |
| North America | 1921400 | 84542 |
| Canada | 1722100 | 75772 |
| Mexico | 10100 | 444 |
| United States | 189200 | 8325 |
| South America | 724200 | 31865 |
| Argentina | 88900 | 3912 |
| Brazil | 519200 | 22845 |
| Bolivia | 1300 | 57 |
| Chile | 1400 | 62 |
| Guyana | 4600 | 202 |
| Paraguay | 8600 | 378 |
| Peru | 100200 | 4409 |
| Europe | 497900 | 21908 |
| Bulgaria | 5100 | 224 |
| Czechia | 119900 | 5276 |
| Denmark (Greenland) | 114000 | 5016 |
| Finland | 2400 | 106 |
| Germany | 7000 | 308 |
| Greece | 7000 | 308 |
| Hungary | 16700 | 735 |
| Italy | 18300 | 805 |
| Portugal | 14000 | 616 |
| Romania | 13200 | 581 |
| Slovak Republic | 43700 | 1923 |
| Slovenia | 23800 | 1047 |
| Spain | 93600 | 4118 |
| Sweden | 19200 | 845 |
| Russia | 1161500 | 51106 |
| Eurasia | 3279800 | 144311 |
| Kazakhstan | 2916800 | 128339 |
| Ukraine | 363000 | 15972 |
| Middle East | 261100 | 11488 |
| Iran, Islamic Republic of | 14800 | 651 |
| Saudi Arabia | 46100 | 2028 |
| Türkiye | 63100 | 2776 |
| Uzbekistan | 137100 | 6032 |
| Asia Pacific | 3606400 | 158682 |
| Australia | 3606400 | 158682 |
| China | 810800 | 35675 |
| India | 252500 | 11110 |
| Asia | 364300 | 16029 |
| Japan | 13200 | 581 |
| Indonesia | 18700 | 823 |
| Mongolia | 306100 | 13468 |
| Pakistan | 22500 | 990 |
| Viet Nam | 3800 | 167 |
| Total | 27084600 | 1191722 |

Figure two: metal/mineral reserve quantities in the European Union

These values were taken from the Raw Material Information System platform, where quantities of each element are reported in tonnes for each country.

Table 8: Reported reserves of minerals in countries of the European Union.

| Country | Mineral | Reported in | Quantity (tonne) | Element / label | Quantity of element (tonne) |
| --- | --- | --- | --- | --- | --- |
| Austria | Lithium | Li | 72937 | Li | 72937 |
|  | Magnesite | Magnesite | 49000 | Mag* | 14125 |
|  | Magnesium | Mg | 49000 | Mg | 49000 |
| Belgium | No data |  |  |  |  |
| Bulgaria | Lead | Pb | 71300 | Pb | 71300 |
|  | Copper | Cu | 144682 | Cu | 144682 |
|  | Zirconium | Zircon (ZrSiO4) | 27300 | Zr | 13586 |
|  | Zinc | Zn | 27300 | Zn | 27300 |
|  | Silver | Ag | 143 | Ag | 143 |
|  | Gold | Au | 64.9 | Au | 65 |
| Croatia | No data |  |  |  |  |
| Cyprus | No data |  |  |  |  |
| Czechia | Coking coal | Coking coal | 413 |  |  |
| Denmark | No data |  |  |  |  |
| Estonia | No data |  |  |  |  |
| Finland | Iron and steel | Fe | 35060200 | Fe | 35060200 |
|  | Nickel | Ni | 4070597 | Ni | 4070597 |
|  | Phosphate rock | P2O5 | 1000000 | P | 436429 |
|  | Cobalt | Coking coal | 312000 |  |  |
|  | Zirconium | Zircon (ZrSiO4) | 9300 | Zr | 4628 |
|  | Lead | Pb | 3500 | Pb | 3500 |
|  | Lithium | Li | 92709 | Li | 92709 |
|  | Zinc | Zn | 9300 | Zn | 9300 |
|  | Copper | Cu | 486590 | Cu | 486590 |
|  | Selenium | Se | 300 | Se | 300 |
|  | Gold | Au | 135 | Au | 135 |
|  | Silver | Ag | 125 | Ag | 125 |
|  | Platinum | Pt | 14.0 | Pt | 14 |
|  | Palladium | Pd | 9.10 | Pd | 9 |
| France | Zirconium | Zircon (ZrSiO4) | 318000 | Zr | 158256 |
|  | Zinc | Zn | 318000 | Zn | 318000 |
|  | Copper | Cu | 103000 | Cu | 103000 |
|  | Gold | Au | 9.75 | Au | 10 |
| Germany | Lithium | Li | 508664 | Li | 508664 |
| Greece | Copper | Cu | 740000 | Cu | 740000 |
|  | Zirconium | Zircon (ZrSiO4) | 468000 | Zr | 232905 |
|  | Zinc | Zn | 468000 | Zn | 468000 |
|  | Nickel | Ni | 353000 | Ni | 353000 |
|  | Lead | Pb | 374000 | Pb | 374000 |
|  | Magnesite | Magnesite | 280000 | Mag | 80716 |
|  | Magnesium | Mg | 280000 | Mg | 280000 |
|  | Perlite | Perlite | 180000 |  |  |
|  | Silver | Ag | 1062 | Ag | 1062 |
|  | Gold | Au | 185 | Au | 185 |
| Hungary | Copper | Cu | 788000 | Cu | 788000 |
|  | Zirconium | Zircon (ZrSiO4) | 575000 | Zr | 286154 |
|  | Zinc | Zn | 575000 | Zn | 575000 |
| Ireland | Zirconium | Zircon (ZrSiO4) | 849000 | Zr | 422513 |
|  | Zinc | Zn | 849000 | Zn | 849000 |
|  | Lead | Pb | 219738 | Pb | 219738 |
|  | Silver | Ag | 0.454 | Ag | 0 |
| Italy | No data |  |  |  |  |
| Latvia | No data |  |  |  |  |
| Lithuania | No data |  |  |  |  |
| Luxembourg | No data |  |  |  |  |
| Malta | No data |  |  |  |  |
| Netherlands | No data |  |  |  |  |
| Poland | Copper | Cu | 18754867 | Cu | 18754867 |
|  | Zirconium | Zircon (ZrSiO4) | 7707000 | Zr | 3835463 |
|  | Zinc | Zn | 7707000 | Zn | 7707000 |
|  | Lead | Pb | 3521000 | Pb | 3521000 |
|  | Coking coal | Coking coal | 21067 |  |  |
|  | Helium | He | 24 | He | 24 |
|  | Selenium | Se | 3000 | Se | 3000 |
|  | Silver | Ag | 47750 | Ag | 47750 |
| Portugal | Lead | Pb | 673000 | Pb | 673000 |
|  | Zirconium | Zircon (ZrSiO4) | 2029000 | Zr | 1009751 |
|  | Zinc | Zinc | 2029000 | Zinc | 2029000 |
|  | Copper | Cu | 538500 | Cu | 538500 |
|  | Tungsten | W | 4579 | W | 4579 |
|  | Tin | Sn | 10222 | Sn | 10222 |
|  | Silver | Ag | 3829 | Ag | 3829 |
|  | Gold | Au | 11.2 | Au | 11 |
| Romania | Copper | Cu | 198522 | Cu | 198522 |
|  | Silver | Ag | 1790 | Ag | 1790 |
|  | Gold | Au | 14451612 | Au | 14451612 |
| Slovakia | Iron and steel | Fe | 941774000 | Fe | 941774000 |
|  | Potash | Potash (K2O) | 67173400 |  |  |
|  | Magnesite | Magnesite | 1200000 | Mag | 345925 |
|  | Tin | Sn | 1709 | Sn | 1709 |
|  | Perlite | Perlite | 30000 |  |  |
|  | Magnesium | Mg | 1200000 | Mg | 1200000 |
| Slovenia | No data |  |  |  |  |
| Spain | Potash | Potash (K2O) | 26800000 |  |  |
|  | Zirconium | Zircon (ZrSiO4) | 3861000 | Zr | 1921464 |
|  | Zinc | Zn | 3861000 | Zn | 3861000 |
|  | Strontium | Sr | 3400000 | Sr | 3400000 |
|  | Copper | Cu | 2280972 | Cu | 2280972 |
|  | Lead | Pb | 1669000 | Pb | 1669000 |
|  | Magnesite | Magnesite | 35000 | Mag | 10089 |
|  | Nickel | Ni | 21000 | Ni | 21000 |
|  | Fluorspar | Fluorspar (CaF2) | 15000 | F | 7300 |
|  | Lithium | Li | 230000 | Li | 230000 |
|  | Tin | Sn | 15241 | Sn | 15241 |
|  | Magnesium | Mg | 35000 | Mg | 35000 |
|  | Tungsten | W | 54827 | W | 54827 |
|  | Silver | Ag | 4522 | Ag | 4522 |
|  | Gold | Au | 14.1 | Au | 14 |
| Sweden | Iron and steel | Fe | 567640200 | Fe | 567640200 |
|  | Selenium | Se | 500 | Se | 500 |
|  | Copper | Cu | 2816340 | Cu | 2816340 |
|  | Zinc | Zn | 3952580 | Zn | 3952580 |
|  | Zirconium | Zircon (ZrSiO4) | 3952580 | Zr | 1967040 |
|  | Lead | Pb | 1668380 | Pb | 1668380 |
|  | Tellurium | Te | 700 | Te | 700 |
|  | Graphite, natural | Graphite | 544693 | G | 544693 |

*Mag refers to magnesium that is estimated from the weight percent of Mg in magnesite. It is unclear whether the estimated quantity of magnesium reported by the RMIS platform falls within the reported magnesite values, thus they were kept separate.

Figure two: calculating the electricity production using the module designs and reserves

To determine the TWh quantity of electricity producible by a particular element in a module, the quantity of reserves [tonnes] is divided by the quantity of the element per m2 of module [kg/m2] to determine the total number/area of modules that can be produced using the reserves [m2]. This value is then multiplied by the assumed electricity production value of 240 [W/m2] and then further multiplied by the 1400 sun-hours [hours].

For example, the M-Sol uses an estimated 0.00162kg/m2 of silver. The European Union’s estimated reserves for silver are 59222 tonnes.

Area of modules=59222*103 kg0.00162kgm2= 3.66*1010 m2

TWh production=3.66*1010[m2]*240 Wm2*1400 Hr*10-12= 12283TWh

The resulting quantity of TWh that each module design could produce is provided in Table 9, Table 10 and Table 11.

Table 9: Solaronix module design output from European Union reserves.

| Element | Quantity reserves (tonnes) | Total area of modules that can be produced (m2) | Scale-up (1000TWh) |
| --- | --- | --- | --- |
| F | 7.30E+03 | 1.05E+11 | 35.3 |
| Sn | 2.72E+04 | 2.61E+10 | 8.78 |
| Zr | 9.85E+06 | 6.94E+11 | 2.33E+02 |
| Ti | 0 | 0 | 0 |
| Pb | 8.20E+06 | 3.72E+12 | 1.25E+03 |
| G | 5.45E+05 | 9.00E+09 | 3.02E+00 |
| Ag | 5.92E+04 | 3.66E+10 | 1.23E+01 |

Table 10: University of Freiburg module design output from European Union reserves.

| Element | Quantity reserves (tonnes) | Total area of modules that can be produced (m2) | Scale-up (1000TWh) |
| --- | --- | --- | --- |
| In | 0 | 0 | 0 |
| Sn | 2.72E+04 | 3.22E+11 | 108 |
| Cs | 0 | 0 | 0 |
| Pb | 8.20E+06 | 9.31E+12 | 3.13E+03 |
| P | 4.36E+05 | 6.47E+14 | 2.17E+05 |
| Al | 0.00E+00 | 0 | 0 |

Table 11: HIERN module design output from European Union reserves.

| Element | Quantity reserves (tonnes) | Total area of modules that can be produced (m2) | Scale-up (1000TWh) |
| --- | --- | --- | --- |
| In | 0.00E+00 | 0 | 0 |
| Sn | 2.72E+04 | 3.22E+11 | 108 |
| Cs | 0.00E+00 | 0 | 0 |
| Pb | 8.20E+06 | 2.37E+12 | 7.97E+02 |
| P | 4.36E+05 | 7.30E+13 | 2.45E+04 |
| Ni | 4.44E+06 | 8.84E+13 | 2.97E+04 |
| Ag | 5.92E+04 | 3.66E+10 | 1.23E+01 |

Figure four: calculating the electricity production using the module designs and secondary resources

The same procedure as above was followed, but the quantity of waste was used from Table 12 rather than the reserves (Urban Mine Platform, 2026). The Figure 4b from the main text then had the end-of-life recycling input rate (EOL-RIR) applied to it. Most of the EOL-RIR percentages are from the RMIS platform (European Commission, 2026), however, the gold, cobalt, molybdenum, and tin recycling rates are from the Joint Research Council (European Commission. Joint Research Centre., 2018).

The results of each module design are shown in Table 13, Table 14 and Table 15.

Table 12: Quantity of waste (tonnes) in 2019 and end-of-life recycling input rate (%) for a range of materials.

| Element | Quantity (tonnes/year) | End-of-life recycling input rate (%) |
| --- | --- | --- |
| Ag | 480 | 19 |
| Al | 4600000 | 21 |
| Au | 66 | 20 |
| Co | 13000 | 35 |
| Cr | 130000 | 21 |
| Cs | 0 | 0 |
| Cu | 650000 | 30 |
| F | 1300 | 1 |
| Ga | 1300 | 0 |
| Graphite | 0 | 0 |
| In | 74 | 1 |
| Li | 7200 | 0 |
| Mg | 1700000 | 7 |
| Mo | 4900 | 30 |
| Nb | 950 | 0 |
| Ni | 110000 | 16 |
| P | 420000 | 0 |
| Pb | 860000 | 80 |
| Pt | 11 | 12 |
| Sn | 15000 | 32 |
| Ti | 760000 | 1 |
| Zn | 270000 | 40 |
| Zr | 0 | 0 |

*There is no data for Cs, Graphite and Zr.

Table 13: Solaronix module design output from European Union waste and end-of-life recycling input rates.

| Element | Waste-based output (1000TWh) | Waste and EOL-RIR output (1000TWh) |
| --- | --- | --- |
| Ag | 9.96E-02 | 1.89E-02 |
| F | 6.28E+00 | 6.28E-02 |
| Pb | 1.31E+02 | 1.05E+02 |
| Sn | 4.85E+00 | 1.55E+00 |
| Ti | 3.11E+01 | 3.11E-01 |

Table 14: University of Freiburg module design output from European Union waste and end-of-life recycling input rates.

| Element | Waste-based output (1000TWh) | Waste and EOL-RIR output (1000TWh) |
| --- | --- | --- |
| Al | 3.82E+03 | 8.01E+02 |
| Cs | 0 | 0 |
| In | 3.12E-02 | 3.12E-04 |
| P | 2.09E+05 | 0.00E+00 |
| Pb | 3.28E+02 | 2.63E+02 |
| Sn | 5.97E+01 | 1.91E+01 |

Table 15: HIERN module design output from European Union waste and end-of-life recycling input rates.

| Element | Waste-based output (1000TWh) | Waste and EOL-RIR output (1000TWh) |
| --- | --- | --- |
| Ag | 9.96E-02 | 1.89E-02 |
| Cs | 0 | 0 |
| In | 3.12E-02 | 3.12E-04 |
| Ni | 7.35E+02 | 1.18E+02 |
| P | 2.36E+04 | 0.00E+00 |
| Pb | 8.36E+01 | 6.69E+01 |
| Sn | 5.97E+01 | 1.91E+01 |

Figure five: concentration of metals/minerals in ore deposits, from waste, and the earth’s crust.

The ore deposit data was taken from a variety of sources, with most being the United States Geological Survey and the British Geological Survey. Table 16 shows the maximum and minimum ore grade data from numerous sources. Some data sources were different reports entirely, some data points come from different parts of the same report. The minimum and maximum across the one to four datapoint range was then plotted onto figure five of the main manuscript. The average ore grade was also taken from various sources. Table 16 has both the hyperlinks directly to the data used for ease of access, as well as the citation of the source. Only ore grades reported as averages were labelled as an ‘average’ datapoint – that is, no average value was calculated. Deposits on the sea floor, soil, mine waste sites and water were generally disregarded.

If values were reported in a mineral weight percent or ppm, the element was isolated using atomic weights and stoichiometric ratios.

Table 16: The maximum, minimum and average ore grades for a range of elements used in perovskite solar cell research.

| Element | Typical grade data point 1 (min wt %) | Typical grade data point 1 (max wt %) | Typical grade data point 2 (min wt %) | Typical grade data point 2 (max wt %) | Typical grade data point 3 (min wt %) | Typical grade data point 3 (max wt %) | Typical grade data point 3 (min wt %) | Typical grade data point 3 (max wt %) | Average datapoint (wt %) | Sources |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Aluminium | 17 | 28 |  |  |  |  |  |  | 24 | (International Aluminium Institute, 2022) (BGR, 2020) |
| Caesium | 4.7 | 30 |  |  |  |  |  |  | 19.0 | (USGS, 2022) (Butterman et al., 2004) |
| Chromium | 17 | 37 |  |  |  |  |  |  |  | (Schulte et al., 2012) |
| Cobalt | 0.01 | 1 | 0.04 | 0.92 | 0.0047 | 0.0115 | 0.007 | 0.02 | 0.24 | (Petavratzi et al., 2019) (Dehaine et al., 2021) (Schulz et al., 2017) |
| Copper | 0.2 | 2 | 0.094 | 1.7 | 0.1 | 8 |  |  | 0.62 | (Bide, 2007) (Crowson, 2012) (Leach et al., 2010) (Calvo et al., 2016) |
| Fluorine | 14.6 | 34 | 29 | 47 | 0.001 | 26 |  |  |  | (Bide, 2011) |
| Gallium | 0.0008 | 0.0812 | 0.9 | 55.1 | 0.031 | 12 | 0.0006 | 0.0275 | 0.0057 | (Schulte & Foley, 2013) |
| Gold | 0.0001 | 0.001 |  |  |  |  |  |  |  | (Calvo et al., 2016) |
| Indium | 0.0001 | 0.01 |  |  |  |  |  |  |  | (USGS, 2024a) |
| Lithium | 0.01 | 0.31 | 0.01 | 1.85 | 0.004 | 0.0066 | 0.54 | 7.3 |  | (Brown, 2016) (Schulz et al., 2017) |
| Lead | 0.18 | 13 | 5 | 15 |  |  |  |  | 1.9 | (Leach et al., 2010) |
| Magnesium | 7 | 29 |  |  |  |  |  |  |  | (USGS, 2024b) |
| Molybdenum | 0.1 | 0.3 | 0.03 | 0.22 |  |  |  |  |  | (Ludington & Plumlee, 2010) (Taylor et al., 2012) |
| Nickel | 0.2 | 3 | 0.66 | 2.4 | 0.5 | 0.3 |  |  | 1.3 | (Bide et al., 2008) (Marsh et al., 2013) (Schulz et al., 2014) |
| Niobium | 0.07 | 8.4 |  |  |  |  |  |  |  | (Shaw & Goodenough, 2011) |
| Palladium | 0.00005 | 0.0005 |  |  |  |  |  |  |  | (Gunn & Benham, 2009) |
| Phosphorus | 1.3 | 16.6 |  |  |  |  |  |  |  | (El Bamiki et al., 2021) |
| Platinum | 0.00005 | 0.0005 | 0.0005 | 0.0015 | 0.091 | 0.015 |  |  |  | (Gunn & Benham, 2009) (Schulz et al., 2017) |
| Silver | 0.010 | 0.048 | 0.00034 | 0.0485 |  |  |  |  | 0.027 | (Ruberti & Massari, 2018) (Leach et al., 2010) (Graybeal & Vikre, 2010) |
| Tin | 0.3 | 1 | 0.0058 | 0.0145 |  |  |  |  |  | (Menzie et al., 1988) (Schulz et al., 2017) |
| Titanium | 0.61 | 12 |  |  |  |  |  |  |  | (Woodruff et al., 2017) |
| Zinc | 0.11 | 24 | 5 | 15 |  |  |  |  | 6 | (Leach et al., 2010) (Christie & Brathwaite, n.d.) |
| Zirconium | 0.0047 | 0.64 | 0.0094 | 0.1 |  |  |  |  |  | (USGS, 2021) (Schulz et al., 2017) |

The concentration of elements in waste electrical and electronic equipment (WEEE) was taken from ten published papers and covered 79 items (Cucchiella et al., 2015; Hlavatska et al., 2021; Holuszko et al., 2022; Oguchi et al., 2011; Paz et al., 2024; Petter et al., 2014; Rocchetti et al., 2015; Tunali et al., 2021; Wang & Xu, 2014; Winslow et al., 2018). Any value reported in ppm was converted to weight percent. An example of this data is demonstrated below (Holuszko et al., 2022).

Table 17: Weight percent of elements in various electrical and electronic equipment, as reported  by Holuszko et al. (Holuszko et al., 2022).

|  | Air conditioner |  | Desktop |  | Laptop |  | Cellphone |  | Printed circuit board |  | Refrigerator |  | Television |  | Washing machine |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Element | Min wt % | Max wt % | Min wt % | Max wt % | Min wt % | Max wt % | Min wt % | Max wt % | Min wt % | Max wt % | Min wt % | Max wt % | Min wt % | Max wt % | Min wt % | Max wt % |
| Al | 8 | 9 | 2 | 4 | 1 | 2 | 3 |  | 2 | 8 | 1 | 2 | 1 | 15 | 0 | 3 |
| Cu | 6 | 19 | 7 | 20 | 1 | 19 | 10 | 33 | 12 | 19 | 3 | 17 | 1 | 21 | 3 | 7 |
| Au | 0.0015 |  | 0.0046 | 0.024 | 0.0032 | 0.063 | 0.003 | 0.15 | 0.0029 | 0.112 | 0.0044 |  | 0.0005 | 0.03 | 0.0017 |  |
| Pd |  |  | 18 | 25 | 0.0019 |  | 0.03 | 0.17 | 0.0033 | 0.022 |  |  | 0 | 0.012 |  |  |
| Ag | 0.0058 |  | 0.0207 | 0.057 | 0.019 | 0.11 | 0.2 | 0.38 | 0.01 | 0.52 | 0.0042 |  | 0.012 | 0.06 | 0.0051 |  |