Supplement Material

Substrate stiffness-dependent regulatory volume decrease and calcium signaling in chondrocytes

Running title: substrate stiffness regulates chondrocyte volume and calcium signaling

Quanyou Zhang1,2,, Min Zhang2, Xiaoan Wu3, Genlai Du4, Xiaochun Wei1, Weiyi Chen2,

1Department of Orthopaedics, the Second Hospital of Shanxi Medical University, Shanxi Key Laboratory of Bone and Soft Tissue Injury Repair, Shanxi Medical University, Taiyuan 030001, China;

2College of Biomedical Engineering, Taiyuan University of Technology, Taiyuan 030024, China;

3Department of Physiology and Biophysics, Miller School of Medicine, University of Miami, Miami, Florida 33136, USA;

4Department of Cell Biology and Medical Genetics, School of Basic Medical Science, Shanxi Medical University, Taiyuan 030001, China.

Corresponding authors:

Table I. The RVD parameters of chondrocyte during swelling and recovering in hypo-osmotic medium (180 mOsm).

| RVD responsive parameters | Stiff (n=29) | Medium (n=27) | Soft (n=32) |
| --- | --- | --- | --- |
| Initial diameter, d0 (m) | 15 ± 3 | 13 ± 3 | 12 ± 2 |
| Maximum diameter, dM (m) | 19 ± 3 | 16 ± 2 | 16 ± 3 |
| Swelling time TS (min) | 13 2 | 9 2 | 8 1 |
| Percentage increase of d (%) | 22 ± 4 | 29 ± 3 | 33 ± 4 |
| Recovery time TR (min) | 20 4 | 31 5 | 34 4 |
| Percent of recovery diameter (%) | 75 9 | 69 6 | 61 8 |
| Responding time TRes (min) | 33 4 | 40 4 | 41 4 |

n is the number of measured cells. All data are shown as mean  s.d

Table II. The elastic and viscoelastic parameters of chondrocytes on varying substrate stiffness in iso-osmotic medium (320 mOsm)

| Mechanical parameters | Stiff (n=32) | Medium (n=27) | Soft (n=36) |
| --- | --- | --- | --- |
| Eelastic (kPa) | 1.6 0.1 | 1.1 0.2 | 1.0 0.1 |
| (s) | 4.5 0.2 | 3.5 0.2 | 3.2 0.1 |
| (s) | 7.4 0.3 | 5.4 0.3 | 5.1 0.2 |
| ER (kPa) | 0.5 0.1 | 0.3 0.1 | 0.2 0.1 |
| E0 (kPa) | 0.8 0.1 | 0.5 0.1 | 0.4 0.1 |
| (kPas) | 1.4 0.1 | 0.7 0.1 | 0.6 0.1 |

n is the number of measured cells. All data are shown as mean s.d

Table III. The relative percentage increase of the mechanical parameters of chondrocytes on varying substrate stiffness in hypo-osmotic medium (180 mOsm) compared to the control group in iso-osmotic medium (320 mOsm).

|  | Eelastic (kPa) | ER (kPa) | E0 (kPa) | (kPas) |
| --- | --- | --- | --- | --- |
| Stiff | 24% | 29% | 30% | 33% |
| Medium | 33% | 19% | 18% | 19% |
| Soft | 43% | 19% | 13% | 16% |

Table IV. The calcium responsive rate of chondrocytes on varying substrate stiffness induced by 4PDD or GSK205 in iso-osmotic medium.

|  | Calcium responsive rate (%) |  |
| --- | --- | --- |
|  | 4PDD treated | GSK205 treated |
| Stiff | 80 ± 5 | 35 ± 4 |
| Medium | 54 ± 4 | 39 ± 3 |
| Soft | 53 ± 6 | 39 ± 4 |

All data are shown as mean  s.d

Table V. The relative percentage increase or decrease of the amplitude and frequency of Ca2+ oscillations in chondrocytes on varying substrate stiffness induced by 4PDD or GSK205 in iso-osmotic medium.

|  | 4PDD- induced relative increase |  |  | GSK205- induced relative decrease |  |
| --- | --- | --- | --- | --- | --- |
|  | Amplitude (F/F0) | Frequency (peaks/min) | Amplitude (F/F0) |  | Frequency (peaks/min) |
| Stiff | 50% | 54% | 59% |  | 52% |
| Medium | 44% | 43% | 46% |  | 37% |
| Soft | 24% | 33% | 46% |  | 24% |

Table VI. The percent of chondrocytes on variable stiffness substrates exhibited both RVD response and Ca2+ oscillations in hypo-osmotic (180 mOsm) medium after treatment of 4PDD or GSK205.

|  | Calcium responsive rate (%) |  |
| --- | --- | --- |
|  | 4PDD treated | GSK205 treated |
| Stiff | 43 ± 5 | 24 ± 3 |
| Medium | 51 ± 5 | 29 ± 2 |
| Soft | 49 ± 5 | 33 ± 5 |

All data are shown as mean  s.d

Table VII. The relative percentage increase or decrease of the amplitude and frequency of Ca2+ oscillations in chondrocyteson varying substrate stiffness induced by 4PDD or GSK205 during cells welling in hypo-osmotic (180 mOsm).

|  | 4PDD- induced relative increase |  | GSK205- induced relative decrease |  |
| --- | --- | --- | --- | --- |
|  | Amplitude (F/F0) | Frequency (peaks/min) | Amplitude (F/F0) | Frequency (peaks/min) |
| Stiff | 22% | 18% | 43% | 44% |
| Medium | 32% | 26% | 59% | 55% |
| Soft | 44% | 37% | 70% | 66% |

Table VIII. The relative percentage increase or decrease of the amplitude and frequency of Ca2+ oscillations in chondrocytes on variable stiffness substrates induced by 4PDD or GSK205 during cell recovering in hypo-osmotic (180 mOsm) medium.

|  | 4PDD- induced relative increase |  | GSK205- induced relative decrease |  |
| --- | --- | --- | --- | --- |
|  | Amplitude(F/F0) | Frequency(peaks/min) | Amplitude(F/F0) | Frequency(peaks/min) |
| Stiff | 37% | 31% | 65% | 54% |
| Medium | 25% | 21% | 53% | 47% |
| Soft | 23% | 23% | 52% | 47% |