Supplementary Information

# Using ZnCo2O4 nanoparticles as the hole transport layer to improve long-term stability of perovskite solar cells

Bo-Rong Jheng,1 Pei-Ting Chiu,1,2 Sheng-Hsiung Yang,1,* and Yung-Liang Tong2

1Institute of Lighting and Energy Photonics, College of Photonics, National Yang Ming Chiao Tung University, No.301, Section 2, Gaofa 3rd Road, Guiren District, Tainan 71150, Taiwan R.O.C.

# 2Green Energy and Environment Research Laboratories, Industrial Technology Research Institute, No.360, Gaofa 2nd Road, Guiren District, Tainan 71150, R.O.C.

*Correspondence: yangsh@mail.nctu.edu.tw

Table S1. Lifetime parameters of TR-PL curves of the perovskite on the FTO substrate, PEDOT:PSS film, and ZnCo2O4 NPs layer.

| substrate | A1 (%) | τ1 (ns) | A2 (%) | τ2 (ns) | τavg (ns) |
| --- | --- | --- | --- | --- | --- |
| FTO | 54.61 | 13.12 | 45.39 | 119.59 | 107.17 |
| PEDOT:PSS film | 58.51 | 11.74 | 41.49 | 101.19 | 88.61 |
| ZnCo2O4 NPs layer | 54.41 | 10.15 | 45.59 | 47.58 | 39.98 |

Figure S1. Cross-sectional SEM images of (a) PEDOT:PSS film and (b) ZnCo2O4 NPs layer deposited on FTO substrates.

Figure S2. Hole mobility of (a) ZnCo2O4 NPs layer and (b) PEDOT:PSS film versus electric field (V/L)0.5.

Figure S3. (a) Transmission spectra of PEDOT:PSS film and ZnCo2O4 NPs layer and (b) absorption spectra of ZnCo2O4 NPs layer.

Figure S4. Performance variation represented as a standard box plot in (a) PCE, (b) JSC, (c) FF, and (d) VOC from 20 devices based on PEDOT:PSS film and ZnCo2O4 NPs layer under forward and reverse scans